TABLE SI. Ultimate load and shear strength from lap-shear testing

| Materials | Ultimate load, kN | Shear strength, MPa |
| --- | --- | --- |
| Neat epoxy cured by J230 | 3.64±0.31 | 11.01±0.87 |
| Neat epoxy cured by J400 | 3.22±0.15 | 10.33±0.66 |
| 2.5 vol% nanocomposite, cured by J230 | 4.31±0.22 | 12.31±0.93 |
| 2.5 vol% nanocomposite, cured by J400 | 4.78±0.65 | 13.89±0.79 |
| 5.0 vol% nanocomposite, cured by J230 | 5.20±0.42 | 16.45±1.36 |
| 5.0vol% nanocomposite, cured by J400 | 6.05±0.43 | 20.09±1.28 |

| (a) |  | (b) |  |
| --- | --- | --- | --- |
| (d) |  | (c) |  |
| FIG. S1. SEM micrograph of CT-fractured surfaces of J400-cured 5 vol% nanocomposites. |

The adhesive toughness (G1c) of DCB specimens was calculated according to ISO25217 ‘corrected beam theory’1

Where:     = Crack length, mm

P = load measured by Instron, N

= displacement of the cross-head of Instron, mm

B = Specimen Width, mm

= crack-length correction, mm. Only an instantly propagated crack was used.

F = large-displacement correction

N = load-block correction

= distance from the centre of the loading pin to the loading-block which is a tab in FIG.S2, mm

= distance from the pin centre to the loading-block edge, mm

FIG.S2 Double cantilever beam specimen (aluminium substrates).

Reference

1.	ISO: 25217 Adhesives -- Determination of the mode 1 adhesive fracture energy of structural adhesive joints using double cantilever beam and tapered double cantilever beam specimens, 24 (2009).