Phase transformation in relaxor - ferroelectric single crystal [Pb(Sc1/2Nb1/2)O3]0.58 -[PbTiO3]0.42

S.V. Rajasekaran1, S. N. Achary2, S. J. Patwe2, R.Jayavel3, G. Mangamma4, A.K. Tyagi4

1Department of Physics, Govt. Arts College, Dharmapuri, India 636705

2Chemistry Division, Bhabha Atomic Research Centre, Mumbai, India 400085

3Crystal Growth Centre, Anna University, Chennai, India 600025

4Surface and Nano science division, Material Science group, IGCAR, Kalpakam, India

Supplementary Information

Refinement plots of the powder XRD data of PSN-42PT recorded at 300°C.

Tetragonal (P4mm):  a = 4.0407(3), c = 4.0461(3) Å, V = 66.06(1) Å3

Monoclinic (Pm): a = 4.0441(2), b = 4.0212(3), c = 4.0731(6) Å, β = 90.02(1)°, V = 66.24(1) Å3