Supporting information

Facile synthesis of the SiO2/Au hybrid microspheres for excellent catalytic performance

Xin-Hui Liu, a Bin-Bin Ding,b Yan-Zhu,a Tai-Ya Wang,a Bi-cui Chen,a Yong Shao, a ,* Ming-Qi Chen,b Pan Zheng,b Yu-Ling Zhao,a Hai-sheng Qianb,

a Department of Chemistry, College of Chemistry and Life Sciences, Zhejiang Normal University, Jinhua 321004, P. R. China.

b Department of Medical Materials and Rehabilitation Engineering, School of Medical Engineering, Hefei University of Technology, Hefei 230009, P. R. China.

The preparation of Ag(NH3)2+ solution. In a typical process, 0.1 mmol NaCl was added to 1 mL 0.1 M AgNO3 solution and white precipitate was formed. Then 2 mL ammonium hydroxide was added to form clear solution.

Fig. S1. XRD patterns of the as-prepared SiO2/Ag hybrid microspheres obtained from 0.25g amorphous silica and 3mL [Ag(NH3)2]+ solution at 180 oC for 24h.

Table S1 Element composition of the as-prepared SiO2/Au microspheres from XPS analyses.

| Name | Atomic% |
| --- | --- |
| Au4f | 0.46 |
| Si2p | 32.01 |
| C1s | 11.66 |
| O1s | 55.86 |
| Total | 100 |

Fig. S2. TEM images of the silica/Au hybrid microspheres obtained from 0.05 g prepared SiO2/Ag microspheres and then 1 mL 1 % (wt %) in aqueous solution when the other condition was kept at the same.

Fig. S3. (a,b) TEM images of the silica/Au hybrid microspheres obtained after eight successive cycles of the catalytic reduction to 4-AP finished.

 Corresponding author. Tel.: +86-579-82282269; fax: +86-579-82282269.

E-mail address: yshao@zjnu.cn (Prof. Shao Y); shqian@hfut.edu.cn (Prof. Qian HS)