Supporting Materials

- Strain rate sensitivity (SRS) and activation volume

(1)

(2)

When we have two loading rates, i.e.  and , and the corresponding fracture strengths,  and , can be given in the following equations.

(3)

(4)

To cancel out k, Eq (3) minus Eq (4), we obtain,

(5)

To find out the maximal SRS, we use      s-1, ,

s-1, ,

mmax===0.06,

To find out the minimal SRS, we use       s-1, ,

s-1, ,

mmin==0.02,

Thus, the measured SRS ranges within 0.02~0.06.

The activation volume (v*) of plastic deformation is inherently related to the strain rate sensitivityS1 by

(6)

## Here k is the Boltzmann constant (1.38×10-23 m2 kg s-2k-1), T is absolute temperature, and  and m are respectively applied stress and SRS.

Here we take σ=864 MPa and m=0.06 to calculate the activation volume of plastic deformation at dynamic loading

=0.135 nm3 =2~3 b3 (︱b︱=0.38 nm for plane spacing in Figure 4 of our manuscript).

The activation volume under quasi-static loading is calculated as follows:

## =0.994nm3=18 b3.

## Here=356 MPa (we take the maximum compressive strength under quasi-static loading) and m=0.02 (we take m=0.02 in order to roughly estimate the maximum activation volume).

- Evaluation of fracture energy dissipation for dynamic/quasi-static compression.

For the quasi-statically compressed sample, the original sample geometry is 2mm x 2mm x 4mm. Upon fracture, the sample was roughly split into two parts with two fracture surfaces. The two fracture surface areas were estimated to be the total of 16mm2(2mm x 4mm x 2).

For the dynamic case, the pristine geometry is 3mm x 3mm x 3mm. The average fragment size is approximately 0.154mm. Here we treat each fragment as an ideal cube. Thus, the created surface area can be estimated to be the total of

Fig. S1. Schematic illustration of dynamic compression process, for simplicity, each irregular-shaped fragment is treated as an idea cube.

Here we introduce k (J/mm2) as the fracture energy and assume it to be a constant. When we consider the volume effect (sample geometry), we can further obtain the fracture energy dissipation per unit volume, as follows.

For the quasi-static case, the fracture energy dissipation per unit volume is 16mm2 k/2mm x 2mm x 4mm=1 J/mm3.

For the dynamic one, the fracture energy dissipation per unit volume is 998mm2 k/3mm x 3mm x 3mm=37 J/mm3. Thus, the ratio of energy dissipations of dynamic fracture to that of the quasi-static fracture is 37.

- Fractograph observation of dynamic compression nacre along cross section

Fig. S2. Fractography observation in the dynamically-compressed nacre along cross section. (a) The fragment size distribution is typically in the range of submillimeter. (b) The fracture surface viewed from c-axis shows that crack propagates, to a large extent, along the biopolymer interface. (c) Microscopic observation on the cross section confirms the interface-dominated crack failure. (d) A close-up examination shows that the aragonite platelets remain comparatively intact.

- Schematic illustrations of crack propagation when loading from c-axis and cross section, respectively.

Fig. S3. Effect of loading direction on the potential crack path. (a) When loading along nacre’s c-axis, the geometrically staggered aragonite platelets posts a critical crack extension resistance. (b) Comparatively, the biopolymer interface favors the crack propagation (stress release) while loading direction is along nacre’s cross section.