Electronic Supplementary Information

Water bath synthesis and enhanced photocatalytic performances of urchin-like micro/nanostructured α-FeOOH

Shenghong Kang, Guozhong Wang, Ming Fang, Huiming Wang, Xianbiao Wang and Weiping Cai*

Key Laboratory of Materials Physics, Centre for Environmental and Energy Nanomaterials, Anhui Key Laboratory of Nanomaterials and Nanotechnology, Institute of Solid State Physics, Chinese Academy of Sciences,

Hefei 230031, P.R. China

Figure S1 Nitrogen sorption isotherms of the urchin-liked α-FeOOH.

Figure S2 Time-dependent optical absorbance spectra of the R6G solution (the starting concentration: 1×10-5M L-1, 30mL) conatining H2O2 (33mmol L-1) and the nanorods α-FeOOH (30mg) after its exposure to xenon lamp for different durations.

Figure S3 The optical absorbance spectra of the R6G solution (the starting concentration: 1×10-5M L-1) with hydrogen peroxide (33m mol L-1) before (a) and after (b) addition of 30mg the as-prepared α-FeOOH catalyst for 60min under the dark condition.

Figure S4 (a) Time-dependent optical absorbance spectra of the R6G solution (the starting concentration: 1×10-5M L-1, 30mL) containing the 30mg P25 after its exposure to xenon lamp for different durations. (b) Degradation percentage of R6G as a function of time.

Figure S5 Degradation percentage of R6G as a function of time for different cycles (details are seen in the text).

# Footnotes

* To whom all correspondence should be addressed

E-mail: wpcai@issp.ac.cn