Supplementary Material

**Ultramicroporous silicon nitride ceramics for CO2 capture**

*Cristina Schitco, \*1 Mahdi Seifollahi Bazarjani, 2 Ralf Riedel, 1 and Aleksander Gurlo 2*

1Technische Universität Darmstadt, Fachbereich Material-und Geowissenschaften, Jovanka-Bontschits-Strasse 2, 64287 Darmstadt, Germany

2Technische Universität Berlin, Fakultät III Prozesswissenschaften, Institut für Werkstoffwissenschaften und -technologien, Fachgebiet Keramische Werkstoffe, Hardenbergstrasse 40, 10623 Berlin, Germany

\*Corresponding author: E-mail: [schitco@materials.tu-darmstadt.de](mailto:schitco@materials.tu-darmstadt.de)


****

FIG S1. The Tóth fit of CO2 adsorption isotherm of HTT600NH up to 15 bars at (a) 273 K and (b) 373 K.

TABLE SI. CO2 adsorption capacities of different materials at 1 bar represented in FIG 5.

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Sample | Specific Surface Area  [m2 g-1] | Pore size  [nm] | Adsorption capacity  [mmol g-1] | Ref. |
| MOMs | SIFSIX-3Zn | 250 | 0.384 | 2.54a) | [1](#_ENREF_1) |
|  | SIFSIX-2-Cu-i | 735 | 0.515 | 5.41a) | [1](#_ENREF_1) |
|  | SIFSIX-2-Cu | 3140 | 1.305 | 1.84a) | [1](#_ENREF_1) |
| Zeolites | Zeolite 13X | 616 | 1.0 | 3.9a) | [2](#_ENREF_2), [3](#_ENREF_3) |
| Nitrides | MSIN-673 | 1009 | 2.3 | 2.6a) | [4](#_ENREF_4) |
|  | HTT600NH | 230 | 0.5 | 2.3b) | This work |
| Activated carbons | AC | 2994 | 2.35 | 2.1a) | [5](#_ENREF_5) |

a) CO2 adsorption at 298 K b) CO2 adsorption at 273 K

1. P. Nugent, Y. Belmabkhout, S.D. Burd, A.J. Cairns, R. Luebke, K. Forrest, T. Pham, S. Ma, B. Space, L. Wojtas, M. Eddaoudi and M.J. Zaworotko: Porous materials with optimal adsorption thermodynamics and kinetics for CO2 separation. *Nature.* **495**(7439), 80 (2013).

2. Z. Liang, M. Marshall and A.L. Chaffee: CO2 Adsorption-Based Separation by Metal Organic Framework (Cu-BTC) versus Zeolite (13X). *Energy Fuels.* **23**(5), 2785 (2009).

3. P.D. Jadhav, R.V. Chatti, R.B. Biniwale, N.K. Labhsetwar, S. Devotta and S.S. Rayalu: Monoethanol Amine Modified Zeolite 13X for CO2 Adsorption at Different Temperatures. *Energy Fuels.* **21**(6), 3555 (2007).

4. H.W. Yang, A.M. Khan, Y.Z. Yuan and S.C. Tsang: Mesoporous Silicon Nitride for Reversible CO2 Capture. *Chemistry-an Asian Journal.* **7**(3), 498 (2012).

5. C. Zhang, W. Song, G. Sun, L. Xie, J. Wang, K. Li, C. Sun, H. Liu, C.E. Snape and T. Drage: CO2 Capture with Activated Carbon Grafted by Nitrogenous Functional Groups. *Energy Fuels.* **27**(8), 4818 (2013).