# Suplementary materials

# Linear and Nonlinear Optical Properties of Aluminum Borate Crystal Al5BO9: Experiment and Calculation

Donghai An,  Min Zhang, * Danni Li, Shilie Pan, * Huimin Chen, * Zhihua Yang,  Yingtao Zhu,  Yi Sun,  Hui Zhang, Yangyang Li

TABLE S1. Atomic coordinates, equivalent isotropic displacement parameters and bond valence sum (BVS) for Al5BO9

| Atoms | Wyckoff positions | x | y | z | U(eq) | BVS |
| --- | --- | --- | --- | --- | --- | --- |
| Al1 | 4a | 0 | 0.4440(1) | 0.8429(3) | 0.007 (1) | 2.75 |
| Al2 | 4a | 0 | 0.2552(1) | 0.8475(3) | 0.008 (1) | 2.78 |
| Al3 | 4a | 0 | 0.2969(1) | 0.4949(3) | 0.007 (1) | 3.08 |
| Al4 | 8b | 0.2519(2) | 0.1165(1) | 0.6610(3) | 0.006 (1) | 3.07 |
| B1 | 4a | 0 | -0.0147(4) | 0.8823(9) | 0.007 (2) | 3.02 |
| O1 | 4a | 0 | 0.1913(2) | 0.5959(6) | 0.006 (1) | 1.84 |
| O2 | 8b | 0.2567(4) | 0.1905(2) | 0.8611(5) | 0.006 (1) | 2.10 |
| O3 | 4a | 0 | 0.5453(3) | 0.7328(6) | 0.007 (1) | 1.97 |
| O4 | 4a | 0 | 0.3521(2) | 0.6978(6) | 0.008 (1) | 2.03 |
| O5 | 4a | 0 | 0.3288(3) | 1.0305(6) | 0.007 (1) | 1.88 |
| O6 | 4a | 0 | 0.0462(3) | 0.7527(6) | 0.006 (1) | 2.07 |
| O7 | 8b | -0.2104(5) | -0.0478(2) | 0.9462(4) | 0.007 (1) | 2.04 |

# TABLE S2. Selected bond lengths and electron population (Å) for Al5BO9

| Bonds | Bond lengths | Optimized bond lengths | electron population | Bonds | Bond lengths | Optimized bond lengths | electron population |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Al1-O3 | 1.736(4) | 1.73685 | 0.48 | Al4-O3 #8 | 1.847(3) | 1.83409 | 0.39 |
| Al1-O4 | 1.771(5) | 1.76487 | 0.41 | Al4-O1 | 1.881(3) | 1.85587 | 0.33 |
| Al1-O7 #1 | 1.824(3) | 1.80271 | 0.39 | Al4-O2 | 1.894(4) | 1.87848 | 0.34 |
| Al1-O7 #2 | 1.824(3) | 1.80271 | 0.39 | Al4-O6 | 1.906(3) | 1.90550 | 0.32 |
| Mean | 1.789 | 1.77679 | / | Al4-O5 #7 | 1.909(3) | 1.90718 | 0.35 |
| Al2-O2#5 | 1.749(3) | 1.74375 | 0.45 | Al4-O7 #9 | 1.956(4) | 2.00606 | 0.25 |
| Al2-O2 | 1.749(3) | 1.74375 | 0.45 | mean | 1.899 | 1.89790 | / |
| Al2-O5 | 1.785(5) | 1.77028 | 0.43 | B1-O6 | 1.350(8) | 1.36704 | 0.83 |
| Al2-O4 | 1.850(4) | 1.80597 | 0.35 | B1-O7 #5 | 1.380(5) | 1.39128 | 0.79 |
| mean | 1.784 | 1.76594 | / | B1-O7 | 1.380(5) | 1.39128 | 0.79 |
| Al3-O2 #6 | 1.727(3) | 1.72312 | 0.47 | mean | 1.369 | 1.38320 | / |
| Al3-O2 #7 | 1.727(3) | 1.72312 | 0.47 |  |  |  |  |
| Al3-O1 | 1.762(4) | 1.74306 | 0.44 |  |  |  |  |
| Al3-O4 | 1.763(5) | 1.76886 | 0.41 |  |  |  |  |
| mean | 1.744 | 1.7395 | / |  |  |  |  |
| Symmetry transformations used to generate equivalent atoms: #1) x+1, y+1/2, z; #2) –x-1/2,z; #3) –x+1, -y+1/2, z+1/2; #4)x-1/2, -y+1/2, z+1/2; #5) -x, y, z; #6) x-1/2, -y+1/2, z-1/2; #7) –x+1/2, -y+1/2, z-1/2; #8) x+1/2, y-1/2, z; #9) -x, -y, z-1/2; #10) -x+1,y, z; #11) –x+1/2,y+1/2, z;#12) x-1/2,y+1/2, z; #13) x-1/2,y-1/2, z; #14)-x,-y,z+1/2 |

FIG. S1. Powder X-ray diffraction patterns of Al5BO9

FIG. S2. TG–DSC curves of the Al5BO9 crystal

FIG. S3. UV-vis–NIR diffuse reflectance spectroscopy of Al5BO9

FIG. S4. Infrared spectrum of Al5BO9

FIG. S5. phase-matching curve for Al5BO9. (The solid curve drawn is to guide the eye and is not a fit to the data.)