Supporting Information

Preparation of Magnetic and Photocatalytic Cenosphere Deposited with Fe3O4/SiO2/Eu-doped TiO2 Core/Shell Nanoparticles

Hui Zhang*, Junli Zhang, Runjun Sun, and Yingxue Zhou

# School of Textile & Materials, Xi’an Polytechnic University, Xi’an 710048, China

*Corresponding author

S1. FESEM images of the original and Fe3O4 coated cenospheres and EDX spectrum of the Fe3O4 coated cenosphere

Figure S1 Surface morphology of the original and Fe3O4 coated cenospheres and EDX spectrum of the Fe3O4 coated cenosphere

S2. Element mapping of the Fe3O4 coated cenospheres

Figure S2 Element mapping for the Fe3O4 coated cenospheres

S3. FESEM images, line scanning map, and EDX spectrum of the Fe3O4/SiO2 coated cenospheres

Figure S3 Surface and cross-section morphologies, line scanning map, and EDX spectrum of the Fe3O4/SiO2 coated cenospheres

S4. FESEM images, line scanning map, and EDX spectrum of the Fe3O4/SiO2/TiO2 coated cenospheres

Figure S4 Surface morphology, line scanning map, and EDX spectrum of the Fe3O4/SiO2/TiO2 coated cenospheres

S5. FESEM images, line scanning map, and EDX spectrum of the Fe3O4/SiO2/Eu-doped (0.1%) TiO2 coated cenospheres

Figure S5 Surface morphology, line scanning map, and EDX spectrum of the Fe3O4/SiO2/Eu-doped (0.1%) TiO2 coated cenospheres

S6. TG and DSC curves

Figure S6 TG (a) and DSC (b) curves of the as-prepared cenospheres

S7. XPS spectra

Figure S7 XPS survey spectra of the Fe3O4/SiO2/TiO2 coated and Fe3O4/SiO2/Eu-doped (0.1%) TiO2 coated cenospheres (a) and XPS spectrum of Eu 3d core-level deconvolution (b).

S8. Results of XPS elemental analysis

Table S1 The results of XPS elemental analysis for the Fe3O4/SiO2/TiO2 coated and Fe3O4/SiO2/Eu-doped (0.1%) TiO2 coated cenospheres

| Cenosphere | Name | Peak BE (eV) | FWHM (eV) | Area (CPS.ev) | Atom percentage (%) |
| --- | --- | --- | --- | --- | --- |
| Fe3O4/SiO2/TiO2 coated | C1s | 284.66 | 2.02 | 10502.01 | 25.86 |
|  | O1s | 530.08 | 2.05 | 49028.51 | 47.25 |
|  | Ti2p | 458.61 | 1.47 | 35586.85 | 12.17 |
|  | Si2p | 103.22 | 2.83 | 4573.18 | 12.67 |
|  | N1s | 400.11 | 0.98 | 1416.2 | 2.06 |
| Fe3O4/SiO2/Eu-doped (0.1%) TiO2 coated | C1s | 284.59 | 1.94 | 12240.42 | 28.81 |
|  | O1s | 530.14 | 2.28 | 53263.26 | 49.08 |
|  | Ti2p | 458.83 | 1.67 | 44706.93 | 14.62 |
|  | Si2p | 102.62 | 3.21 | 2469.83 | 6.54 |
|  | Eu3d | 1133.37 | 6.23 | 14126.69 | 0.95 |

S9. PL spectra

Figure S8 PL spectra of the Fe3O4/SiO2/TiO2 coated and Fe3O4/SiO2/Eu-doped (0.1%) TiO2 coated cenospheres

S10. Photo-decolorization rate constant (k value) of MB solution

Figure S9 Effect of Eu3+ doping concentration on the photo-decolorization rate constant (k value) of MB solution for the TiO2 coated and Eu-doped TiO2 coated cenospheres under (a) UV and (b) visible light irradiation

S11. Effect of UV irradiation time on the photocatalytic degradation of MB solution

Figure S10 Effect of UV irradiation time on the photocatalytic degradation of MB solution for the as-prepared cenospheres

S12. Repeated photocatalytic degradation of MB solution

Figure S11 Effect of experimental cycle on the photocatalytic degradation of MB solution for Fe3O4/SiO2/Eu-doped (0.1%) TiO2 coated cenospheres