*Supporting Information*

*for*

**Visible-Light Responsive Plasmonic Ag2O/Ag/g-C3N4 Nanosheets with Enhanced Photocatalytic degradation of RhB**

**Shurong Fu, Yiming He, Qi Wu, Ying Wu\*, Tinghua Wu\***

*Zhejiang Key Laboratory for Reactive Chemistry on Solid Surfaces, Institute of Physical Chemistry, Zhejiang Normal University, Jinhua 321004, China*

Corresponding author, Tel.: +86 0579 82282234; Fax: +86 0579 82282595.

E-mail: yingwu@zjnu.cn (Y. Wu), thwu@zjnu.cn (T. Wu).

|  |  |  |
| --- | --- | --- |
| element | weight percentage | tu2.tifatom percentage |
| C K | 31.76 | 35.38 |
| N K | 63.46 | 60.62 |
| O K | 4.78 | 4.00 |
| total | 100.00 |  |


未标题-4.tif



**FIG. S1 EDS spectrum of g-C3N4 NS**


|  |  |  |
| --- | --- | --- |
| element | weight percentage | tu-1.tifatom percentage |
| C K | 28.89 | 34.68 |
| N K | 52.45 | 53.98 |
| O K | 11.53 | 10.39 |
| Ag L | 7.13 | 0.95 |
| total | 100.00 |  |

**未标题-5.tif**

**FIG. S2 EDS spectrum of Ag(10.0)/g-C3N4 NS**

**tu-1.tif**

****

****

**FIG. S3 Mapping spectrum of Ag(10.0)/g-C3N4 NS**