Hydrothermal Synthesis of 3D Ba5Ta4O15 Flower-like Microsphere Photocatalyst with High Photocatalytic Properties

Dongbo Xua,b, Weidong Shia,b,*, Chao Xub, Songbo Yangb, Hongye Baib, Chengjie Song,c Biyi Chenb

aSchool of Energy and Power Engineering, Jiangsu University, Zhenjiang, 212013, P. R. China.

bSchool of Chemistry and Chemical Engineering, Jiangsu University, Zhenjiang, 212013, P. R. China.

cSchool of Environmental and Safety Engineering, Changzhou University,

Changzhou, 213164, P. R. China.

E-mail: swd1978@ujs.edu.cn;

Fig. S1 XRD patterns of Ba5Ta4O15 produced by hydrothermal method at 160, 180, and 200 °C, respectively.

Fig. S2 XRD patterns of the as-prepared Ba5Ta4O15 at 200 °C for different times.

Fig. S3 The 3D Ba5Ta4O15 flower-like microsphere SEM images: (a) 160 °C, Ba(OH)2 0.40 M, 7 days; (b) 180 °C, Ba(OH)2 0.40 M, 7 days; (c) 5 days, 200 °C, Ba(OH)2 0.40 M; (d) 6 days, 200 °C, Ba(OH)2 0.40 M;

Fig. S4 XRD patterns of Ba5Ta4O15: a, SSR; b, hydrothermal method.

Fig S5 TEM, HRTEM and SAED images of the flower-like Ba5Ta4O15 microcrystal.