Supporting Information

Effect of pressure on crystal structure and charge transport properties of 2,6-diphenylanthracene

Kadali Chaitanya and Xue-Hai Ju

Key Laboratory of Soft Chemistry and Functional Materials of MOE, School of Chemical Engineering, Nanjing University of Science and Technology, Nanjing 210094, P. R. China.

Table S1: The Lattice Constants, volume and density obtained at different electric field with GGA/ PBE for 2,6-DPA at Ambient Pressure

| Electric field (V/nm) | a (Å) | b (Å) | c (Å) | α (˚) | β (˚) | γ (˚) | Volume (Å3 ) | Density (g – cm3) | Eg (eV) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | 18.109 | 7.526 | 6.269 | 90 | 90.627 | 90 | 854.52 | 1.284 | 1.651 |
| 0.514 | 18.121 | 7.547 | 6.287 | 90 | 90.301 | 90 | 859.937 | 1.276 | 1.658 |
| 1.54 | 18.116 | 7.530 | 6.261 | 90 | 90.589 | 90 | 854.227 | 1.284 | 1.653 |
| 2.57 | 18.12 | 7.545 | 6.281 | 90 | 90.410 | 90 | 858.88 | 1.277 | 1.657 |
| 3.60 | 18.121 | 7.542 | 6.273 | 90 | 90.524 | 90 | 857.384 | 1.279 | 1.656 |
| 4.63 | 18.107 | 7.546 | 6.263 | 90 | 90.632 | 90 | 855.719 | 1.282 | 1.659 |
| 8.017 | 18.123 | 7.549 | 6.284 | 90 | 90.332 | 90 | 859.911 | 1.276 | 1.651 |

Table S2: Comparison of the molecular geometry obtained with LDA/CA-PZ, GGA/PBE, GGA/PW91, and the experimental data for 2, 6 - DPA at ambient pressure

|  |  |  | Bond lengths |  |  |  |  |  | Bond angles |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Number | Atom1 | Atom2 | Exp | GGA | LDA | PW91 |  | Number | Atom1 | Atom2 | Atom3 | Exp | GGA | LDA | PW91 |
| 1 | C1 | H1 | 0.9498 | 1.0896 | 1.0927 | 1.0874 |  | 1 | H1 | C1 | C2 | 119.41 | 118.66 | 118.69 | 118.54 |
| 2 | C1 | C2 | 1.3901 | 1.3934 | 1.3711 | 1.3826 |  | 2 | H1 | C1 | C6 | 119.5 | 120.67 | 120.92 | 120.89 |
| 3 | C1 | C6 | 1.4014 | 1.4079 | 1.3888 | 1.4013 |  | 3 | C2 | C1 | C6 | 121.09 | 120.66 | 120.39 | 120.54 |
| 4 | C2 | H2 | 0.95 | 1.0896 | 1.0909 | 1.0834 |  | 4 | C1 | C2 | H2 | 119.84 | 119.24 | 119.75 | 119.26 |
| 5 | C2 | C3 | 1.3835 | 1.3952 | 1.3742 | 1.3854 |  | 5 | C1 | C2 | C3 | 120.34 | 120.64 | 120.75 | 120.94 |
| 6 | C3 | H3 | 0.9499 | 1.0914 | 1.0938 | 1.0861 |  | 6 | H2 | C2 | C3 | 119.82 | 120.11 | 119.49 | 119.77 |
| 7 | C3 | C4 | 1.3868 | 1.3964 | 1.3763 | 1.3901 |  | 7 | C2 | C3 | H3 | 120.23 | 120.26 | 119.23 | 118.75 |
| 8 | C4 | H4 | 0.95 | 1.0905 | 1.097 | 1.0898 |  | 8 | C2 | C3 | C4 | 119.49 | 119.44 | 119.69 | 119.56 |
| 9 | C4 | C5 | 1.3894 | 1.3921 | 1.3781 | 1.3925 |  | 9 | H3 | C3 | C4 | 120.27 | 120.3 | 121.08 | 121.68 |
| 10 | C5 | H5 | 0.9498 | 1.0896 | 1.0916 | 1.0866 |  | 10 | C3 | C4 | H4 | 119.91 | 120.74 | 120.22 | 120.61 |
| 11 | C5 | C6 | 1.3989 | 1.4067 | 1.3881 | 1.3996 |  | 11 | C3 | C4 | C5 | 120.27 | 119.91 | 119.56 | 119.45 |
| 12 | C6 | C7 | 1.4886 | 1.48 | 1.4506 | 1.4723 |  | 12 | H4 | C4 | C5 | 119.81 | 119.36 | 120.2 | 119.93 |
| 13 | C7 | C8 | 1.4346 | 1.4295 | 1.4108 | 1.4282 |  | 13 | C4 | C5 | H5 | 119.44 | 118.69 | 119.32 | 118.74 |
| 14 | C7 | C12 | 1.376 | 1.384 | 1.3687 | 1.379 |  | 14 | C4 | C5 | C6 | 121.17 | 121.46 | 121.24 | 121.52 |
| 15 | C8 | H8 | 0.9493 | 1.0892 | 1.0942 | 1.0869 |  | 15 | H5 | C5 | C6 | 119.39 | 119.73 | 119.44 | 119.74 |
| 16 | C8 | C9 | 1.3594 | 1.3652 | 1.3542 | 1.3626 |  | 16 | C1 | C6 | C5 | 117.63 | 117.84 | 118.11 | 117.88 |
| 17 | C9 | H9 | 0.9498 | 1.0919 | 1.0936 | 1.0876 |  | 17 | C1 | C6 | C7 | 120.78 | 120.83 | 120.65 | 120.22 |
| 18 | C9 | C10 | 1.4297 | 1.4234 | 1.403 | 1.417 |  | 18 | C5 | C6 | C7 | 121.59 | 121.3 | 121.21 | 121.83 |
| 19 | C10 | C11 | 1.4376 | 1.4438 | 1.4238 | 1.439 |  | 19 | C6 | C7 | C8 | 120.24 | 119.92 | 120 | 120.61 |
| 20 | C10 | C13 | 1.3947 | 1.3971 | 1.3802 | 1.3921 |  | 20 | C6 | C7 | C12 | 121.67 | 121.71 | 121.43 | 121.41 |
| 21 | C11 | C12 | 1.4267 | 1.4207 | 1.4004 | 1.4133 |  | 21 | C8 | C7 | C12 | 118.06 | 118.35 | 118.52 | 117.91 |
| 22 | C11 | C13 | 1.3998 | 1.4032 | 1.386 | 1.3954 |  | 22 | C7 | C8 | H8 | 119.12 | 119.64 | 119.86 | 120.24 |
| 23 | C12 | H12 | 0.95 | 1.0921 | 1.0968 | 1.0887 |  | 23 | C7 | C8 | C9 | 121.79 | 121.29 | 121.42 | 121.42 |
| 24 | C13 | H13 | 0.9502 | 1.0917 | 1.0955 | 1.0894 |  | 24 | H8 | C8 | C9 | 119.09 | 119.06 | 118.71 | 118.33 |
| 25 | C13 | C11 | 1.3998 | 1.4032 | 1.386 | 1.3954 |  | 25 | C8 | C9 | H9 | 119.44 | 119.88 | 120.17 | 119.73 |
| 26 | C1 | H1 | 0.9498 | 1.0896 | 1.0927 | 1.0874 |  | 26 | C8 | C9 | C10 | 121.05 | 121.34 | 120.88 | 121.34 |
| 27 | C1 | C2 | 1.3901 | 1.3934 | 1.3711 | 1.3826 |  | 27 | H9 | C9 | C10 | 119.51 | 118.77 | 118.93 | 118.93 |
| 28 | C1 | C6 | 1.4014 | 1.4079 | 1.3888 | 1.4013 |  | 28 | C9 | C10 | C11 | 118.03 | 118.23 | 118.2 | 117.93 |
| 29 | C2 | H2 | 0.95 | 1.0896 | 1.0909 | 1.0834 |  | 29 | C9 | C10 | C13 | 122.39 | 121.02 | 122.04 | 122.46 |
| 30 | C2 | C3 | 1.3835 | 1.3952 | 1.3742 | 1.3854 |  | 30 | C11 | C10 | C13 | 119.59 | 120.75 | 119.76 | 119.6 |
| 31 | C3 | H3 | 0.9499 | 1.0914 | 1.0938 | 1.0861 |  | 31 | C10 | C11 | C12 | 118.9 | 118.62 | 119.29 | 118.89 |
| 32 | C3 | C4 | 1.3868 | 1.3964 | 1.3763 | 1.3901 |  | 32 | C10 | C11 | C13 | 118.88 | 118.49 | 119.1 | 119.31 |
| 33 | C4 | H4 | 0.95 | 1.0905 | 1.097 | 1.0898 |  | 33 | C12 | C11 | C13 | 122.17 | 122.9 | 121.55 | 121.74 |
| 34 | C4 | C5 | 1.3894 | 1.3921 | 1.3781 | 1.3925 |  | 34 | C7 | C12 | C11 | 122.03 | 122.06 | 121.28 | 122.16 |
| 35 | C5 | H5 | 0.9498 | 1.0896 | 1.0916 | 1.0866 |  | 35 | C7 | C12 | H12 | 119.03 | 120.14 | 121.49 | 120.62 |
| 36 | C5 | C6 | 1.3989 | 1.4067 | 1.3881 | 1.3996 |  | 36 | C11 | C12 | H12 | 118.95 | 117.67 | 117 | 117.04 |
| 37 | C6 | C7 | 1.4886 | 1.48 | 1.4506 | 1.4723 |  | 37 | C10 | C13 | H13 | 119.19 | 119.36 | 118.99 | 119.2 |
| 38 | C7 | C8 | 1.4346 | 1.4295 | 1.4108 | 1.4282 |  | 38 | C10 | C13 | C11 | 121.54 | 120.77 | 121.14 | 121.08 |
| 39 | C7 | C12 | 1.376 | 1.384 | 1.3687 | 1.379 |  | 39 | H13 | C13 | C11 | 119.27 | 119.87 | 119.86 | 119.7 |
| 40 | C8 | H8 | 0.9493 | 1.0892 | 1.0942 | 1.0869 |  | 40 | H1 | C1 | C2 | 119.41 | 118.66 | 118.69 | 118.54 |
| 41 | C8 | C9 | 1.3594 | 1.3652 | 1.3542 | 1.3626 |  | 41 | H1 | C1 | C6 | 119.5 | 120.67 | 120.92 | 120.89 |
| 42 | C9 | H9 | 0.9498 | 1.0919 | 1.0936 | 1.0876 |  | 42 | C2 | C1 | C6 | 121.09 | 120.66 | 120.39 | 120.54 |
| 43 | C9 | C10 | 1.4297 | 1.4234 | 1.403 | 1.417 |  | 43 | C1 | C2 | H2 | 119.84 | 119.24 | 119.75 | 119.26 |
| 44 | C10 | C11 | 1.4376 | 1.4438 | 1.4238 | 1.439 |  | 44 | C1 | C2 | C3 | 120.34 | 120.64 | 120.75 | 120.94 |
| 45 | C10 | C13 | 1.3947 | 1.3971 | 1.3802 | 1.3921 |  | 45 | H2 | C2 | C3 | 119.82 | 120.11 | 119.49 | 119.77 |
| 46 | C11 | C12 | 1.4267 | 1.4207 | 1.4004 | 1.4133 |  | 46 | C2 | C3 | H3 | 120.23 | 120.26 | 119.23 | 118.75 |
| 47 | C12 | H12 | 0.95 | 1.0921 | 1.0968 | 1.0887 |  | 47 | C2 | C3 | C4 | 119.49 | 119.44 | 119.69 | 119.56 |
| 48 | C13 | H13 | 0.9502 | 1.0917 | 1.0955 | 1.0894 |  | 48 | H3 | C3 | C4 | 120.27 | 120.3 | 121.08 | 121.68 |
|  |  |  |  |  |  |  |  | 49 | C3 | C4 | H4 | 119.91 | 120.74 | 120.22 | 120.61 |
|  |  |  |  |  |  |  |  | 50 | C3 | C4 | C5 | 120.27 | 119.91 | 119.56 | 119.45 |
|  |  |  |  |  |  |  |  | 51 | H4 | C4 | C5 | 119.81 | 119.36 | 120.2 | 119.93 |
|  |  |  |  |  |  |  |  | 52 | C4 | C5 | H5 | 119.44 | 118.69 | 119.32 | 118.74 |
|  |  |  |  |  |  |  |  | 53 | C4 | C5 | C6 | 121.17 | 121.46 | 121.24 | 121.52 |
|  |  |  |  |  |  |  |  | 54 | H5 | C5 | C6 | 119.39 | 119.73 | 119.44 | 119.74 |
|  |  |  |  |  |  |  |  | 55 | C1 | C6 | C5 | 117.63 | 117.84 | 118.11 | 117.88 |
|  |  |  |  |  |  |  |  | 56 | C1 | C6 | C7 | 120.78 | 120.83 | 120.65 | 120.22 |
|  |  |  |  |  |  |  |  | 57 | C5 | C6 | C7 | 121.59 | 121.3 | 121.21 | 121.83 |
|  |  |  |  |  |  |  |  | 58 | C6 | C7 | C8 | 120.24 | 119.92 | 120 | 120.61 |
|  |  |  |  |  |  |  |  | 59 | C6 | C7 | C12 | 121.67 | 121.71 | 121.43 | 121.41 |
|  |  |  |  |  |  |  |  | 60 | C8 | C7 | C12 | 118.06 | 118.35 | 118.52 | 117.91 |
|  |  |  |  |  |  |  |  | 61 | C7 | C8 | H8 | 119.12 | 119.64 | 119.86 | 120.24 |
|  |  |  |  |  |  |  |  | 62 | C7 | C8 | C9 | 121.79 | 121.29 | 121.42 | 121.42 |
|  |  |  |  |  |  |  |  | 63 | H8 | C8 | C9 | 119.09 | 119.06 | 118.71 | 118.33 |
|  |  |  |  |  |  |  |  | 64 | C8 | C9 | H9 | 119.44 | 119.88 | 120.17 | 119.73 |
|  |  |  |  |  |  |  |  | 65 | C8 | C9 | C10 | 121.05 | 121.34 | 120.88 | 121.34 |
|  |  |  |  |  |  |  |  | 66 | H9 | C9 | C10 | 119.51 | 118.77 | 118.93 | 118.93 |
|  |  |  |  |  |  |  |  | 67 | C9 | C10 | C11 | 118.03 | 118.23 | 118.2 | 117.93 |
|  |  |  |  |  |  |  |  | 68 | C9 | C10 | C13 | 122.39 | 121.02 | 122.04 | 122.46 |
|  |  |  |  |  |  |  |  | 69 | C11 | C10 | C13 | 119.59 | 120.75 | 119.76 | 119.6 |
|  |  |  |  |  |  |  |  | 70 | C13 | C11 | C10 | 118.88 | 118.49 | 119.1 | 119.31 |
|  |  |  |  |  |  |  |  | 71 | C13 | C11 | C12 | 122.17 | 122.9 | 121.55 | 121.74 |
|  |  |  |  |  |  |  |  | 72 | C10 | C11 | C12 | 118.9 | 118.62 | 119.29 | 118.89 |
|  |  |  |  |  |  |  |  | 73 | C7 | C12 | C11 | 122.03 | 122.06 | 121.28 | 122.16 |
|  |  |  |  |  |  |  |  | 74 | C7 | C12 | H12 | 119.03 | 120.14 | 121.49 | 120.62 |
|  |  |  |  |  |  |  |  | 75 | C11 | C12 | H12 | 118.95 | 117.67 | 117 | 117.04 |
|  |  |  |  |  |  |  |  | 76 | C11 | C13 | C10 | 121.54 | 120.77 | 121.14 | 121.08 |
|  |  |  |  |  |  |  |  | 77 | C11 | C13 | H13 | 119.27 | 119.87 | 119.86 | 119.7 |
|  |  |  |  |  |  |  |  | 78 | C10 | C13 | H13 | 119.19 | 119.36 | 118.99 | 119.2 |

Figure S1: Hirshfeld surfaces and derived fingerprint plots (dnorm) of 2, 6 – DPA at 0 – 10 GPa. Fingerprint plots show the distance from the Hirshfeld surface to the nearest nucleus inside of the surface (di) and from the Hirshfeld to the nucleus outside of the surface (de). Contraction of the crystal contacts is clearly visible by a general shift of the plot to smaller de/di values. The longer contacts outside the surface (de) are decreased between the ambient pressure (ca 2.4 Å) and 10 GPa (2.0-2.2 Å). A similar compression is observed for the di type contacts (from 2.4 Å to 2.0 Å).

Figure S2. Electronic spectra calculated at the CAM-B3LYP/6-31G(d,p) level  for (a) an isolated molecule, dimers in the d1 and d2 directions of 2,6-DPA at ambient condition and for (b) the dimer in the d2 direction of 2,6-DPA at different hydrostatic pressures.

Figure S3:. The self-consistent band structures of 2,6-DPA crystal under diﬀerent pressures. The Fermi energy is shown as a dashed horizontal line.

# Footnotes

E-mail: xhju@njust.edu.cn; Fax: +86-25-84431622; Tel: +86-25-84315947-801