Supporting Information

Aerosol Synthesis of Phase Pure Iodine/Iodic Biocide Microparticles Tao Wu, Andrew SyBing, Xizheng Wang and Michael R. Zachariah)

Department of Chemistry and Biochemistry and Department of Chemical and Biomolecular Engineering, University of Maryland, College Park, MD 20742, USA

FIG. S1. The SEM images and XRD pattern of as-received HIO3

FIG. S2. TGA and DSC curves of HIO3 under argon environment at a heating rate of 5 ºC/min.

002

210

21-1

11-1

11-1

21-1

210

011

-121

103

200

103

-121

200

110

200

FIG. S3. The XRD patterns of HIO3 at different temperatures

A                                                                                  B

212

012

102

110

C

FIG. S4. TGA/DSC (A) and XRD (B) of as-prepared I4O9• xH2O before vacuum drying treatment and XRD (C) of as-prepared I4O9• xH2O and as-received HIO3.

-121

103

200

012

002

110

A                                                                                         B

-121

103

200

-121

103

200

C                                                                                   D

103

-121

200

200

103

-121

E                                                                                F

FIG. S5. XRD patterns of the product by annealing of HIO3 at 139 (A), 150 (B), 180 (C) and 260 °C (D) for one hour, respectively. XRD patterns of the product by annealing of HIO3 at 150 (E) and 180 (F) for two minutes, respectively.

Table SI. Listed hkl values for each phase in each XRD pattern.

| PDF#22-0338 I2O5 |  | PDF#21-1126 HI3O8 |  |
| --- | --- | --- | --- |
| 2θ (º) | hkl values | 2θ (º) | hkl values |
| 21.29 | -111 | 22.72 | 112 |
| 1.87 | -102 | 23.14 | 020 |
| 22.9 | 002 | 23.58 | 200 |
| 24.4 | 210 | 26.27 | 103 |
| 24.71 | -211 | 27.16 | -121 |
| 26.67 | 102 | 28.03 | 022 |
| 28.13 | -112 | 35.26 | 123 |
| 28.77 | -302 | 36.88 | -222 |
| 28.96 | 012 | 43.71 | 321 |
| 29.06 | 211 |  |  |
| 29.94 | -212 |  |  |
| 33.86 | -312 |  |  |
| 33.99 | 400 |  |  |
| 35.02 | -402 |  |  |
| 37.04 | 212 |  |  |
| 37.3 | 021 |  |  |
| 38.5 | 410 |  |  |

Address all correspondence to this author.

e-mail: mrz@umd.edu