Electronic Supplementary Information (ESI) for

Zinc cobalt bimetallic nanoparticles embedded in porous nitrogen-doped carbon frameworks for the reduction of nitro compounds

Xuejuan Xu, Hui Li, Hongtao Xie, Yuhua Ma, Tingxiang Chen, Jide Wang *

Key Laboratory of Oil and Gas Fine Chemicals, Ministry of Education & Xinjiang Uygur

Autonomous Region, College of Chemistry and Chemical Engineering of Xinjiang University, Urumqi, 830046, China.

E-mail: awangjd@sina.cn(J.D.Wang);

270997380@qq.com(X. J. Xu);

Tel/Fax: +86-991-8582087

FIG.S1. Elemental mapping of Zn0.3Co2.7-ZIF.

FIG.S2. EDS spectrum and Element content of the Zn0.3Co2.7-ZIF.

FIG.S3. TG curve under N2 condition of Zn0.3Co2.7-ZIF.

FIG.S4. Elemental mapping of Zn0.3Co2.7@NC.

FIG.S5. EDS spectrum and Element content of Zn0.3Co2.7@NC.

FIG.S6. Spectrogram of the reduction reaction for the conversion of 2-NP catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S7. Spectrogram of the reduction reaction for the conversion of 2, 4-dinitrophenol catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S8. Spectrogram of the reduction reaction for the conversion of 3-nitroaniline catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S9. Spectrogram of the reduction reaction for the conversion of p-nitrotoluene catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S10. Spectrogram of the reduction reaction for the conversion of p-chloronitrobenzene catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S11. Spectrogram of the reduction reaction for the conversion of p-nitrobenzaldehyde catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S12. Spectrogram of the reduction reaction for the conversion of p-nitroacetophenone catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S13. Spectrogram of the reduction reaction for the conversion of p-nitrophenylacetonitrile catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S14. Spectrogram of the reduction reaction for the conversion of 5-nitroindole catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S15. Spectrogram of the reduction reaction for the conversion of 6-nitrobenzoimidazole catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIGGURE CAPTION:

FIG.S1. Elemental mapping of Zn0.3Co2.7-ZIF.

FIG.S2. EDS spectrum and Element content of the Zn0.3Co2.7-ZIF.

FIG.S3. TG curve under N2 condition of Zn0.3Co2.7-ZIF.

FIG.S4. Elemental mapping of Zn0.3Co2.7@NC.

FIG.S5. EDS spectrum and Element content of Zn0.3Co2.7@NC.

FIG.S6. Spectrogram of the reduction reaction for the conversion of 2-NP catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S7. Spectrogram of the reduction reaction for the conversion of 2, 4-dinitrophenol catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S8. Spectrogram of the reduction reaction for the conversion of 3-nitroaniline catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S9. Spectrogram of the reduction reaction for the conversion of p-nitrotoluene catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S10. Spectrogram of the reduction reaction for the conversion of p-chloronitrobenzene catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S11. Spectrogram of the reduction reaction for the conversion of p-nitrobenzaldehyde catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S12. Spectrogram of the reduction reaction for the conversion of p-nitroacetophenone catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S13. Spectrogram of the reduction reaction for the conversion of p-nitrophenylacetonitrile catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S14. Spectrogram of the reduction reaction for the conversion of 5-nitroindole catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).

FIG.S15. Spectrogram of the reduction reaction for the conversion of 6-nitrobenzoimidazole catalyzed by Zn0.3Co2.7@NC in the presence of NaBH4 (T= 25℃, the amount of the catalyst is 0.02 mg/ml).