Supplementary Materials

Controlled synthesis and photocatalytic performance of waxberry-like Ni11(HPO3)8(OH)6 microballs

Yu Zhang1,2, Zhijian Peng1,*, Xiuli Fu2,*

1 School of Engineering and Technology, China University of Geosciences, Beijing 100083, PR China

2 State Key Laboratory of Information Photonics and Optical Communications, and School of Science,Beijing University of Posts and Telecommunications, Beijing 100876, P. R. China

3School of Science, China University of Geosciences, Beijing 100083, PR China

The authors would like to thank the financial support for this work from the National Natural Science Foundation of China (grant nos. 11274052, 11674035, and 61274015), and Fund of State Key Laboratory of Information Photonics and Optical Communications (Beijing University of Posts and Telecommunications).

Yu Zhang, et al., Journal of Materials Research, Figure S1

Figure S1. Variation of capacitance (C) with the applied potential in 3 M KOH presented in the Mott Schottky relationship for Ni11(HPO3)8(OH)6. The capacitance was determined by electrochemical impedance spectroscopy.

Yu Zhang, et al., Journal of Materials Research, Figure S2

Figure S2. Plots of (a) (αhν)2 and (b) (αhν)0.5 against the photon energy (hν) for Ni11(HPO3)8(OH)6 photocatalyst.

Yu Zhang, et al., Journal of Materials Research, Table S1

Table S1. Comparison of the photocatalytic performance of the Ni11(HPO3)8(OH)6 photocatalysts for organic dyes (MB and RhB) with that of reported commonly photocatalysts tested under similar conditions.

| Catalysts | Light source | Catalyst concentration (g/L) | Decolorization rate , K (min-1) | Ref. |
| --- | --- | --- | --- | --- |
|  |  |  | MB | RhB |  |
| Ni11(HPO3)8(OH)6 | 500 W mercury lamp | 1 | 73.9% in 90 min, 0.0143 | 48.3% in 90 min, 0.00661 | This work |
| TiO2/MoO3 | 500 W Xe lamp | 1 | - | 91.49% in 150 min, 0.0118 | [S1] |
| TiO2-rGO-PDMAA | 300 W Xe lamp | 2 | 100% in 100 min, 0.0516 | - | [S2] |
| N-doped TiO2 | ultraviolet lamp | 0.2 | 91% in 60 min, 0.044 | - | [S3] |
| N-doped TiO2 | 400 W tungsten halogen lamp (λ≥420nm) | 1 | - | 50% in 120 min, - | [S4] |
| Fe3O4/ZnO/Ag3VO4/AgI | 50 W LED source | 0.4 | -, 0.0236 | 100% in 70min, 0.044 | [S5] |
| ZnO nanorod | 400 W UV lamp | 0.2 | 92.2% in120 min, 0.0027 | - | [S6] |

References

[S1] H. Liu, T. Lv, C.k. Zhu, and Z.F. Zhu: Direct bandgap narrowing of TiO2/MoO3 heterostructure composites for enhanced solar-driven photocatalytic activity. Sol. Energ. Mat. Sol. C 153, 1 (2016).

[S2] D.B. Wu, M. Yi, H.Y. Duan, J.Y. Xu, and Q.G. Wang: Tough TiO2-rGO-PDMAA nanocomposite hydrogel via one-pot UV polymerization and reduction for photodegradation of methylene blue. Carbon 108, 394 (2016).

[S3] N.C.T. Martins, J. Angelo, A.V Girao, T. Trindade,L. Andrade, and A. Mendes: N-doped carbon quantum dots/TiO2 composite with improved photocatalytic activity. Appl. Catal. B-environ. 193, 67 (2016).

[S4] O. Ruzimuradov, S. Nurmanov, M. Hojamberdiev, R.M. Prasad, A. Gurlo, J. Broetz, K. Nakanishi, and R. Riedel: Fabrication of nitrogen-doped TiO2 monolith with well-defined macroporous and bicrystalline framework and its photocatalytic performance under visible light. J. Eur. Ceram. Soc. 34, 809 (2014).

[S5] A. Habibi-Yangjeh, and M. Shekofteh-Gohari: Fe3O4/ZnO/Ag3VO4/AgI nanocomposites: Quaternary magnetic photocatalysts with excellent activity in degradation of water pollutants under visible light. Sep. Purif. Technol. 166, 63 (2016).

[S6] S. Ghayempour, M. Montazer, and M.M. Rad: Tragacanth Gum Biopolymer as Reducing and Stabilizing Agent in Biosonosynthesis of Urchin-like ZnO Nanorod Arrays: A Low Cytotoxic Photocatalyst with Antibacterial and Antifungal Properties. Carbohyd. Polym. 136, 232 (2016).

# Text boxes

(b)

(a)