Supplementary Material

One-pot synthesis of in situ carbon decorated Cu3P particles with enhanced electrocatalytic hydrogen evolution performance

Mingyu Pi

College of Physics, Chongqing University, Chongqing, 401331, China;

Tao Yang

College of Chemical Engineering, Chongqing University, Chongqing, 401331, China;

Shuxia Wang and Shijian Chen*

College of Physics, Chongqing University, Chongqing, 401331, China.

*Corresponding author: Dr. Shijian Chen, E-mail: sjchen@cqu.edu.cn, Tel: +86-2365678362.

Fig. S1. (a) Nitrogen adsorption/desorption isotherm and (b) the pore-size distribution curve of the Cu3P@C hybrid.

Fig. S2. (a) SEM and (b) TEM images for the pure Cu3P nanoparticles.

Fig. S3. Mechanism picture for electrocatalytic H2 evolution over carbon decorated Cu3P particles.

Table 1. Comparison of HER performance for the Cu3P@C with other reported Cu3P catalysts (NWs: nanowires, NSs: nanosheets, NPs: nanoparticles and NCs: nanocubes).

| Catalyst | Current Density (mA cm-2) | Corresponding overpotential (mV) | Reference |
| --- | --- | --- | --- |
| Cu3P@C | 10 | 203 | This work |
| Cu3P |  | 263 |  |
| Cu3P NWs/CF | 10 | 143 | Angew. Chem. Int. Ed., 2014, 53, 9577-9581 |
| Cu3P NSs/NF | 10 | 105 | ACS Appl. Mater. Interfaces, 2017, 9, 2240-2248 |
| Cu3P NCs | 10 | ~300 | RSC Adv., 2016, 6, 9672-9677 |
| Cu3P NPs | 10 | ~350 | Electrochim. Acta,2016, 199, 99-107 |