Supporting Information for

Intercalation Makes the Difference with TiS2: Boosting Electrocatalytic Water Oxidation Activity Through Co Intercalation

Dr. Aron J. Huckaba,*,a Maryline Ralaiarisoa,b Cho Kyung Taek,a Dr. Emad Oveisi,c Prof. Norbert Koch,b Prof. M. K. Nazeeruddina

# a Dr. Aron J. Huckaba, Cho Kyung Taek, Prof. M.K. Nazeeruddin

GMF, Institute of Chemical Sciences and Engineering, EPFL Valais, Rue de L’Indutrie, 1951 Sion, Switzerland

# b Maryline Ralaiarisoa, Prof. Norbert Koch

Humboldt Universitat zu Berlin, Institut für Physik & IRIS Adlershof , Brook-Taylor-Strasse 6, 12489 Berlin, Germany

c Dr. Emad Oveisi

Interdisciplinary Centre for Electron Microscopy, EPFL, 1015 Lausanne, Switzerland

Table of Contents

Figure S1. SEM image of a: CoTiS2 materials cast on FTO substrate.  b: TiS2 materials cast on FTO substrate. c: CuTiS2 materials cast on FTO substrate.  d: Cross-Sectional image of as-prepared CoTiS2 film measured at 2 kV. e: Cross-Sectional image of as-prepared CoTiS2 film measured at 2 kV. f: Cross-Sectional EDX image of as-prepared CoTiS2 film with C, Ti, Co, S, Sn, Si indicated. ………………………………………………..………………..……..3

Figure S2. Left panel: secondary electron cut-offs (SECO) and right panel: large range valence band spectrum of TiS2 on FTO.1 The inset shows the valence band spectrum in the lower binding energy region…………………….……….…………………………………...……………………….3

Figure S3. XPS core level spectra of O 1s, C 1s, and Sn 3d5/2 in CuTiS2 (a, b, and c, respectively) and in CoTiS2 (d, e, and f, respectively). The Sn 3d5/2 intensity is detected from the underlying FTO substrate. …………….……….………………..………………………...4

Figure S4. Left: Cyclic Voltammetry measurement of as-prepared and oxidized TiS2 thin films in 1 M NaOH under O2 as collected (reference to Ag/AgCl). Right: Chronoamperometry measurement of as-prepared and oxidized TiS2 thin films in 1M NaOH under O2 as collected (reference to Ag/AgCl). .……………………………………..………………………...………………………………..4

Figure S5. Cyclic Voltammetry measurement of pristine and oxidized TiS2 thin films in 1 M NaOH under O2. Left: in reference to NHE. Right: Data as collected (reference to Ag/AgCl).5

Figure S6. Chronoamperometric measurement of pristine TiS2 materials in 1 M NaOH under O2 atmosphere at 10 mAcm-2. Left: in reference to NHE. Right: Data as collected (reference to Ag/AgCl).…………..…………………………………………………..………………….......5

Figure S7. Chronoamperometric measurement of pristine CoTiS2 in 1 M NaOH under O2 atmosphere at 10 mAcm-2.  ……………………….……………………………………….….5

Figure S8. Linear Scan Voltammetry scan of oxidized CoTiS2 thin film in 1 M NaOH under O2 atmosphere at 10mV/s. . ………………….….……..……………..……………………….6

Figure S9. Tafel Plot derived from chronoamperometry data of oxidized CoTiS2 thin film in 1 M NaOH under O2 atmosphere. …………………………………..……….……………….…………………………………....6

Figure S1. SEM image of a: CoTiS2 materials cast on FTO substrate.  b: TiS2 materials cast on FTO substrate. c: CuTiS2 materials cast on FTO substrate.  d: Cross-Sectional image of as-prepared CoTiS2 film measured at 2 kV. e: Cross-Sectional image of as-prepared CoTiS2 film measured at 2 kV. f: Cross-Sectional EDX image of as-prepared CoTiS2 film with C, Ti, Co, S, Sn, Si indicated.

Figure S2. Left panel: secondary electron cut-offs (SECO) and right panel: large range valence band spectrum of TiS2 on FTO.1 The inset shows the valence band spectrum in the lower binding energy region

Figure S3. XPS core level spectra of O 1s, C 1s, and Sn 3d5/2 in CuTiS2 (a, b, and c, respectively) and in CoTiS2 (d, e, and f, respectively). The Sn 3d5/2 intensity is detected from the underlying FTO substrate.

Figure S4. Left: Cyclic Voltammetry measurement of as-prepared and oxidized TiS2 thin films in 1 M NaOH under O2 as collected (reference to Ag/AgCl). Right: Chronoamperometry measurement of as-prepared and oxidized TiS2 thin films in 1M NaOH under O2 as collected (reference to Ag/AgCl).

Figure S5. Cyclic Voltammetry measurement of pristine and oxidized TiS2 thin films in 1 M NaOH under O2. Left: in reference to NHE. Right: Data as collected (reference to Ag/AgCl).

Figure S6. Chronoamperometric measurement of pristine TiS2 materials in 1 M NaOH under O2 atmosphere at 10 mAcm-2. Left: in reference to NHE. Right: Data as collected (reference to Ag/AgCl).

Figure S7. Chronoamperometric measurement of as preparedCoTiS2 in 1 M NaOH under O2 atmosphere at 10 mAcm-2.

Figure S8. Linear Scan Voltammetry scan of oxidized CoTiS2 thin film in 1 M NaOH under O2 atmosphere at 10mV/s.

Figure S9. Tafel Plot derived from chronoamperometry data of oxidized CoTiS2 thin film in 1 M NaOH under O2 atmosphere.

References

1.	A. J. Huckaba, S. Gharibzadeh, M. Ralaiarisoa, C. Roldan-Carmona, N. Mohammadian, G. Grancini, Y. Lee, P. Amsalem, E. J. Plichta, N. Koch, A. Moshaii, and M. K. Nazeeruddin: Low cost TiS2 as Hole Transport Material for Perovskite Solar Cells. Small Methods. Published Online September 12, 2017.