Supporting Information for

### Paulownia tomentosa derived porous carbon with enhanced sodium storage

Pan Wanga,b, Xifei Li*a,b, Xiaojia Lia,b, Hui Shanb, Dejun Li*a, Xueliang Sun*c,a

aTianjin International Joint Research Centre of Surface Technology for Energy Storage Materials, College of Physics and Materials Science, Tianjin Normal University, Tianjin 300387, China E-mail: xfli2011@hotmail.com 
bInstitute of Advanced Clean Energy, Xi'an University of Technology, Xi'an 710048, China 
cNanomaterials and Energy Lab, Department of Mechanical and Materials Engineering, Western University, London, Ontario, N6A 5B9, Canada, E-mail: xsun9@uwo.ca

Fig. S1 SEM images of the as-obtained PTPC-5h.

Fig. S2 Cycle performance of PTPC-3, PTPC-4, PTPC-5 and PTPC-7 electrodes at a current density of 0.05 A g-1.

To optimize the mass ratio of PTPC electrode, more representative samples were designed, which were denoted as PTPC-3, PTPC-4, PCPT-5 and PTPC-7. Fig. S2 compared the cycle performance of different samples. The PTPC-3 and PTPC-7 almost exhibited the similar specific capacities after 100 cycles, as a result, we chose the mass ratio of 1:4, 1:5 and 1:7, rather than 1:3, 1:5 and 1:7 to further optimize electrochemical performance.

Table. S1 Kinetic parameters at various cycles of PTPC-5 electrodes

| Cycle | Rs (Ω) | Rct (Ω) | Zw (Ω) |
| --- | --- | --- | --- |
| 0 | 10.95 | 585.9 | 1010 |
| 1st | 4.638 | 189.1 | 2270 |
| 4th | 4.589 | 179.7 | 5473 |
| 15th | 2.978 | 166.5 | 5207 |
| 50th | 6.287 | 171.5 | 2393 |