Supporting Information

Wetting and brazing of Ni-coated WC–8Co cemented carbide using Cu–19Ni–5Al alloy as filler metal：Microstructural evolution and joint mechanical properties

Zhang Xiangzhao1, Huang Zhikun1, Liu Guiwu1,*, Wang Tingting1, Yang Jian1, Shao Haicheng1, Qiao Guanjun1,2,*

1School of materials Science and Engineering, Jiangsu University, Zhenjiang 212013, China

2State Key Laboratory for Mechanical Behavior of Materials, Xi’an Jiaotong University, Xi’an 710049, China

China

E-mail address: gwliu76@ujs.edu.cn (G.W. Liu); gjqiao@ujs.edu.cn (G.J. Qiao).

TABLE SI. Chemical compositions of phases in the interlayer marked in Fig. 4

| Position | Composition (at.%) |
| --- | --- |
|  | Cu | Al | Ni | Co | Fe |
| A | 12.2 | 19.5 | 30.5 | 29.3 | 8.5 |
| B | 80.4 | 10.9 | 7.1 | - | 1.6 |
| C | 50.1 | 15.1 | 22.4 | 4.6 | 7.8 |
| D | 9.2 | 19.3 | 29.6 | 28.2 | 13.7 |