Supplementary Information

FIG. S1. NH3-TPD profiles of different catalysts.

FIG. S2. Stability test of the catalysts within SO2 and H2O.

FIG. S3. Stability test of the catalysts within 30 h at 250 °C.

TABLE S1 Quantitative analysis of the H2-TPR profiles of samples.

| Simples | Peak Ⅰ(A) |  | Peak Ⅱ(A) |  |
| --- | --- | --- | --- | --- |
|  | ① ② ③ | Total | ④ ⑤ | Total |
| Ce/MnTiOx/ATP | 1.8 4.1 2.1 | 8.0 | 0.5 0.2 | 0.7 |
| Ce-MnTiOx/ATP | 4.0 2.2 1.9 | 8.1 | 2.1 0.5 | 2.6 |

TABLE S2 NH3 absorption capacity of the catalyst samples.

| Samples | NH3-TPD results (mmol g-1) |
| --- | --- |
| Ce/MnTiOx/ATP | 115-295 °C | 295-570 °C | 570-800 °C | Total |
|  | 0.160 | 0.149 | 0.136 | 0.445 |
| Ce-MnTiOx/ATP | 115-325 °C | 325-650 °C | 650-800 °C | Total |
|  | 0.158 | 0.174 | 0.148 | 0.480 |