SUPPLEMENTARY MATERIAL

Toward the design of interstitial nonmetals co-doping for Mg-based hydrides as hydrogen storage material

Zhen Wu, Luying Zhu and Fusheng Yang

School of Chemical Engineering and Technology, Xi’an Jiaotong University, Xi’an 710049, P. R. China

Serge N. Nyamsi,

HySA Systems Competence Centre, South African Institute for Advanced Materials Chemistry (SAIAMC), University of the Western Cape, Bellville, 7535, South Africa

E Porpatham,

School of Mechanical Engineering, VIT University, Vellore, 632014, India

Zaoxiao Zhang*

State Key Laboratory of Multiphase Flow in Power Engineering, School of Chemical Engineering and Technology, Xi’an Jiaotong University, Xi’an 710049, P. R. China

*Corresponding author, Email: zhangzx@mail.xjtu.edu.cn Fax(Tel):86-29-82660689

FIG. S1. Crystal structures of pure Mg2Ni and its hydride unit cells. (a) Mg2Ni, and (b) Mg2NiH4. (green - Mg, blue - Ni, cyan - H) (Color online)

FIG. S2. Relationship between the cutoff energy and total energy. (Color online)

FIG. S3. Variations of the free energy with temperature for the pure Mg2Ni and its hydride and their B+N co-doped counterparts. (a) Mg2Ni and Mg2NiB0.25N0.25, and (b) Mg2NiH4 and Mg2NiB0.25N0.25H4. (Color online)

TABLE SⅠ. Atomic positions of the atoms Mg and Ni in Mg2Ni unit cell with the space group P6222.

| Atom | Wyckoff position | x | y | z |
| --- | --- | --- | --- | --- |
| Mg1 | 6f | 0.5 | 0 | 1/9 |
| Mg2 | 6i | 1/6 | 1/3 | 0 |
| Ni1 | 3b | 0 | 0 | 1/6 |
| Ni2 | 3d | 0 | 0.5 | 1/6 |

TABLE SⅡ. Atomic positions of the atoms Mg, Ni and H in Mg2NiH4 unit cell with the space group C2/c.

| Atom | Wyckoff position | x | y | z |
| --- | --- | --- | --- | --- |
| Mg1 | 8f | 0.2652 | 0.4827 | 0.0754 |
| Mg2 | 4e | 0 | 0.0144 | 0.25 |
| Mg3 | 4e | 0 | 0.5130 | 0.25 |
| Ni | 8f | 0.1194 | 0.2308 | 0.0832 |
| H1 | 8f | 0.2113 | 0.2995 | 0.3037 |
| H2 | 8f | 0.1360 | 0.3163 | 0.8811 |
| H3 | 8f | 0.0105 | 0.2868 | 0.0537 |
| H4 | 8f | 0.1306 | 0.995 | 0.0815 |

TABLE SⅢ. Total energies of Mg2NiB0.25N0.25 and Mg2NiB0.25N0.25H4 with all possible interstitial sites of co-doping B and N after the geometry optimization.

| Crystals | Total energies of the primitive cell (eV) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Mg2NiB0.25N0.25 | 2-#1 | 2-#2 | 2-#3 | 2-#4 | 2-#5 | 2-#6 |
|  | -3389.32 | -3389.38 | -3388.52 | -3388.47 | -3389.22 | -3389.02 |
| Mg2NiB0.25N0.25H4 | 3-#1 | 3-#2 | 3-#3 | 3-#4 | 3-#5 | 3-#6 |
|  | -3456.87 | -3456.86 | -3456.79 | -3456.85 | -3456.82 | -3456.90 |

TABLE SⅣ. Atomic positions in Mg2NiB0.25N0.25unit cell with the space group P6222.

| Label | Atom | x | y | z |
| --- | --- | --- | --- | --- |
| Mg1 | Mg | 0.5000 | 0.0000 | 0.1110 |
| Mg2 | Mg | 0.0000 | 0.5000 | 0.7777 |
| Mg3 | Mg | 0.5000 | 0.5000 | 0.4443 |
| Mg4 | Mg | -0.0000 | 0.5000 | 0.5557 |
| Mg5 | Mg | 0.5000 | 0.0000 | 0.8890 |
| Mg6 | Mg | 0.5000 | 0.5000 | 0.2223 |
| Mg7 | Mg | 0.1665 | 0.3330 | 0.0000 |
| Mg8 | Mg | 0.6670 | 0.8335 | 0.6667 |
| Mg9 | Mg | 0.1665 | 0.8335 | 0.3333 |
| Mg10 | Mg | 0.8335 | 0.6670 | 0.0000 |
| Mg11 | Mg | 0.3330 | 0.1665 | 0.6667 |
| Mg12 | Mg | 0.8335 | 0.1665 | 0.3333 |
| Ni1 | Ni | 0.0000 | 0.0000 | 0.1667 |
| Ni2 | Ni | 0.0000 | 0.0000 | 0.8333 |
| Ni3 | Ni | 0.0000 | 0.0000 | 0.5000 |
| Ni4 | Ni | 0.0000 | 0.5000 | 0.1667 |
| Ni5 | Ni | 0.5000 | 0.5000 | 0.8333 |
| Ni6 | Ni | 0.5000 | 0.0000 | 0.5000 |
| NE1b | B0.5N0.5a | 0.5000 | 0.5000 | 0.3333 |
| NE2b | B | 0.5000 | 0.0000 | 0.0000 |
| NE3b | N | 0.0000 | 0.5000 | 0.6667 |

a: The atom consists of 50% B and 50% N

b: 3c Wyckoff position for interstitial nonmetals

TABLE SⅤ. Atomic positions in Mg2NiB0.25N0.25H4 unit cell with the space group C2/c.

| Label | Atom | x | y | z |
| --- | --- | --- | --- | --- |
| Mg1 | Mg | 0.2652 | 0.4827 | 0.0754 |
| Mg2 | Mg | 0.7652 | 0.9827 | 0.0754 |
| Mg3 | Mg | 0.7348 | 0.4827 | 0.4246 |
| Mg4 | Mg | 0.2348 | 0.9827 | 0.4246 |
| Mg5 | Mg | 0.7348 | 0.5173 | 0.9246 |
| Mg6 | Mg | 0.2348 | 0.0173 | 0.9246 |
| Mg7 | Mg | 0.2652 | 0.5173 | 0.5754 |
| Mg8 | Mg | 0.7652 | 0.0173 | 0.5754 |
| Mg9 | Mg | 0.0000 | 0.0244 | 0.2500 |
| Mg10 | Mg | 0.0000 | 0.5130 | 0.2500 |
| Mg11 | Mg | 0.5000 | 0.5244 | 0.2500 |
| Mg12 | Mg | 0.5000 | 0.0130 | 0.2500 |
| Mg13 | Mg | 0.0000 | 0.9756 | 0.7500 |
| Mg14 | Mg | 0.0000 | 0.4870 | 0.7500 |
| Mg15 | Mg | 0.5000 | 0.4756 | 0.7500 |
| Mg16 | Mg | 0.5000 | 0.9870 | 0.7500 |
| Ni1 | Ni | 0.1194 | 0.2308 | 0.0832 |
| Ni2 | Ni | 0.6194 | 0.7308 | 0.0832 |
| Ni3 | Ni | 0.8806 | 0.2308 | 0.4168 |
| Ni4 | Ni | 0.3806 | 0.7308 | 0.4168 |
| Ni5 | Ni | 0.8806 | 0.7692 | 0.9168 |
| Ni6 | Ni | 0.3806 | 0.2692 | 0.9168 |
| Ni7 | Ni | 0.1194 | 0.7692 | 0.5832 |
| Ni8 | Ni | 0.6194 | 0.2692 | 0.5832 |
| H1 | H | 0.2113 | 0.2995 | 0.3037 |
| H2 | H | 0.1360 | 0.3163 | -0.1189 |
| H3 | H | 0.0105 | 0.2868 | 0.0537 |
| H4 | H | 0.1306 | -0.0050 | 0.0815 |
| H5 | H | 0.7113 | 0.7995 | 0.3037 |
| H6 | H | 0.6360 | 0.8163 | -0.1189 |
| H7 | H | 0.5105 | 0.7868 | 0.0537 |
| H8 | H | 0.6306 | 0.4950 | 0.0815 |
| H9 | H | 0.7887 | 0.2995 | 0.1963 |
| H10 | H | 0.8640 | 0.3163 | 0.6189 |
| H11 | H | 0.9895 | 0.2868 | 0.4463 |
| H12 | H | 0.8694 | -0.0050 | 0.4185 |
| H13 | H | 0.2887 | 0.7995 | 0.1963 |
| H14 | H | 0.3640 | 0.8163 | 0.6189 |
| H15 | H | 0.4895 | 0.7868 | 0.4463 |
| H16 | H | 0.3694 | 0.4950 | 0.4185 |
| H17 | H | 0.7887 | 0.7005 | 0.6963 |
| H18 | H | 0.8640 | 0.6837 | 1.1189 |
| H19 | H | 0.9895 | 0.7132 | 0.9463 |
| H20 | H | 0.8694 | 1.0050 | 0.9185 |
| H21 | H | 0.2887 | 0.2005 | 0.6963 |
| H22 | H | 0.3640 | 0.1837 | 1.1189 |
| H23 | H | 0.4895 | 0.2132 | 0.9463 |
| H24 | H | 0.3694 | 0.5050 | 0.9185 |
| H25 | H | 0.2113 | 0.7005 | 0.8037 |
| H26 | H | 0.1360 | 0.6837 | 0.3811 |
| H27 | H | 0.0105 | 0.7132 | 0.5537 |
| H28 | H | 0.1306 | 1.0050 | 0.5815 |
| H29 | H | 0.7113 | 0.2005 | 0.8037 |
| H30 | H | 0.6360 | 0.1837 | 0.3811 |
| H31 | H | 0.5105 | 0.2132 | 0.5537 |
| H32 | H | 0.6306 | 0.5050 | 0.5815 |
| NE1a | B | 0.7500 | 0.2500 | 0.5000 |
| NE2a | B | 0.2500 | 0.7500 | 0.5000 |
| NE3a | N | 0.2500 | 0.2500 | 0.0000 |
| NE4a | N | 0.7500 | 0.7500 | 0.0000 |

a: 4c Wyckoff position for interstitial nonmetals