Supplementary material for Journal of Materials Research

A green, steam-modified delignification method to low lignin delignified wood for thick, large, high transparent wood composites

Huayang Li, Xuelian Guo, Yuming He, Rongbo Zheng*

a Yunnan Province Key Laboratory of Wood Adhesives and Glued Products, College of Chemical Engineering, Southwest Forestry University, Kunming 650224, P. R. China.

b Wetland college, Southwest Forestry University, Kunming 650224, P. R. China.

*Corresponding author. E-mail: rbzheng@swfu.edu.cn.Tel: +86-87163863377

Supporting Information

Figures

Figure S1. The color changes of Ra-pine during the H2O2 steam delignification process.

Figure S2. The remaining lignin content of Ra-pinewood during the steam-based delignification process.

Figure S3. Optical images of 5 pieces of Ra delignified basswoods with dimension of 100 mm x 50 mm x 20 mm obtained by H2O2 steam delignification process.

Figure S4. Optical properties of a 210 mm × 190 mm x 0.8 mm thick Ro-type transparent wood composite.

Figure S5. Optical image of a 0.8 mm thick Ro-type transparent wood sample with size of 210 mm × 190 mm on A4 sheet with text (the font is 12).

Figure S6. Optical transmittance of a 2 mm thick epoxy resin film.

Table S1 The summary of solution-based delignification for different wood samples.

| Wood species/ chemicals | Wood dimension / mm | Delignification time / h | Lignin content/% |
| --- | --- | --- | --- |
| Balsa/ NaClO2 [3] | 50 x 50 x 0.7-8.0 a | 6 (below 3 mm) 12 (5, 8 mm) | 2.9 |
| Balsa/NaClO2 [17] | 100 x 100 x 1.5 | 6h | 2.5 |
| Beech/NaClO2 [4] | Thickness: 0.1-0.7 | 12 | No data |
| Cathay poplar/ NaClO2/H2O2 [13, 5] | 20 x 20 x 0.5; 20 x 10 x 0.5 | 12 + 4 | No data |
| Basswood/ NaOH + Na2SO3; H2O2 [2, 7, 9] | 50 x 50 x 3 | 3 + 3 | About 2 |
|  | 40 x 40 x 5 | 3 + 3 | No data |
|  | 14 thickness b | No data | No data |
|  | 30 x 22 x 1 | 12 | No data |
| Beech/ NaOH + Na2SO3; H2O2 [8] | 40 x 50 x 5 | 48 | No data |
| Spruce/H2O2 + HAc [10] | 100 x 20 x 10 c | 6 | No data |
| Basswood/pine /NaClO [15, 16] | 50.8 x 50.8 x 0.25 | 3-5 | No data |
|  | 44.5 x 44.5 x 0.8 | 3 | No data |
| Balsa wood/ peracetic acid [14] | 20 x 20 x 1 20 x 5 x 5 50 x 50 x 5 | 3 6 12 | 5.5 |

a No data for 100 mm x 100 mm size and 5-8 mm thickness; b No data for 14 mm thickness delignified basswood. c The complete lignin removal can be directly concluded from the entire absence of the lignin specific IR bands.

Table S2 The comparison of transparent wood composites obtained by solution-based and steam-based delignification.

| Wood species/ chemicals | Wood dimension /mm | Lignin content/ % | Transmittance/haze/ % |
| --- | --- | --- | --- |
| L (Ro) type |  |  |  |
| Balsa/ NaClO2 [3] | 50 x 50 x 0.7-3.7 a | 2.9 | 90/50 (0.7 mm) 78/70 (1.2 mm) 62/78 (2.3 mm) 40/80 (3.7 mm) |
| Balsa/NaClO2 [17] | 100 x 100 x 1.5 | 2.5 | 86/70 |
| Balsa/NaClO2 [18] b | 1.5 thickness 10 thickness | 2.5 No data | 92/50 60/76 |
| Basswood/ NaOH +Na2SO3; H2O2 [2] | 50 x 50 x 3 | 1.5 | 78/90 |
| Basswood/H2O2 steam (ours) | 210 x 190 x 0.8; | 1.06 | 90/80 |
| R (Ra) type |  |  |  |
| Basswood/ NaOH +Na2SO3; H2O2 [2, 7, 9] | 50 x 50 x 3 | About 2 | 90/95 |
|  | 40 x 40 x 5 | No data | 90/95 |
|  | 14 mm thickness c | No data | No data |
|  | 30 x 22 x 1 | No data | 90±5/90±5 |
| Beech/ NaOH + Na2SO3; H2O2 [8] | 40 x 50 x 5 No data 86 (550 nm) | No data No data 86 (550 nm) | 86/90 No data 86 (550 nm) |
| Basswood/pine/ H2O2 steam (ours) | 100 x 50 x 5; 100 x 50 x 10 100 x 50 x 20 | 0.84 0.96 0.94 | 87/90 70/95 40/97 |

a No data for 100 mm x 100 mm size and 5-8 mm thickness. b The high transmittance was realized by interface manipulation through acetylation of delignified wood template. c No data for 14 mm thickness delignified basswood.

Table S3 Reaction conditions of basswood samples with different dimension and cutting direction.

| Size and thickness /mm | Time /h | Lignin content /% |
| --- | --- | --- |
| Ra 100x50x5 | 4 | 0.84 |
| Ra 100x50x10 | 5 | 0.96 |
| Ra 100x50x20 | 12 | 0.94 |
| Ra 50x50x20 a | 4 | 1.03 |
| Ra 100x50x40 a | 20 | 1.16 |
| Ra (pine) 50 x 50 x 5 | 8 | 0.82 |
| Ro 210x190x0.8 | 4 | 1.06 |

a: The Ra type basswood was steam delignified with H2O2/HAc ( volumetric ratio of 5:4)