Supplementary Materials

# Modified carbon nanotubes for water-based cathode slurries for lithium-sulfur batteries

Olesya O. Kapitanova,a* Kirill V. Mironovich,a Daniil E. Melezhenko,a Viktoria V. Rokosovina,a Serafima Yu. Ryzhenkova,a Sergey V. Korneev, a Tatyana B. Shatalova,a X.Xu, a Filipp S. Napolskiy,b Daniil M. Itkisa,b and Victor A. Krivchenkoa,c

a Moscow State University, Leninskie Gory, 1, b.3, 119991, Moscow, Russia

b Dubna University, Universitetskaya Str. 19, 141980, Dubna, Russia

c Moscow Institute of Physics and Technology, 9 Institutskiy per., Dolgoprudny, Moscow Region, 141701, Russia

* olesya.kapitanova@gmail.com

FIG. S1. IR spectra of CNTs (a), oxidized CNTs before (b) and after 1 (c) and 4 (d) hour hydrothermal reduction.

FIG. S2. A lower magnifications SEM characterization of sulfur-GO composite (a), electrode coatings based on S-GO composite and pristine CNTs (b), CNTs after 1 (c) and 4 (d) hours hydrothermal reduction, respectively.

FIG. S3. Electrochemical characterization of the electrodes based on sulfur-GO composite with different conductive additives: CNTs (triangle), CNTs after 1 (square) and 4 (circle) hour hydrothermal reduction; cycling performances of the electrodes at current density of 50 mA/g (calculated per 1 g of electrode coating). Right inset – schematic of the electrode coatings based on S-GO composite and pristine CNTs and modified CNTs.

FIG. S4. CVA measurements ((a) 1st, (b) 2nd, 3rd (c) cycles) of GO at 5 mV/s in 1 M solution of LiClO4 in thetramethylenesulfone in the potential range of 0 – 2.5 V vs. Li+/Li. Inset – same measurements in the potential range of 1.5 – 2.5 V vs. Li+/Li demonstrate negligible electrochemical activity of the redox of GO in investigated range.

FIG. S5. IR spectra of GO before (a) and after CVA measurements (3 cycles) at 1.5 – 2.5 V (b) and 0 – 2.5 V vs. Li+/Li (c) at 5 mV/s in 1 M solution of LiClO4 in thetramethylenesulfone.