Supplementary Material

Facile preparation of three-dimensional honeycomb nitrogen -doped carbon materials for supercapacitor applications

Hongjuan Zhang, Zunli Moa), Ruibin Guo, Nijuan Liu, Min Yan, Ruijuan Wang, Hangkong Feng, and Xiaojiao Wei

A research Center of Gansu Military and Civilian Integration Advanced Structural Materials, College of Chemistry and Chemical Engineering, Northwest Normal University, Lanzhou 730070, China

FIG. S1. SEM images of as-prepared 3D-HNCMs under different temperature and alkali ratios. (a) 3D-HNCMs-600. (b) 3D-HNCMs-700. (c) 3D-HNCMs-800. (d) 3D-HNCMs-1:2. (e) 3D-HNCMs-1:3. and (f) 3D-HNCMs-1:4.

FIG. S2. (a) CV curves of the symmetric supercapacitor at various scan rates. (b) GCD curves of the symmetric supercapacitor at various current densities. (c) Ragone plots of the symmetric supercapacitor.

TABLE. SI. Surface area and pore-structure parameters of 3D-HNCMs and 3D-PNCMs.

| Samples | SBET a (m2 g−1) | Smicrob (m2 g−1) | Smesoc (m2g−1) | Vtotald (cm3 g−1) |
| --- | --- | --- | --- | --- |
| 3D-HNCMs | 2094.28 | 1839.81 | 254.47 | 1.26 |
| 3D-PNCMs | 943.43 | 196.06 | 747.37 | 0.48 |

a BET surface area.        b micropore surface area.

c mesopore surface area.    d total pore volume.

TABLE. SII. Chemical composition of 3D-HNCMs and 3D-PNCMs.

| Sample | Element composition by EDS (wt%) a |
| --- | --- |
|  | C | N | O |
| 3D-HNCMs | 76.98 | 5.59 | 17.43 |
| 3D-PNCMs | 81.29 | 2.81 | 15.90 |

a Energy Dispersive spectrometer (EDS) measurement.

TABLE. SIII. Binding energies and relative surface nitrogen source ratio obtained by fitting the N 1s XPS spectra.

| Sample | Binding energy (eV) | Ratio (at%) |
| --- | --- | --- |
| N type |  | 3D-HNCMs | 3D-PNCMs |
| Pyridinic N | 398.5 ± 0.3 | 36.02 | 19.4 |
| Pyrrolic N | 400.5 ± 0.3 | 41.85 | 44.54 |
| Quaternary N | 401.5 ± 0.3 | 22.12 | 36.05 |