Synthesis, crystal structure, photoluminescence and electroluminescence properties of a new compound containing diphenylmethylene, carbazole and malononitrile units

Zhaofeng Shia, Dayong Zhanga, Jinnan Huob, Hongbo Wangb, Junsheng Yua*, Heping Shib*, Ben Zhong Tangc*

- School of Information and Communication Engineering and School of Photoelectric Science and Engineering, University of Electronic Science and Technology of China, Chengdu, 611731, China. E-mail: jsyu@uestc.edu.cn

- School of Chemistry and Chemical Engineering, Shanxi University, Taiyuan 030006, China. E-mail: hepingshi@sxu.edu.cn

- Department of Chemistry, Institute for Advanced Study, Division of Biomedical Engineering, Division of Life Science, State Key Laboratory of Molecular Neuroscience, Institute of Molecular Functional Materials, The Hong Kong University of Science and Technology, Clear Water Bay, Kowloon, Hong Kong, China. E-mail: tangbenz@ust.hk

Electronic Supplementary Information (ESI)

1H NMR of compound 1

1H NMR of DCPTMM

13C NMR of DCPTMM

Mass spectrum of DCPTMM

The XRD pattern of DCPTMM

Fig. S1 Thermogravimetric analysis curve of DCPTMM

Fig. S2 Differential scanning calorimetry curve of DCPTMM

Fig. S3 UV-vis absorption spectrum of DCPTMM in THF

Fig. S4 Fluorescence emission spectrum of DCPTMM in THF

Fig. S5 Scanning electron microscope (SEM) images of DCPTMM

LUMO (2.803 eV)                       HOMO (5.615eV)

Fig. S6 LUMO and HOMO of DCPTMM

Fig. S7 The electroluminescence (EL) spectrum of device A

Fig. S8 The CIE chromaticity coordinates of device A

Crystallographic CIF files. CCDC 1892153 can be obtained free of charge via http://www.ccdc.cam.ac.uk/conts/retrieving.html, or from the Cambridge Crystallographic Data Centre, 12 Union Road, Cambridge CB2 1EZ, UK; fax: (+44) 1223-336-033; or e-mail: deposit@ccdc.cam.ac.uk