Supplementary information

Thermodynamic properties of lanthanum, neodymium, gadolinium hafnates (Ln2Hf2O7) using the KEMS results

Viktor A. Vorozhtcov1, Valentina L. Stolyarova1,a), Mikhail V. Chislov1, Irina A. Zvereva1, Elizaveta P. Simonenko2, Nikolay P. Simonenko2

1Saint Petersburg State University, Universitetskaya nab. 7/9, Saint Petersburg 199034, Russia

2Kurnakov Institute of General and Inorganic Chemistry of the Russian Academy of Sciences, Moscow 119991, Russia

a)Corresponding author.

E-mail address:

Prof. Valentina L. Stolyarova v.stolyarova@spbu.ru

Table SI: The La2Hf2O7 heat capacities (Cp) in J/(mol×K) obtained in the present study by differential scanning calorimetry in the temperature range 350-840 K.

| T, K | Cp | T, K | Cp | T, K | Cp | T, K | Cp | T, K | Cp |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| I | II | I | II | I | II | I | II | I | II |
| 350.1 | 233.6 | 389.1 | 238.1 | 428.1 | 243.3 | 467.1 | 246.6 | 506.1 | 250.1 |
| 351.1 | 233.6 | 390.1 | 238.2 | 429.1 | 243.4 | 468.1 | 246.7 | 507.1 | 250.1 |
| 352.1 | 233.7 | 391.1 | 238.4 | 430.1 | 243.5 | 469.1 | 246.8 | 508.1 | 250.2 |
| 353.1 | 233.8 | 392.1 | 238.5 | 431.1 | 243.6 | 470.1 | 246.9 | 509.1 | 250.2 |
| 354.1 | 233.8 | 393.1 | 238.6 | 432.1 | 243.7 | 471.1 | 247.1 | 510.1 | 250.3 |
| 355.1 | 233.9 | 394.1 | 238.8 | 433.1 | 243.8 | 472.1 | 247.2 | 511.1 | 250.3 |
| 356.1 | 234.0 | 395.1 | 238.9 | 434.1 | 243.9 | 473.1 | 247.3 | 512.1 | 250.4 |
| 357.1 | 234.2 | 396.1 | 239.0 | 435.1 | 244.0 | 474.1 | 247.4 | 513.1 | 250.4 |
| 358.1 | 234.3 | 397.1 | 239.2 | 436.1 | 244.1 | 475.1 | 247.5 | 514.1 | 250.4 |
| 359.1 | 234.4 | 398.1 | 239.3 | 437.1 | 244.1 | 476.1 | 247.7 | 515.1 | 250.5 |
| 359.8 | 234.4 | 398.8 | 239.4 | 437.8 | 244.2 | 476.8 | 247.8 | 515.8 | 250.5 |
| 360.8 | 234.5 | 399.8 | 239.6 | 438.8 | 244.3 | 477.8 | 247.9 | 516.8 | 250.5 |
| 361.8 | 234.7 | 400.8 | 239.7 | 439.8 | 244.4 | 478.8 | 248.0 | 517.8 | 250.6 |
| 362.8 | 234.8 | 401.8 | 239.9 | 440.8 | 244.5 | 479.8 | 248.1 | 518.8 | 250.6 |
| 363.8 | 234.9 | 402.8 | 240.1 | 441.8 | 244.6 | 480.8 | 248.2 | 519.8 | 250.6 |
| 364.8 | 235.0 | 403.8 | 240.2 | 442.8 | 244.7 | 481.8 | 248.3 | 520.8 | 250.7 |
| 365.8 | 235.1 | 404.8 | 240.4 | 443.8 | 244.8 | 482.8 | 248.5 | 521.8 | 250.7 |
| 366.8 | 235.2 | 405.8 | 240.5 | 444.8 | 244.9 | 483.8 | 248.6 | 522.8 | 250.7 |
| 367.8 | 235.4 | 406.8 | 240.6 | 445.8 | 245.0 | 484.8 | 248.7 | 523.8 | 250.7 |
| 368.8 | 235.5 | 407.8 | 240.8 | 446.8 | 245.0 | 485.8 | 248.8 | 524.8 | 250.8 |
| 369.6 | 235.5 | 408.6 | 240.9 | 447.6 | 245.1 | 486.6 | 248.9 | 525.6 | 250.8 |
| 370.6 | 235.7 | 409.6 | 241.0 | 448.6 | 245.2 | 487.6 | 249.0 | 526.6 | 250.8 |
| 371.6 | 235.8 | 410.6 | 241.1 | 449.6 | 245.3 | 488.6 | 249.0 | 527.6 | 250.9 |
| 372.6 | 235.9 | 411.6 | 241.3 | 450.6 | 245.3 | 489.6 | 249.1 | 528.6 | 250.9 |
| 373.6 | 236.0 | 412.6 | 241.4 | 451.6 | 245.4 | 490.6 | 249.2 | 529.6 | 250.9 |
| 374.6 | 236.2 | 413.6 | 241.5 | 452.6 | 245.5 | 491.6 | 249.3 | 530.6 | 250.9 |
| 375.6 | 236.3 | 414.6 | 241.7 | 453.6 | 245.5 | 492.6 | 249.4 | 531.6 | 250.9 |
| 376.6 | 236.4 | 415.6 | 241.8 | 454.6 | 245.6 | 493.6 | 249.4 | 532.6 | 251.0 |
| 377.6 | 236.6 | 416.6 | 241.9 | 455.6 | 245.7 | 494.6 | 249.5 | 533.6 | 251.0 |
| 378.6 | 236.7 | 417.6 | 242.0 | 456.6 | 245.8 | 495.6 | 249.5 | 534.6 | 251.0 |
| 379.3 | 236.8 | 418.3 | 242.1 | 457.3 | 245.8 | 496.3 | 249.6 | 535.3 | 251.0 |
| 380.3 | 236.9 | 419.3 | 242.2 | 458.3 | 245.9 | 497.3 | 249.6 | 536.3 | 251.0 |
| 381.3 | 237.1 | 420.3 | 242.4 | 459.3 | 245.9 | 498.3 | 249.7 | 537.3 | 251.0 |
| 382.3 | 237.2 | 421.3 | 242.5 | 460.3 | 246.0 | 499.3 | 249.8 | 538.3 | 251.0 |
| 383.3 | 237.3 | 422.3 | 242.6 | 461.3 | 246.1 | 500.3 | 249.8 | 539.3 | 251.1 |
| 384.3 | 237.5 | 423.3 | 242.7 | 462.3 | 246.2 | 501.3 | 249.8 | 540.3 | 251.1 |
| 385.3 | 237.6 | 424.3 | 242.8 | 463.3 | 246.3 | 502.3 | 249.9 | 541.3 | 251.1 |
| 386.3 | 237.7 | 425.3 | 243.0 | 464.3 | 246.3 | 503.3 | 250.0 | 542.3 | 251.1 |
| 387.3 | 237.8 | 426.3 | 243.1 | 465.3 | 246.4 | 504.3 | 250.0 | 543.3 | 251.1 |
| 388.3 | 238.0 | 427.3 | 243.2 | 466.3 | 246.5 | 505.3 | 250.1 | 544.3 | 251.1 |

Table SI (continued):

| I | II | I | II | I | II | I | II | I | II |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 545.1 | 251.2 | 584.1 | 252.1 | 623.1 | 253.8 | 662.1 | 254.6 | 701.1 | 254.1 |
| 546.1 | 251.2 | 585.1 | 252.1 | 624.1 | 253.8 | 663.1 | 254.6 | 702.1 | 254.1 |
| 547.1 | 251.2 | 586.1 | 252.1 | 625.1 | 253.8 | 664.1 | 254.6 | 703.1 | 254.2 |
| 548.1 | 251.3 | 587.1 | 252.1 | 626.1 | 253.8 | 665.1 | 254.5 | 704.1 | 254.2 |
| 549.1 | 251.3 | 588.1 | 252.1 | 627.1 | 253.8 | 666.1 | 254.5 | 705.1 | 254.2 |
| 550.1 | 251.3 | 589.1 | 252.1 | 628.1 | 253.8 | 667.1 | 254.5 | 706.1 | 254.3 |
| 551.1 | 251.3 | 590.1 | 252.1 | 629.1 | 253.9 | 668.1 | 254.4 | 707.1 | 254.3 |
| 552.1 | 251.4 | 591.1 | 252.2 | 630.1 | 253.9 | 669.1 | 254.4 | 708.1 | 254.3 |
| 553.1 | 251.4 | 592.1 | 252.2 | 631.1 | 253.9 | 670.1 | 254.4 | 709.1 | 254.4 |
| 554.1 | 251.4 | 593.1 | 252.2 | 632.1 | 253.9 | 671.1 | 254.4 | 710.1 | 254.4 |
| 554.8 | 251.5 | 593.8 | 252.3 | 632.8 | 254.0 | 671.8 | 254.3 | 710.8 | 254.4 |
| 555.8 | 251.5 | 594.8 | 252.3 | 633.8 | 254.0 | 672.8 | 254.3 | 711.8 | 254.4 |
| 556.8 | 251.5 | 595.8 | 252.4 | 634.8 | 254.0 | 673.8 | 254.3 | 712.8 | 254.4 |
| 557.8 | 251.6 | 596.8 | 252.4 | 635.8 | 254.1 | 674.8 | 254.3 | 713.8 | 254.4 |
| 558.8 | 251.6 | 597.8 | 252.5 | 636.8 | 254.1 | 675.8 | 254.2 | 714.8 | 254.5 |
| 559.8 | 251.7 | 598.8 | 252.6 | 637.8 | 254.1 | 676.8 | 254.2 | 715.8 | 254.5 |
| 560.8 | 251.7 | 599.8 | 252.6 | 638.8 | 254.1 | 677.8 | 254.2 | 716.8 | 254.5 |
| 561.8 | 251.7 | 600.8 | 252.7 | 639.8 | 254.2 | 678.8 | 254.1 | 717.8 | 254.5 |
| 562.8 | 251.8 | 601.8 | 252.8 | 640.8 | 254.2 | 679.8 | 254.1 | 718.8 | 254.5 |
| 563.8 | 251.8 | 602.8 | 252.8 | 641.8 | 254.2 | 680.8 | 254.1 | 719.8 | 254.5 |
| 564.6 | 251.8 | 603.6 | 252.9 | 642.6 | 254.3 | 681.6 | 254.1 | 720.6 | 254.6 |
| 565.6 | 251.9 | 604.6 | 253.0 | 643.6 | 254.3 | 682.6 | 254.1 | 721.6 | 254.6 |
| 566.6 | 251.9 | 605.6 | 253.0 | 644.6 | 254.3 | 683.6 | 254.1 | 722.6 | 254.6 |
| 567.6 | 251.9 | 606.6 | 253.1 | 645.6 | 254.3 | 684.6 | 254.1 | 723.6 | 254.6 |
| 568.6 | 252.0 | 607.6 | 253.2 | 646.6 | 254.4 | 685.6 | 254.1 | 724.6 | 254.6 |
| 569.6 | 252.0 | 608.6 | 253.2 | 647.6 | 254.4 | 686.6 | 254.0 | 725.6 | 254.6 |
| 570.6 | 252.0 | 609.6 | 253.3 | 648.6 | 254.4 | 687.6 | 254.0 | 726.6 | 254.6 |
| 571.6 | 252.0 | 610.6 | 253.3 | 649.6 | 254.5 | 688.6 | 254.0 | 727.6 | 254.6 |
| 572.6 | 252.0 | 611.6 | 253.4 | 650.6 | 254.5 | 689.6 | 254.0 | 728.6 | 254.6 |
| 573.6 | 252.0 | 612.6 | 253.4 | 651.6 | 254.6 | 690.6 | 254.0 | 729.6 | 254.6 |
| 574.3 | 252.0 | 613.3 | 253.5 | 652.3 | 254.6 | 691.3 | 254.0 | 730.3 | 254.5 |
| 575.3 | 252.0 | 614.3 | 253.5 | 653.3 | 254.6 | 692.3 | 254.0 | 731.3 | 254.5 |
| 576.3 | 252.1 | 615.3 | 253.6 | 654.3 | 254.6 | 693.3 | 254.0 | 732.3 | 254.5 |
| 577.3 | 252.1 | 616.3 | 253.6 | 655.3 | 254.6 | 694.3 | 254.0 | 733.3 | 254.5 |
| 578.3 | 252.0 | 617.3 | 253.6 | 656.3 | 254.7 | 695.3 | 254.0 | 734.3 | 254.5 |
| 579.3 | 252.0 | 618.3 | 253.7 | 657.3 | 254.7 | 696.3 | 254.1 | 735.3 | 254.6 |
| 580.3 | 252.0 | 619.3 | 253.7 | 658.3 | 254.7 | 697.3 | 254.1 | 736.3 | 254.6 |
| 581.3 | 252.0 | 620.3 | 253.7 | 659.3 | 254.7 | 698.3 | 254.1 | 737.3 | 254.6 |
| 582.3 | 252.0 | 621.3 | 253.7 | 660.3 | 254.6 | 699.3 | 254.1 | 738.3 | 254.6 |
| 583.3 | 252.1 | 622.3 | 253.7 | 661.3 | 254.6 | 700.3 | 254.1 | 739.3 | 254.7 |

Table SI (continued):

| I | II | I | II | I | II |
| --- | --- | --- | --- | --- | --- |
| 740.1 | 254.7 | 774.3 | 254.6 | 808.3 | 254.1 |
| 741.1 | 254.7 | 775.3 | 254.6 | 809.3 | 254.1 |
| 742.1 | 254.7 | 776.3 | 254.6 | 810.3 | 254.1 |
| 743.1 | 254.7 | 777.3 | 254.5 | 811.3 | 254.1 |
| 744.1 | 254.8 | 778.3 | 254.5 | 812.3 | 254.2 |
| 745.1 | 254.8 | 779.1 | 254.5 | 813.3 | 254.2 |
| 746.1 | 254.8 | 780.1 | 254.4 | 814.3 | 254.2 |
| 747.1 | 254.8 | 781.1 | 254.4 | 815.3 | 254.3 |
| 748.1 | 254.8 | 782.1 | 254.3 | 816.3 | 254.3 |
| 749.1 | 254.8 | 783.1 | 254.3 | 817.3 | 254.3 |
| 749.8 | 254.9 | 784.1 | 254.3 | 818.1 | 254.3 |
| 750.8 | 254.9 | 785.1 | 254.2 | 819.1 | 254.3 |
| 751.8 | 254.9 | 786.1 | 254.2 | 820.1 | 254.4 |
| 752.8 | 255.0 | 787.1 | 254.2 | 821.1 | 254.4 |
| 753.8 | 255.0 | 788.1 | 254.2 | 822.1 | 254.4 |
| 754.8 | 255.1 | 788.8 | 254.1 | 823.1 | 254.5 |
| 755.8 | 255.1 | 789.8 | 254.1 | 824.1 | 254.5 |
| 756.8 | 255.1 | 790.8 | 254.1 | 825.1 | 254.5 |
| 757.8 | 255.1 | 791.8 | 254.1 | 826.1 | 254.6 |
| 758.8 | 255.2 | 792.8 | 254.1 | 827.1 | 254.6 |
| 759.6 | 255.2 | 793.8 | 254.1 | 827.8 | 254.6 |
| 760.6 | 255.1 | 794.8 | 254.1 | 828.8 | 254.6 |
| 761.6 | 255.1 | 795.8 | 254.1 | 829.8 | 254.7 |
| 762.6 | 255.1 | 796.8 | 254.1 | 830.8 | 254.7 |
| 763.6 | 255.1 | 797.8 | 254.1 | 831.8 | 254.8 |
| 764.6 | 255.1 | 798.6 | 254.1 | 832.8 | 254.8 |
| 765.6 | 255.0 | 799.6 | 254.1 | 833.8 | 254.8 |
| 766.6 | 255.0 | 800.6 | 254.1 | 834.8 | 254.8 |
| 767.6 | 254.9 | 801.6 | 254.1 | 835.8 | 254.8 |
| 768.6 | 254.9 | 802.6 | 254.2 | 836.8 | 254.9 |
| 769.3 | 254.9 | 803.6 | 254.1 | 837.6 | 254.9 |
| 770.3 | 254.8 | 804.6 | 254.1 | 838.6 | 255.0 |
| 771.3 | 254.8 | 805.6 | 254.1 | 839.6 | 255.0 |
| 772.3 | 254.7 | 806.6 | 254.1 | 840.6 | 255.0 |
| 773.3 | 254.7 | 807.6 | 254.1 |  |  |

Table SII: The Gd2Hf2O7 heat capacities (Cp) in J/(mol×K) obtained in the present study by differential scanning calorimetry in the temperature range 390-750 K.

| T, K | Cp | T, K | Cp | T, K | Cp | T, K | Cp |
| --- | --- | --- | --- | --- | --- | --- | --- |
| I | II | I | II | I | II | I | II |
| 391.0 | 234.4 | 431.0 | 235.8 | 471.0 | 234.9 | 511.0 | 236.7 |
| 392.0 | 234.4 | 432.0 | 235.7 | 472.0 | 234.9 | 512.0 | 236.8 |
| 393.0 | 234.5 | 433.0 | 235.7 | 473.0 | 235.0 | 513.0 | 236.8 |
| 394.0 | 234.5 | 434.0 | 235.7 | 474.0 | 235.0 | 514.0 | 236.9 |
| 395.0 | 234.6 | 435.0 | 235.6 | 475.0 | 235.1 | 515.0 | 236.9 |
| 396.0 | 234.6 | 436.0 | 235.6 | 476.0 | 235.2 | 516.0 | 237.0 |
| 397.0 | 234.6 | 437.0 | 235.6 | 477.0 | 235.3 | 517.0 | 237.0 |
| 398.0 | 234.6 | 438.0 | 235.6 | 478.0 | 235.4 | 518.0 | 237.1 |
| 399.0 | 234.6 | 439.0 | 235.6 | 479.0 | 235.5 | 519.0 | 237.2 |
| 400.0 | 234.7 | 440.0 | 235.6 | 480.0 | 235.6 | 520.0 | 237.2 |
| 401.0 | 234.7 | 441.0 | 235.6 | 481.0 | 235.6 | 521.0 | 237.2 |
| 402.0 | 234.7 | 442.0 | 235.6 | 482.0 | 235.7 | 522.0 | 237.3 |
| 403.0 | 234.7 | 443.0 | 235.6 | 483.0 | 235.8 | 523.0 | 237.4 |
| 404.0 | 234.7 | 444.0 | 235.7 | 484.0 | 235.8 | 524.0 | 237.4 |
| 405.0 | 234.8 | 445.0 | 235.7 | 485.0 | 235.9 | 525.0 | 237.5 |
| 406.0 | 234.8 | 446.0 | 235.6 | 486.0 | 235.9 | 526.0 | 237.5 |
| 407.0 | 234.9 | 447.0 | 235.6 | 487.0 | 236.0 | 527.0 | 237.6 |
| 408.0 | 235.0 | 448.0 | 235.6 | 488.0 | 236.1 | 528.0 | 237.6 |
| 409.0 | 235.0 | 449.0 | 235.6 | 489.0 | 236.1 | 529.0 | 237.7 |
| 410.0 | 235.1 | 450.0 | 235.6 | 490.0 | 236.2 | 530.0 | 237.8 |
| 411.0 | 235.2 | 451.0 | 235.6 | 491.0 | 236.2 | 531.0 | 237.9 |
| 412.0 | 235.3 | 452.0 | 235.6 | 492.0 | 236.3 | 532.0 | 238.0 |
| 413.0 | 235.4 | 453.0 | 235.6 | 493.0 | 236.3 | 533.0 | 238.2 |
| 414.0 | 235.4 | 454.0 | 235.5 | 494.0 | 236.4 | 534.0 | 238.3 |
| 415.0 | 235.5 | 455.0 | 235.6 | 495.0 | 236.5 | 535.0 | 238.4 |
| 416.0 | 235.5 | 456.0 | 235.5 | 496.0 | 236.5 | 536.0 | 238.5 |
| 417.0 | 235.6 | 457.0 | 235.5 | 497.0 | 236.5 | 537.0 | 238.6 |
| 418.0 | 235.7 | 458.0 | 235.5 | 498.0 | 236.5 | 538.0 | 238.7 |
| 419.0 | 235.7 | 459.0 | 235.5 | 499.0 | 236.5 | 539.0 | 238.8 |
| 420.0 | 235.7 | 460.0 | 235.4 | 500.0 | 236.5 | 540.0 | 238.8 |
| 421.0 | 235.7 | 461.0 | 235.3 | 501.0 | 236.6 | 541.0 | 238.9 |
| 422.0 | 235.7 | 462.0 | 235.3 | 502.0 | 236.6 | 542.0 | 238.9 |
| 423.0 | 235.8 | 463.0 | 235.2 | 503.0 | 236.5 | 543.0 | 239.0 |
| 424.0 | 235.8 | 464.0 | 235.2 | 504.0 | 236.5 | 544.0 | 239.1 |
| 425.0 | 235.8 | 465.0 | 235.1 | 505.0 | 236.6 | 545.0 | 239.1 |
| 426.0 | 235.8 | 466.0 | 235.0 | 506.0 | 236.6 | 546.0 | 239.2 |
| 427.0 | 235.8 | 467.0 | 235.0 | 507.0 | 236.6 | 547.0 | 239.3 |
| 428.0 | 235.8 | 468.0 | 234.9 | 508.0 | 236.7 | 548.0 | 239.3 |
| 429.0 | 235.8 | 469.0 | 234.9 | 509.0 | 236.7 | 549.0 | 239.4 |
| 430.0 | 235.8 | 470.0 | 234.9 | 510.0 | 236.7 | 550.0 | 239.5 |

Table SII (continued):

| I | II | I | II | I | II | I | II | I | II |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 551.0 | 239.6 | 591.0 | 245.5 | 631.0 | 248.6 | 671.0 | 248.6 | 711.0 | 250.2 |
| 552.0 | 239.7 | 592.0 | 245.7 | 632.0 | 248.7 | 672.0 | 248.6 | 712.0 | 250.2 |
| 553.0 | 239.8 | 593.0 | 245.9 | 633.0 | 248.8 | 673.0 | 248.5 | 713.0 | 250.2 |
| 554.0 | 239.8 | 594.0 | 246.1 | 634.0 | 248.9 | 674.0 | 248.5 | 714.0 | 250.2 |
| 555.0 | 239.9 | 595.0 | 246.2 | 635.0 | 248.9 | 675.0 | 248.4 | 715.0 | 250.1 |
| 556.0 | 240.0 | 596.0 | 246.3 | 636.0 | 248.9 | 676.0 | 248.3 | 716.0 | 250.1 |
| 557.0 | 240.1 | 597.0 | 246.5 | 637.0 | 249.0 | 677.0 | 248.3 | 717.0 | 250.0 |
| 558.0 | 240.3 | 598.0 | 246.6 | 638.0 | 248.9 | 678.0 | 248.2 | 718.0 | 249.9 |
| 559.0 | 240.4 | 599.0 | 246.7 | 639.0 | 248.8 | 679.0 | 248.2 | 719.0 | 249.8 |
| 560.0 | 240.5 | 600.0 | 246.8 | 640.0 | 248.8 | 680.0 | 248.2 | 720.0 | 249.7 |
| 561.0 | 240.6 | 601.0 | 246.9 | 641.0 | 248.8 | 681.0 | 248.2 | 721.0 | 249.6 |
| 562.0 | 240.8 | 602.0 | 247.0 | 642.0 | 248.8 | 682.0 | 248.2 | 722.0 | 249.6 |
| 563.0 | 240.9 | 603.0 | 247.1 | 643.0 | 248.7 | 683.0 | 248.2 | 723.0 | 249.5 |
| 564.0 | 241.0 | 604.0 | 247.2 | 644.0 | 248.6 | 684.0 | 248.3 | 724.0 | 249.4 |
| 565.0 | 241.1 | 605.0 | 247.4 | 645.0 | 248.6 | 685.0 | 248.4 | 725.0 | 249.3 |
| 566.0 | 241.2 | 606.0 | 247.5 | 646.0 | 248.6 | 686.0 | 248.5 | 726.0 | 249.3 |
| 567.0 | 241.3 | 607.0 | 247.7 | 647.0 | 248.6 | 687.0 | 248.5 | 727.0 | 249.3 |
| 568.0 | 241.4 | 608.0 | 247.8 | 648.0 | 248.6 | 688.0 | 248.6 | 728.0 | 249.3 |
| 569.0 | 241.5 | 609.0 | 247.9 | 649.0 | 248.6 | 689.0 | 248.6 | 729.0 | 249.2 |
| 570.0 | 241.6 | 610.0 | 248.0 | 650.0 | 248.6 | 690.0 | 248.7 | 730.0 | 249.1 |
| 571.0 | 241.8 | 611.0 | 248.1 | 651.0 | 248.6 | 691.0 | 248.8 | 731.0 | 249.1 |
| 572.0 | 241.9 | 612.0 | 248.2 | 652.0 | 248.6 | 692.0 | 248.8 | 732.0 | 249.0 |
| 573.0 | 242.1 | 613.0 | 248.2 | 653.0 | 248.6 | 693.0 | 248.8 | 733.0 | 249.1 |
| 574.0 | 242.2 | 614.0 | 248.2 | 654.0 | 248.6 | 694.0 | 248.8 | 734.0 | 249.1 |
| 575.0 | 242.4 | 615.0 | 248.2 | 655.0 | 248.6 | 695.0 | 248.8 | 735.0 | 249.0 |
| 576.0 | 242.6 | 616.0 | 248.2 | 656.0 | 248.5 | 696.0 | 248.8 | 736.0 | 248.9 |
| 577.0 | 242.8 | 617.0 | 248.2 | 657.0 | 248.5 | 697.0 | 248.8 | 737.0 | 248.9 |
| 578.0 | 242.9 | 618.0 | 248.2 | 658.0 | 248.6 | 698.0 | 248.8 | 738.0 | 248.9 |
| 579.0 | 243.1 | 619.0 | 248.2 | 659.0 | 248.5 | 699.0 | 248.9 | 739.0 | 249.0 |
| 580.0 | 243.2 | 620.0 | 248.1 | 660.0 | 248.5 | 700.0 | 248.9 | 740.0 | 249.0 |
| 581.0 | 243.4 | 621.0 | 248.1 | 661.0 | 248.5 | 701.0 | 249.0 | 741.0 | 249.0 |
| 582.0 | 243.6 | 622.0 | 248.1 | 662.0 | 248.5 | 702.0 | 249.1 | 742.0 | 249.1 |
| 583.0 | 243.8 | 623.0 | 248.1 | 663.0 | 248.5 | 703.0 | 249.2 | 743.0 | 249.1 |
| 584.0 | 243.9 | 624.0 | 248.1 | 664.0 | 248.6 | 704.0 | 249.3 | 744.0 | 249.1 |
| 585.0 | 244.2 | 625.0 | 248.2 | 665.0 | 248.6 | 705.0 | 249.4 | 745.0 | 249.2 |
| 586.0 | 244.4 | 626.0 | 248.2 | 666.0 | 248.6 | 706.0 | 249.6 | 746.0 | 249.3 |
| 587.0 | 244.6 | 627.0 | 248.3 | 667.0 | 248.5 | 707.0 | 249.7 | 747.0 | 249.4 |
| 588.0 | 244.8 | 628.0 | 248.3 | 668.0 | 248.6 | 708.0 | 249.8 | 748.0 | 249.5 |
| 589.0 | 245.0 | 629.0 | 248.4 | 669.0 | 248.6 | 709.0 | 250.0 | 749.0 | 249.6 |
| 590.0 | 245.2 | 630.0 | 248.5 | 670.0 | 248.6 | 710.0 | 250.1 | 750.0 | 249.7 |

Figure S1: Relative deviation ΔCp of the experimental La2Hf2O7 heat capacities Cp from smoothed temperature dependence of the La2Hf2O7 heat capacities Cp(S) according to Equation 4 in the temperature range 350-840 K, where ΔCp = [Cp - Cp(S)]/Cp(S)×100%.

Figure S2: Relative deviation ΔCp of the experimental Gd2Hf2O7 heat capacities Cp from smoothed temperature dependence of the Gd2Hf2O7 heat capacities Cp(S) according to Equation 5 in the temperature range 390-750 K, where ΔCp = [Cp - Cp(S)]/Cp(S)×100%.