Supporting Information for

Inorganic coordination polymer quantum sheets@graphene oxide composite photocatalysts: performance and mechanism

Shixiong Li1,*, Qiaoling Mo1, Xiaoxia Lai1, Yufeng Chen1, Chuansong Lin1, Yan Lu1, Beiling Liao2,*

1School of Chemical Engineering and Resource Recycling, Wuzhou University, Wuzhou, 543002, China

2School of Chemistry and Biological Engineering, Hechi University, Hechi, 546300, P. R. China

*Correspondence Email: lsx1324@163.com; liaobeiling1324@163.com

Figure S1. The TEM image of 10.6% ICPQS@GO.

Figure S2. (a) The XPS of core level region of Cu(2p) in ICPQS. Cu(2p3/2,1/2) peaks are resolved into sets of spin-orbit doublets. For Cu(2P3/2), Cu(I) is characteristic of peak at 932.5 eV (peak I) with no satellite peak and Cu(II) has main peak at 935.1 eV (peak II) with a shakeup satellite (peak III) at higher binding energies. The shakeup satellites are characteristic of materials having a d9 configuration in the ground state. Peaks IV and V come from Cu(2p1/2) core; (b) The XPS of ICPQS.

Figure S3. The N2 adsorption/desorption experiment of ICPQS.

Figure S4. Cyclic voltammograms of (a) ICPQS, (b) 5.1%ICPQS@GO, (c) 10.6%ICPQS@GO, and (d)15.3% ICPQS@GO on platinum plates in an acetonitrile solution of 0.1 mol·L-1 Bu4NPF6 at a sweep rate of 0.1 V·s-1.

Figure S5. The first-order kinetics of MB degradation of (a) ICPQS, (b) 5.1%ICPQS@GO, (c) 10.6% ICPQS@GO, and (d) 15.3% ICPQS@GO.

Figure S6. ESI mass spectra of ICPQS@GO composite photocatalysts photocatalytic degradation MB.

Table SI. The redox potential of ICPQS and ICPQS@GO composite photocatalysts.

| Photocatalysts | Redox potential (eV) |
| --- | --- |
| ICPQS | 2.46 |
| 5.1%ICPQS@GO | 2.43 |
| 10.6% ICPQS@GO | 2.26 |
| 15.3% ICPQS@GO | 2.35 |