A novel approach of preparing zinc adipate as β-nucleating agent toward to polypropylene engineering

Supplementary Materials

Wenli Peng1,2, Wenxia Liu3, Wenxue Zhang3*, Ke Li1,2, Xin Liu1,2, Zhenbin Chen1,2*, Zhenghua Tang5,6, Zhen Liu4*

1State Key Laboratory of Gansu Advanced Non-ferrous Metal Materials, Lanzhou University of Technology, Lanzhou, Gansu, China,730050

2School of Material Science and Engineering, Lanzhou University of Technology, Lanzhou, Gansu, China, 730050

# 3Lanzhou Petrochemical Research Center，PetroChina，Lanzhou 730060，Gansu，China

4Department of Physics and Engineering, Frostburg State University, Maryland, United States, 21532

# 5Guangzhou Key Laboratory for Surface Chemistry of Energy Materials, New Energy Research Institute, School of Environment and Energy, South China University of Technology, Guangzhou Higher Education Mega Centre, Guangzhou, 5100067, China

# 6Guangdong Provincial Key Laboratory of Atmospheric Environment and Pollution Control, Guangdong Provincial Engineering and Technology Research Center for Environmental Risk Prevention and Emergency Disposal, School of Environment and Energy, South China University of Technology, Guangzhou Higher Education Mega Centre, Guangzhou, 510006, China

# Corresponding Authors: Wenxue Zhang; Zhenbin Chen; Zhen Liu

*E-mail: suiyeyijian@126.com; zhenbinchen@163.com; zhenliu8@gmail.com

FIG.S1 Effect of different molar ratios of adipic acid and zinc hydroxide on the melting behavior of PP. ((a) Adi-Zn(OH)2 (1:1); (b) Adi-Zn(OH)2 (1:2); (c) Adi-Zn(OH)2 (1:3))

FIG.S2 Effect of different cooling rates on the crystallization peak temperatures of pure PP and nucleated PP

FIG.S3 Relative crystallinity of pure PP and nucleated PP at different cooling rates. (a) pure PP; (b) 0.1 wt%, Adi-Zn(OH)2 (1:2); (c) 0.2 wt%, Adi-Zn(OH)2 (1:2)

FIG.S4 Plots of ln (-ln(1-Xv(T)) versus T for pure PP and nucleated PP. (a) pure PP; (b) 0.1 wt%, Adi-Zn(OH)2 (1:2); (c) 0.2 wt%, Adi-Zn(OH)2 (1:2)