Supplementary material for: Preparation of multicolored carbon quantum dots using HNO3/HClO4 oxidation of graphitized carbon

Chao Tan, Songlin Zuo*, Yunyang Zhao and Baoshou Shen

College of Chemical Engineering, Nanjing Forestry University, Jiangsu Provincial Key Lab for the Chemistry and Utilization of Agro-forest Biomass, Nanjing 210037, China

Corresponding Author: zslnl@njfu.com.cn

FIG. S1: (a-e) XPS spectra of N-CQDs, 1500-CQDs, 2000-CQDs, 2500-CQDs, 2000-rCQDs, respectively.

TABLE SI: The relative mole content of carbon functional groups of CQDs.

| Samples | The relative mole fraction of carbon-containing groups/% |
| --- | --- |
|  | C-C | C-O | C=O | O=C-O |
| N-CQDs | 65.99 | 11.20 | 12.02 | 10.79 |
| 1500-CQDs | 68.50 | 4.98 | 15.02 | 11.50 |
| 2000-CQDs | 69.51 | 5.44 | 13.84 | 11.21 |
| 2500-CQDs | 71.12 | 5.15 | 12.16 | 11.57 |
| 2000-rCQDs | 63.63 | 12.16 | 7.16 | 17.07 |

FIG. S2: (a-e) High-resolution O1s peaks of N-CQDs, 1500-CQDs, 2000-CQDs, 2500-CQDs, 2000-rCQDs, respectively.

TABLE SII: The relative mole content of oxygen functional groups of CQDs.

| Samples | The relative mole fraction of oxygen-containing groups/% |
| --- | --- |
|  | C=O | C-O | C-OH |
| N-CQDs | 29.97 | 32.48 | 37.55 |
| 1500-CQDs | 47.64 | 29.16 | 23.20 |
| 2000-CQDs | 50.36 | 35.61 | 14.03 |
| 2500-CQDs | 64.48 | 20.38 | 15.14 |
| 2000-rCQDs | 37.38 | 34.32 | 28.30 |

FIG. S3: (a-e) High-resolution N1s peaks of N-CQDs, 1500-CQDs, 2000-CQDs, 2500-CQDs,2000-rCQDs, respectively.

TABLE SIII: The relative mole content of nitrogen functional groups of CQDs.

| Samples | The relative mole fraction of nitrogen-containing groups/% |
| --- | --- |
|  | -NH2 | NH4+ | -NO2 |
| N-CQDs | 35.06 | 51.81 | 13.13 |
| 1500-CQDs | 29.02 | 65.32 | 5.66 |
| 2000-CQDs | 33.16 | 55.10 | 11.74 |
| 2500-CQDs | 37.69 | 55.01 | 7.30 |
| 2000-rCQDs | 35.17 | 15.69 | 49.14 |

TABLE SIV: The elemental contents of different CQDs.

| Samples | Elemental contents/wt.% |
| --- | --- |
|  | C | H | O | N | S |
| N-CQDs | 44.89 | 2.79 | 44.12 | 8.12 | 0.08 |
| 1500-CQDs | 41.26 | 3.52 | 41.77 | 11.07 | 0.08 |
| 2000-CQDs | 37.05 | 3.18 | 41.31 | 9.09 | 0.08 |
| 2500-CQDs | 37.78 | 3.91 | 47.95 | 11.59 | 0.07 |
| 2000-rCQDs | 36.60 | 1.76 | 47.06 | 2.31 | 0.06 |

FIG. S4: (a-e) Effect of excitation wavelength on fluorescence intensity of N-CQDs, 1500-CQDs, 2000-CQDs, 2500-CQDs, 2000-rCQDs, respectively.

FIG. S5: (a-e) Time-resolved fluorescence decay curve of the of N-CQDs, 1500-CQDs, 2000-CQDs, 2500-CQDs, 2000-rCQDs, respectively. (λ ex=350 nm).