**Electro-assisted ammonium persulfate activation to promote the introduction of N and S into TiO2 film: enhancing** **its photoelectrocatalytic performance under solar**

Changxin Li1, Yan Liu1, Yanzong Zhang1\*, Lulu Long1,2, Fei Shen1,2, Gang Yang1,2, Xiaohong Zhang1, Yan He1, Lilin Wang1 and Shihuai Deng1,2

1 College of Environment, Sichuan Agricultural University, Chengdu, Sichuan 611130, China

2 Institute of Ecological and Environmental Sciences, Sichuan Agricultural University, Chengdu, Sichuan 611130, China

**Corresponding author**: Yanzong Zhang, Prof, College of Environment, Sichuan Agricultural University, Hui Ming Road, 611130, Chengdu, Sichuan, China.

**E-mail:** yzzhang@sicau.edu.cn

****

**FIG. S1** (a) TEM image of the NOx/S6+-TiO2 film, (b) partial enlarged view of (a), and (c) its high-resolution region of crystalline material.



**FIG. S2** Photoluminescence (PL) spectra of the NOx/S6+-TiO2 film with excitation wavelength at 380 nm.

****

**FIG. S3** The kinetic curves of methyl orange using the NOx/S6+-TiO2 film.

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Simulated pollutants | co (mg/L) | Methods | Reaction conditions | color removal % | Ref. |
| Methyl orange | 20 | Anodizing, electrolyte: 0.07 mg/mL graphene + 100 mg/L Mg(NO3)2·6H2O | 40 mL, 0.5 M NaCl, sunlight (90080 lx) for 2 h, 2 V | 97.00/ | [[1](#_ENREF_1)] |
| Methylene blue | 10 | Sol-gel and coating, electrolyte: - | 50 mL, 0.05 M Na2SO4, 450 W metal halide lamp (λ > 420 nm) for 4 h, 1.4 V | 92.9 | [[2](#_ENREF_2)] |
| Methyl orange | 10 | Anodizing, electrolyte: 0.1M H3PO3 + 0.2M NH4F | 50 mL , 0.2 M Na2S, 300 W Xe for 3 h, 0.5 V | 89 | [[3](#_ENREF_3)] |
| Rhodamine B | 5 | Two-step oxidation in 5 wt% oxalic acid and 0.15 wt% TiCl3 solution respectively | 20 mL, 0.1 M H3PO3, 500 W Xe for 2 h, 0.8 V | 53 | [[4](#_ENREF_4)] |
| Methyl orange | 20 | Anodizing, electrolyte:1.5 wt% HNO3 and 1.0 wt% H2O+EG | 40 mL , 0.5 M NaCl, sunlight (90830 lx) for 150 min, 2 V | 95.00 | [[5](#_ENREF_5)] |
| Methylene blue | 20 | -- | 40 mL ,0.01 M Na2SO4, 350W Xe (200-1200nm) for 240 min, 2 V | 60 | [[6](#_ENREF_6)] |
| Methyl orange | 20 | anodisation. electrolyte: 1/12M C2H2O4·2H2O + 0.5 wt% NH4F | 500 mL, 0.1 M Na2SO4, 300 W Xe for 2 h, 2.0 V | 92 | [[7](#_ENREF_7)] |
| Methyl orange | 20 | anodisation and magnetron sputtering. 90 vol% ethylene glycol + 0.6 wt% [EPy][BF4] + 10 vol% H2O | 40 mL, 0.5 M NaCl, 150 W Xe for 15 min, 2.0 V | 100 | [[8](#_ENREF_8)] |
| Methylene blue | 5 | -- | 50 mL, 500 W Xe with a 420 nm cut-off filter for 60 min | 83% | [[9](#_ENREF_9)] |
| Methylene blue | 3.739 | Dip-coating method with preheating and post-heating treatments: - | 6.5 mL, UV lamp with 365 nm 60 uW/cm2 about 40 min | 100 | [[10](#_ENREF_10)] |

**TABLE SI** Percent of color removals for selected PEC treatments of several representative dye wastewaters using different photoanodes.

“-” : Using different solutions for each step, “--” : Complicated operation with many steps

**References**

1 **Y. Liu, Y. Zhang, L. Wang, G. Yang, F. Shen, S. Deng, X. Zhang, Y. He, Y. Hu, and X. Chen:** Fast and Large-Scale Anodizing Synthesis of Pine-Cone TiO2 for Solar-Driven Photocatalysis. *Catalysts*. 7, 229 (2017).

2 **D. Liu, R. Tian, J. Wang, E. Nie, X. Piao, X. Li, and Z. Sun:** Photoelectrocatalytic degradation of methylene blue using F doped TiO2 photoelectrode under visible light irradiation. *Chemosphere*. 185, 574 (2017).

3 **L. Guisheng, W. Ling, L. Fang, X. Pengpeng, Z. Dieqing, and L. Hexing:** Photoelectrocatalytic degradation of organic pollutants via a CdS quantum dots enhanced TiO2 nanotube array electrode under visible light irradiation. *Nanoscale*. 5, 2118 (2013).

4 **B. Tan, Y. Zhang, and M. Long:** Large-scale preparation of nanoporous TiO2 film on titanium substrate with improved photoelectrochemical performance. *Nanoscale Res. Lett*. 9, 190 (2014).

5 **Y. Liu, K. Mu, Y. Zhang, L. Wang, G. Yang, F. Shen, S. Deng, X. Zhang, and S. Zhang:** Facile synthesis of a narrow-gap titanium dioxide anatase/rutile nanofiber film on titanium foil with high photocatalytic activity under sunlight. *Int. J. Hydrogen Energ*. 41, 10327 (2016).

6 **D. Li, J. Jia, Y. Zhang, N. Wang, X. Guo, and X. Yu:** Preparation and characterization of Nano-graphite/TiO2 composite photoelectrode for photoelectrocatalytic degradation of hazardous pollutant. *J. Hazard. Mater*. 315, 1 (2016).

7 **Y. Su, S. Han, X. Zhang, X. Chen, and L. Lei:** Preparation and visible-light-driven photoelectrocatalytic properties of boron-doped TiO2 nanotubes. *Mater. Chem. Phys*. 110, 239 (2008).

8 **L. Yan, S. Dong, Y. Zhang, L. Wang, Y. Gang, S. Fei, S. Deng, X. Zhang, and S. Zhang:** Anodized TiO2 nanotubes coated with Pt nanoparticles for enhanced photoelectrocatalytic activity. *J. Mater. Res.* 32, 757 (2017).

9 **C. Li, Z. Zhao, H. Shindume Lomboleni, H. Huang, and Z. Peng:** Enhanced visible photocatalytic activity of nitrogen doped single-crystal-like TiO2 by synergistic treatment with urea and mixed nitrates. *J. Mater. Res.* 32, 737 (2016).

10 **N. Wada, Y. Yokomizo, C. Yogi, M. Katayama, A. Tanaka, K. Kojima, Y. Inada, and K. Ozutsumi:** Effect of adding Au nanoparticles to TiO2 films on crystallization, phase transformation, and photocatalysis. *J. Mater. Res*. 33, 467 (2018).