Supporting Information

Template Assisted Synthesis of Porous TiO2 Photoanode for Efficient Dye-Sensitized Solar Cells

Chunmei Lv2, Xiuwen Wang2, Qun Li1, Chunyan Li1, Qiuyun Ouyang1, Yongjun Liu1, Lihong Qi1, *

1 College of Physics and Optoelectronics Engineering, Harbin Engineering University, No. 145 Nantong Street, Nangang District, Harbin, 150001, China

E-mail: lihongqi@hrbeu.edu.cn

2 College of Materials Science and Engineering, Qiqihar University, No. 42 Wenhua Street, Jianhua District, Qiqihar 161006, China

Supplementary results

TABLE SI Nitrogen adsorption-desorption parameters of the different samples

| Samples | P25 | S-1 | S-1.5 | S-2 |
| --- | --- | --- | --- | --- |
| Surface area (m2/g) | 44.21 | 47.69 | 50.72 | 51.94 |
| Pore size (nm) | 23.85 | 23.63 | 21.83 | 21.36 |

TABLE SII Photovoltaic parameters of DSSCs with the different photoanodes

| Photoanodes | Voc (V) | Jsc (mA/cm2) | FF | PCE (%) | Ref. |
| --- | --- | --- | --- | --- | --- |
| Meso-TiO2 | 0.59 | 15.9 | 0.69 | 6.50 | S1 |
| TiO2 NPGs | 0.73 | 16.3 | 0.70 | 8.41 | S2 |
| Mesoporous TiO2 | 0.69 | 15.42 | 0.66 | 7.94 | S3 |
| Hierarchically structured multi-layer TiO2 | 0.82 | 20.3 | 0.68 | 11.43 | S4 |
| Sea urchin-like anatase TiO2 | 0.67 | 11.49 | 0.56 | 4.32 | S5 |
| Highly connected hierarchical textured TiO2 | 0.81 | 14.3 | 0.71 | 8.2 | S6 |
| Mesoporous TiO2 | 0.67 | 13.56 | 0.68 | 6.18 | S7 |
| 3D Ordered Mesoporous TiO2 | 0.74 | 14.32 | 0.70 | 7.43 | S8 |
| S-1.5/P25 | 0.727 | 17.43 | 0.66 | 8.31 | This work |

TABLE SIII The parameters obtained from Nyquist plots

| Samples | Rs (Ω) | C1 (F) | R1 (Ω) | ZDif | R2 (Ω) | C2 (F) |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Y0 (S) | B (S1/2) |  |  |
| S-1/P25 | 35.71 | 2.11×10-5 | 1.059 | 0.041 | 0.38 | 13.87 | 1.52×10-3 |
| S-1.5/P25 | 28.85 | 2.24×10-5 | 0.930 | 0.036 | 0.30 | 7.31 | 1.85×10-3 |
| S-2/P25 | 36.59 | 2.28×10-5 | 1.167 | 0.030 | 0.29 | 6.64 | 2.24×10-3 |
| P25 | 31.80 | 2.67×10-5 | 1.042 | 0.052 | 0.39 | 9.38 | 2.34×10-3 |

References

S1. K. Pan, W. Zhou, G. Tian, Q. Pan, C. Tian, T. Xie, Y. Dong, D. Wang, and H. Fu: Dye-sensitised solar cells based on large-pore mesoporous TiO2 with controllable pore diameters. Eur. J. Inorg. Chem. 2011, 4730-4737 (2011).

S2. W.-Y. Cheng, J.R. Deka, Y.-C. Chiang, A. Rogeau, and S.-Y. Lu: One-step, surfactant-free hydrothermal method for syntheses of mesoporous TiO2 nanoparticle aggregates and their Applications in high efficiency dye-sensitized solar cells, Chem. Mater. 24, 3255-3262 (2012).

S3. X. Miao, K. Pan, Y. Liao, W. Zhou, Q. Pan, G. Tian, and G. Wang: Controlled synthesis of mesoporous anatase TiO2 microspheres as a scattering layer to enhance the photoelectrical conversion efficiency. J. Mater. Chem. A 1, 9853-9861 (2013).

S4. Y.-J. Chang, E.-H. Kong, Y.-C. Park, and H.M. Jang: Broadband light confinement using a hierarchically structured TiO2 multi-layer for dye-sensitized solar cells. J. Mater. Chem. A 1, 9707-9713 (2013).

S5. K. Fan, T. Peng, J. Chen, X. Zhang, and R. Li: A simple preparation method for quasi-solid-state flexible dye-sensitized solar cells by using sea urchin-like anatase TiO2 microspheres. J. Power Sources 222, 38-44 (2013).

S6. J. Lin, A. Nattestad, H. Yu, Y. Bai, L. Wang, S.X. Dou, and J.H. Kim: Highly connected hierarchical textured TiO2 spheres as photoanodes for dye-sensitized solar cells. J. Mater. Chem. A 2, 8902-8909 (2014).

S7. J.-D. Peng, C.-P. Lee, D. Velayutham, V. Suryanarayanan, and K.-C. Ho: Dye-sensitized solar cells containing mesoporous TiO2 spheres as photoanodes and methyl sulfate anion based biionic liquid electrolytes. J. Mater. Chem. A 3, 6383-6391 (2015).

S8. Y. Xiong, D. He, Y. Jin, P.J. Cameron, and K.J. Edler: Ordered mesoporous particles in titania films with hierarchical structure as scattering layers in dye-sensitized solar cells. J. Phys. Chem. C 119, 22552-22559 (2015).