Supplementary material

for   :

Face-sharing octahedra in Cs3Al2F9 and Cs2AlF5

A. Le Bail, L'. Smrčok

S1 - Indexing the Cs2AlF5 powder pattern with the McMaille software - page 2

S2 - Indexing the Cs3Al2F9 powder pattern with the McMaille software - page 7

S3 - Thermal decomposition products of Cs2AlF5 at 300°C ( CsAl3F10 + ?
(including the powder pattern .dat file) - page 11

S4 - TABLE CAL(for calibration). Experimental and optimized bond and contact distances in the structure of α-CsAlF4. Differences are reported as optimized-observed - page 21

S5 - CIF file for Cs2AlF5  from Rietveld refinement (including the Fullprof .pcr and .dat files) and DFT - page 22

S6 - CIF file for Cs3Al2F9  from Rietveld refinement (including the Fullprof .pcr and .dat files) and DFT - page 45

S1 - Indexing the Cs2AlF5 powder pattern with the McMaille software

Entry .dat file :

CS2ALB  =   Cs2AlF5 recuit 280°C

! Wavelength, zeropoint, Ngrid

1.540560   0.0300 0

! Codes for symmetry

0 0 0 1 0 0

! W, Nind

0.300  0

!Pmin, Pmax, Vmin, Vmax, Rmin, Rmax, Rmaxref

2. 15. 8. 1000. 0.01 0.15 0.50

! Ntests, Nruns

-2000 20

!  2-theta   Intensity

6.863189      0.7000000

10.37970      0.5000000

13.83965      0.3000000

15.52731       3.500000

15.89567       6.200000

16.99976       1.400000

17.37973       1.500000

20.87522       15.00000

21.16902       28.60000

22.01257       9.900000

22.27164       5.900000

24.39718       13.00000

25.14242       20.90000

26.10848       50.60000

26.34942       79.20000

27.26614       100.0000

28.00227       50.20000

29.02906       2.700000

29.67504       5.800000

31.34971       5.400000

31.51914       3.000000

32.13332       10.90000

32.30080       8.200000

32.94125       6.000000

34.38702       13.10000

35.16815       32.40000

36.04454       17.70000

36.73397       4.900000

37.23899       2.900000

37.47316       6.900000

37.90495       24.10000

38.66415       51.00000

39.48064       9.800000

40.07586       4.000000

40.79317       2.700000

41.24511      0.7000000

41.98161       7.400000

42.62964       8.700000

43.14249       4.500000

43.31881       3.300000

43.93362       2.800000

44.44424       2.900000

44.93521       11.80000

45.49868       9.900000

45.65652       12.80000

46.24939       5.900000

46.82557       4.400000

47.35118       5.900000

47.81019       11.00000

48.39875       7.800000

48.57895       11.50000

49.11695       14.50000

49.62295       3.500000

50.00873       9.600000

50.52570       4.000000

51.24197       8.100000

51.67676       5.500000

52.16567       4.800000

52.34723       3.600000

52.79168       2.200000

Output .imp file :

=================================================================

McMaille version 4.00     by A. Le Bail - 2006 - alb@cristal.org

=================================================================

Using generic filename : cs2alb-O

Number of Processors :           1

CS2ALB  =   Cs2AlF5 recuit 280°C

Wavelength :   1.54056 Zeropoint :   0.0300

===============================================================================

Monte Carlo cell generation

===============================================================================

Width of the columnar profile shape, W  =    0.3000

Max non-indexed reflections, NIND  =    0

Min/Max Rp, Rmaxref   9.9999998E-03  0.1500000      0.5000000

N of runs           20

N of MC events in cubic           2000.00000000000

N of MC events in tetra/hexa      40000.0000000000

N of MC events in orthorhombic    800000.000000000

N of MC events in monoclinic      16000000.0000000

N of MC events in triclinic       320000000.000000

2-THETA     d(A)    Iobs       W

6.893  12.8128     0.700     0.300

10.410   8.4910     0.500     0.300

13.870   6.3796     0.300     0.300

15.557   5.6912     3.500     0.300

15.926   5.5604     6.200     0.300

17.030   5.2023     1.400     0.300

17.410   5.0896     1.500     0.300

20.905   4.2458    15.000     0.300

21.199   4.1876    28.600     0.300

22.043   4.0292     9.900     0.300

22.302   3.9830     5.900     0.300

24.427   3.6410    13.000     0.300

25.172   3.5349    20.900     0.300

26.138   3.4064    50.600     0.300

26.379   3.3758    79.200     0.300

27.296   3.2645   100.000     0.300

28.032   3.1804    50.200     0.300

29.059   3.0703     2.700     0.300

29.705   3.0050     5.800     0.300

31.380   2.8484     5.400     0.300

31.549   2.8334     3.000     0.300

32.163   2.7807    10.900     0.300

32.331   2.7667     8.200     0.300

32.971   2.7144     6.000     0.300

34.417   2.6036    13.100     0.300

35.198   2.5476    32.400     0.300

36.075   2.4877    17.700     0.300

36.764   2.4426     4.900     0.300

37.269   2.4107     2.900     0.300

37.503   2.3962     6.900     0.300

37.935   2.3699    24.100     0.300

38.694   2.3251    51.000     0.300

39.511   2.2789     9.800     0.300

40.106   2.2464     4.000     0.300

40.823   2.2086     2.700     0.300

41.275   2.1855     0.700     0.300

42.012   2.1488     7.400     0.300

42.660   2.1177     8.700     0.300

43.172   2.0937     4.500     0.300

43.349   2.0856     3.300     0.300

43.964   2.0579     2.800     0.300

44.474   2.0354     2.900     0.300

44.965   2.0143    11.800     0.300

45.529   1.9907     9.900     0.300

45.687   1.9842    12.800     0.300

46.279   1.9601     5.900     0.300

46.856   1.9374     4.400     0.300

47.381   1.9171     5.900     0.300

47.840   1.8998    11.000     0.300

48.429   1.8780     7.800     0.300

48.609   1.8715    11.500     0.300

49.147   1.8523    14.500     0.300

49.653   1.8346     3.500     0.300

50.039   1.8213     9.600     0.300

50.556   1.8039     4.000     0.300

51.272   1.7804     8.100     0.300

51.707   1.7664     5.500     0.300

52.196   1.7510     4.800     0.300

52.377   1.7454     3.600     0.300

52.822   1.7317     2.200     0.300

dmax =    12.81277

Be sure that your choice of max cell parameters

ensures the exploration of all possibilities.

Dmin =    1.711727

20-May-2014     11 hour 18 min 57 Sec

===============================================================================

RESULTS - RESULTS - RESULTS - RESULTS

===============================================================================

EXPLORED CELL PARAMETERS AND VOLUMES:

===============================================================================

Orthorhombic Monte Carlo search :

Max(a,b,c), V    15.00000       15.00000       15.00000       1000.000

===============================================================================

FINAL LIST OF CELL PROPOSALS, sorted by McM20 :

===============================================================================

Global list as produced in the .ckm file

(IN=number of indexed lines)

The correct cell has some chances to be just below

IN  F.o.M.    Volume   V/V1      a        b        c       alpha   beta    gamma   Bravais lattice

60  132.54    925.123  1.00      6.3610  11.4108  12.7456  90.000  90.000  90.000    P  Ortho ***

===============================================================================

FINAL LIST OF CELL PROPOSALS, sorted by F(20) :

===============================================================================

Global list (IN=number of indexed lines)

The correct cell has some chances to be just below

IN  F(20)     Volume   V/V1      a        b        c       alpha   beta    gamma   Bravais lattice

60   51.52    925.123  1.00      6.3610  11.4108  12.7456  90.000  90.000  90.000    P  Ortho ***

===============================================================================

FINAL LIST OF CELL PROPOSALS, sorted by M(20) :

===============================================================================

Global list   (IN=number of indexed lines)

The correct cell has some chances to be just below

IN  M(20)     Volume   V/V1      a        b        c       alpha   beta    gamma   Bravais lattice

60   33.47    925.123  1.00      6.3610  11.4108  12.7456  90.000  90.000  90.000    P  Ortho ***

===============================================================================

See for the highest F.o.M. above the cell(s) with highest symmetry, if any

(Cubic, hexagonal, etc), they could correspond to the the right solution

==============================================================================

Cells sorted by symmetry

Rp     Vol     Vol/V1 Ind Nsol    a        b         c      alpha  beta  gamma

Orthorhombic cells

0.041    925.123  1.00  60  25   6.3610  11.4108  12.7456  90.000  90.000  90.000

WARNING - WARNING - WARNING :

Same solution found Nsol =           25  times,

you should probably reduce the test numbers...

"Best" cell with largest McM20 :

--------------------------------

PROGRAM *** CELREF ***  (J.LAUGIER & A.FILHOL 10/78)

OBSERVABLE NUMBER    :    60

ITERATION NUMBER :    10

REFINEMENT CONSTRAINTS : NO

INITIAL VALUES :

ZERO    LAMBDA      A        B        C      ALPHA     BETA    GAMMA

1.       0.       1.       1.       1.       0.       0.       0.

0.000    1.5406   6.3610  11.4108  12.7456   90.000   90.000   90.000

RECIPROCAL CELL :   0.15721  0.08764  0.07846   90.000   90.000   90.000

VOLUME (A**3)  :      925.123

NUMBER OF INDEPENDENT PARAMETERS :     4

FINAL VALUES   : (STANDARD DEVIATIONS : 2nd LINE)

ZERO    LAMBDA      A        B        C      ALPHA     BETA    GAMMA

-0.002    1.5406   6.3619  11.4104  12.7481   90.000   90.000   90.000

0.005    0.0000   0.0010   0.0018   0.0018    0.000    0.000    0.000

RECIPROCAL CELL :   0.15719  0.08764  0.07844   90.000   90.000   90.000

VOLUME (A**3)  :      925.406

H     K     L  TH(OBS)    TH-ZERO    TH(CALC)     DIFF.

0     0     1     6.893      6.892      6.928     -0.037

0     1     1    10.410     10.408     10.396      0.012

0     0     2    13.870     13.868     13.882     -0.014

1     0     1    15.557     15.556     15.554      0.002

0     1     2    15.926     15.924     15.913      0.011

0     2     1    17.030     17.028     17.013      0.016

1     1     1    17.410     17.408     17.395      0.013

1     2     0    20.905     20.904     20.897      0.007

1     1     2    21.199     21.197     21.194      0.003

1     2     1    22.043     22.041     22.040      0.001

0     1     3    22.302     22.300     22.306     -0.006

0     3     1    24.427     24.426     24.402      0.024

1     2     2    25.172     25.171     25.175     -0.004

0     2     3    26.138     26.137     26.126      0.011

1     1     3    26.379     26.378     26.382     -0.004

1     3     0    27.296     27.295     27.296     -0.001

2     0     0    28.032     28.031     28.028      0.003

0     1     4    29.059     29.057     29.067     -0.009

1     2     3    29.705     29.703     29.714     -0.011

1     0     4    31.380     31.378     31.367      0.011

0     3     3    31.549     31.548     31.542      0.005

0     2     4    32.163     32.162     32.144      0.018

1     1     4    32.331     32.329     32.356     -0.027

2     2     1    32.971     32.970     32.969      0.000

0     4     2    34.417     34.415     34.415      0.000

2     2     2    35.198     35.197     35.209     -0.012

0     1     5    36.075     36.073     36.066      0.007

0     3     4    36.764     36.762     36.761      0.002

1     4     2    37.269     37.267     37.284     -0.017

2     3     1    37.503     37.502     37.496      0.005

0     4     3    37.935     37.933     37.959     -0.025

2     2     3    38.694     38.693     38.689      0.003

2     3     2    39.511     39.509     39.513     -0.003

0     5     1    40.106     40.104     40.107     -0.003

2     1     4    40.823     40.822     40.819      0.003

1     2     5    41.275     41.274     41.264      0.009

0     5     2    42.012     42.010     42.018     -0.008

0     3     5    42.660     42.658     42.657      0.001

2     2     4    43.172     43.171     43.161      0.010

3     1     0    43.349     43.347     43.364     -0.016

3     1     1    43.964     43.962     43.970     -0.008

1     5     2    44.474     44.473     44.470      0.002

2     4     2    44.965     44.964     44.953      0.010

0     2     6    45.529     45.527     45.519      0.008

1     1     6    45.687     45.685     45.677      0.008

2     1     5    46.279     46.278     46.286     -0.008

2     3     4    46.856     46.854     46.854      0.000

1     5     3    47.381     47.380     47.382     -0.003

1     2     6    47.840     47.839     47.828      0.010

2     2     5    48.429     48.427     48.416      0.011

3     1     3    48.609     48.607     48.601      0.006

3     3     0    49.147     49.145     49.149     -0.004

2     5     1    49.653     49.651     49.642      0.009

1     4     5    50.039     50.037     50.036      0.001

1     6     1    50.556     50.554     50.561     -0.007

2     5     2    51.272     51.270     51.270      0.001

2     0     6    51.707     51.705     51.694      0.011

1     0     7    52.196     52.194     52.201     -0.007

2     1     6    52.377     52.376     52.357      0.019

1     1     7    52.822     52.820     52.859     -0.039

M(20) =     35.67

F(20) =     54.61 (  0.0099,  37)

Final Rp on the .prf =   0.1395022

===============================================================================

THE SELECTION OF THE "BEST" CELL

based on McM20, Rp, F(20), M(20), V, high symmetry ?

DEPENDS ON YOU, EXCLUSIVELY.

However...

It is suggested that the correct cell could be :

===============================================================================

IN  F.o.M.    Volume             a        b        c       alpha   beta    gamma   Bravais lattice

60  132.54    925.123            6.3610  11.4108  12.7456  90.000  90.000  90.000    P  Ortho ***

Found            3  time(s) head of the best lists

===============================================================================

S2 - Indexing the Cs3Al2F9 powder pattern with the McMaille software

Entry .dat file :

Cs3Al2F9   CSAL01  EVA

! Wavelength, zeropoint, Ngrid

1.540560  -0.0550 0

! Codes for symmetry

1 1 0 0 0 0

! W, Nind

0.300  0

!Pmin, Pmax, Vmin, Vmax, Rmin, Rmax, Rmaxref

2. 20. 8. 600. 0.01 0.15 0.50

! Ntests, Nruns

-2000 20

!  2-theta   Intensity

12.04000      0.2000000

16.41700       6.000000

20.41100       2.300000

24.51600       100.0000

28.56600       65.20000

29.37800       3.800000

33.09900       14.90000

36.66800       14.00000

37.97600       70.10000

40.36800       10.30000

44.25600       9.400000

46.32900       3.000000

47.11300       12.30000

48.19400       23.70000

50.18600       14.30000

50.57300       13.70000

54.12400       1.600000

54.58200       1.400000

55.34400      0.8000000

58.75400       11.50000

59.06600       16.50000

61.75300       1.400000

63.37600       1.700000

64.00700       3.600000

64.89400       13.80000

66.79600       6.000000

69.40200       1.300000

70.70700       2.700000

71.54000       5.500000

72.37500       4.900000

73.50700      0.7000000

73.97500       4.300000

74.20000       3.800000

79.53500       6.300000

81.08700       2.400000

81.37700       5.400000

84.91900       2.000000

88.10100       1.500000

88.28900       2.600000

Output .imp file :

=================================================================

McMaille version 4.00     by A. Le Bail - 2006 - alb@cristal.org

=================================================================

Using generic filename : cs3al2F9-h

Number of Processors :           1

Cs3Al2F9   CSAL01  EVA

Wavelength :   1.54056 Zeropoint :  -0.0550

===============================================================================

Monte Carlo cell generation

===============================================================================

Width of the columnar profile shape, W  =    0.3000

Max non-indexed reflections, NIND  =    0

Min/Max Rp, Rmaxref   9.9999998E-03  0.1500000      0.5000000

N of runs           20

N of MC events in cubic           2000.00000000000

N of MC events in tetra/hexa      40000.0000000000

N of MC events in orthorhombic    800000.000000000

N of MC events in monoclinic      16000000.0000000

N of MC events in triclinic       320000000.000000

2-THETA     d(A)    Iobs       W

11.985   7.3783     0.200     0.300

16.362   5.4130     6.000     0.300

20.356   4.3591     2.300     0.300

24.461   3.6361   100.000     0.300

28.511   3.1281    65.200     0.300

29.323   3.0433     3.800     0.300

33.044   2.7086    14.900     0.300

36.613   2.4523    14.000     0.300

37.921   2.3707    70.100     0.300

40.313   2.2354    10.300     0.300

44.201   2.0474     9.400     0.300

46.274   1.9603     3.000     0.300

47.058   1.9295    12.300     0.300

48.139   1.8887    23.700     0.300

50.131   1.8182    14.300     0.300

50.518   1.8052    13.700     0.300

54.069   1.6947     1.600     0.300

54.527   1.6815     1.400     0.300

55.289   1.6601     0.800     0.300

58.699   1.5716    11.500     0.300

59.011   1.5640    16.500     0.300

61.698   1.5022     1.400     0.300

63.321   1.4675     1.700     0.300

63.952   1.4546     3.600     0.300

64.839   1.4368    13.800     0.300

66.741   1.4004     6.000     0.300

69.347   1.3540     1.300     0.300

70.652   1.3321     2.700     0.300

71.485   1.3186     5.500     0.300

72.320   1.3055     4.900     0.300

73.452   1.2881     0.700     0.300

73.920   1.2811     4.300     0.300

74.145   1.2778     3.800     0.300

79.480   1.2049     6.300     0.300

81.032   1.1857     2.400     0.300

81.322   1.1822     5.400     0.300

84.864   1.1416     2.000     0.300

88.046   1.1084     1.500     0.300

88.234   1.1065     2.600     0.300

dmax =    7.378283

Be sure that your choice of max cell parameters

ensures the exploration of all possibilities.

Dmin =    1.086524

20-May-2014     14 hour 44 min 12 Sec

===============================================================================

RESULTS - RESULTS - RESULTS - RESULTS

===============================================================================

EXPLORED CELL PARAMETERS AND VOLUMES:

===============================================================================

Cubic Monte Carlo search :

Max a, V    20.00000       600.0000

Hexagonal/Trigonal/Rhomboedral Monte Carlo search :

Max(a,c), V    20.00000       20.00000       600.0000

===============================================================================

FINAL LIST OF CELL PROPOSALS, sorted by McM20 :

===============================================================================

Global list as produced in the .ckm file

(IN=number of indexed lines)

The correct cell has some chances to be just below

IN  F.o.M.    Volume   V/V1      a        b        c       alpha   beta    gamma   Bravais lattice

39  177.77    498.663  1.00      6.2555   6.2555  14.7150  90.000  90.000 120.000    P  Hexag ****

===============================================================================

FINAL LIST OF CELL PROPOSALS, sorted by F(20) :

===============================================================================

Global list (IN=number of indexed lines)

The correct cell has some chances to be just below

IN  F(20)     Volume   V/V1      a        b        c       alpha   beta    gamma   Bravais lattice

39   35.94    498.663  1.00      6.2555   6.2555  14.7150  90.000  90.000 120.000    P  Hexag ****

===============================================================================

FINAL LIST OF CELL PROPOSALS, sorted by M(20) :

===============================================================================

Global list   (IN=number of indexed lines)

The correct cell has some chances to be just below

IN  M(20)     Volume   V/V1      a        b        c       alpha   beta    gamma   Bravais lattice

39   40.33    498.663  1.00      6.2555   6.2555  14.7150  90.000  90.000 120.000    P  Hexag ****

===============================================================================

See for the highest F.o.M. above the cell(s) with highest symmetry, if any

(Cubic, hexagonal, etc), they could correspond to the the right solution

===============================================================================

Cells sorted by symmetry

Rp     Vol     Vol/V1 Ind Nsol    a        b         c      alpha  beta  gamma

Hexagonal/trigonal cells

0.048    498.663  1.00  39  25   6.2555   6.2555  14.7150  90.000  90.000 120.000

WARNING - WARNING - WARNING :

Same solution found Nsol =           25  times,

you should probably reduce the test numbers...

"Best" cell with largest McM20 :

--------------------------------

PROGRAM *** CELREF ***  (J.LAUGIER & A.FILHOL 10/78)

OBSERVABLE NUMBER    :    39

ITERATION NUMBER :    10

REFINEMENT CONSTRAINTS : A=B

INITIAL VALUES :

ZERO    LAMBDA      A        B        C      ALPHA     BETA    GAMMA

1.       0.       1.       0.       1.       0.       0.       0.

0.000    1.5406   6.2555   6.2555  14.7150   90.000   90.000  120.000

RECIPROCAL CELL :   0.18459  0.18459  0.06796   90.000   90.000   60.000

VOLUME (A**3)  :      498.663

NUMBER OF INDEPENDENT PARAMETERS :     3

FINAL VALUES   : (STANDARD DEVIATIONS : 2nd LINE)

ZERO    LAMBDA      A        B        C      ALPHA     BETA    GAMMA

0.000    1.5406   6.2550   6.2550  14.7175   90.000   90.000  120.000

0.007    0.0000   0.0008   0.0008   0.0021    0.000    0.000    0.000

RECIPROCAL CELL :   0.18460  0.18460  0.06795   90.000   90.000   60.000

VOLUME (A**3)  :      498.682

H     K     L  TH(OBS)    TH-ZERO    TH(CALC)     DIFF.

0     0     2    11.985     11.985     12.017     -0.031

1     0     0    16.362     16.362     16.350      0.013

1     0     2    20.356     20.356     20.340      0.016

1     0     3    24.461     24.461     24.460      0.002

1     1     0    28.511     28.511     28.516     -0.005

1     0     4    29.323     29.323     29.319      0.004

2     0     0    33.044     33.044     33.045     -0.001

0     0     6    36.613     36.613     36.604      0.009

2     0     3    37.921     37.921     37.914      0.008

1     0     6    40.313     40.313     40.329     -0.016

2     1     0    44.201     44.201     44.199      0.003

1     0     7    46.274     46.274     46.282     -0.007

1     1     6    47.058     47.058     47.042      0.016

2     1     3    48.139     48.139     48.117      0.023

2     0     6    50.131     50.131     50.132     -0.001

3     0     0    50.518     50.518     50.503      0.016

3     0     3    54.069     54.069     54.074     -0.005

2     1     5    54.527     54.527     54.552     -0.025

2     0     7    55.289     55.289     55.264      0.026

2     1     6    58.699     58.699     58.688      0.011

2     2     0    59.011     59.011     59.021     -0.009

3     1     0    61.698     61.698     61.687      0.011

2     1     7    63.321     63.321     63.354     -0.032

3     0     6    63.952     63.952     63.971     -0.019

3     1     3    64.839     64.839     64.851     -0.011

2     0     9    66.741     66.741     66.766     -0.025

4     0     0    69.347     69.347     69.331      0.016

4     0     2    70.652     70.652     70.667     -0.015

2     2     6    71.485     71.485     71.488     -0.003

4     0     3    72.320     72.320     72.322     -0.002

3     0     8    73.452     73.452     73.416      0.037

3     1     6    73.920     73.920     73.915      0.005

2     1     9    74.145     74.145     74.147     -0.002

3     2     3    79.480     79.480     79.494     -0.013

4     0     6    81.032     81.032     81.040     -0.008

4     1     0    81.322     81.322     81.328     -0.006

1     1    12    84.864     84.864     84.849      0.015

3     2     6    88.046     88.046     88.027      0.019

3     1     9    88.234     88.234     88.251     -0.016

M(20) =     40.32

F(20) =     35.93 (  0.0118,  47)

Final Rp on the .prf =   9.9705011E-02

===============================================================================

THE SELECTION OF THE "BEST" CELL

based on McM20, Rp, F(20), M(20), V, high symmetry ?

DEPENDS ON YOU, EXCLUSIVELY.

However...

It is suggested that the correct cell could be :

===============================================================================

IN  F.o.M.    Volume             a        b        c       alpha   beta    gamma   Bravais lattice

39  177.77    498.663            6.2555   6.2555  14.7150  90.000  90.000 120.000    P  Hexag ****

Found            3  time(s) head of the best lists

===============================================================================

S3 - Thermal decomposition products of Cs2AlF5 at 300°C ( CsAl3F10 + ?
(including the powder pattern .dat files)

- Search-match among Cs/Al/F phases using the Bruker EVA software combined with the ICDD-JCPDS PDF :

- Attempt to index the peaks unexplained by CsAl3F10 :

Entry file for the McMaille software :

CSHT20...

! Wavelength, zeropoint, Ngrid

1.540560   0.0000 0

! Codes for symmetry

1 1 1 0 0 0

! W, Nind

0.300  3

!Pmin, Pmax, Vmin, Vmax, Rmin, Rmax, Rmaxref

2. 30. 8. 1000. 0.01 0.15 0.50

! Ntests, Nruns

-2000 20

!  2-theta   Intensity

12.04400       1.900000

16.74100       6.400000

18.12900       12.50000

22.86500       100.0000

25.87100       71.80000

28.26400       82.00000

32.64100       17.00000

32.99600       12.30000

36.43400       48.00000

43.70200       10.20000

46.69800       30.80000

48.01900       7.600000

48.52100       11.40000

49.96600       10.90000

Output .imp file :

=================================================================

McMaille version 4.00     by A. Le Bail - 2006 - alb@cristal.org

=================================================================

Using generic filename : CSHT20-EVA2

Number of Processors :           1

CSHT20...

Wavelength :   1.54056 Zeropoint :   0.0000

===============================================================================

Monte Carlo cell generation

===============================================================================

Width of the columnar profile shape, W  =    0.3000

Max non-indexed reflections, NIND  =    3

Min/Max Rp, Rmaxref   9.9999998E-03  0.1500000      0.5000000

N of runs           20

N of MC events in cubic           2000.00000000000

N of MC events in tetra/hexa      40000.0000000000

N of MC events in orthorhombic    800000.000000000

N of MC events in monoclinic      16000000.0000000

N of MC events in triclinic       320000000.000000

2-THETA     d(A)    Iobs       W

12.044   7.3423     1.900     0.300

16.741   5.2913     6.400     0.300

18.129   4.8892    12.500     0.300

22.865   3.8861   100.000     0.300

25.871   3.4410    71.800     0.300

28.264   3.1549    82.000     0.300

32.641   2.7411    17.000     0.300

32.996   2.7124    12.300     0.300

36.434   2.4640    48.000     0.300

43.702   2.0696    10.200     0.300

46.698   1.9435    30.800     0.300

48.019   1.8931     7.600     0.300

48.521   1.8747    11.400     0.300

49.966   1.8238    10.900     0.300

dmax =    7.342271

Be sure that your choice of max cell parameters

ensures the exploration of all possibilities.

Dmin =    1.803798

8-Jan-2014     15 hour 17 min 32 Sec

===============================================================================

RESULTS - RESULTS - RESULTS - RESULTS

===============================================================================

EXPLORED CELL PARAMETERS AND VOLUMES:

===============================================================================

Cubic Monte Carlo search :

Max a, V    30.00000       1000.000

Hexagonal/Trigonal/Rhomboedral Monte Carlo search :

Max(a,c), V    30.00000       30.00000       1000.000

Tetragonal Monte Carlo search :

Max(a,c), V    30.00000       30.00000       1000.000

===============================================================================

FINAL LIST OF CELL PROPOSALS, sorted by McM20 :

===============================================================================

Global list as produced in the .ckm file

(IN=number of indexed lines)

The correct cell has some chances to be just below

IN  F.o.M.    Volume   V/V1      a        b        c       alpha   beta    gamma   Bravais lattice

13   85.86    763.398  1.00      6.3179   6.3179  22.0840  90.000  90.000 120.000    P  Hexag ****

===============================================================================

FINAL LIST OF CELL PROPOSALS, sorted by F(20) :

===============================================================================

Global list (IN=number of indexed lines)

The correct cell has some chances to be just below

IN  F(20)     Volume   V/V1      a        b        c       alpha   beta    gamma   Bravais lattice

13   28.80    763.398  1.00      6.3179   6.3179  22.0840  90.000  90.000 120.000    P  Hexag ****

===============================================================================

FINAL LIST OF CELL PROPOSALS, sorted by M(20) :

===============================================================================

Global list   (IN=number of indexed lines)

The correct cell has some chances to be just below

IN  M(20)     Volume   V/V1      a        b        c       alpha   beta    gamma   Bravais lattice

13   38.35    763.398  1.00      6.3179   6.3179  22.0840  90.000  90.000 120.000    P  Hexag ****

===============================================================================

See for the highest F.o.M. above the cell(s) with highest symmetry, if any

(Cubic, hexagonal, etc), they could correspond to the the right solution

===============================================================================

Cells sorted by symmetry

Rp     Vol     Vol/V1 Ind Nsol    a        b         c      alpha  beta  gamma

Hexagonal/trigonal cells

0.108    763.398  1.00  13  25   6.3179   6.3179  22.0840  90.000  90.000 120.000

WARNING - WARNING - WARNING :

Same solution found Nsol =           25  times,

you should probably reduce the test numbers...

"Best" cell with largest McM20 :

--------------------------------

PROGRAM *** CELREF ***  (J.LAUGIER & A.FILHOL 10/78)

OBSERVABLE NUMBER    :    12

ITERATION NUMBER :    10

REFINEMENT CONSTRAINTS : A=B

INITIAL VALUES :

ZERO    LAMBDA      A        B        C      ALPHA     BETA    GAMMA

1.       0.       1.       0.       1.       0.       0.       0.

0.000    1.5406   6.3179   6.3179  22.0840   90.000   90.000  120.000

RECIPROCAL CELL :   0.18277  0.18277  0.04528   90.000   90.000   60.000

VOLUME (A**3)  :      763.398

NUMBER OF INDEPENDENT PARAMETERS :     3

FINAL VALUES   : (STANDARD DEVIATIONS : 2nd LINE)

ZERO    LAMBDA      A        B        C      ALPHA     BETA    GAMMA

-0.039    1.5406   6.3241   6.3241  22.1142   90.000   90.000  120.000

0.022    0.0000   0.0040   0.0040   0.0205    0.000    0.000    0.000

RECIPROCAL CELL :   0.18259  0.18259  0.04522   90.000   90.000   60.000

VOLUME (A**3)  :      765.952

H     K     L  TH(OBS)    TH-ZERO    TH(CALC)     DIFF.

0     0     3    12.044     12.005     11.996      0.009

1     0     2    18.129     18.090     18.060      0.030

1     0     4    22.865     22.826     22.837     -0.011

1     0     5    25.871     25.832     25.871     -0.040

0     0     7    28.264     28.225     28.225      0.000

1     1     4    32.641     32.602     32.596      0.006

2     0     1    32.996     32.957     32.931      0.026

1     0     8    36.434     36.395     36.376      0.019

2     1     0    43.702     43.663     43.691     -0.028

2     0     8    46.698     46.659     46.650      0.009

2     1     5    48.521     48.482     48.516     -0.034

3     0     0    49.966     49.927     49.913      0.014

Final Rp on the .prf =   0.2722650

===============================================================================

THE SELECTION OF THE "BEST" CELL

based on McM20, Rp, F(20), M(20), V, high symmetry ?

DEPENDS ON YOU, EXCLUSIVELY.

However...

It is suggested that the correct cell could be :

===============================================================================

IN  F.o.M.    Volume             a        b        c       alpha   beta    gamma   Bravais lattice

13   85.86    763.398            6.3179   6.3179  22.0840  90.000  90.000 120.000    P  Hexag ****

Found            3  time(s) head of the best lists

===============================================================================

Powder data, for the thermal decomposition products of Cs2AlF5, measured at room temperature, CuKalpha :

5.000  0.020  77.000

2258      2330      2417      2334      2262      2299      2210      2277

2321      2343      2174      2242      2178      2105      2128      2193

2153      2084      2244      2155      2040      2128      1987      2093

2106      2018      2102      2022      2053      1990      2006      1996

1888      1946      1944      1990      1967      1930      1916      1963

1908      2017      1963      1881      1927      1853      1822      1787

1911      1852      1896      1825      1862      1819      1775      1742

1790      1774      1836      1750      1755      1733      1788      1785

1773      1698      1770      1716      1711      1702      1705      1663

1728      1678      1654      1656      1690      1633      1615      1663

1644      1598      1647      1578      1617      1628      1665      1614

1598      1650      1614      1573      1664      1653      1625      1587

1564      1597      1585      1635      1624      1654      1532      1676

1559      1567      1586      1504      1541      1477      1430      1435

1383      1472      1409      1414      1502      1418      1351      1437

1348      1443      1350      1427      1338      1382      1393      1302

1403      1389      1403      1313      1316      1307      1334      1314

1229      1306      1286      1355      1305      1350      1321      1374

1217      1293      1301      1275      1248      1202      1276      1284

1240      1185      1234      1306      1216      1268      1226      1197

1198      1226      1226      1149      1222      1183      1169      1197

1168      1191      1181      1188      1141      1111      1114      1126

1171      1116      1163      1202      1189      1134      1133      1155

1141      1148      1129      1124      1117      1047      1107      1070

1071      1047      1066      1080      1095      1117      1163      1086

1031      1140      1055      1056      1060       982       978      1050

1105      1019      1016      1080      1033      1055      1073      1040

1045      1062      1019       971      1027      1011      1032       980

1035      1041      1020      1010       924       975       957       954

1041       970      1004       936      1025       924       988      1000

989      1001       978      1007       926       981       973       946

945       943       936       933       926       905       928       875

883       924       925       907       828       879       899       887

881       852       885       879       842       847       857       887

871       840       892       863       897       965       881       839

857       831       836       829       795       873       806       866

818       856       831       855       816       846       869       798

857       875       853       830       845       818       799       821

830       816       740       840       796       835       827       771

811       822       803       821       848       781       811       833

825       852       817       830       850       851       802       876

878       876       865       897       913       865       900       944

988      1020      1055      1149      1173      1248      1162      1112

1065       957      1006       931       941       956       963      1078

1038      1010      1020       888       906       820       762       733

756       729       776       768       721       752       710       758

742       735       689       677       655       714       676       676

727       695       656       672       736       696       714       704

704       695       689       696       624       706       653       687

696       691       714       729       675       684       641       648

657       673       671       689       640       648       697       660

645       661       669       676       638       674       652       649

639       636       605       661       669       607       625       641

645       641       635       625       664       615       644       654

651       615       638       676       604       618       657       639

682       633       659       627       676       653       691       643

610       656       661       640       656       656       648       585

630       568       629       676       609       644       614       596

618       653       616       594       613       607       605       579

629       569       601       658       603       636       573       605

583       656       591       599       613       631       612       627

630       617       579       595       612       616       559       584

613       538       603       536       605       583       588       582

621       614       601       592       586       617       587       567

591       529       529       566       524       586       557       516

560       591       582       516       580       536       596       584

567       588       563       578       557       535       564       549

578       551       537       559       534       525       560       581

598       575       560       566       545       546       548       553

565       589       550       547       519       530       548       539

579       586       590       590       639       607       646       632

664       638       620       680       707       707       759       763

838       841       875       870       926       927       944      1061

1219      1304      1421      1554      1538      1506      1379      1254

1034       934       806       738       694       665       636       618

630       622       598       525       600       585       563       594

562       570       581       596       585       657       600       622

596       583       613       568       601       590       605       614

629       616       602       663       640       638       643       691

695       719       680       710       712       708       736       806

759       801       872       866       904       931      1007      1054

1087      1157      1218      1417      1583      1732      1944      2231

2433      2449      2454      2299      1960      1643      1324      1095

879       819       675       634       641       573       540       558

555       534       515       545       512       498       535       516

521       501       514       496       478       522       494       484

517       567       559       606       627       566       554       561

499       507       489       498       513       482       535       555

504       518       486       541       534       502       514       522

502       549       548       544       574       534       550       554

541       536       558       503       514       536       547       503

545       492       550       549       503       607       550       606

541       574       551       538       495       478       524       509

499       486       469       428       458       499       475       449

444       453       489       452       493       468       491       462

478       463       476       455       418       458       455       481

470       430       468       484       447       461       494       488

473       463       443       464       473       458       503       459

511       531       500       546       541       576       559       602

584       604       673       706       723       744       793       864

997      1043      1118      1085      1166      1120      1116      1054

1004      1021      1077      1064      1082      1144      1207      1256

1371      1527      1552      1584      1585      1560      1508      1409

1378      1276      1209      1122      1196      1222      1169      1241

1174      1229      1259      1297      1380      1447      1429      1496

1371      1455      1350      1277      1259      1133      1156      1056

1047       968       968       920       908       876       904       954

959       950       897       983       987      1010      1019      1071

1071      1112      1214      1262      1325      1419      1524      1609

1707      1832      1873      1980      2175      2233      2395      2561

2828      3138      3414      3832      4321      4826      5526      6370

7345      8470      9951     11794     13872     15247     16031     15622

14186     11854      9438      7124      5365      3984      2926      2321

1838      1599      1343      1203      1116      1031       976       959

993       925      1004       951       940       984       987      1045

1139      1199      1281      1468      1607      1736      1919      2303

2685      3165      3676      4062      3987      4052      3605      2994

2379      1889      1416      1119       934       814       743       660

735       664       698       656       669       650       689       722

763       780       789       813       800       834       823       788

742       711       679       684       682       656       638       609

691       698       635       705       723       749       750       764

818       965       937      1040      1073       989       925       877

838       734       736       666       642       688       679       713

693       723       690       719       769       740       777       726

746       752       807       798       775       827       806       805

821       821       791       824       855       835       852       889

1034      1108      1153      1345      1330      1335      1294      1346

1370      1420      1493      1546      1745      1807      1898      2142

2297      2598      3009      3297      3735      4180      4764      5591

6575      7891      9116     10476     11139     11356     10747      9897

8337      6662      5446      4302      3367      2675      2204      1993

1819      1665      1660      1597      1591      1667      1680      1755

1876      1915      1935      1935      1832      1839      1658      1625

1443      1364      1399      1285      1261      1284      1193      1112

1154      1148      1146      1038      1056      1009      1095      1057

1016      1039      1059      1102      1023       990      1073      1057

1034      1094      1049      1095      1048      1099      1112      1160

1178      1263      1241      1378      1374      1441      1534      1573

1703      1788      1903      1981      2244      2448      2810      3232

3649      4002      4452      4543      4616      4537      4319      3929

3703      3336      2969      2641      2552      2384      2246      2145

2050      2092      2058      2074      2093      2095      2015      2146

2249      2262      2415      2534      2809      2820      3052      3156

3539      3807      4159      4665      5113      5751      6577      7493

8369      9813     11069     12397     12634     12823     12090     11285

9699      8154      6538      5301      4257      3427      2725      2468

2064      1880      1714      1574      1483      1436      1423      1312

1280      1347      1278      1262      1245      1168      1096      1207

1235      1180      1145      1238      1131      1052       994       980

877       790       741       667       647       624       611       568

569       555       525       510       567       454       473       491

479       518       492       492       514       472       512       483

466       483       515       487       440       387       437       439

450       408       418       419       422       428       416       396

405       390       405       401       407       433       435       402

414       434       372       407       385       408       380       357

387       361       390       401       394       346       407       356

384       357       359       368       378       369       377       377

385       397       362       390       369       372       389       385

382       382       390       444       434       379       411       426

464       434       425       454       467       481       473       477

463       446       483       446       470       506       613       621

595       542       577       482       493       501       436       408

379       364       391       354       341       357       356       348

367       349       335       321       330       344       351       342

333       362       369       336       355       326       363       378

411       364       353       410       396       378       398       456

392       411       413       387       406       377       414       344

401       397       386       372       406       386       402       405

459       497       473       473       483       566       639       621

627       661       738       721       801       850       909      1037

1198      1324      1466      1756      2061      2424      2639      2780

2782      2680      2363      2172      1986      1709      1507      1401

1277      1223      1318      1434      1522      1626      1826      2028

2124      2213      2083      1991      1790      1612      1511      1269

1138       948       848       761       646       662       625       592

535       531       553       540       540       486       521       566

493       535       501       615       581       634       660       710

790       932      1023      1091      1296      1296      1437      1383

1431      1321      1296      1186      1075       925       784       758

625       594       574       503       504       479       490       491

494       515       490       510       480       478       471       484

444       451       405       409       392       421       385       377

389       417       399       389       387       393       395       396

428       431       442       414       427       419       440       449

464       432       467       489       482       533       452       456

561       564       539       518       487       489       501       570

486       502       525       512       567       518       510       522

546       570       582       601       605       566       663       684

705       825       810       819       911       944      1024      1078

1170      1247      1395      1503      1680      1753      1962      2033

2123      2012      1909      1874      1694      1548      1355      1256

1185      1072      1032       985      1003      1017      1007      1050

1086      1165      1250      1367      1423      1531      1771      1883

2256      2459      2969      3195      3768      4218      4663      5143

5662      6245      6868      7367      7553      7495      7547      7469

7418      7290      7518      7834      8025      8429      8496      8445

8396      8069      7499      6800      6095      5237      4319      3510

2951      2374      1983      1601      1385      1158      1109       969

879       860       782       711       714       643       700       634

634       625       587       581       559       582       610       613

570       603       584       642       622       644       634       662

714       614       637       597       589       556       529       513

475       533       546       502       570       489       489       542

517       499       553       598       627       619       633       669

713       738       840       912       869       901       880       882

939       905       871       862       847       939       891      1040

1030      1118      1172      1348      1409      1589      1649      1765

1896      2050      2301      2493      2903      3394      4131      4725

5563      6526      7306      7670      7753      7674      6871      6402

5569      4723      4009      3294      2597      2089      1651      1469

1254      1061       928       850       760       732       680       732

720       626       696       695       610       664       649       640

648       653       651       544       599       555       578       513

526       485       485       443       453       449       484       448

457       423       452       467       449       463       433       426

450       473       506       519       465       506       542       587

565       638       619       605       574       555       569       526

479       466       428       427       353       373       327       333

311       336       297       320       284       336       323       288

329       307       311       356       313       342       351       319

357       371       355       354       335       309       371       345

382       358       406       364       390       399       426       450

450       390       395       414       449       420       376       428

414       393       416       384       371       390       337       358

363       327       373       343       307       312       335       295

286       302       316       337       308       295       320       342

298       301       293       332       315       318       311       286

294       317       337       310       345       370       313       331

355       342       351       363       330       342       351       349

358       340       378       343       393       391       388       400

368       370       340       327       338       351       349       370

337       332       342       326       360       317       355       365

357       358       370       404       446       425       437       494

541       524       589       576       629       655       660       657

765       769       786       902       840       809       810       869

824       787       792       852       755       713       767       708

642       672       652       646       603       609       615       631

552       626       599       579       596       683       658       623

707       714       691       774       793       889       844       889

990      1080      1189      1337      1493      1529      1656      1770

1738      1776      1750      1742      1706      1818      1702      1756

1926      1990      2198      2302      2568      2683      2895      3096

3350      3423      3618      3394      3204      3004      2890      2416

2210      2010      1675      1531      1332      1120      1035       915

896       883       795       864       778       840       814       862

861       860       893       827       863       759       733       730

656       653       611       572       533       514       533       461

493       511       443       457       509       437       432       427

463       428       433       428       464       451       504       499

422       499       502       450       497       472       512       504

549       594       581       577       606       588       574       611

629       585       609       576       620       583       603       624

629       630       649       665       628       652       665       615

610       627       571       569       556       600       582       558

568       559       596       546       580       622       611       573

649       620       633       697       644       709       771       803

821       901       924       940       997      1120      1192      1305

1331      1544      1661      1910      2165      2337      2691      3009

3317      3480      3997      4187      4551      4805      4897      4645

4599      4510      4471      4434      4230      4028      3854      3460

3070      2909      2639      2349      2156      1885      1641      1509

1338      1166      1098      1088       966       948       892       873

866       822       910       802       776       712       730       723

698       669       604       641       635       536       560       557

509       603       555       561       584       552       556       593

597       629       629       632       685       753       707       795

806       903      1020      1091      1151      1267      1321      1336

1393      1314      1277      1257      1326      1288      1271      1287

1312      1205      1243      1215      1198      1141      1117      1186

1177      1218      1239      1423      1407      1574      1722      1825

1873      1830      1867      1775      1738      1724      1518      1466

1338      1252      1187      1038       876       855       753       769

693       684       621       605       588       567       557       521

528       535       532       546       557       537       553       562

587       620       621       643       637       666       649       672

659       634       626       591       561       612       546       520

514       559       542       526       531       534       530       550

615       579       669       695       699       761       786       816

909       971      1087      1163      1258      1377      1527      1613

1793      1835      1756      1772      1619      1553      1495      1377

1289      1196       992       939       834       777       708       669

613       601       527       539       503       506       489       450

455       453       419       400       413       401       429       408

388       421       414       381       429       410       407       357

380       355       383       354       350       362       358       330

375       339       345       341       315       352       379       337

321       325       328       340       339       324       355       352

367       366       338       364       340       355       376       398

336       400       387       372       419       418       421       428

419       416       410       448       440       436       400       378

425       428       400       399       378       419       407       423

422       435       451       517       519       518       608       642

720       780       751       795       814       713       763       768

638       658       631       590       541       478       483       426

413       419       445       410       443       454       485       493

494       498       502       519       551       578       656       683

721       888       906       931      1058      1170      1170      1175

1174      1172      1190      1095      1120      1127      1066      1147

1106      1095      1140      1126      1088      1081      1043      1006

925       884       861       804       772       695       696       549

560       511       482       423       432       433       445       416

360       371       377       357       359       338       359       359

318       330       347       334       336       314       315       337

350       341       332       349       341       350       344       340

353       346       407       368       357       333       337       339

320       317       318       346       343       340       332       347

367       337       333       368       332       335       321       334

362       307       326       295       310       303       326       319

295       295       307       271       269       278       315       305

317       317       301       289       322       330       305       328

314       332       379       367       387       397       416       459

434       497       491       535       514       571       622       638

720       806       850       963      1017       982      1028      1037

1053       963       967       938       814       783       751       726

600       566       535       495       456       400       431       434

406       419       425       391       385       388       419       404

376       371       429       429       453       458       498       513

562       637       569       614       672       666       718       723

787       768       861       899      1028      1111      1205      1285

1421      1435      1479      1384      1372      1371      1331      1344

1323      1393      1324      1287      1272      1300      1103      1094

967       942       869       786       814       740       634       621

578       506       469       446       424       434       427       402

408       375       406       412       405       393       401       378

408       435       392       415       441       424       406       442

423       431       464       441       490       457       472       517

506       580       539       659       618       695       751       737

776       735       757       835       756       772       727       761

696       671       719       705       660       638       659       651

635       688       688       710       709       755       726       797

798       886       872       954       993      1033      1117      1260

1415      1474      1659      1727      1641      1660      1667      1570

1454      1353      1388      1214      1177      1158      1004       922

815       758       676       683       602       603       603       593

587       536       460       502       489       482       506       476

443       453       463       457       456       469       430       432

442       445       484       450       488       445       465       436

472       448       443       425       437       455       430       425

406       421       396       406       371       391       408       397

403       436       457       441       431       471       499       462

481       489       546       508       536       530       553       574

615       622       621       640       583       582       576       587

603       585       602       557       625       570       534       553

534       574       543       579       535       549       562       609

579       538       589       597       637       588       621       665

681       665       678       708       755       793       870       813

836       910       922       948       964       889       844       785

830       830       839       817       815       793       775       792

819       842       855       861       949      1010      1139      1095

1183      1233      1217      1144      1088      1152      1147      1124

1081      1041       977       899       807       877       774       746

718       635       656       658       621       609       606       577

538       596       555       488       574       505       526       488

492       559       545       515       512       536       596       614

622       717       704       714       690       655       718       643

592       668       647       579       611       567       541       484

502       462       486       476       474       406       417       422

408       396       425       411       414       401       444       420

436       458       444       440       478       505       490       493

511       541       516       526       532       527       526       535

557       542       553       555       560       565       617       577

591       657       693       737       796       843       845       898

953      1047      1129      1266      1330      1437      1435      1531

1581      1567      1571      1594      1558      1586      1457      1379

1306      1280      1227      1086      1071       923       988       836

807       731       741       697       649       679       603       657

635       612       598       662       635       649       627       678

704       687       754       823       833       909       982      1042

1035      1041      1097      1073      1103      1090      1133      1170

1195      1271      1174      1266      1241      1160      1096      1036

1075       986       969      1049       988       993       965       983

952       968      1049      1056      1111      1154      1238      1294

1328      1237      1199      1195      1126      1087      1073      1012

977       917       906       844       802       669       694       643

585       528       533       483       458       464       432       404

404       406       403       361       391       343       331       394

351       332       361       361       357       337       354       373

413       377       373       397       383       395       401       417

390       449       458       500       483       566       554       681

746       866       942       925       891       765       770       692

656       608       654       640       610       566       533       475

426       415       365       338       350       349       310       320

309       306       290       342       300       305       298       296

294       289       287       291       281       299       304       269

309       309       262       289       301       326       293       343

300       333       310       294       334       335       329       289

314       313       330       323       315       290       276       330

331       275       304       298       302       333       339       324

315       310       303       276       324       300       325       311

348       324       267       320       317       340       321       329

293       329       303       320       309       307       312       309

335       319       333       370       379       387       393       370

373       420       432       445       488       508       471       594

619       674       739       699       767       718       745       730

760       730       772       790       730       731       652       695

645       618       615       573       561       540       544       546

512       483       475       410       467       447       414       413

397       382       374       389       320       365       359       322

310       305       326       322       320       325       332       361

337       315       330       334       321       329       307       331

294       319       327       329       302       310       348       345

337       354       328       362       337       342       353       392

391       411       401       418       409       456       487       495

465       548       554       524       559       549       533       539

570       602       648       621       681       662       641       726

732       745       699       670       641       607       647       679

669       615       661       648       630       651       603       616

654       676       703       734       697       810       822       949

990      1052      1105      1112      1170      1277      1253      1289

1274      1217      1341      1329      1180      1230      1170      1169

1070      1085       977      1000       964       939       856       917

899       892       842       878       833       839       735       723

781       720       692       637       715       678       662       697

682       685       690       740       803       757       793       835

797       846       855       750       767       712       695       682

744       645       683       622       660       608       599       552

577       540       535       534       545       506       557       579

531       575       592       594       605       603       693       655

630       644       566       601       584       535       553       540

532       559       548       514       486       448       487       441

456       459       426       437       427       449       474       425

439       495       439       412       457       461       397       396

403       443       416       414       401       392       378       417

329       384       375       389       366       382       371       440

391       376       345       403       408       391       394       409

436       419       441       430       412       432       460       483

583       483       529       606       637       655       671       676

656       650       648       586       584       594       563       541

538       529       501       460       490       495       468       433

426       410       383       373       343       376       410       373

384       375       367       342       336       364       367       343

388       338       386       332       384       354       373       342

391       420       401       415       409       403       444       416

426       426       400       413       400       379       393       381

413       404       405       384       405       375       370       354

358       374       376       345       349       377       335       363

337       368       366       379       337       372       386       371

388       427       435       414       416       452       452       475

480       527       558       554       548       513       578       557

534       559       572       563       542       494       561       508

490       488       550       485       505       464       498       507

428       453       429       386       429       416       430       400

363       388       373       346       369       403       354       343

345       341       323       354       347       329       343       335

357       316       334       351       331       303       282       356

306       327       358       342       330       306       382       337

341       369       371       360       367       381       388       418

387       445       513       432       448       468       488       431

442

S4 - TABLE CAL. Experimental and optimized bond and contact distances in the structure of α-CsAlF4. Differences are reported as optimized-observed.

| Al-F | d | Cs-F | D |
| --- | --- | --- | --- |
| F3 [x-y,-y,-z ] | 1.757(11) -.001 | F3 | 3.134(7) -.011 |
| F3 | 1.757(9) -.001 | F3 [x,y,1+z] | 3.134(7) -.011 |
| F1 [1-x+y,1-x,-z] | 1.824(11) .011 | F3 [x-y,-y,-z ] | 3.134(10) -.011 |
| F1 [-y,-1+x-y,z | 1.824(8) .011 | F3 [x-y,-y,1-z ] | 3.134(10) -.011 |
| F2 | 1.8581(5) .0 | F3 [1-x,-x+y,1+z] | 3.155(8) .004 |
| F2 [x,y,-1+z ] | 1.8581(5) .0 | F3 [1-x,-x+y,z] | 3.155(8) .004 |
|  |  | F3 [1-y,x-y,z] | 3.155(9) .004 |
|  |  | F3 [1-y,x-y,1+z] | 3.155(9) .004 |
|  |  | F1 | 3.216(9) .009 |
|  |  | F1 [x,y,1+z ] | 3.216(9) .009 |
|  |  | F2 | 3.445(10) -0.03 |
|  |  | F2 [1-y,x-y,z ] | 3.544(6) 0.006 |
|  |  | F2 [1-x+y,-x,z ] | 3.544(11) 0.006 |
| F…F <2.506(12) -2.594(8)> <2.517 - 2.590> |  |  |  |

S5 - CIF file for Cs2AlF5  from Rietveld refinement (including the Fullprof .pcr and .dat files) and DFT

data_Cs2AlF5

_audit_update_record

;

2014-05-19 # Formatted by publCIF

;

_publ_requested_journal            'Powder Diffraction'

_journal_name_full                   'Powder Diffraction'

_journal_year                        ?

_journal_volume                      ?

_journal_issue                       ?

_journal_page_first                  ?

_journal_page_last                   ?

#=============================================================================

# 1. SUBMISSION DETAILS

_publ_contact_author_name        'Armel Le Bail'

_publ_contact_author_address

;

Universit\'e du Maine, Institut des Mol\'ecules et des Mat\'eriaux du Mans,

CNRS UMR 6283, 72085 Le Mans, France

;

_publ_contact_author_email           'armel.le_bail@univ-lemans.fr'

_publ_contact_author_fax             '33 (0)2 43 83 35 06'

_publ_contact_author_phone           '33 (0)2 43 83 33 47'

# Definition of non standard CIF items (Reliability indices used in FULLPROF)

loop_

_publ_manuscript_incl_extra_item

_publ_manuscript_incl_extra_info

_publ_manuscript_incl_extra_defn

#      Name                               Explanation                 Standard?

#     ------                              -----------                 ---------

'_pd_proc_ls_prof_cR_factor'    'Prof. R-factor CORRECTED for background'   no

'_pd_proc_ls_prof_cwR_factor'   'wProf.R-factor CORRECTED for background'   no

'_pd_proc_ls_prof_cwR_expected' 'wProf.Expected CORRECTED for background'   no

'_pd_proc_ls_prof_chi2'         'Chi-square for all considered points'      no

'_pd_proc_ls_prof_echi2'        'Chi-2 for points with Bragg contribution'  no

#=============================================================================

# 3. TITLE AND AUTHOR LIST

_publ_section_title

;

Face-sharing octahedra in Cs~2~AlF~5~ and Cs~3~Al~2~F~9~

;

_publ_section_title_footnote

.

# The loop structure below should contain the names and addresses of all

# authors, in the required order of publication. Repeat as necessary.

loop_

_publ_author_name

_publ_author_address

'Le Bail, Armel'

;

Universit\'e du Maine, Institut des Mol\'ecules et des Mat\'eriaux du Mans,

CNRS UMR 6283, 72085 Le Mans, France

;

'Smrcok, Lubomir'

;

Institute of Inorganic Chemistry, Slovak Academy of Sciences, Dubravska

cesta 9, 845 36 Bratislava, Slovak Republic

;

_publ_section_abstract

;

Face-sharing octahedra in Cs~2~AlF~5~ and Cs~3~Al~2~F~9~

;

#=============================================================================

# 5. CHEMICAL DATA

_chemical_name_systematic

?

_chemical_name_common             ?

_chemical_formula_moiety          'Al2 F9, Al F6, 6(Cs)'

_chemical_formula_structural      ?

_chemical_formula_analytical      ?

_chemical_formula_iupac           ?

_chemical_formula_sum             'Al3 Cs6 F15'

_chemical_formula_weight          1163.40

_chemical_melting_point           ?

_chemical_compound_source         ?       # for minerals and

# natural products

loop_

_atom_type_symbol

_atom_type_scat_Cromer_Mann_a1

_atom_type_scat_Cromer_Mann_b1

_atom_type_scat_Cromer_Mann_a2

_atom_type_scat_Cromer_Mann_b2

_atom_type_scat_Cromer_Mann_a3

_atom_type_scat_Cromer_Mann_b3

_atom_type_scat_Cromer_Mann_a4

_atom_type_scat_Cromer_Mann_b4

_atom_type_scat_Cromer_Mann_c

_atom_type_scat_dispersion_real

_atom_type_scat_dispersion_imag

_atom_type_scat_source

Cs  20.35240   3.55200  19.12780   0.30860  10.28210  23.71280

0.96150  59.45650   3.27910  -0.7460   7.90500

International_Tables_for_Crystallography_Vol.C(1991)_Tables_6.1.1.4_and_6.1.1.5

Al   4.17448   1.93816   3.38760   4.14553   1.20296   0.22875

0.52814   8.28524   0.70679   0.21300   0.24600

International_Tables_for_Crystallography_Vol.C(1991)_Tables_6.1.1.4_and_6.1.1.5

F    3.63220   5.27756   3.51057  14.73530   1.26064   0.44226

0.94071  47.34370   0.65340   0.07300   0.05300

International_Tables_for_Crystallography_Vol.C(1991)_Tables_6.1.1.4_and_6.1.1.5

#=============================================================================

# 6. POWDER SPECIMEN AND CRYSTAL DATA

_symmetry_cell_setting                orthorhombic

_symmetry_space_group_name_H-M       'P m n 21'

_symmetry_space_group_name_Hall      'P 2ac -2'

loop_

_symmetry_equiv_pos_as_xyz   #<--must include 'x,y,z'

'x,y,z'

'-x,y,z'

'x+1/2,-y,z+1/2'

'-x+1/2,-y,z+1/2'

_cell_length_a                       6.36216(17)

_cell_length_b                       12.7523(4)

_cell_length_c                       11.4102(3)

_cell_angle_alpha                    90.00000

_cell_angle_beta                     90.00000

_cell_angle_gamma                    90.00000

_cell_volume                         925.73(5)

_cell_formula_units_Z                2

_cell_measurement_temperature        295

_pd_char_colour                   white

_exptl_crystal_density_diffrn     4.174

_exptl_crystal_F_000               1008.0

_diffrn_ambient_temperature          295

_diffrn_radiation_source         'X-ray tube'

_diffrn_radiation_type           'CuK\a'

_diffrn_radiation_wavelength     1.5418

_diffrn_radiation_monochromator      graphite

_diffrn_measurement_device_type      'Siemens D500'

_diffrn_measurement_method           'step scan'

# The following three fields describe the preparation of the specimen.

# The cooling rate is in K/min.  The pressure at which the sample was

# prepared is in kPa.  The temperature of preparation is in K.

_pd_prep_cool_rate                ?

_pd_prep_pressure                 ?

_pd_prep_temperature              ?

# The next four fields are normally only needed for transmission experiments.

_exptl_absorpt_coefficient_mu        93.792

_exptl_absorpt_correction_type       ?

_exptl_absorpt_process_details       ?

_exptl_absorpt_correction_T_min      ?

_exptl_absorpt_correction_T_max      ?

#=============================================================================

#  The following four items give details of the measured (not processed)

#  powder pattern.  Angles are in degrees.

_pd_meas_number_of_points         6701

_pd_meas_2theta_range_min         5.00000

_pd_meas_2theta_range_max         139.00000

_pd_meas_2theta_range_inc         0.020000

#=============================================================================

# 8. REFINEMENT DATA

_refine_special_details

?

# Use the next field to give any special details about the fitting of the

# powder pattern.

_pd_proc_ls_special_details

?

# The next three items are given as text.

_pd_proc_ls_profile_function      ?

_pd_proc_ls_background_function   ?

_pd_proc_ls_pref_orient_corr

?

#  The following profile R-factors are NOT CORRECTED for background

#  The sum is extended to all non-excluded points.

#  These are the current CIF standard

_pd_proc_ls_prof_R_factor                4.5449

_pd_proc_ls_prof_wR_factor               6.2085

_pd_proc_ls_prof_wR_expected             2.4165

#  The following profile R-factors are CORRECTED for background

#  The sum is extended to all non-excluded points.

#  These items are not in the current CIF standard, but are defined above

_pd_proc_ls_prof_cR_factor               10.4134

_pd_proc_ls_prof_cwR_factor              11.7231

_pd_proc_ls_prof_cwR_expected             4.5629

#  The following items are not in the CIF standard, but are defined above

_pd_proc_ls_prof_chi2                 6.6010

_pd_proc_ls_prof_echi2                6.6010

#  Items related to LS refinement

_refine_ls_R_I_factor                 3.9530

_refine_ls_number_reflns                  998

_refine_ls_number_parameters                93

_refine_ls_number_restraints                25

_refine_ls_goodness_of_fit_all            2.569

_refine_ls_shift/su_max                   0.03

# The following four items apply to angular dispersive measurements.

# 2theta minimum, maximum and increment (in degrees) are for the

# intensities used in the refinement.

_pd_proc_2theta_range_min                5.0579

_pd_proc_2theta_range_max              139.0579

_pd_proc_2theta_range_inc              0.020000

_pd_proc_wavelength                    1.540560

_pd_block_diffractogram_id        ?  # The id used for the block containing

# the powder pattern profile (section 11)

# Give appropriate details in the next two text fields.

_pd_proc_info_excluded_regions    ?

_pd_proc_info_data_reduction      ?

# The following items are used to identify the programs used.

_computing_data_collection           ?

_computing_structure_solution        ESPOIR

_computing_structure_refinement      FULLPROF

_computing_molecular_graphics        DIAMOND

_computing_publication_material      ?

#=============================================================================

# 9. ATOMIC COORDINATES AND DISPLACEMENT PARAMETERS

loop_

_atom_site_label

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_occupancy

_atom_site_adp_type              # Not in version 2.0.1

_atom_site_type_symbol

Cs1  0.00000  0.9882(4)  0.00000  0.0307(9)  1.00000 Uiso Cs

Cs2  0.00000  0.3385(4)  0.9682(5)  0.0307(9)  1.00000 Uiso Cs

Cs3  0.00000  0.6478(3)  0.0453(5)  0.0307(9)  1.00000 Uiso Cs

Cs4  0.00000  0.4375(3)  0.3199(6)  0.0307(9)  1.00000 Uiso Cs

Cs5  0.00000  0.7730(3)  0.6689(6)  0.0307(9)  1.00000 Uiso Cs

Cs6  0.00000  0.1814(3)  0.6670(5)  0.0307(9)  1.00000 Uiso Cs

Al1  0.50000  0.0923(6)  0.8404(7)  0.005(3)  1.00000 Uiso Al

Al2  0.00000  0.4759(6)  0.6720(7)  0.005(3)  1.00000 Uiso Al

Al3  0.50000 -0.1094(6)  0.8433(7)  0.005(3)  1.00000 Uiso Al

F1  0.2993(19)  0.1651(10)  0.9002(9)  0.020(2)  1.00000 Uiso F

F2  0.3167(17) -0.0083(6)  0.7755(10)  0.020(2)  1.00000 Uiso F

F3  0.50000  0.1707(12)  0.7152(8)  0.020(2)  1.00000 Uiso F

F4  0.50000 -0.0085(7)  0.9643(7)  0.020(2)  1.00000 Uiso F

F5  0.212(2)  0.5463(13)  0.6065(13)  0.020(2)  1.00000 Uiso F

F6 -0.208(2)  0.4012(11)  0.7411(13)  0.020(2)  1.00000 Uiso F

F7  0.00000  0.5744(13)  0.7839(14)  0.020(2)  1.00000 Uiso F

F8  0.00000  0.3780(12)  0.5602(14)  0.020(2)  1.00000 Uiso F

F9  0.2925(19) -0.1796(10)  0.9002(9)  0.020(2)  1.00000 Uiso F

F10  0.50000 -0.1828(12)  0.7152(8)  0.020(2)  1.00000 Uiso F

#=============================================================================

#                       MOLECULAR GEOMETRY                                    #

#=============================================================================#

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

Al1   F1    1.720(13)     1_555 ?

Al1   F2    1.885(11)     1_555 ?

Al1   F3    1.744(14)     1_555 ?

Al1   F4    1.911(12)     1_555 ?

Al2   F5    1.784(15)     1_555 ?

Al2   F6    1.811(15)     1_555 ?

Al2   F7    1.791(18)     1_555 ?

Al2   F8    1.785(17)     1_555 ?

Al3   F2    1.903(11)     1_555 ?

Al3   F4    1.887(12)     1_555 ?

Al3   F9    1.722(13)     1_555 ?

Al3   F10   1.736(14)     1_555 ?

Al1   Al3   2.572(11)     1_555 ?

Cs1   F1    3.164(13)     1_564 ?

Cs1   F2    3.259(11)     1_564 ?

Cs1   F2    3.363(11)     3_464 ?

Cs1   F3    3.184(12)     3_464 ?

Cs1   F4    3.2073(10)    1_564 ?

Cs1   F9    3.056(13)     1_564 ?

Cs1   F10   3.491(13)     3_464 ?

Cs2   F1    3.020(13)     1_555 ?

Cs2   F5    2.829(15)     3_465 ?

Cs2   F6    3.017(15)     1_555 ?

Cs2   F7    3.670(17)     1_555 ?

Cs2   F10   3.448(13)     3_455 ?

Cs3   F3    3.019(14)     3_464 ?

Cs3   F5    3.158(16)     3_464 ?

Cs3   F6    2.972(15)     3_564 ?

Cs3   F7    3.126(17)     1_554 ?

Cs3   F8    3.2026(19)    3_464 ?

Cs3   F9    3.324(13)     1_564 ?

Cs4   F5    3.054(15)     3_464 ?

Cs4   F6    2.914(14)     3_564 ?

Cs4   F7    3.211(2)      3_464 ?

Cs4   F8    2.845(17)     1_555 ?

Cs4   F9    3.660(13)     3_454 ?

Cs4   F10   3.461(15)     3_454 ?

Cs5   F1    3.414(12)     3_464 ?

Cs5   F2    3.649(10)     1_565 ?

Cs5   F4    3.804(10)     3_464 ?

Cs5   F5    3.269(16)     1_555 ?

Cs5   F7    2.852(17)     1_555 ?

Cs5   F9    3.285(12)     1_565 ?

Cs5   F10   3.274(3)      1_465 ?

Cs6   F1    3.279(12)     1_555 ?

Cs6   F2    3.383(10)     1_555 ?

Cs6   F3    3.2312(20)    1_555 ?

Cs6   F4    3.195(10)     3_454 ?

Cs6   F6    3.213(14)     1_555 ?

Cs6   F8    2.788(16)     1_555 ?

Cs6   F9    3.318(12)     3_454 ?

F1    F1    3.808(17)     2_555 ?

F1    F1    2.554(17)     2_655 ?

F1    F2    2.632(15)     1_555 ?

F1    F2    3.589(16)     2_655 ?

F1    F3    2.468(13)     1_555 ?

F1    F4    2.658(15)     1_555 ?

F1    F6    3.563(19)     2_555 ?

F2    F1    2.632(15)     1_555 ?

F2    F1    3.589(16)     2_655 ?

F2    F2    2.332(15)     2_655 ?

F2    F3    2.654(16)     1_555 ?

F2    F4    2.450(13)     1_555 ?

F2    F9    2.612(15)     1_555 ?

F2    F9    3.603(16)     2_655 ?

F2    F10   2.605(16)     1_555 ?

F3    F1    2.468(13)     1_555 ?

F3    F2    2.654(16)     1_555 ?

F3    F4    3.647(15)     1_555 ?

F3    F6    3.490(19)     1_655 ?

F4    F1    2.658(15)     1_555 ?

F4    F2    2.450(13)     1_555 ?

F4    F3    3.647(15)     1_555 ?

F4    F9    2.653(15)     1_555 ?

F4    F10   3.608(15)     1_555 ?

F5    F5    2.698(18)     2_555 ?

F5    F5    3.665(18)     2_655 ?

F5    F6    3.595(20)     1_555 ?

F5    F6    2.40(2)       2_555 ?

F5    F7    2.459(20)     1_555 ?

F5    F8    2.59(2)       1_555 ?

F6    F1    3.563(19)     2_555 ?

F6    F3    3.490(19)     1_455 ?

F6    F5    3.595(20)     1_555 ?

F6    F5    2.40(2)       2_555 ?

F6    F6    3.716(18)     2_455 ?

F6    F6    2.647(18)     2_555 ?

F6    F7    2.621(20)     1_555 ?

F6    F8    2.470(20)     1_555 ?

F7    F5    2.459(20)     1_555 ?

F7    F6    2.621(20)     1_555 ?

F7    F8    3.58(2)       1_555 ?

F7    F9    3.881(19)     1_565 ?

F8    F5    2.59(2)       1_555 ?

F8    F6    2.470(20)     1_555 ?

F8    F7    3.58(2)       1_555 ?

F8    F9    3.388(19)     3_454 ?

F9    F2    2.612(15)     1_555 ?

F9    F2    3.603(16)     2_655 ?

F9    F4    2.653(15)     1_555 ?

F9    F7    3.881(19)     1_545 ?

F9    F8    3.388(19)     3_555 ?

F9    F9    3.722(17)     2_555 ?

F9    F9    2.640(17)     2_655 ?

F9    F10   2.490(13)     1_555 ?

F10   F2    2.605(16)     1_555 ?

F10   F4    3.608(15)     1_555 ?

F10   F9    2.490(13)     1_555 ?

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

F1   Al1  F1   95.9(10)       1_555    2_655 ?

F1   Al1  F2   93.7(9)        1_555    1_555 ?

F1   Al1  F2   169.2(11)      1_555    2_655 ?

F1   Al1  F3   90.9(9)        1_555    1_555 ?

F1   Al1  F4   94.0(9)        1_555    1_555 ?

F2   Al1  F2   76.4(8)        1_555    2_655 ?

F2   Al1  F3   93.9(9)        1_555    1_555 ?

F2   Al1  F4   80.4(7)        1_555    1_555 ?

F3   Al1  F4   172.7(11)      1_555    1_555 ?

F5   Al2  F5   98.2(11)       1_555    2_555 ?

F5   Al2  F6   177.8(14)      1_555    1_555 ?

F5   Al2  F6   84.0(11)       1_555    2_555 ?

F5   Al2  F7   86.9(11)       1_555    1_555 ?

F5   Al2  F8   93.0(12)       1_555    1_555 ?

F6   Al2  F6   93.9(11)       1_555    2_555 ?

F6   Al2  F7   93.4(12)       1_555    1_555 ?

F6   Al2  F8   86.7(11)       1_555    1_555 ?

F7   Al2  F8   179.9(17)      1_555    1_555 ?

F2   Al3  F2   75.6(7)        1_555    2_655 ?

F2   Al3  F4   80.5(7)        1_555    1_555 ?

F2   Al3  F9   92.0(9)        1_555    1_555 ?

F2   Al3  F9   167.2(11)      1_555    2_655 ?

F2   Al3  F10  91.3(9)        1_555    1_555 ?

F4   Al3  F9   94.5(9)        1_555    1_555 ?

F4   Al3  F10  169.7(11)      1_555    1_555 ?

F9   Al3  F9   100.1(11)      1_555    2_655 ?

F9   Al3  F10  92.1(9)        1_555    1_555 ?

Al1  F2   Al3  85.5(7)        1_555    1_555 ?

Al1  F4   Al3  85.3(7)        1_555    1_555 ?

_iucr_refine_instructions_details

;

Fullprof .pcr file, modified to fit inside 80 columns

followed by the .dat file   and   DFT optimization CIF

COMM Cs2AlF5   Pmn21

! Current global Chi2 (Bragg contrib.) =      6.601

! Files => DAT-file: pmn21-2.dat,  PCR-file: pmn21-2

!Job Npr Nph Nba Nex Nsc Nor Dum Iwg Ilo Ias Res Ste Nre Cry Uni Cor Opt Aut

0   5   3  37   2   0   1   1   0   0   1   0   0   0   0   0   0   0   0

!

!Ipr Ppl Ioc Mat Pcr Ls1 Ls2 Ls3 NLI Prf Ins Rpa Sym Hkl Fou Sho Ana

0   0   1   0   2   0   4   0   0  -3   0  -1   1   0   2   1   1

!

! Lambda1  Lambda2    Ratio    Bkpos    Wdt    Cthm     muR   AsyLim

!  Rpolarz  2nd-muR -> Patt# 1

1.540560 1.544390  0.50000   50.000 15.0000  0.7990  0.0000   90.00

0.0000  0.0000

!

!NCY  Eps  R_at  R_an  R_pr  R_gl     Thmin       Step       Thmax

!  PSD    Sent0

8  0.01  0.40  0.40  0.40  0.60      5.0000   0.020000   139.0000

0.000   0.000

!

!2Theta/TOF/E(Kev)   Background  for Pattern#  1

5.0458      6196.3809        521.00

5.3125      5852.8750        531.00

5.7292      5209.8838        541.00

7.1875      4020.1123        551.00

7.7800      3897.9067        561.00

8.7500      3367.3289        571.00

11.0417      2586.0649        581.00

12.8125      2331.7996        591.00

14.7917      1958.0409        601.00

18.5417      1842.7588        611.00

23.4375      1507.1937        621.00

25.0000      1314.9084        911.00

26.8000       427.2518        901.00

27.0000      1363.9010        791.00

30.3125       673.0379        631.00

33.2292       899.6513        641.00

37.0000       936.8129        801.00

41.6667       714.7286        651.00

47.0000       817.6890        811.00

53.2292       704.0854        661.00

55.6250       602.2286        391.00

59.6875       641.4581        411.00

62.0000       646.1372        821.00

67.0000       656.9584        831.00

72.3958       649.3607        201.00

78.0000       663.3190        841.00

84.1667       550.9722        221.00

89.0625       511.6830        371.00

96.4583       604.1265        401.00

101.0000       585.5984        851.00

107.2917       632.4729        701.00

115.4167       586.6902        711.00

119.0000       633.7708        861.00

123.9583       558.5566        721.00

128.8542       766.8923        731.00

135.8333       800.8095        741.00

138.3333       666.4922        751.00

!

! Excluded regions (LowT  HighT) for Pattern#  1

2.00        5.00

138.50      180.00

!

!

93    !Number of refined parameters

!

!  Zero    Code    SyCos    Code   SySin    Code  Lambda     Code MORE ->Patt# 1

-0.05785  431.0  0.00000    0.0  0.00000    0.0 0.000000    0.00   0

!-------------------------------------------------------------------------------

!  Data for PHASE number:   1  ==> Current R_Bragg for Pattern#  1:     3.95

!-------------------------------------------------------------------------------

Cs2AlF5

!

!Nat Dis Ang Pr1 Pr2 Pr3 Jbt Irf Isy Str Furth       ATZ    Nvk Npr More

19  25   0 1.0 0.0 0.0   0   0   0   0   0       2326.707   0   5   1

!

!Jvi Jdi Hel Sol Mom Ter  Brind   RMua    RMub    RMuc   Jtyp  Nsp_Ref

!Ph_Shift N_Domains

0   3   0   0   0   0  1.0000  0.0000  0.0000  0.0000    0      0

0      0

!

! Max_dst(dist) (angles)  Bond-Valence Calc.

4.0000      3.5000        1

P M N 21                 <--Space group symbol

!Atom   Typ       X        Y        Z     Biso       Occ     In Fin N_t Spc

! /Codes

Cs1    Cs+1    0.00000  0.98817  0.00000  2.42439   0.50000   0   0   0    0

0.00    21.00     0.00   871.00      0.00

Cs2    Cs+1    0.00000  0.33853  0.96817  2.42439   0.50000   0   0   0    0

0.00    31.00    41.00   871.00      0.00

Cs3    Cs+1    0.00000  0.64776  0.04529  2.42439   0.50000   0   0   0    0

0.00    51.00    61.00   871.00      0.00

Cs4    Cs+1    0.00000  0.43747  0.31990  2.42439   0.50000   0   0   0    0

0.00    71.00    81.00   871.00      0.00

Cs5    Cs+1    0.00000  0.77301  0.66888  2.42439   0.50000   0   0   0    0

0.00    91.00   101.00   871.00      0.00

Cs6    Cs+1    0.00000  0.18141  0.66702  2.42439   0.50000   0   0   0    0

0.00   111.00   121.00   871.00      0.00

Al1    Al+3    0.50000  0.09230  0.84039  0.42319   0.50000   0   0   0    0

0.00   131.00   141.00   881.00      0.00

Al2    Al+3    0.00000  0.47592  0.67203  0.42319   0.50000   0   0   0    0

0.00   241.00   251.00   881.00      0.00

Al3    Al+3    0.50000 -0.10940  0.84329  0.42319   0.50000   0   0   0    0

0.00   421.00   361.00   881.00      0.00

F1     F-1     0.29926  0.16510  0.90019  1.59221   1.00000   0   0   0    0

151.00   161.00   171.00   891.00      0.00

F2     F-1     0.31668 -0.00827  0.77553  1.59221   1.00000   0   0   0    0

761.00   181.00   191.00   891.00      0.00

F3     F-1     0.50000  0.17069  0.71517  1.59221   0.50000   0   0   0    0

0.00   931.00   211.00   891.00      0.00

F4     F-1     0.50000 -0.00847  0.96426  1.59221   0.50000   0   0   0    0

0.00   691.00   231.00   891.00      0.00

F5     F-1     0.21197  0.54629  0.60649  1.59221   1.00000   0   0   0    0

261.00   271.00   281.00   891.00      0.00

F6     F-1    -0.20818  0.40122  0.74108  1.59221   1.00000   0   0   0    0

921.00   291.00   301.00   891.00      0.00

F7     F-1     0.00000  0.57444  0.78393  1.59221   0.50000   0   0   0    0

0.00   311.00   321.00   891.00      0.00

F8     F-1     0.00000  0.37804  0.56024  1.59221   0.50000   0   0   0    0

0.00   331.00   341.00   891.00      0.00

F9     F-1     0.29252 -0.17965  0.90019  1.59221   1.00000   0   0   0    0

771.00   381.00   171.00   891.00      0.00

F10    F-1     0.50000 -0.18278  0.71517  1.59221   0.50000   0   0   0    0

0.00   681.00   211.00   891.00      0.00

!-------> Profile Parameters for Pattern #  1

!  Scale        Shape1      Bov      Str1      Str2      Str3   Strain-Model

0.33227E-03   1.33812   0.00000   0.00000   0.00000   0.00000       0

11.00000   441.000     0.000     0.000     0.000     0.000

!       U         V          W           X          Y        GauSiz   LorSiz

!Size-Model

0.220087  -0.150260   0.052154  -0.012115   0.000000   0.000000   0.000000

0

351.000    451.000    461.000    781.000      0.000      0.000      0.000

!     a          b         c        alpha      beta       gamma

!   #Cell Info

6.362158  12.752314  11.410244  90.000000  90.000000  90.000000

471.00000  481.00000  491.00000    0.00000    0.00000    0.00000

!  Pref1    Pref2      Asy1     Asy2     Asy3     Asy4

1.00000  0.00000  0.04672  0.02986  0.00000  0.00000

0.00     0.00   501.00   511.00     0.00     0.00

! Soft distance constraints:

Al1  F1     1    0.00000    0.00000    0.00000    1.75000    0.01000

Al1  F2     1    0.00000    0.00000    0.00000    1.90000    0.01000

Al1  F3     1    0.00000    0.00000    0.00000    1.75000    0.01000

Al1  F4     1    0.00000    0.00000    0.00000    1.90000    0.01000

Al2  F5     1    0.00000    0.00000    0.00000    1.81000    0.01000

Al2  F6     1    0.00000    0.00000    0.00000    1.81000    0.01000

Al2  F7     1    0.00000    0.00000    0.00000    1.81000    0.01000

Al2  F8     1    0.00000    0.00000    0.00000    1.81000    0.01000

Al3  F9     1    0.00000    0.00000    0.00000    1.75000    0.01000

Al3  F10    1    0.00000    0.00000    0.00000    1.75000    0.01000

Al3  F4     1    0.00000    0.00000    0.00000    1.90000    0.01000

Al3  F2     1    0.00000    0.00000    0.00000    1.90000    0.01000

F1   F2     1    0.00000    0.00000    0.00000    2.56000    0.02000

F1   F3     1    0.00000    0.00000    0.00000    2.56000    0.02000

F1   F4     1    0.00000    0.00000    0.00000    2.56000    0.02000

F2   F3     1    0.00000    0.00000    0.00000    2.56000    0.02000

F2   F4     1    0.00000    0.00000    0.00000    2.56000    0.02000

F5   F7     1    0.00000    0.00000    0.00000    2.56000    0.02000

F5   F8     1    0.00000    0.00000    0.00000    2.56000    0.02000

F6   F7     1    0.00000    0.00000    0.00000    2.56000    0.02000

F6   F8     1    0.00000    0.00000    0.00000    2.56000    0.02000

F9   F2     1    0.00000    0.00000    0.00000    2.56000    0.02000

F9   F4     1    0.00000    0.00000    0.00000    2.56000    0.02000

F9   F10    1    0.00000    0.00000    0.00000    2.56000    0.02000

F10  F2     1    0.00000    0.00000    0.00000    2.56000    0.02000

!-------------------------------------------------------------------------------

!  Data for PHASE number:   2  ==> Current R_Bragg for Pattern#  1:     1.76

!-------------------------------------------------------------------------------

Impurity..

!

!Nat Dis Ang Pr1 Pr2 Pr3 Jbt Irf Isy Str Furth       ATZ    Nvk Npr More

0   0   0 1.0 0.0 0.0   2   2   0   0   0          0.000   0   5   0

!

R -3 M                   <--Space group symbol

!-------> Profile Parameters for Pattern #  1

!  Scale        Shape1      Bov      Str1      Str2      Str3   Strain-Model

0.10000E-02   0.79296   0.00000   0.00000   0.00000   0.00000       0

0.00000     0.000     0.000     0.000     0.000     0.000

!       U         V          W           X          Y        GauSiz   LorSiz

!Size-Model

0.140780  -0.113627   0.051255   0.000000   0.000000   0.000000   0.000000

0

0.000      0.000      0.000      0.000      0.000      0.000      0.000

!     a          b         c        alpha      beta       gamma      #Cell Info

6.335784   6.335784  22.244698  90.000000  90.000000 120.000000

0.00000    0.00000    0.00000    0.00000    0.00000    0.00000

!  Pref1    Pref2      Asy1     Asy2     Asy3     Asy4

1.00000  0.00000  0.20675 -0.00784  0.00000  0.00000

0.00     0.00     0.00     0.00     0.00     0.00

!-------------------------------------------------------------------------------

!  Data for PHASE number:   3  ==> Current R_Bragg for Pattern#  1:     6.54

!-------------------------------------------------------------------------------

Cs3Al2F9

!

!Nat Dis Ang Pr1 Pr2 Pr3 Jbt Irf Isy Str Furth       ATZ    Nvk Npr More

5   0   0 1.0 0.0 0.0   0   0   0   0   0       7184.619   0   5   1

!

!Jvi Jdi Hel Sol Mom Ter  Brind   RMua    RMub    RMuc   Jtyp  Nsp_Ref Ph_Shift

!N_Domains

0   3   0   0   0   0  1.0000  0.0000  0.0000  0.0000    0      0      0

0

!

! Max_dst(dist) (angles)  Bond-Valence Calc.

4.0000      3.5000        1

P 63/M M C               <--Space group symbol

!Atom   Typ       X        Y        Z     Biso       Occ     In Fin N_t Spc

! /Codes

CS1    CS+1    0.33333  0.66667  0.75000  2.23247   0.20000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

CS2    CS+1    0.33333  0.66667  0.42690  1.77334   0.40000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

AL1    AL+3    0.00000  0.00000  0.16459  1.93256   0.40000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

F1     F-1     0.14000  0.28000  0.25000  3.61021   0.60000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

F2     F-1     0.13260  0.26520  0.58280  3.61021   1.20000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

!-------> Profile Parameters for Pattern #  1

!  Scale        Shape1      Bov      Str1      Str2      Str3   Strain-Model

0.59016E-05   0.74002   0.00000   0.00000   0.00000   0.00000       0

671.00000     0.000     0.000     0.000     0.000     0.000

!       U         V          W           X          Y        GauSiz   LorSiz

!Size-Model

0.140780  -0.113627   0.051255   0.000000   0.000000   0.000000   0.000000

0

0.000      0.000      0.000      0.000      0.000      0.000      0.000

!     a          b         c        alpha      beta       gamma      #Cell Info

6.253500   6.253500  14.719301  90.000000  90.000000 120.000000

0.00000    0.00000    0.00000    0.00000    0.00000    0.00000

!  Pref1    Pref2      Asy1     Asy2     Asy3     Asy4

1.00000  0.00000  0.07024  0.07963  0.00000  0.00000

0.00     0.00     0.00     0.00     0.00     0.00

!  2Th1/TOF1    2Th2/TOF2  Pattern # 1

5.000     138.500       1

Fullprof .dat file  :

5.000    0.02000   139.000

6265      6202      6170      5912      6241      6115      6191      6153

6109      6040      6020      5983      5982      5903      5849      5820

5829      5798      5754      5719      5679      5716      5687      5625

5593      5573      5547      5531      5515      5444      5455      5409

5399      5375      5375      5321      5312      5251      5223      5233

5216      5195      5142      5146      5092      5097      5104      5093

5095      5079      5052      4997      4953      4903      4928      4879

4926      4897      4893      4884      4863      4846      4819      4818

4763      4751      4714      4742      4759      4787      4696      4697

4627      4658      4678      4661      4617      4622      4580      4638

4584      4602      4527      4505      4487      4522      4510      4585

4551      4571      4628      4603      4612      4592      4549      4505

4550      4426      4452      4392      4358      4291      4320      4245

4279      4237      4199      4108      4134      4162      4168      4178

4135      4126      4134      4137      4077      4055      3988      4073

4019      4038      4051      4090      4054      4094      4003      3985

3973      3970      3935      3960      3949      3940      3916      3899

3859      3881      3920      3871      3840      3824      3792      3838

3841      3803      3790      3809      3788      3817      3784      3816

3774      3781      3750      3749      3731      3724      3706      3687

3665      3678      3642      3631      3585      3614      3574      3598

3614      3568      3548      3539      3509      3537      3560      3503

3537      3484      3526      3513      3507      3467      3449      3427

3463      3466      3464      3457      3407      3364      3360      3352

3361      3365      3382      3384      3370      3328      3350      3331

3362      3330      3319      3275      3274      3253      3281      3238

3264      3224      3213      3217      3251      3252      3248      3217

3176      3170      3160      3127      3083      3107      3084      3108

3150      3129      3116      3138      3134      3127      3125      3070

3069      3078      3076      3057      3059      3039      3061      3082

3055      3035      3039      3063      3027      3034      3029      3003

2981      3000      2954      2953      2959      2943      2943      2961

2957      2985      2982      2976      2988      2984      2991      2985

2972      2973      2966      2970      2985      2983      2988      2987

2933      2899      2884      2872      2852      2842      2842      2792

2792      2802      2783      2789      2817      2764      2755      2708

2692      2732      2745      2738      2741      2690      2711      2718

2709      2707      2704      2697      2693      2617      2628      2649

2621      2669      2696      2636      2675      2677      2626      2594

2602      2557      2609      2634      2626      2593      2611      2619

2614      2580      2515      2513      2534      2561      2552      2556

2516      2497      2508      2500      2518      2549      2533      2507

2530      2516      2495      2493      2473      2480      2499      2498

2460      2483      2474      2451      2456      2479      2473      2439

2436      2389      2399      2427      2454      2431      2461      2438

2413      2385      2387      2357      2365      2352      2404      2397

2378      2334      2311      2296      2349      2346      2330      2305

2299      2304      2339      2370      2327      2308      2335      2331

2321      2360      2339      2328      2334      2312      2266      2283

2284      2284      2266      2256      2260      2262      2287      2308

2272      2272      2278      2273      2284      2272      2241      2297

2280      2233      2229      2226      2249      2300      2257      2225

2244      2255      2288      2287      2259      2239      2230      2217

2232      2262      2247      2238      2255      2270      2249      2275

2268      2277      2323      2337      2285      2250      2263      2288

2299      2264      2249      2217      2209      2238      2224      2187

2200      2198      2182      2172      2168      2114      2093      2092

2112      2117      2179      2197      2164      2121      2114      2104

2126      2144      2078      2049      2063      2114      2171      2173

2130      2130      2092      2081      2105      2085      2063      2073

2095      2071      2055      2064      2059      2076      2120      2064

2010      2057      2093      2099      2105      2108      2066      2109

2118      2051      2021      2065      2084      2108      2120      2141

2142      2148      2182      2195      2227      2254      2257      2260

2307      2337      2351      2340      2373      2413      2484      2558

2675      2740      2809      2868      2917      2981      3080      3080

2991      2826      2664      2548      2527      2559      2613      2669

2726      2821      2935      3040      3198      3370      3534      3711

3857      3901      3843      3652      3366      3051      2747      2462

2280      2182      2112      2115      2153      2166      2135      2095

2060      2073      2126      2126      2114      2091      2079      2122

2156      2113      2117      2081      2031      2064      2096      2072

2063      2086      2131      2182      2178      2163      2161      2194

2232      2192      2109      2084      2066      2051      2097      2117

2153      2190      2192      2160      2196      2256      2313      2324

2338      2322      2291      2275      2270      2251      2267      2291

2285      2246      2225      2246      2216      2245      2263      2232

2217      2298      2306      2328      2298      2221      2139      2118

2098      2063      2054      2044      2026      2001      1986      2006

2038      2003      1981      1978      1969      1977      1976      1955

1923      1929      1975      1938      1931      1996      1975      1946

2002      2022      2019      2032      1995      1925      1888      1884

1873      1863      1893      1889      1878      1880      1889      1868

1849      1839      1843      1855      1851      1826      1797      1853

1868      1871      1858      1829      1792      1786      1763      1813

1865      1835      1788      1784      1788      1896      1955      1882

1794      1786      1803      1848      1879      1863      1838      1864

1908      1877      1882      1895      1893      1870      1860      1863

1895      1929      1937      1943      1962      1991      1990      1956

1916      1912      1922      1892      1889      1914      1911      1893

1893      1867      1868      1916      1925      1929      1947      1978

1984      1993      1995      1994      2016      2038      2058      2080

2116      2125      2162      2174      2188      2184      2205      2211

2226      2192      2151      2083      2048      2001      1982      1942

1926      1900      1907      1936      1958      1952      1946      1944

1963      2027      2042      2043      2052      2043      2036      2037

2090      2119      2128      2136      2166      2214      2287      2292

2302      2367      2491      2640      2765      2843      2966      3114

3308      3537      3790      4079      4464      4843      5261      5660

6029      6217      6236      6016      5740      5419      5242      5172

5342      5660      6142      6671      7315      8133      9071      9884

10410     10287      9621      8477      7158      5785      4652      3722

3209      2966      2935      2841      2697      2540      2458      2469

2490      2501      2449      2421      2397      2415      2378      2378

2341      2354      2366      2434      2436      2446      2418      2424

2486      2614      2724      2919      3076      3253      3505      3799

4073      4392      4570      4554      4451      4239      3943      3636

3311      3066      3017      3061      3143      3199      3231      3289

3316      3273      3127      2863      2616      2423      2300      2237

2245      2231      2266      2272      2269      2260      2308      2416

2552      2675      2772      2838      2882      2919      2900      2841

2722      2563      2392      2233      2104      2016      1934      1876

1824      1789      1757      1742      1722      1714      1668      1633

1641      1642      1652      1646      1588      1536      1550      1596

1644      1669      1646      1610      1570      1599      1613      1601

1582      1574      1590      1621      1620      1577      1552      1509

1525      1532      1564      1564      1593      1561      1545      1553

1611      1639      1669      1649      1618      1594      1592      1580

1599      1630      1669      1696      1736      1743      1789      1804

1847      1887      1926      1956      2010      2069      2151      2254

2361      2533      2721      2979      3273      3590      3980      4435

4829      5202      5354      5198      4792      4215      3577      3061

2632      2305      2098      1964      1970      2005      2087      2100

2103      2034      2010      1986      2045      2126      2253      2328

2395      2437      2546      2673      2911      3122      3403      3720

4120      4549      5056      5597      6233      6868      7463      7725

7615      7027      6141      5068      4161      3403      2964      2702

2583      2500      2431      2358      2276      2194      2077      2057

2086      2191      2292      2352      2353      2373      2455      2611

2787      2987      3158      3294      3478      3608      3716      3851

3987      4170      4429      4649      4968      5470      6072      6881

7750      8835     10015     11365     12866     14370     15668     16610

16824     16226     15266     14335     13854     14162     15195     16750

18826     21190     23501     25128     25628     24439     21690     17854

13924     10411      8057      6396      5369      4608      4121      3851

3762      3599      3421      3182      2987      2888      2838      2778

2761      2762      2828      2913      3041      3152      3316      3572

3869      4200      4543      4880      5327      5952      6721      7613

8656      9825     11449     13638     16300     19423     22904     26402

29586     31706     31997     30187     26572     21894     17259     13330

10411      8320      6933      5915      5341      5015      4781      4511

4294      4048      3868      3781      3797      3813      3917      4003

4116      4369      4688      5054      5533      6052      6740      7686

8856     10246     11750     13236     14673     15869     16573     16350

15096     12971     10573      8340      6660      5497      4742      4196

3866      3595      3425      3228      3012      2815      2665      2569

2473      2351      2330      2423      2660      2917      3130      3204

3043      2742      2324      1893      1612      1479      1386      1382

1330      1317      1308      1325      1351      1349      1388      1425

1457      1494      1535      1513      1579      1612      1679      1730

1797      1830      1827      1808      1749      1645      1562      1473

1345      1309      1245      1242      1285      1286      1303      1325

1286      1276      1263      1242      1270      1287      1297      1313

1367      1441      1554      1688      1806      1953      2137      2331

2535      2692      2727      2671      2462      2194      1925      1651

1482      1362      1248      1199      1188      1140      1156      1119

1083      1077      1046      1030      1006       967       948       918

887       894       880       883       865       864       868       882

889       883       872       877       882       877       874       855

870       899       916       914       895       884       876       895

935       960       985      1003       982       949       925       930

977      1013      1025       987       948       936       931       954

990       988      1014      1014      1015      1047      1101      1147

1194      1196      1185      1174      1223      1371      1551      1725

1883      2007      2162      2320      2444      2534      2516      2415

2283      2070      1955      1900      1847      1815      1787      1652

1559      1441      1320      1214      1186      1157      1159      1155

1130      1084      1091      1114      1150      1206      1266      1326

1398      1486      1598      1748      1958      2177      2422      2705

3016      3374      3745      4014      4216      4244      4138      3972

3753      3542      3454      3414      3384      3393      3365      3313

3222      3012      2651      2284      1945      1731      1610      1501

1409      1330      1303      1294      1281      1269      1230      1206

1210      1245      1296      1363      1424      1509      1587      1713

1880      2072      2312      2524      2675      2728      2696      2551

2312      2019      1766      1558      1431      1327      1210      1093

999       936       909       935       947       958       948       921

910       918       922       971       987       983       997      1007

1050      1117      1171      1202      1217      1266      1318      1342

1367      1357      1291      1241      1197      1142      1124      1128

1092      1053      1022       992      1020      1064      1092      1096

1090      1081      1108      1133      1194      1257      1296      1350

1421      1473      1583      1689      1823      2016      2260      2529

2933      3371      3893      4366      4713      4901      4863      4589

4135      3609      3084      2704      2395      2214      2072      2024

1998      1967      1929      1912      1880      1878      1927      1940

1971      2036      2109      2199      2290      2365      2423      2508

2612      2761      3011      3412      3933      4561      5383      6280

7325      8472      9527     10319     10862     10798     10136      9010

7543      6049      4826      3897      3276      2905      2676      2523

2374      2239      2119      2011      1920      1862      1784      1764

1755      1724      1699      1654      1596      1595      1576      1599

1649      1683      1742      1810      1866      1963      2096      2272

2452      2734      3094      3546      4159      4827      5416      5990

6320      6325      6012      5464      4659      3955      3328      2839

2553      2426      2274      2189      2098      2023      2023      2042

2051      2083      2075      2072      2085      2095      2102      2142

2109      2070      2027      1967      1925      1927      1972      2070

2182      2274      2352      2370      2328      2229      2054      1822

1604      1410      1285      1177      1144      1135      1144      1178

1224      1182      1173      1155      1156      1195      1267      1311

1370      1454      1551      1650      1706      1745      1710      1700

1738      1877      2022      2226      2438      2619      2784      2925

2968      2892      2758      2519      2326      2166      2080      2060

2062      2089      2190      2333      2499      2803      3210      3743

4384      5232      6109      7019      7807      8285      8261      7859

7078      6122      5173      4396      3744      3312      2988      2724

2490      2299      2151      2115      2108      2182      2268      2311

2359      2438      2482      2608      2827      3077      3393      3809

4164      4649      5259      5929      6717      7823      9106     10721

12580     14405     15828     16595     16359     14998     12953     10528

8292      6533      5485      4760      4294      3792      3347      2867

2592      2371      2265      2203      2227      2215      2209      2129

2032      1940      1868      1800      1772      1706      1668      1668

1656      1661      1686      1734      1838      2010      2234      2508

2856      3198      3481      3748      3849      3775      3574      3148

2622      2196      1835      1576      1448      1397      1353      1361

1338      1280      1205      1191      1134      1091      1057      1098

1103      1175      1257      1348      1465      1618      1730      1855

1965      2040      2072      2056      1941      1792      1631      1497

1420      1420      1383      1358      1341      1298      1253      1235

1201      1165      1151      1121      1104      1093      1093      1100

1145      1165      1181      1168      1170      1159      1187      1206

1263      1314      1411      1496      1599      1641      1659      1591

1479      1303      1168      1040       990       973       970       954

945       934       919       903       901       923       929       948

968       984      1011      1033      1040      1042      1027       980

952       915       890       861       846       829       827       830

828       813       835       856       876       927       913       910

899       913       962      1037      1084      1158      1203      1259

1340      1426      1556      1719      1920      2190      2488      2774

3006      3097      3027      2844      2543      2235      1982      1807

1700      1600      1517      1446      1380      1337      1350      1349

1357      1413      1513      1618      1767      1940      2072      2292

2557      2780      2991      3116      3181      3251      3286      3313

3418      3464      3489      3457      3286      3000      2694      2329

2013      1771      1573      1463      1386      1345      1320      1314

1279      1289      1301      1338      1394      1520      1624      1751

1905      2026      2132      2182      2142      2056      1977      1882

1832      1812      1809      1819      1810      1776      1734      1635

1514      1402      1286      1220      1165      1123      1101      1079

1063      1047       996       995       999      1031      1083      1134

1181      1214      1244      1265      1299      1347      1396      1454

1513      1575      1639      1647      1605      1553      1486      1406

1331      1284      1256      1225      1223      1224      1246      1269

1260      1226      1204      1186      1181      1209      1262      1356

1467      1543      1611      1676      1702      1690      1650      1584

1508      1438      1425      1396      1390      1393      1421      1423

1491      1553      1635      1731      1889      2054      2347      2722

3092      3506      3881      4217      4409      4446      4302      4150

3957      3814      3570      3324      3024      2747      2486      2237

2026      1927      1865      1822      1782      1752      1725      1809

1913      2023      2164      2341      2550      2821      3097      3389

3591      3754      3855      3919      3992      4115      4266      4494

4659      4754      4693      4425      4038      3650      3225      2817

2458      2161      1925      1765      1632      1524      1453      1429

1412      1367      1346      1358      1388      1412      1449      1525

1629      1801      1981      2159      2319      2474      2557      2589

2540      2362      2139      1904      1684      1568      1495      1492

1499      1489      1462      1451      1421      1454      1439      1455

1459      1441      1452      1477      1521      1586      1657      1720

1828      1961      2080      2138      2139      2085      1987      1864

1753      1667      1593      1532      1452      1364      1293      1248

1217      1219      1220      1249      1296      1380      1454      1548

1648      1812      2040      2263      2458      2570      2592      2509

2375      2202      2047      1887      1743      1652      1612      1619

1640      1694      1762      1863      1989      2143      2350      2688

3040      3368      3695      3937      4113      4159      4038      3781

3539      3235      2956      2664      2429      2248      2175      2143

2180      2231      2275      2281      2209      2115      2053      1975

1948      1966      2062      2197      2365      2528      2717      2872

2993      3074      3131      3183      3192      3226      3276      3442

3695      3992      4199      4310      4236      3972      3544      3062

2613      2245      2016      1838      1763      1766      1771      1773

1776      1804      1860      1971      2106      2290      2496      2827

3133      3541      4024      4476      4833      5135      5237      5166

4819      4272      3604      2986      2486      2143      1873      1716

1627      1542      1491      1437      1364      1323      1314      1325

1373      1397      1455      1565      1660      1770      1833      1836

1845      1810      1706      1654      1608      1585      1624      1656

1674      1791      1900      2033      2189      2350      2557      2872

3207      3485      3696      3713      3590      3298      2895      2461

2113      1810      1645      1473      1386      1393      1397      1374

1342      1249      1247      1261      1259      1277      1341      1447

1593      1737      1848      1923      1998      1983      1916      1804

1676      1598      1556      1484      1434      1341      1277      1266

1227      1177      1126      1074      1069      1086      1062      1064

1080      1102      1152      1213      1236      1281      1343      1425

1529      1693      1897      2138      2426      2714      2944      3159

3265      3190      3033      2768      2447      2180      1871      1678

1634      1571      1544      1515      1446      1507      1564      1615

1699      1803      1962      2194      2313      2434      2452      2396

2298      2189      1983      1839      1693      1588      1493      1450

1385      1360      1327      1345      1335      1402      1451      1515

1580      1701      1804      1958      2086      2179      2217      2195

2120      2051      1937      1861      1810      1753      1794      1840

1847      1829      1744      1592      1494      1356      1244      1186

1137      1166      1208      1243      1305      1385      1409      1454

1432      1410      1408      1409      1418      1417      1426      1412

1399      1353      1313      1231      1168      1069      1010       946

909       857       843       836       860       884       906       882

848       803       772       773       776       758       748       778

793       827       844       829       825       835       815       825

841       847       874       896       917       969      1005      1058

1129      1206      1286      1385      1433      1456      1413      1394

1364      1369      1394      1418      1388      1414      1367      1305

1261      1228      1174      1195      1180      1167      1195      1272

1339      1489      1603      1743      1928      2197      2418      2664

2781      2782      2677      2483      2159      1871      1619      1442

1333      1236      1159      1132      1120      1109      1078      1035

1034      1063      1070      1068      1115      1164      1229      1268

1273      1266      1254      1183      1097       995       935       887

846       824       809       800       815       811       820       800

790       756       745       733       772       764       785       777

756       739       759       734       732       733       734       766

768       727       735       748       761       776       749       729

776       841       882       912       927       963      1007      1113

1210      1282      1357      1467      1569      1687      1761      1791

1814      1878      1896      1851      1752      1638      1566      1540

1514      1517      1527      1593      1718      1899      2083      2302

2614      2941      3256      3542      3690      3670      3576      3298

2935      2603      2305      1998      1778      1626      1491      1446

1390      1284      1212      1153      1096      1055      1010       967

965       969       979      1005      1018      1039      1058      1065

1038      1034      1002       997      1004      1023      1024      1038

1034      1034      1033      1023       980       945       933       937

930       945       944       986      1038      1154      1246      1369

1472      1601      1720      1908      2068      2201      2265      2221

2117      1969      1785      1638      1499      1394      1325      1313

1286      1305      1320      1333      1384      1480      1598      1740

1944      2166      2415      2688      2899      3047      3093      3042

2847      2598      2313      2067      1832      1685      1627      1589

1608      1648      1669      1728      1831      1909      1940      1936

1910      1879      1832      1760      1678      1540      1432      1375

1310      1251      1210      1174      1136      1156      1156      1171

1191      1248      1253      1247      1208      1147      1132      1147

1181      1238      1306      1349      1449      1530      1562      1569

1567      1537      1523      1499      1412      1322      1240      1138

1055      1026       971       909       863       799       773       793

800       784       774       776       775       792       792       814

818       824       828       815       773       765       765       739

731       717       691       670       691       704       705       751

796       813       839       876       879       896       948       968

972       998      1008       987       992       983       977       977

998      1019      1036      1115      1219      1296      1407      1522

1631      1753      1882      1968      2053      2074      2054      1988

1879      1764      1642      1523      1402      1328      1251      1217

1182      1196      1196      1215      1228      1283      1316      1379

1433      1459      1433      1449      1424      1359      1293      1212

1112      1082      1075      1054      1045      1040      1025      1010

1006      1006       993      1016      1039      1021      1034      1079

1142      1229      1332      1408      1492      1604      1697      1751

1788      1769      1689      1636      1558      1485      1431      1399

1371      1418      1430      1494      1559      1637      1767      1941

2063      2220      2304      2327      2327      2269      2131      2017

1889      1791      1692      1625      1552      1499      1481      1509

1524      1558      1603      1650      1776      1970      2112      2210

2272      2300      2328      2380      2382      2363      2367      2446

2536      2623      2599      2467      2289      2120      1944      1816

1662      1570      1502      1524      1562      1610      1637      1632

1583      1586      1595      1566      1527      1430      1335      1253

1245      1255      1245      1206      1164      1101      1075      1051

1029       986       947       951       961       943       961       945

942       975       990      1003      1027      1047      1081      1103

1087      1080      1040      1035      1054      1073      1058      1060

1040      1073      1113      1160      1207      1262      1333      1418

1509      1628      1789      1975      2141      2287      2435      2540

2585      2563      2417      2233      2088      1959      1836      1703

1596      1486      1428      1396      1425      1408      1408      1363

1312      1256      1291      1277      1281      1233      1184      1129

1128      1118      1157      1130      1123      1100      1122      1176

1254      1301      1341      1388      1492      1628      1804      1996

2118      2287      2442      2562      2623      2592      2463      2274

2055      1846      1677      1554      1507      1431      1428      1405

1402      1360      1317      1234      1175      1080      1022       944

946       951       958       936       943       918       937       955

997       994       999       952       933       927       938       953

958       934       955       964       994       997       996       975

975       966      1000       973       970       968       981      1009

1053      1080      1113      1144      1223      1343      1463      1580

1701      1808      1950      2077      2139      2186      2196      2177

2114      1988      1828      1684      1588      1501      1429      1367

1283      1202      1190      1162      1153      1133      1098      1080

1102      1160      1234      1244      1204      1138      1080      1026

1015       973       909       860       831       834       874       877

894       868       840       853       899       906       892       843

799       792       847       891       917       938       931       954

987      1001       989       970       922       897       923       965

983      1017      1025      1034      1100      1139      1169      1186

1157      1145      1151      1131      1150      1165      1185      1223

1220      1230      1253      1277      1342      1410      1441      1513

1560      1680      1804      1963      2127      2237      2300      2373

2349      2310      2222      2073      1922      1739      1613      1511

1426      1381      1305      1234      1261      1285      1319      1383

1405      1488      1606      1695      1781      1860      1850      1825

1784      1730      1676      1607      1498      1387      1260      1193

1136      1084      1034       985       937       925       915       890

886       838       811       784       770       766       797       796

774       773       781       807       830       856       866       904

959       990      1051      1096      1173      1219      1278      1312

1360      1390      1399      1364      1332      1325      1304      1310

1278      1232      1173      1114      1059      1038      1016       973

955       932       922       924       919       931       968       956

954       935       918       924       951       916       925       917

931       947       937       912       918       917       959      1034

1048      1080      1122      1126      1173      1233      1261      1294

1306      1276      1276      1246      1220      1220      1230      1227

1265      1242      1213      1207      1168      1129      1110      1056

1019      1016       981       993      1012      1017      1045      1064

1065      1103      1160      1195      1253      1257      1225      1217

1179      1160      1141      1118      1066      1042       976       983

995      1026      1042      1066      1065      1099      1126      1147

1174      1207      1202      1172      1142      1099      1097      1097

1063      1032      1034      1013      1041      1081      1133      1194

1278      1364      1469      1581      1671      1722      1748      1742

1665      1585      1500      1407      1301      1190      1092      1043

1000       964       948       953       963       974       984       977

976       947       889       885       913       914       912       889

838       805       792       783       802       816       793       798

810       825       866       903       923       984      1020      1057

1093      1116      1113      1138      1122      1121      1104      1070

1069      1108      1093      1087      1125      1182      1259      1341

1419      1459      1543      1605      1637      1667      1694      1686

1696      1691      1660      1612      1555      1491      1440      1428

1391      1363      1402      1390      1429      1490      1527      1586

1622      1628      1617      1569      1485      1416      1310      1248

1159      1093      1048      1007       984       971       976       999

1024      1027      1048      1064      1097      1138      1128      1112

1113      1082      1075      1067      1032       990       970       903

867       884       896       872       884       860       863       935

955       973      1013      1039      1053      1078      1101      1126

1155      1196      1189      1195      1241      1266      1315      1341

1317      1283      1248      1229      1237      1242      1238      1241

1265      1276      1295      1283      1248      1211      1211      1206

1209      1192      1169      1134      1114      1093      1078      1065

1072      1063      1063      1083      1115      1122      1155      1188

1231      1300      1376      1406      1456      1503      1512      1474

1453      1396      1336      1310      1293      1243      1249      1237

1238      1269      1333      1414      1525      1616      1717      1763

1789      1827      1817      1779      1723      1595      1435      1306

1162      1061      1034      1025      1001       999       966       913

909       935       951       966       987       965       944       933

937       949       985       982       935       896       870       851

858       858       850       851       850       807       799       827

866       894       926       915       924       944       963       998

1070      1115      1166      1184      1175      1191      1241      1306

1382      1449      1466      1518      1589      1685      1776      1864

1909      1944      1945      1914      1848      1769      1684      1598

1525      1466      1398      1363      1318      1280      1259      1224

1194      1210      1196      1221      1229      1237      1235      1231

1202      1197      1168      1157      1129      1092      1035      1024

988       962       943       903       864       862       832       818

794       791       788       794       800       797       770       777

782       801       803       812       806       788       780       787

795       823       828       820       797       814       838       854

864       898       908       933       948       944       957       980

991      1008      1012      1028      1057      1088      1142      1216

1310      1416      1473      1499      1506      1539      1557      1552

1565      1535      1487      1441      1360      1284      1258      1231

1207      1179      1178      1158      1129      1129      1115      1144

1201      1229      1214      1211      1215      1248      1288      1305

1335      1337      1380      1419      1460      1500      1590      1623

1638      1601      1583      1527      1491      1505      1499      1476

1505      1502      1520      1576      1622      1686      1750      1817

1874      1881      1899      1913      1878      1861      1824      1743

1661      1582      1476      1408      1355      1294      1228      1189

1119      1047       996       947       944       934       948       943

943       928       925       886       897       906       898       940

947       967       979       980       943       949       920       934

940       972      1014       997       962       906       856       858

885       888       949       976       999      1012       974       998

1058      1101      1137      1126      1113      1115      1089      1051

998       943       978       950       915       854       805       766

749       712       729       730       768       772       726       703

705       706       708       712       723       733       724       716

684       688       700       711       731       747       765       798

785       780       818       856       905       940       934       944

972       973       952       920       909       906       898       892

885       903       938       939       939       987      1031      1122

1153      1115      1083      1062      1041      1049      1023       980

967       921       898       854       836       841       864       845

847       848       872       910       932       953       950       966

966       963       928       904       866       856       826       812

793       738       704       676       640       662       692       713

723       705       675       681       680       684       701       697

727       731       721       693       692       704       768       814

850       872       906       948       993      1015      1024      1014

1018      1028      1023      1000      1002       978       958       947

919       881       882       892       927       949       949       964

1001      1026      1042      1032       999       987      1007       969

926       896       854       836       821       784       774       791

784       802       766       745       745       767       781       808

820       838       836       825       805       769       732       723

701       703       709       695       677       656       622       602

609       624       655       663       646       613       620       627

658       667       641       619       625       641       670       678

670       666       690       700       709       717       707       720

760       781       797       808       778       780       795       821

855       888       887       913       940       939       922       911

878       895       902       908       881       869       859       876

858       855       857       871       860       866       835       810

806       819       800       811       794       829       863       880

877       877       859       893       931       938       935       929

896       864       841       817       825       824       797       780

754       742       744       733       733       735       717       702

677       642       644       642       662       670       686       684

678       663       651       656       665       680       720       738

733       745       721       704       725       753       808       862

909       936       947       946       967       956       955       961

963       942       924       876       862       856       839       821

809       806       811       817       792       774       782       796

825       847       835       825       834       837       863       870

852       863       900       927       939       946       934       930

940       920       915       889       873       840       808       767

736       713       701       715       731       733       705       691

672       700       691       716       724       735       746       768

757       759       750       740       750       767       785       774

764       734       705       679       670       681       717       763

780       791       763       744       735       757       778       815

833       861       835       815       783       753       763       801

825       824       832       823       816       823       809       772

781       821       832       864       825       789       745       745

724       729       714       711       707       708       698       655

658       640       662       660       663       632       646       632

639       624       599       587       578       607       613       617

590       589       583       600       602       607       603       605

625       624       637       619       627       618       634       639

639       633       658       664       669       677       675       665

661       650       646       656       682       671       690       691

703       738       770       762       781       785       778       802

813       814       833       842       828       831       825       809

819       838       842       849       856       846       876       918

906       886       865       827       832       867       870       882

873       852       839       839       811       769       743       741

727       744       754       740       740       724       699       693

688       662       649       656       677       678       681       668

654       675       671       653       644       639       625       635

633       632       644       639       642       644       641       636

645       621       646       655       678       675       676       667

665       650       684       688       716       746       754       753

766       762       771       792       834       859       901       940

929       898       892       885       904       927       936       936

954       980       960       935       921       881       859       853

846       874       874       850       831       799       808       814

804       808       828       848       857       829       799       756

728       737       724       726       718       716       691       678

648       645       636       670       685       696       688       687

664       676       682       693       683       723       733       759

779       774       742       756       752       755       768       787

790       817       844       876       887       921       931       941

979      1015      1035      1073      1091      1109      1161      1185

1228      1294      1316      1361      1394      1394      1403      1396

1337      1338      1360      1410      1449      1418      1376      1334

1290      1281      1235      1164      1115      1062      1017      1041

1012      1011       964       930       911       939       946       992

975       968       963       951       958       988       969       965

927       912       917       927       914       900       862       861

871       879       858       838       846       832       851       868

855       865       886       895       931       944       942       934

928       931       932       941       942       938       933       915

897       914       935       944       945       934       933       924

890       877       852       836       859       867       856       879

886       885       881       861       835       847       881       906

938       941       943       946       929       933       926       904

903       895       882       896       886       861       849       840

822       828       839       831       857       867       868       885

900       899       923       914       897       891       882       873

851       817       793       794       783       765       741       725

714       721       709       706       701       669       661       648

644       668       663       632       640       640       649       665

669       655       652       634       623       647       675       706

722       710       680       678       676       690       703       710

704       727       754       788       836       859       870       869

889       900       946       963       973       969       985       982

974       940       928       921       920       929       937       948

973       967       943       914       893       884       876       872

883       890       886       878       829       839       820       814

801       815       771       818       812       806       824       831

800       819       810       783       802       798       810       818

826       794       770       749       736       726       753       775

798       819       848       829       838       847       855       872

893       888       920       948       953       964       943       912

894       911       924       951       944       926       903       898

892       885       845       826       814       808       801       832

829       829       771       734       692       699       726       768

754       755       748       748       768       781       788       782

784       789       802       812       813       833       837       855

870       886       875       899       908       942       957       979

977       972       970       952       939       936       918       906

912       917       938       947       923       924       915       931

938       952       954       946       934       943       943       957

960       939       951       948       923       914       877       873

870       853       806       801       783       803       792       784

758       752       741       755       763       786       807       814

796       802       824       866       893       902       883       900

922       972       987       992       977       981       958       946

937       929       934       933       921       908       908       910

909       916       883       887       856       835       813       818

784       762       748       749       768       788       792       758

751       754       739       730       718       714       732       748

727       732       743       737       729       723       682       669

684       688       710       740       742       735       721       687

686       686       708       732       767       775       776       777

796       807       831       814       804       804       836       878

930       972      1007      1004       996       988      1003      1035

1040      1047      1045      1058      1093      1104      1112      1141

1139      1128      1103      1055      1045      1054      1081      1082

1062      1030       990       968       964       932       901       889

873       880       867       859       860       856       845       821

775       771       773       778       772       771       781       789

783       777       768       752       768       761       755       769

789       785       790       788       797       821       841       846

862       884       907       933       941       931       944       956

957       953       948       945       967       995       971       943

931       931       924       925       891       894       916       932

926       917       894       890       902       912       913       915

967      1005      1055      1069      1059      1019      1041      1035

1040       992       973       939       964       978       996       960

923       924       908       894       876       865       852       895

883       877       866       901       919       948       927       887

848       866       892       931       960       961       946       955

940       924       929       907       881       852       810       784

796       808       822       822       796       765       755       747

758       766       745       747       727       735       749       763

761       779       760       768       759       743       731       744

747       744       748       737       735       750       765       778

797       791       776       757       747       740       736       750

765       784       804       820       856       889       900       905

886       870       866       870       869       902       887       876

856       859       851       878       864       868       867       853

850       867       877       886       873       845       831       833

791       775       769       763       766       781       738       744

756       752       760       745       725       719       727       735

746       738       720       736       730       715       718       708

702       733       748       741       737       705       701       709

744       743       744       737       734       770       787       792

830       827       832       858       838       822       844       831

857       862       865       862       876       872       875       857

851       845       816       783       786       786       795       828

815       796       808       782       777       782       770       748

744       714       706       702       723       744       773       777

771       765       765       762       754       750       755       742

753       774       785       780       770       749       773       788

789       788       785       787       797       784       776       787

787       812       838       874       906       915       921       957

994      1027      1022      1020      1024      1004      1012      1001

985       984       995       977      1004      1002      1006       993

993       965       942       915       917       947       972       967

950       955       931       944       965       970       971       984

933       932       936       935       942       945       936       927

904       875       855       840       844       823       839       827

808       794       790       771       807       808       788       783

780       770       785       789       747       729       714       700

723       752       746       725       733       726       754       761

757       734       748       764       769       762       734       728

738       774       788       817       793       793       784       804

828       836       798       802       794       819       832       815

799       819       813       835       834       838       854       862

857       874       853       831       814       817       816       829

822       819       823       848       864       884       890       892

897       879       886       890       882       903       929       962

993       999       984       984       976       984       988       987

989       980       975       954       956       951       956       947

967       966       970       947       908       863       850       825

820       838       858       855       882       864       855       844

823       779       788       790       797       793       772       751

764       788       798       810       811       803       781       765

758       757       780       796       804       810       815       812

827       835       861       859       854       843       859       831

822       817       818       836       881       883       874       867

840       833       853       868       876       861       856       879

920       940       945       923       912       944       958       985

999      1014      1011      1003       968       963       981      1007

1021      1030      1025      1023      1028       995       971       964

960       954       929       884       874       858       885       896

925       953       953       909       860       819       824       842

841       835       811       832       859       879       895       891

890       922       940       934       913       889       845       853

869       888       883       906       874       880       891       901

889       884       865       862       858       871       874       854

847       854       858       879       903       912       915       930

949       949       959       959       955       986      1006       999

999       966       957       954       939       933       956       926

894       866       815       823       854       849       819       822

800       819       818       811       792       793       789       807

812       815       812       791       759       771       773       770

779       776       793       805       805       806       798       785

794       764       758       771       784       789       792       768

769       766       801       838       863       893       888       861

834       837       847       866       877       874       877       883

906       920       923       885       880       868       865       886

893       888       894       882       869       878       890       913

944       935       922       897       872       866       889       885

874       882       898       896       890       889       872       877

881       867       871       867       835       796       772       767

788       817       832       826       821       804       783       805

807       798       788       782       785       806       791       780

769       756       786       814       840       858       860       844

817       792       799       802       804       840       840       847

865       855       834       818       802       798       794       790

824       833       838       820       795       792       796       816

841       854       868       901       863       834       832       847

867       911       895       892       914       923       920       912

901       897       928       945       948       941       946       912

903       890       886       885       927       929       949       951

942       936       955       938       939       925       905       901

924       923       911       889       891       893       904       890

853       849       890       895       890       873       843       829

846       842       842       855       871       858       860       880

870       847       831       815       808       829       818       825

821       813       786       771       763       805       834       865

857       839       815       806       795       814       820       801

781       800       792       795       817       816       824       837

815       802       840       868       872       850       823       809

832       854       860       851       862       874       879       906

940       940       960       960       947       939       959       947

954       978      1028      1025      1049      1072      1088      1100

1119      1072      1059      1090      1097      1096      1084      1052

1035      1017      1006      1013      1031      1046      1062      1048

1028      1004       992       967       965       949       911       916

906       890       885       854       821       852       856       855

873       854       844       845       834       806       817       811

822       832       853       852       865       868       875       911

906       919       930       934       929       951       915       920

922       929       913       897       897       887       891       902

901       901       910       910       911       913       921       952

939       951       936       902       905       919       928       970

970       955       950       926       930       916       898       902

882       876       882       876       884       876       845       831

831       856       891       897       902       884       880       875

862       843       849       830       858       866       868       884

877       868       886       887       900       909       892       890

894       888       894       881       882       882       893       914

931       938       951       935       921       914       902       884

886       881       875       881       873       844       837       828

825       824       823       826       839       843       841       818

813       799       807       803       789       776       800       802

842       873       868       858       860       830       833       845

853       865       865       869       876       848       851       864

849       864       854       826       822       844       857       864

858       842       815       783       802       801       839       851

850       835       829       802       798       800       788       814

815       823       818       825       788       783       790       807

810       832       814       812       810       814       831       862

862       837       818       808       830       860       869       839

837       833       815       817       809       801       794       824

830       819       809       813       792       806       814       804

823       850       848       835       828       821       815       824

814       812       833       830       830       871       867       870

859       859       846       856       867       868       882       897

917       905       921       899       906       895       928       933

927       932       940       939       963       993      1010      1013

989       946       928       935       947       943       955       931

910       924       912       916       913       901       890       914

926       921       905       923       904       910       926       917

921       926       875       868       868       888       927       945

944       930       888       871       852       841       878       895

894       901       877       854       864       869       866       864

872       857       861       872       872       869       911       924

917       904       890       860       856       847       841       836

865       881       878       867       877       870       889       898

900       904       930       936       926       921       907       891

902       892       876       889       891       895       895       889

885       892       889       906       923       932       927       929

884       862       875       895       914       933       899       864

863       866       888       913       901       891       869       858

868       874       860       859       854       857       883       903

892       863       849       835       841       861       856       843

849       857       852       853       853       838       848       842

836       832       834       853       877       868       862       828

814       835       850       847       839       826       841       838

835       828       790       773       765       779       807       832

834       805       779       779       781       776       781       785

800       792       785       783       783       808       820       819

826       818       818       812       797       819       847       844

873       881       874       883       885       869       872       896

875       877       876       867       850       876       881       886

883       873       853       815       836       836       842       863

877       884       908       913       890       894       872       875

890       914       913       929       926       910       929       917

910       916       929       932       968       970       994      1021

1025      1037      1041      1045      1057      1062      1054      1031

1005      1016      1036      1020      1030      1014       998      1005

1001       987      1011      1020      1007      1014      1013      1003

989       964       936       924       926       913       927       926

924       913       872       854       896       929       942       950

909       887       902       890       887       895       894       915

920       890       892       867       850       860       859       850

868       875       888       900       898       859       830       823

835       869       893       876       856       853       839       860

874       870       871       864       852       851       860       868

897       912       927       909       915       896       900       911

924       932       937       916       919       924       929       947

935       905       904       907       918       945       964       954

946       927       925       923       956       997      1027      1029

1012       980       966       980       980       988       989       983

948       951       949       957       965       964       951       975

997      1015      1023      1011      1017      1005       975       974

1002      1017      1059      1047      1022      1008      1000      1004

1031      1048      1052      1056      1048      1044      1051      1060

1056      1071      1081      1084      1107      1106      1102      1086

1076      1072      1084      1106      1122      1098      1090      1060

1037      1051      1088      1083      1088      1075      1070      1053

1070      1039      1008      1006      1017      1005      1030      1029

1019      1016      1000       981       992      1007      1007      1020

1032      1057      1095      1126      1105      1088      1073      1041

1027      1033      1053      1051      1057      1042      1036      1039

1030      1001       981       997      1034      1061      1048      1070

1044      1039      1024      1021      1040      1070      1027      1019

1009      1035      1053      1060       988       947       935       961

985      1009       987       981       990      1018      1030      1004

981       983       982      1011      1013       983       952       939

947       963       990       994       993       973       958       937

962       976       998       969       962       948       972       994

1000       953       940       918       928       935       943       912

881       884       887       895       894       886       883       903

913       918       881       877       877       871       875       902

918       933       907       849       827       851       886       910

907       890       873       880       888       880       882       886

882       890       911       937       962       995       993       972

959       958       963       994       999      1020      1004       981

964       987       991      1006       993       992       986      1005

983       964       983      1006      1031      1057      1057      1058

1071      1052      1047      1033      1018      1031      1059      1055

1080      1044      1008      1029      1033      1036      1072      1039

1020      1027      1004      1025      1035      1016      1027      1011

1011      1035      1034      1017      1033      1024      1017      1028

1019       994      1003      1010       989      1015      1023      1022

1032      1051      1027      1053      1055      1037      1048      1047

1027      1034      1020       999      1001       987       979       987

987       969       955       944       939       950       964       956

960       961       960       959       954       967       977       980

964       947       919       916       911       911       909       924

923       913       920       923       925       944       942       944

968       960       943       957       958       979      1012      1019

1009       998       989       988       981       980       975       966

970       989       982       971       959       952       938       943

949       979      1003      1002       965       921

;

#DFT optimization CIF  :

data_cs2alf5DFT

_symmetry_cell_setting                Orthorhombic

_symmetry_space_group_name_H-M       'P m n 21'

_symmetry_space_group_name_Hall      'P 2ac -2'

loop_

_symmetry_equiv_pos_as_xyz   #<--must include 'x,y,z'

'x,y,z'

'-x,y,z'

'x+1/2,-y,z+1/2'

'-x+1/2,-y,z+1/2'

_cell_length_a         6.3622

_cell_length_b        12.7523

_cell_length_c        11.4102

_cell_angle_alpha        90.0000

_cell_angle_beta         90.0000

_cell_angle_gamma        90.0000

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

cs1   cs         .000000        .991113        .006632

cs2   cs         .000000        .335981        .968232

cs3   cs         .000000        .647034        .049287

cs4   cs         .000000        .441018        .322978

cs5   cs         .000000        .766218        .674025

cs6   cs         .000000        .181968        .673709

al1   al         .500000        .090853        .842366

al2   al         .000001        .472746        .680252

al3   al         .499998       -.121437        .834820

f1       f         .292259        .154571        .911610

f2       f         .314664       -.013864        .778480

f3       f         .499999        .158347        .709385

f4       f         .500000       -.018350        .958061

f5       f         .202289        .552719        .611529

f6       f        -.201943        .392100        .748968

f7       f         .000000        .560161        .807367

f8       f         .000005        .382140        .558295

f9       f         .290501       -.188001        .899606

f10      f         .499997       -.186538        .699901

#===============================================================================

# 10. MOLECULAR GEOMETRY

_geom_special_details

;

Bond distances, angles etc. have been calculated using the

rounded fractional coordinates. All su's are estimated

from the variances of the (full) variance-covariance matrix.

The cell esds are taken into account in the estimation of

distances, angles and torsion angles

;

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_1

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

Al1     F1           1.7411                     .       .                   yes

Al1     F2           1.9248                     .       .                   yes

Al1     F3           1.7445                     .       .                   yes

Al1     F4           1.9188                     .       .                   yes

Al1     F1           1.7411                     .     3_655                 yes

Al1     F2           1.9248                     .     3_655                 yes

Al3     F2           1.9198                     .       .                   yes

Al3     F4           1.9250                     .       .                   yes

Al3     F9           1.7446                     .       .                   yes

Al3     F10          1.7490                     .       .                   yes

Al3     F2           1.9198                     .     3_655                 yes

Al3     F9           1.7446                     .     3_655                 yes

Al2     F5           1.8197                     .       .                   yes

Al2     F6           1.8229                     .       .                   yes

Al2     F7           1.8293                     .       .                   yes

Al2     F8           1.8087                     .       .                   yes

Al2     F5           1.8197                     .     3_555                 yes

Al2     F6           1.8229                     .     3_555                 yes

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_2

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

F1      Al1     F2            91.75             .       .       .           yes

F1      Al1     F3            99.47             .       .       .           yes

F1      Al1     F4            91.52             .       .       .           yes

F1      Al1     F1            98.77             .       .     3_655         yes

F1      Al1     F2           163.88             .       .     3_655         yes

F2      Al1     F3            90.74             .       .       .           yes

F2      Al1     F4            75.94             .       .       .           yes

F1      Al1     F2           163.88           3_655     .       .           yes

F2      Al1     F2            75.55             .       .     3_655         yes

F3      Al1     F4           163.03             .       .       .           yes

F1      Al1     F3            99.47           3_655     .       .           yes

F2      Al1     F3            90.74           3_655     .       .           yes

F1      Al1     F4            91.52           3_655     .       .           yes

F2      Al1     F4            75.94           3_655     .       .           yes

F1      Al1     F2            91.75           3_655     .     3_655         yes

F2      Al3     F4            75.91             .       .       .           yes

F2      Al3     F9            91.16             .       .       .           yes

F2      Al3     F10           92.55             .       .       .           yes

F2      Al3     F2            75.79             .       .     3_655         yes

F2      Al3     F9           163.50             .       .     3_655         yes

F4      Al3     F9            91.30             .       .       .           yes

F4      Al3     F10          165.27             .       .       .           yes

F2      Al3     F4            75.91           3_655     .       .           yes

F4      Al3     F9            91.30             .       .     3_655         yes

F9      Al3     F10           98.16             .       .       .           yes

F2      Al3     F9           163.50           3_655     .       .           yes

F9      Al3     F9            99.64             .       .     3_655         yes

F2      Al3     F10           92.55           3_655     .       .           yes

F9      Al3     F10           98.16           3_655     .       .           yes

F2      Al3     F9            91.16           3_655     .     3_655         yes

F6      Al2     F8            88.31           3_555     .       .           yes

F5      Al2     F6           179.74           3_555     .     3_555         yes

F5      Al2     F6           179.74             .       .       .           yes

F5      Al2     F7            90.01             .       .       .           yes

F5      Al2     F8            91.52             .       .       .           yes

F5      Al2     F5            90.02             .       .     3_555         yes

F5      Al2     F6            90.17             .       .     3_555         yes

F6      Al2     F7            90.16             .       .       .           yes

F6      Al2     F8            88.31             .       .       .           yes

F5      Al2     F6            90.17           3_555     .       .           yes

F6      Al2     F6            89.63             .       .     3_555         yes

F7      Al2     F8           177.84             .       .       .           yes

F5      Al2     F7            90.01           3_555     .       .           yes

F6      Al2     F7            90.16           3_555     .       .           yes

F5      Al2     F8            91.52           3_555     .       .           yes

Al1     F2      Al3           89.58             .       .       .           yes

Al1     F4      Al3           89.60             .       .       .           yes

loop_

_geom_torsion_atom_site_label_1

_geom_torsion_atom_site_label_2

_geom_torsion_atom_site_label_3

_geom_torsion_atom_site_label_4

_geom_torsion

_geom_torsion_site_symmetry_1

_geom_torsion_site_symmetry_2

_geom_torsion_site_symmetry_3

_geom_torsion_site_symmetry_4

_geom_torsion_publ_flag

F1      Al1     F2      Al3         -130.42     .       .       .       .   no

F3      Al1     F2      Al3          130.09     .       .       .       .   no

F4      Al1     F2      Al3          -39.29     .       .       .       .   no

F2      Al1     F2      Al3           39.52   3_655     .       .       .   no

F1      Al1     F4      Al3          130.59     .       .       .       .   no

F2      Al1     F4      Al3           39.16     .       .       .       .   no

F2      Al1     F2      Al3          -39.52     .       .     3_655     .   no

F4      Al3     F2      Al1           39.15     .       .       .       .   no

F9      Al3     F2      Al1          130.20     .       .       .       .   no

F10     Al3     F2      Al1         -131.58     .       .       .       .   no

F2      Al3     F2      Al1          -39.59   3_655     .       .       .   no

F2      Al3     F4      Al1          -39.29     .       .       .       .   no

F9      Al3     F4      Al1         -130.16     .       .       .       .   no

F2      Al3     F2      Al1           39.59     .       .     3_655     .   no

S6 - CIF file for Cs3Al2F9  from Rietveld refinement (including the Fullprof .pcr and .dat files) and DFT

data_Cs3Al2F9

_audit_update_record

;

2014-05-19 # Formatted by publCIF

;

_publ_requested_journal            'Powder Diffraction'

_journal_name_full                   'Powder Diffraction'

_journal_year                        ?

_journal_volume                      ?

_journal_issue                       ?

_journal_page_first                  ?

_journal_page_last                   ?

#=============================================================================

# 1. SUBMISSION DETAILS

_publ_contact_author_name        'Armel Le Bail'

_publ_contact_author_address

;

Universit\'e du Maine, Institut des Mol\'ecules et des Mat\'eriaux du Mans,

CNRS UMR 6283, 72085 Le Mans, France

;

_publ_contact_author_email           'armel.le_bail@univ-lemans.fr'

_publ_contact_author_fax             '33 (0)2 43 83 35 06'

_publ_contact_author_phone           '33 (0)2 43 83 33 47'

# Definition of non standard CIF items (Reliability indices used in FULLPROF)

loop_

_publ_manuscript_incl_extra_item

_publ_manuscript_incl_extra_info

_publ_manuscript_incl_extra_defn

#      Name                               Explanation                 Standard?

#     ------                              -----------                 ---------

'_pd_proc_ls_prof_cR_factor'    'Prof. R-factor CORRECTED for background'   no

'_pd_proc_ls_prof_cwR_factor'   'wProf.R-factor CORRECTED for background'   no

'_pd_proc_ls_prof_cwR_expected' 'wProf.Expected CORRECTED for background'   no

'_pd_proc_ls_prof_chi2'         'Chi-square for all considered points'      no

'_pd_proc_ls_prof_echi2'        'Chi-2 for points with Bragg contribution'  no

#=============================================================================

# 3. TITLE AND AUTHOR LIST

_publ_section_title

;

Face-sharing octahedra in Cs~2~AlF~5~ and Cs~3~Al~2~F~9~

;

_publ_section_title_footnote

.

# The loop structure below should contain the names and addresses of all

# authors, in the required order of publication. Repeat as necessary.

loop_

_publ_author_name

_publ_author_address

'Le Bail, Armel'

;

Universit\'e du Maine, Institut des Mol\'ecules et des Mat\'eriaux du Mans,

CNRS UMR 6283, 72085 Le Mans, France

;

'Smrcok, Lubomir'

;

Institute of Inorganic Chemistry, Slovak Academy of Sciences, Dubravska

cesta 9, 845 36 Bratislava, Slovak Republic

;

_publ_section_abstract

;

Face-sharing octahedra in Cs~2~AlF~5~ and Cs~3~Al~2~F~9~

;

#=============================================================================

#=============================================================================

# 5. CHEMICAL DATA

_chemical_name_systematic

?

_chemical_name_common             ?

_chemical_formula_moiety          'Al2 F9, 3(Cs)'

_chemical_formula_structural      ?

_chemical_formula_analytical      ?

_chemical_formula_iupac           ?

_chemical_formula_sum             'Al2 Cs3 F9'

_chemical_formula_weight          623.69

_chemical_melting_point           ?

_chemical_compound_source         ?       # for minerals and

# natural products

loop_

_atom_type_symbol

_atom_type_scat_Cromer_Mann_a1

_atom_type_scat_Cromer_Mann_b1

_atom_type_scat_Cromer_Mann_a2

_atom_type_scat_Cromer_Mann_b2

_atom_type_scat_Cromer_Mann_a3

_atom_type_scat_Cromer_Mann_b3

_atom_type_scat_Cromer_Mann_a4

_atom_type_scat_Cromer_Mann_b4

_atom_type_scat_Cromer_Mann_c

_atom_type_scat_dispersion_real

_atom_type_scat_dispersion_imag

_atom_type_scat_source

Cs  20.35240   3.55200  19.12780   0.30860  10.28210  23.71280

0.96150  59.45650   3.27910  -0.7460   7.90500

International_Tables_for_Crystallography_Vol.C(1991)_Tables_6.1.1.4_and_6.1.1.5

Al   4.17448   1.93816   3.38760   4.14553   1.20296   0.22875

0.52814   8.28524   0.70679   0.21300   0.24600

International_Tables_for_Crystallography_Vol.C(1991)_Tables_6.1.1.4_and_6.1.1.5

F    3.63220   5.27756   3.51057  14.73530   1.26064   0.44226

0.94071  47.34370   0.65340   0.07300   0.05300

International_Tables_for_Crystallography_Vol.C(1991)_Tables_6.1.1.4_and_6.1.1.5

#=============================================================================

# 6. POWDER SPECIMEN AND CRYSTAL DATA

_symmetry_cell_setting                hexagonal

_symmetry_space_group_name_H-M       'P 63/m m c'

_symmetry_space_group_name_Hall      '-P 6c 2c'

loop_

_symmetry_equiv_pos_as_xyz   #<--must include 'x,y,z'

'x,y,z'

'x-y,x,z+1/2'

'-y,x-y,z'

'-x,-y,z+1/2'

'-x+y,-x,z'

'y,-x+y,z+1/2'

'-y,-x,z'

'-x,-x+y,z+1/2'

'-x+y,y,z'

'y,x,z+1/2'

'x,x-y,z'

'x-y,-y,z+1/2'

'-x,-y,-z'

'-x+y,-x,-z+1/2'

'y,-x+y,-z'

'x,y,-z+1/2'

'x-y,x,-z'

'-y,x-y,-z+1/2'

'y,x,-z'

'x,x-y,-z+1/2'

'x-y,-y,-z'

'-y,-x,-z+1/2'

'-x,-x+y,-z'

'-x+y,y,-z+1/2'

_cell_length_a                        6.25350(19)

_cell_length_b                       6.25350(19)

_cell_length_c                       14.7193(6)

_cell_angle_alpha                    90.00000

_cell_angle_beta                     90.00000

_cell_angle_gamma                    120.00000

_cell_volume                         498.50(3)

_cell_formula_units_Z                2

_cell_measurement_temperature        295

_pd_char_colour                   white

_exptl_crystal_density_diffrn     4.155

_exptl_crystal_F_000               544.0

_diffrn_ambient_temperature          295

_diffrn_radiation_source         'X-ray tube'

_diffrn_radiation_type           'CuK\a'

_diffrn_radiation_wavelength     1.5418

_diffrn_radiation_monochromator      graphite

_diffrn_measurement_device_type      'Siemens D500'

_diffrn_measurement_method           'step scan'

# The following three fields describe the preparation of the specimen.

# The cooling rate is in K/min.  The pressure at which the sample was

# prepared is in kPa.  The temperature of preparation is in K.

_pd_prep_cool_rate                ?

_pd_prep_pressure                 ?

_pd_prep_temperature              ?

# The next four fields are normally only needed for transmission experiments.

_exptl_absorpt_coefficient_mu        87.832

_exptl_absorpt_correction_type       ?

_exptl_absorpt_process_details       ?

_exptl_absorpt_correction_T_min      ?

_exptl_absorpt_correction_T_max      ?

#=============================================================================

#  The following four items give details of the measured (not processed)

#  powder pattern.  Angles are in degrees.

_pd_meas_number_of_points         3001

_pd_meas_2theta_range_min         10.00000

_pd_meas_2theta_range_max         130.00000

_pd_meas_2theta_range_inc         0.040000

#=============================================================================

# 8. REFINEMENT DATA

_refine_special_details

?

# Use the next field to give any special details about the fitting of the

# powder pattern.

_pd_proc_ls_special_details

?

# The next three items are given as text.

_pd_proc_ls_profile_function      ?

_pd_proc_ls_background_function   ?

_pd_proc_ls_pref_orient_corr

?

#  The following profile R-factors are NOT CORRECTED for background

#  The sum is extended to all non-excluded points.

#  These are the current CIF standard

_pd_proc_ls_prof_R_factor                9.0741

_pd_proc_ls_prof_wR_factor              12.4418

_pd_proc_ls_prof_wR_expected             3.9430

#  The following profile R-factors are CORRECTED for background

#  The sum is extended to all non-excluded points.

#  These items are not in the current CIF standard, but are defined above

_pd_proc_ls_prof_cR_factor               16.3283

_pd_proc_ls_prof_cwR_factor              19.2966

_pd_proc_ls_prof_cwR_expected             6.1154

#  The following items are not in the CIF standard, but are defined above

_pd_proc_ls_prof_chi2                 9.9565

_pd_proc_ls_prof_echi2                9.9565

#  Items related to LS refinement

_refine_ls_R_I_factor                 5.9856

_refine_ls_number_reflns                   199

_refine_ls_number_parameters                61

_refine_ls_number_restraints                 0

_refine_ls_goodness_of_fit_all                         3.154

_refine_ls_shift/su_max                   0.03

# The following four items apply to angular dispersive measurements.

# 2theta minimum, maximum and increment (in degrees) are for the

# intensities used in the refinement.

_pd_proc_2theta_range_min                9.9674

_pd_proc_2theta_range_max              129.9674

_pd_proc_2theta_range_inc              0.040000

_pd_proc_wavelength                    1.540560

_pd_block_diffractogram_id        ?  # The id used for the block containing

# the powder pattern profile (section 11)

# Give appropriate details in the next two text fields.

_pd_proc_info_excluded_regions    ?

_pd_proc_info_data_reduction      ?

# The following items are used to identify the programs used.

_computing_data_collection           ?

_computing_structure_solution        ?

_computing_structure_refinement      FULLPROF

_computing_molecular_graphics        DIAMOND

_computing_publication_material      ?

#=============================================================================

# 9. ATOMIC COORDINATES AND DISPLACEMENT PARAMETERS

loop_

_atom_site_label

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_occupancy

_atom_site_adp_type              # Not in version 2.0.1

_atom_site_type_symbol

CS1  0.33333  0.66667  0.75000  0.031(5)  1.00000 Uani CS

CS2  0.33333  0.66667  0.4267(3)  0.025(3)  1.00000 Uani CS

AL1  0.00000  0.00000  0.1653(17)  0.021(3)  1.00000 Uiso AL

F1  0.140(2)  0.281(2)  0.25000  0.039(3)  1.00000 Uiso F

F2  0.265(2)  0.132(2)  0.0958(11)  0.039(3)  1.00000 Uiso F

loop_

_atom_site_aniso_label

_atom_site_aniso_U_11

_atom_site_aniso_U_22

_atom_site_aniso_U_33

_atom_site_aniso_U_12

_atom_site_aniso_U_13

_atom_site_aniso_U_23

_atom_site_aniso_type_symbol

Cs1  0.032(5)  0.032(5)  0.028(4)  0.016(5)  0.00000  0.00000  Cs

Cs2  0.018(3)  0.018(3)  0.039(3)  0.009(3)   0.00000  0.00000  Cs

#=============================================================================#

#                       MOLECULAR GEOMETRY                                    #

#=============================================================================#

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

CS1   AL1   3.820(8)      2_555 ?

CS1   AL1   3.820(8)      2_565 ?

CS1   AL1   3.820(8)      2_665 ?

CS1   AL1   3.820(8)     13_556 ?

CS1   AL1   3.820(8)     13_566 ?

CS1   AL1   3.820(8)     13_666 ?

CS1   F1    3.143(9)      2_555 ?

CS1   F1    3.136(9)      2_665 ?

CS1   F1    3.136(14)     4_565 ?

CS1   F1    3.143(14)     4_665 ?

CS1   F1    3.136(14)     6_555 ?

CS1   F1    3.143(14)     6_565 ?

CS1   F1    3.136(9)      8_555 ?

CS1   F1    3.143(9)      8_665 ?

CS1   F1    3.136(14)    10_565 ?

CS1   F2    3.144(14)     2_555 ?

CS1   F2    3.144(14)     4_665 ?

CS1   F2    3.144(16)     6_565 ?

CS1   F2    3.144(14)     8_665 ?

CS1   F2    3.144(16)    12_565 ?

CS1   F2    3.144(14)    13_666 ?

CS1   F2    3.144(16)    15_566 ?

CS1   F2    3.144(14)    17_556 ?

CS1   F2    3.144(16)    21_566 ?

CS1   F2    3.144(14)    23_666 ?

CS2   AL1   3.856(9)     14_555 ?

CS2   AL1   3.856(9)     14_565 ?

CS2   AL1   3.856(9)     14_665 ?

CS2   F1    3.336(8)      1_555 ?

CS2   F1    3.336(8)      3_665 ?

CS2   F1    3.336(10)     5_565 ?

CS2   F1    3.336(10)    11_565 ?

CS2   F2    3.306(15)     2_555 ?

CS2   F2    3.306(15)     4_665 ?

CS2   F2    3.306(16)     6_565 ?

CS2   F2    3.306(15)     8_665 ?

CS2   F2    3.306(16)    12_565 ?

CS2   F2    3.169(15)    14_565 ?

CS2   F2    3.163(13)    14_665 ?

CS2   F2    3.169(13)    16_555 ?

CS2   F2    3.163(15)    16_565 ?

CS2   F2    3.163(9)     18_555 ?

CS2   F2    3.169(9)     18_665 ?

CS2   F2    3.169(15)    20_565 ?

CS2   F2    3.169(13)    22_665 ?

CS2   F2    3.169(9)     24_555 ?

CS2   F2    3.163(9)     24_665 ?

AL1   CS1   3.820(8)      2_544 ?

AL1   CS1   3.820(8)      2_554 ?

AL1   CS1   3.820(8)      2_654 ?

AL1   CS2   3.856(9)     14_455 ?

AL1   CS2   3.856(9)     14_555 ?

AL1   CS2   3.856(9)     14_565 ?

AL1   AL1   2.49(4)      14_555 ?

AL1   F1    1.967(18)     1_555 ?

AL1   F1    1.967(18)     3_555 ?

AL1   F1    1.967(20)     5_555 ?

AL1   F1    1.967(20)    11_555 ?

AL1   F2    1.762(19)     1_555 ?

AL1   F2    1.76(2)       3_555 ?

AL1   F2    1.762(19)     5_555 ?

AL1   F2    1.76(2)       9_555 ?

AL1   F2    3.80(3)      14_555 ?

AL1   F2    3.80(3)      16_555 ?

AL1   F2    3.80(3)      18_555 ?

AL1   F2    3.80(3)      24_555 ?

F1    CS1   3.136(14)     2_554 ?

F1    CS1   3.143(14)     2_654 ?

F1    CS2   3.336(8)      1_555 ?

F1    CS2   3.336(8)     14_565 ?

F1    AL1   1.967(18)     1_555 ?

F1    AL1   1.967(18)    14_555 ?

F1    F1    2.636(13)     3_555 ?

F1    F1    3.618(13)     3_665 ?

F1    F1    2.636(20)     5_555 ?

F1    F1    3.618(20)     5_565 ?

F1    F1    2.639(20)    11_555 ?

F1    F1    3.615(20)    11_565 ?

F1    F2    2.713(18)     1_555 ?

F1    F2    2.707(16)     3_555 ?

F1    F2    3.728(16)     5_555 ?

F1    F2    2.710(16)     9_555 ?

F1    F2    3.728(16)    14_555 ?

F1    F2    2.713(18)    16_555 ?

F1    F2    2.707(16)    18_555 ?

F1    F2    2.710(16)    24_555 ?

F2    CS1   3.144(14)     2_654 ?

F2    CS2   3.306(15)     2_654 ?

F2    CS2   3.163(15)    14_555 ?

F2    CS2   3.169(13)    14_565 ?

F2    AL1   1.762(19)     1_555 ?

F2    AL1   3.80(3)      14_555 ?

F2    F1    2.713(18)     1_555 ?

F2    F1    3.728(16)     3_555 ?

F2    F1    2.707(16)     5_555 ?

F2    F1    2.710(16)    11_555 ?

F2    F2    2.486(20)     3_555 ?

F2    F2    3.768(20)     3_655 ?

F2    F2    2.486(13)     5_555 ?

F2    F2    3.768(13)     5_665 ?

F2    F2    3.771(13)     7_665 ?

F2    F2    2.489(20)     9_555 ?

F2    F2    3.765(20)     9_655 ?

F2    F2    3.16(2)      15_555 ?

F2    F2    3.16(2)      17_555 ?

F2    F2    3.16(2)      21_555 ?

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

F1   AL1  F1   84.1(9)        1_555    3_555 ?

F1   AL1  F1   84.1(11)       1_555    5_555 ?

F1   AL1  F1   84.2(11)       1_555   11_555 ?

F1   AL1  F2   93.2(12)       1_555    1_555 ?

F1   AL1  F2   92.9(11)       1_555    3_555 ?

F1   AL1  F2   176.2(13)      1_555    5_555 ?

F1   AL1  F2   93.0(11)       1_555    9_555 ?

F1   AL1  F1   84.1(11)       3_555    5_555 ?

F1   AL1  F1   84.0(11)       3_555   11_555 ?

F1   AL1  F2   176.2(13)      3_555    1_555 ?

F1   AL1  F2   93.2(11)       3_555    3_555 ?

F1   AL1  F2   92.9(11)       3_555    5_555 ?

F1   AL1  F2   93.0(11)       3_555    9_555 ?

F1   AL1  F2   92.9(11)       5_555    1_555 ?

F1   AL1  F2   176.2(15)      5_555    3_555 ?

F1   AL1  F2   93.2(11)       5_555    5_555 ?

F1   AL1  F2   176.2(15)      5_555    9_555 ?

F1   AL1  F2   93.0(11)      11_555    1_555 ?

F1   AL1  F2   176.2(15)     11_555    3_555 ?

F1   AL1  F2   93.0(11)      11_555    5_555 ?

F1   AL1  F2   176.2(15)     11_555    9_555 ?

F2   AL1  F2   89.7(13)       1_555    3_555 ?

F2   AL1  F2   89.7(11)       1_555    5_555 ?

F2   AL1  F2   89.8(13)       1_555    9_555 ?

F2   AL1  F2   89.7(13)       3_555    5_555 ?

F2   AL1  F2   89.5(13)       5_555    9_555 ?

_iucr_refine_instructions_details

;

Fullprof .pcr file, modified to fit inside 80 columns

followed by the .dat file

COMM Cs3Al2F9   P63/mmc

! Current global Chi2 (Bragg contrib.) =      9.957

! Files => DAT-file: c3alf9.dat,  PCR-file: cs3alf9

!Job Npr Nph Nba Nex Nsc Nor Dum Iwg Ilo Ias Res Ste Nre Cry Uni Cor Opt Aut

0   5   4  32   6   0   1   1   0   0   1   0   0   0   0   0   0   0   0

!

!Ipr Ppl Ioc Mat Pcr Ls1 Ls2 Ls3 NLI Prf Ins Rpa Sym Hkl Fou Sho Ana

0   0   1   0   2   0   4   0   0  -3   0  -1   1   0   2   1   1

!

! Lambda1  Lambda2    Ratio    Bkpos    Wdt    Cthm     muR   AsyLim   Rpolarz

2nd-muR -> Patt# 1

1.540560 1.544390  0.50000   50.000 15.0000  0.7990  0.0000   90.00    0.0000

0.0000

!

!NCY  Eps  R_at  R_an  R_pr  R_gl     Thmin       Step       Thmax    PSD

Sent0

40  0.01  0.40  0.40  0.40  0.60     10.0000   0.040000   130.0000   0.000

0.000

!

!2Theta/TOF/E(Kev)   Background  for Pattern#  1

10.0800      1237.3416        271.00

10.9375      1091.0760        281.00

12.3958       923.5492        291.00

14.1667       764.9097        301.00

15.8333       685.4295        311.00

18.4375       510.0298        321.00

20.9375       456.3604        331.00

23.1250       425.9053        341.00

26.7708       334.6360        351.00

31.4583       256.9339        361.00

36.3542       286.2851        371.00

41.1458       242.8928        381.00

43.6458       219.9503        391.00

45.5208       245.0227        401.00

48.8542       205.2159        411.00

51.4583       259.5942        421.00

53.2292       247.7850        431.00

55.7292       218.0686        441.00

57.3958       210.8313        451.00

62.8125       235.8992        461.00

69.2708       193.0987        471.00

76.6667       226.2447        481.00

86.1458       179.8128        491.00

91.6667       200.2521        501.00

98.5417       195.5887        511.00

104.0625       219.4581        521.00

110.6250       228.9737        531.00

115.7292       247.4248        541.00

120.0000       243.9465        551.00

123.0208       245.5163        561.00

126.6667       257.3810        571.00

129.4792       277.8023        581.00

!

! Excluded regions (LowT  HighT) for Pattern#  1

2.00       10.00

14.95       15.65

22.21       22.65

25.72       26.15

27.73       28.06

130.00      180.00

!

!

61    !Number of refined parameters

!

!  Zero    Code    SyCos    Code   SySin    Code  Lambda     Code MORE ->Patt#

1

0.03263   81.0  0.00000    0.0  0.00000    0.0 0.000000    0.00   0

!------------------------------------------------------------------------------

!  Data for PHASE number:   1  ==> Current R_Bragg for Pattern#  1:     5.99

!------------------------------------------------------------------------------

Cs3Al2F9

!

!Nat Dis Ang Pr1 Pr2 Pr3 Jbt Irf Isy Str Furth       ATZ    Nvk Npr More

5   0   0 1.0 0.0 0.0   0   0   0   0   0       7184.619   0   5   1

!

!Jvi Jdi Hel Sol Mom Ter  Brind   RMua    RMub    RMuc   Jtyp  Nsp_Ref Ph_Shift

N_Domains

0   3   0   0   0   0  1.0000  0.0000  0.0000  0.0000    0     0      0      0

!

! Max_dst(dist) (angles)  Bond-Valence Calc.

4.0000      3.5000        1

P 63/M M C               <--Space group symbol

!Atom   Typ       X        Y        Z     Biso       Occ     In Fin N_t Spc

/Codes

!    beta11   beta22   beta33   beta12   beta13   beta23  /Codes

CS1    CS+1    0.33333  0.66667  0.75000  0.00000   0.20000   0   0   2    0

0.00     0.00     0.00     0.00      0.00

0.02167  0.02167  0.00252  0.01084  0.00000   0.00000

141.00   141.00   601.00   140.50     0.00      0.00

CS2    CS+1    0.33333  0.66667  0.42668  0.00000   0.40000   0   0   2    0

0.00     0.00   151.00     0.00      0.00

0.01180  0.01180  0.00352  0.00590  0.00000   0.00000

221.00   221.00   611.00   220.50     0.00      0.00

AL1    AL+3    0.00000  0.00000  0.16532  1.63773   0.40000   0   0   0    0

0.00     0.00   161.00   201.00      0.00

F1     F-1     0.14033  0.28067  0.25000  3.06518   0.60000   0   0   0    0

170.50   171.00     0.00   211.00      0.00

F2     F-1     0.26485  0.13243  0.09578  3.06518   1.20000   0   0   0    0

181.00   180.50   191.00   211.00      0.00

!-------> Profile Parameters for Pattern #  1

!  Scale        Shape1      Bov      Str1      Str2      Str3   Strain-Model

0.67833E-04   0.69993   0.00000   0.00000   0.00000   0.00000       0

11.00000    41.000     0.000     0.000     0.000     0.000

!       U         V          W           X          Y        GauSiz   LorSiz

Size-Model

0.056933  -0.058197   0.033344  -0.000254   0.000000   0.000000   0.000000  0

251.000    131.000     51.000    261.000      0.000      0.000      0.000

!     a          b         c        alpha      beta       gamma      #Cell Info

6.253500   6.253500  14.719303  90.000000  90.000000 120.000000

91.00000   91.00000  101.00000    0.00000    0.00000   91.00000

!  Pref1    Pref2      Asy1     Asy2     Asy3     Asy4

1.00000  0.00000  0.07152  0.08016  0.00000  0.00000

0.00     0.00    61.00    71.00     0.00     0.00

!------------------------------------------------------------------------------

!  Data for PHASE number:   2  ==> Current R_Bragg for Pattern#  1:     8.61

!------------------------------------------------------------------------------

alpha-AlF3

!

!Nat Dis Ang Pr1 Pr2 Pr3 Jbt Irf Isy Str Furth       ATZ    Nvk Npr More

2   0   0 1.0 0.0 0.0   0   0   0   0   0       2902.236   0   5   1

!

!Jvi Jdi Hel Sol Mom Ter  Brind   RMua    RMub    RMuc   Jtyp  Nsp_Ref Ph_Shift

N_Domains

0   3   0   0   0   0  1.0000  0.0000  0.0000  0.0000    0      0   0      0

!

! Max_dst(dist) (angles)  Bond-Valence Calc.

4.0000      3.5000        1

R -3 C                   <--Space group symbol

!Atom   Typ       X        Y        Z     Biso       Occ     In Fin N_t Spc

/Codes

AL1    AL+3    0.00000  0.00000  0.00000  0.19660   0.40000   0   0   0    0

0.00     0.00     0.00   230.50      0.00

F1     F-1     0.42644  0.00000  0.25000  0.39322   1.20000   0   0   0    0

241.00     0.00     0.00   231.00      0.00

!-------> Profile Parameters for Pattern #  1

!  Scale        Shape1      Bov      Str1      Str2      Str3   Strain-Model

0.12946E-03   0.69993   0.00000   0.00000   0.00000   0.00000       0

21.00000    41.000     0.000     0.000     0.000     0.000

!       U         V          W           X          Y        GauSiz   LorSiz

Size-Model

0.056933  -0.058197   0.033344  -0.000254   0.000000   0.000000   0.000000  0

251.000    131.000     51.000    261.000      0.000      0.000      0.000

!     a          b         c        alpha      beta       gamma      #Cell Info

4.926463   4.926463  12.441175  90.000000  90.000000 120.000000

111.00000  111.00000  121.00000    0.00000    0.00000  111.00000

!  Pref1    Pref2      Asy1     Asy2     Asy3     Asy4

1.00000  0.00000  0.07152  0.08016  0.00000  0.00000

0.00     0.00    61.00    71.00     0.00     0.00

!-------------------------------------------------------------------------------

!  Data for PHASE number:   3  ==> Current R_Bragg for Pattern#  1:    18.14

!-------------------------------------------------------------------------------

gamma-CsAlF4

!

!Nat Dis Ang Pr1 Pr2 Pr3 Jbt Irf Isy Str Furth       ATZ    Nvk Npr More

14   0   0 1.0 0.0 0.0   0   0   0   0   0       1811.563   0   5   1

!

!Jvi Jdi Hel Sol Mom Ter  Brind   RMua    RMub    RMuc   Jtyp  Nsp_Ref Ph_Shift

N_Domains

0   3   0   0   0   0  1.0000  0.0000  0.0000  0.0000    0      0     0    0

!

! Max_dst(dist) (angles)  Bond-Valence Calc.

4.0000      3.5000        1

P N M A                  <--Space group symbol

!Atom   Typ       X        Y        Z     Biso       Occ     In Fin N_t Spc

/Codes

CS1    CS      0.19200  0.25000  0.81790  0.80000   0.40000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

CS2    CS      0.37760  0.25000  0.04130  0.80000   0.40000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

CS3    CS      0.06640  0.25000  0.22860  0.80000   0.40000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

AL1    AL      0.26260  0.75000  0.92080  0.80000   0.40000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

AL2    AL      0.00000  0.00000  0.00000  0.80000   0.40000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

AL3    AL      0.29370  0.25000  0.62990  0.80000   0.40000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

F1     F       0.20370  0.04800  0.65990  0.80000   0.80000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

F2     F       0.29000  0.25000  0.32570  0.80000   0.40000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

F3     F       0.22540  0.25000  0.53210  0.80000   0.40000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

F4     F       0.44320  0.75000  0.50810  0.80000   0.40000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

F5     F       0.36860  0.07000  0.44150  0.80000   0.80000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

F6     F       0.41550  0.43500  0.58100  0.80000   0.80000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

F7     F       0.39950  0.25000  0.71090  0.80000   0.40000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

F8     F       0.36840  0.57000  0.91440  0.80000   0.80000   0   0   0    0

0.00     0.00     0.00     0.00      0.00

!-------> Profile Parameters for Pattern #  1

!  Scale        Shape1      Bov      Str1      Str2      Str3   Strain-Model

0.23971E-04   0.69993   0.00000   0.00000   0.00000   0.00000       0

31.00000    41.000     0.000     0.000     0.000     0.000

!       U         V          W           X          Y        GauSiz   LorSiz

Size-Model

0.056933  -0.058197   0.033344  -0.000254   0.000000   0.000000   0.000000  0

251.000    131.000     51.000    261.000      0.000      0.000      0.000

!     a          b         c        alpha      beta       gamma      #Cell Info

10.557600   6.750000  17.595398  90.000000  90.000000  90.000000

0.00000    0.00000    0.00000    0.00000    0.00000    0.00000

!  Pref1    Pref2      Asy1     Asy2     Asy3     Asy4

1.00000  0.00000  0.07152  0.08016  0.00000  0.00000

0.00     0.00    61.00    71.00     0.00     0.00

!------------------------------------------------------------------------------

!  Data for PHASE number:   4  ==> Current R_Bragg for Pattern#  1:     5.60

!------------------------------------------------------------------------------

Cs3AlF6

!

!Nat Dis Ang Pr1 Pr2 Pr3 Jbt Irf Isy Str Furth       ATZ    Nvk Npr More

0   0   0 1.0 0.0 0.0   2   2   0   0   0          0.000   0   5   1

!

!Jvi Jdi Hel Sol Mom Ter  Brind   RMua    RMub    RMuc   Jtyp  Nsp_Ref Ph_Shift

N_Domains

0   3   0   0   0   0  1.0000  0.0000  0.0000  0.0000    0      0    0    0

!

! Max_dst(dist) (angles)  Bond-Valence Calc.

4.0000      3.5000        1

F M -3 M                 <--Space group symbol

!-------> Profile Parameters for Pattern #  1

!  Scale        Shape1      Bov      Str1      Str2      Str3   Strain-Model

0.10000E-04   0.69993   0.00000   0.00000   0.00000   0.00000       0

0.00000    41.000     0.000     0.000     0.000     0.000

!       U         V          W           X          Y        GauSiz   LorSiz

Size-Model

0.056933  -0.058197   0.033344  -0.000254   0.000000   0.000000   0.000000  0

251.000    131.000     51.000    261.000      0.000      0.000      0.000

!     a          b         c        alpha      beta       gamma      #Cell Info

9.223959   9.223959   9.223959  90.000000  90.000000  90.000000

591.00000  591.00000  591.00000    0.00000    0.00000    0.00000

!  Pref1    Pref2      Asy1     Asy2     Asy3     Asy4

1.00000  0.00000  0.07152  0.08016  0.00000  0.00000

0.00     0.00    61.00    71.00     0.00     0.00

!  2Th1/TOF1    2Th2/TOF2  Pattern # 1

10.000     130.000       1

The Fullprof .dat  file :

10.000   0.04   130.000

1264      1260      1304      1254      1191      1148      1249      1247

1177      1250      1130      1194      1137      1152      1189      1175

1146      1096      1172      1115      1065      1144      1119      1099

1105      1102      1155      1012      1077      1049      1102      1044

1038      1000      1034      1077      1006      1046      1060      1002

1105      1050       978       990       999       980       981      1030

969       978       966      1003       956       944       950       955

957       948       964       936       922       950       962       903

955       975       877       983       856       935       898       902

834       894       833       905       878       876       898       868

896       828       859       837       889       836       894       790

825       826       827       867       771       780       792       810

772       831       777       805       808       798       799       788

780       803       801       824       750       789       755       743

783       796       717       741       728       753       749       696

739       692       733       744       655       786       758       765

771       724       756       815       912       889       917       861

749       747       718       702       642       622       680       680

712       652       641       726       674       729       716       772

817       900       989      1088      1068      1117      1377      1727

2203      2191      1674      1133       762       717       677       768

735       763       731       719       700       710       708       680

722       703       715       730       766       852       990      1217

1119       983       799       810       760       695       670       623

585       561       566       543       564       504       528       534

547       513       510       567       574       534       535       607

571       600       627       569       600       616       755       816

818       695       628       565       525       449       571       497

503       528       507       493       498       552       529       553

626       591       554       537       526       493       475       509

500       483       504       520       520       529       521       525

557       526       550       531       566       620       607       703

691       767       804       962      1087      1106       800       643

502       496       464       468       483       457       471       442

470       445       430       477       503       440       482       457

474       529       469       510       546       504       524       550

598       602       587       607       693       844       986      1071

1043      1198      1418      1523      1638      1733      1191       701

570       534       531       603       617       730       743       951

1255      1545      1380      1115       887       851       811       668

592       429       432       411       402       433       405       444

408       415       486       465       502       571       604       596

589       730       892      1094      1423      1594      2689      3071

2649      1565       831       673       644       772       834      1006

1261      1544      2341      2975      3750      4382      5107      6306

9000     13488     20940     26628     24479     15497      7540      2834

1360       907       736       743       727       709       779       904

1068      1279      1460      1660      1932      2412      3193      4495

5385      4987      3130      1622       868       648       713       763

705       686       687       767       920      1005       932      1028

971      1171      1187      1033       862       902       917       985

1157      1342      1833      2144      1893      1369       967       686

667       671       670       671       612       567       424       416

467       508       525       553       678       694       860      1045

1284      1643      2210      2502      2474      1927      1323       780

571       532       474       497       549       590       655       653

747       834       825       826       762       846       945      1137

1552      1950      2371      2864      3316      4188      5708      8570

15473     16292     14512      8964      4232      1940       918       698

564       545       496       590       648       697       734       613

611       640       743       934      1229      1335      1225       906

764       687       773       696       704       576       558       618

884      1275      1037       895       582       435       329       349

313       313       387       375       437       542       565       637

621       479       354       356       272       313       276       317

317       310       308       311       375       352       352       387

417       373       362       339       333       290       290       348

328       318       319       347       339       412       497       703

1007      1023       918       666       348       277       286       298

265       271       319       332       390       406       390       380

345       373       405       408       483       447       399       437

410       448       546       584       678       774       925      1404

1968      3556      3909      3658      2547      1487       760       411

381       386       408       547       690       579       534       526

543       534       564       472       376       359       343       337

346       365       345       339       340       426       444       603

842       824       877       724       683       752       869       919

914       993       869       785       675       533       526       481

516       693       921      1125      1019       835       618       479

436       402       443       498       531       547       623       550

622       610       576       561       597       555       479       404

373       313       319       285       326       299       328       330

328       405       450       528       574       701       758      1015

1344      2194      3412      3439      2878      2132      1217       765

500       389       381       369       379       377       343       381

411       435       502       470       537       532       602       589

627       842      1056      1325      1712      2139      2480      3127

3864      6361     11094     16044     15987     13703      9802      5327

2650      1352       767       686       627       608       566       489

463       452       416       393       399       363       397       321

326       342       364       394       459       638       804       635

724       800       820       807       698       587       500       424

393       379       438       414       478       569       958      1465

1462      1522      1430      1082       878       727       713       856

961       940       775       806       790       923      1405      2424

2648      2180      1899      1322       788       525       366       366

321       316       299       299       300       289       283       310

348       346       323       324       271       292       273       365

425       451       388       380       371       297       281       263

267       289       326       321       323       350       331       302

347       358       345       361       341       324       397       417

472       490       515       562       650       685       751       854

914      1364      1788      1570      1258      1035       701       449

353       328       279       282       296       281       294       235

306       249       282       279       285       302       309       360

397       514       577       607       649       825       918       865

813       841       801       793       746       782       912      1294

2071      2357      1851      1637      1298       817       473       397

354       368       327       349       332       374       339       336

402       436       557       512       448       432       397       355

321       336       308       327       318       292       332       325

355       322       338       285       279       244       278       299

331       358       387       387       416       412       408       403

419       469       558       775       929       906       811       718

569       470       411       390       343       395       413       455

552       550       574       698       864      1243      1932      2899

2979      2434      2161      1685      1203       870       565       440

445       392       344       314       307       329       347       378

389       471       544       738       771       917       977      1246

1757      3341      5256      5465      4238      4032      3240      2197

1541      1131       951       872       807       661       462       426

420       385       363       350       320       302       294       300

303       292       313       363       321       313       360       291

289       336       307       327       321       301       384       394

423       488       531       518       538       545       561       588

632       796      1080      1743      2750      3368      2704      2284

2073      1621      1136       938      1121      2046      3066      2674

1988      1882      1551      1029       669       468       386       351

346       366       469       454       408       449       437       389

395       383       317       303       309       281       282       266

302       344       368       363       463       480       558       698

1064      1580      1674      1342      1188      1067       864       551

422       364       350       303       288       314       356       370

386       374       372       375       404       345       337       295

269       268       259       246       255       274       255       266

274       264       265       220       255       292       313       335

322       343       303       294       288       337       434       532

490       463       412       437       494       447       527       593

588       536       525       509       511       485       478       413

397       480       555       566       487       455       431       471

453       461       429       394       414       402       364       331

301       278       269       266       343       369       403       356

346       312       295       257       221       250       199       236

220       260       244       270       260       303       391       409

336       343       347       338       285       262       316       295

343       369       382       342       328       339       289       282

289       271       309       263       270       283       264       257

236       261       255       209       237       222       262       288

262       318       308       321       352       396       483       571

537       475       471       526       475       473       439       453

475       561       861      1225      1298      1025       877       909

865       723       552       535       556       580       673       839

1224      1887      2669      2722      2152      2004      2064      2278

2453      2631      3314      3923      3269      2695      2576      2288

1528      1131       829       643       456       364       351       319

321       299       303       302       284       311       337       438

355       360       342       343       344       305       319       298

343       309       386       336       361       302       325       329

321       317       277       280       278       290       282       317

316       424       459       572       562       506       448       503

447       389       338       397       404       458       385       408

398       435       368       368       453       536       544       488

409       427       371       343       321       252       269       276

258       252       233       252       249       243       239       238

269       225       253       247       212       220       229       219

259       267       270       273       302       328       363       398

399       401       438       406       420       526       632       641

553       510       549       644       723       651       570       543

504       507       495       512       580       845       999       927

786       671       666       642       515       442       412       410

352       318       346       409       482       481       474       571

609       752      1037      1766      3007      3112      2419      1875

1687      1841      1510      1059       711       489       437       425

422       408       401       433       505       544       579       583

571       481       465       461       429       393       332       331

308       266       267       296       243       233       239       240

253       241       265       306       322       362       388       422

449       557       793      1190      1493      1175       919       805

819       757       624       451       308       298       300       337

344       339       343       315       322       321       275       296

303       272       328       359       324       289       256       259

315       258       259       237       244       274       243       243

270       332       282       235       262       250       274       280

243       219       244       231       237       261       233       225

223       252       203       235       255       238       265       276

269       268       316       364       490       508       480       435

395       414       388       319       293       305       278       273

256       282       247       227       281       281       288       289

291       301       268       332       342       375       388       370

344       390       461       520       552       642       814       640

594       474       493       548       478       343       342       288

324       326       352       315       399       378       447       517

685      1101      1370      1328      1176       871       808       910

861       690       547       455       344       356       352       348

356       357       397       368       452       634      1022      1256

1180       922       708       728       789       674       609       439

417       389       381       359       336       343       350       319

317       293       302       306       301       299       324       280

299       326       374       380       390       388       404       376

399       417       458       469       576       698      1005      1140

1148       938       789      1043      1377      1281      1004       676

541       622       594       474       369       307       295       243

288       268       241       243       257       274       233       265

309       325       327       311       274       259       325       345

350       291       325       354       375       388       405       396

488       543       525       482       390       390       378       438

397       359       375       356       301       266       302       286

262       287       270       285       277       274       231       217

256       240       242       248       256       238       238       215

240       259       239       232       260       230       245       244

273       255       242       280       317       371       399       440

412       383       377       383       379       360       387       382

376       392       379       340       336       350       368       422

394       381       373       329       349       342       338       299

299       268       290       266       250       264       273       251

221       265       231       263       277       263       292       312

290       309       312       299       349       344       389       443

658       972      1445      1487      1184       871       684       736

839       872       657       525       388       399       392       363

377       453       451       397       408       363       433       460

453       352       379       342       333       427       352       353

359       328       346       316       326       338       383       434

593       716       619       580       546       510       650      1021

1349      1446      1037       695       527       601       832       785

702       606       486       390       344       352       321       297

329       285       280       286       275       260       248       255

252       254       271       214       207       238       234       255

257       236       218       253       261       261       283       284

326       423       552       602       480       362       299       360

419       425       343       336       314       258       236       243

260       279       283       264       226       216       227       241

252       237       245       219       228       242       238       262

263       229       228       217       229       246       247       274

286       306       314       315       364       374       518       622

640       651       633       529       508       474       442       451

436       373       304       308       243       217       231       233

238       206       230       209       225       201       213       209

202       224       226       231       228       230       218       201

191       223       203       199       224       201       244       230

250       218       232       220       237       254       251       245

261       278       311       296       332       310       290       281

286       322       315       330       311       262       248       224

244       252       240       239       223       283       277       325

279       270       248       275       319       356       435       501

522       530       489       589       699       814       800       655

465       420       407       465       418       396       335       248

272       241       215       222       201       244       223       224

236       209       207       237       231       215       224       237

224       262       272       272       245       270       235       244

235       226       234       221       256       221       235       218

216       223       219       237       217       221       255       225

264       272       238       247       248       271       285       338

382       344       336       336       304       266       250       263

274       246       251       224       230       219       230       225

198       226       210       229       211       219       228       209

222       218       225       254       244       286       298       303

311       309       296       314       306       326       340       391

445       493       552       460       411       386       365       382

468       514       622       756       678       599       485       433

375       379       457       474       464       416       310       291

271       254       279       306       276       307       350       415

381       388       309       290       295       301       320       305

340       285       290       262       248       261       270       332

353       329       336       298       293       308       264       283

261       267       290       296       328       311       311       294

274       257       328       294       365       365       412       430

414       416       558       638       766       760       704       534

462       428       407       401       469       433       384       321

300       276       262       273       277       283       255       236

261       239       251       239       239       245       234       253

290       263       282       271       279       287       307       255

250       272       268       258       319       332       300       326

285       288       255       270       240       285       254       280

283       273       261       264       247       266       274       273

254       272       245       246       248       225       249       266

245       238       227       252       236       226       243       229

238       228       215       241       250       257       276       275

276       307       341       413       468       411       444       310

310       302       316       320       334       363       330       294

336       298       294       279       262       289       293       295

341       292       316       271       296       243       235       284

296       281       274       256       274       261       268       293

287       303       331       358       394       520       613       723

629       510       393       356       338       383       429       476

495       454       379       322       275       267       269       283

314       275       277       290       237       267       255       268

276       288       325       292       279       309       323       296

300       357       378       405       484       582       703       615

572       544       609       661       632       602       565       496

468       394       412       435       456       410       357       301

308       324       382       363       331       343       279       283

286       249       270       260       290       285       264       275

311       277       272       239       252       213       237       261

253       259       248       255       239       249       238       256

283       244       270       245       251       274       274       310

330       312       364       315       297       286       282       335

302       322       304       293       264       286       271       279

268       259       282       254       244       260       257       254

231       254       245       260       282       276       300       311

299       326       346       385       435       440       472       426

430       389       382       321       356       360       358       394

332       369       299       290       272       269       267       288

273       301       305       352       415       446       463       387

357       299       270       311       316       339       346       375

345       330       324       318       318       338       368       380

490       604       719       675       563       496       395       330

317       390       404       456       478       432       341       343

324       338       308       314       321       304       292       293

271       285       279       261       307       332       304       274

301       254       253       282       265       312       312       385

408       433       500       486       409       378       343       316

343       320       385       398       402       375       320       280

300       246       253       249       311       249       241       272

252       230       232       241       242       248       190       242

241       241       264       257       261       249       245       257

281       273       280       274       306       287       291       292

331       337       356       379       393       383       428       401

373       333       333       322       318       338       354       353

404       343       310       323       314       292       321       309

295       311       308       318       248       305       250       295

280       288       289       332       305       288       281       280

261       300       245       282       267       283       295       264

310       293       371       378       401       391       392       426

426       451       428       356       363       333       335       344

349       336       344       347       351       336       320       302

289       290       260       270       307       287       288       304

318       299       276       306       313       341       335       348

352       373       317       251       273       229       296       290

279       273       270       287       265       290       256       268

277       256       220       256       232       290       311       289

294       271       274       281       299       320       329       372

356       356       340       319       336       310       323       303

340       345       360       326       352       327       327       308

306       334       391       400       464       511       506       619

566       555       464       434       437       411       468       486

503       541       473       455       428       358       359       326

332       375       381       332       301       309       298       259

277       277       247       246       250       260       271       257

250       276       272       281       289       292       287       289

297       307       289       263       280       243       261       271

292       289       321       282       288       270       309       323

269       313       276       308       246       265       256       263

272       296       277       268       284       293       303       296

291       303       320       270       292       278       285       311

262       268       255       283       311       249       276       288

276       271       297       254       274       261       274       281

279       278       284       351       319       356       383       376

352       376       349       365       336       325       292       309

307       347       346       404       408       400       405       380

403       351       336       357       339       307       324       304

309       359       340       336       350       352       323       306

301       300       283       298       254       263       298       296

261       275       302       304       327       322       311       301

347       357       390       426       501       440       386       362

322       320       363       301       315       348       317       321

353       358       375       347       305       327       308       328

319       292       316       284       291       339       312       319

320       309       345       358       362       374       378       376

371       405       353       375       363       371       383       346

394       436       431       434       453       467       492       594

601       656       657       631       550       535       446       418

396       382       376       438       438       420       422       464

481       426       378       365       327       306       336       275

297       308       299       297       283       289       291       265

278       254       308       305       307       335       292       278

306       327       307       300       283       299       298       340

281       295       328       351       313       326       360       320

383       333       342       346       340       362       347       343

345       412       429       426       425       419       407       392

364       346       345       317       308       353       346       330

351       358       364       356       401       341       327       342

330       308       315       337       335       318       312       320

322       347       319       365       345       334       383       373

375       395       385       394       436       510       511       521

513       498       490       460       435       407       457       453

459

;

data_cs3alf9DFT

_symmetry_cell_setting                               hexagonal

_symmetry_space_group_name_Hall                   '-P 6c 2c'

_symmetry_space_group_name_H-M                    'P 63/m m c'

_symmetry_Int_Tables_number                             194

loop_

_symmetry_equiv_pos_site_id

_symmetry_equiv_pos_as_xyz

1 x,y,z

2 x-y,x,1/2+z

3 -y,x-y,z

4 -x,-y,1/2+z

5 -x+y,-x,z

6 y,-x+y,1/2+z

7 -y,-x,1/2-z

8 x-y,-y,-z

9 x,x-y,1/2-z

10 y,x,-z

11 -x+y,y,1/2-z

12 -x,-x+y,-z

13 -x,-y,-z

14 -x+y,-x,1/2-z

15 y,-x+y,-z

16 x,y,1/2-z

17 x-y,x,-z

18 -y,x-y,1/2-z

19 y,x,1/2+z

20 -x+y,y,z

21 -x,-x+y,1/2+z

22 -y,-x,z

23 x-y,-y,1/2+z

24 x,x-y,z

_cell_length_a                                          6.25325

_cell_length_b                                          6.25325

_cell_length_c                                         14.71930

_cell_angle_alpha                                            90

_cell_angle_beta                                             90

_cell_angle_gamma                                           120

_cell_volume                                            498.459

_cell_formula_units_Z                                 2

_cell_measurement_temperature                     295

# 9. ATOMIC COORDINATES AND DISPLACEMENT PARAMETERS

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_thermal_displace_type

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_occupancy

_atom_site_U_iso_or_equiv

_atom_site_calc_flag

_atom_site_refinement_flags

_atom_site_disorder_assembly

_atom_site_disorder_group

Al1 Al Uiso 0.00000 0.00000 0.15737 1.000 0.0500 . . . .

F1 F Uiso 0.12575 0.25149 0.25000 1.000 0.0500 . . . .

F2 F Uiso 0.28282 0.14141 0.10071 1.000 0.0500 . . . .

Cs1 Cs Uiso 0.33333 0.66667 0.75000 1.000 0.0500 . . . .

Cs2 Cs Uiso 0.33333 0.66667 0.43622 1.000 0.0500 . . . .

#===============================================================================

# 10. MOLECULAR GEOMETRY

_geom_special_details

;

Bond distances, angles etc. have been calculated using the

rounded fractional coordinates. All su's are estimated

from the variances of the (full) variance-covariance matrix.

The cell esds are taken into account in the estimation of

distances, angles and torsion angles

;

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_1

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

Al1     F1           1.9271                     .       .                   yes

Al1     F2           1.7439                     .       .                   yes

Al1     F1           1.9271                     .     3_555                 yes

Al1     F2           1.7439                     .     3_555                 yes

Al1     F1           1.9271                     .     5_555                 yes

Al1     F2           1.7439                     .     5_555                 yes

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_2

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

F1      Al1     F2            91.60             .       .       .           yes

F1      Al1     F1            75.47             .       .     3_555         yes

F1      Al1     F2            91.60             .       .     3_555         yes

F1      Al1     F1            75.47             .       .     5_555         yes

F1      Al1     F2           163.54             .       .     5_555         yes

F1      Al1     F2           163.54           3_555     .       .           yes

F2      Al1     F2            99.03             .       .     3_555         yes

F1      Al1     F2            91.60           5_555     .       .           yes

F2      Al1     F2            99.03             .       .     5_555         yes

F1      Al1     F2            91.60           3_555     .     3_555         yes

F1      Al1     F1            75.47           3_555     .     5_555         yes

F1      Al1     F2            91.60           3_555     .     5_555         yes

F1      Al1     F2           163.54           5_555     .     3_555         yes

F2      Al1     F2            99.03           3_555     .     5_555         yes

F1      Al1     F2            91.60           5_555     .     5_555         yes

Al1     F1      Al1           90.06             .       .     7_555         yes