Figure SI. FT-IR (A) and 1H-NMR (B) spectra of nicotine 2,6-dihydroxybenzoate.

Table SI Crystal and experimental data of nicotine 2,6-dihydroxybenzoate

| Empirical formula | C17H20N2O4 |
| --- | --- |
| Formula weight | 316.35 |
| Temperature/K | 293.15 |
| Crystal system | monoclinic |
| Space group | P21 |
| a/Å | 7.7108(7) |
| b/Å | 11.6910(12) |
| c/Å | 9.4114(12) |
| α/° | 90 |
| β/° | 108.996(12) |
| γ/° | 90 |
| Volume/Å3 | 802.21(16) |
| Z | 2 |
| ρcalcg/cm3 | 1.310 |
| μ/mm-1 | 0.094 |
| F(000) | 336.0 |
| Crystal size/mm3 | 0.35 × 0.3 × 0.25 |
| Radiation | Mo Kα (λ = 0.71073) |
| 2θ range for data collection/° | 5.96 to 52.744 |
| Index ranges | -9 ≤ h ≤ 9, -14 ≤ k ≤ 9, -11 ≤ l ≤ 8 |
| Reflections collected | 3783 |
| Independent reflections | 2506 [Rint = 0.0154, Rsigma = 0.0356] |
| Data/restraints/parameters | 2506/1/211 |
| Goodness-of-fit on F2 | 1.030 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0432, wR2 = 0.0861 |
| Final R indexes [all data] | R1 = 0.0633, wR2 = 0.0981 |
| Largest diff. peak/hole / e Å-3 | 0.10/-0.16 |
| Flack parameter | -0.8(7) |

Figure SII. The single crystal structure of nicotine 2,6-dihydroxybenzoate.