Supporting Information

Comparative study of the isothermal solid-state reaction systems of kaolinite-Na2CO3 and kaolinite-quartz-Na2CO3 for coal gangue activation

Kezhou Yan*, Yaru Guo, Yuanyuan Zhang, Yanxia Guo, Fangqin Cheng*

State Environmental Protection Key Laboratory on Efficient Resource-utilization Techniques of Coal Waste, Institute of Resources and Environmental Engineering, Shanxi University, Taiyuan 030006, China

* Corresponding author:

Kezhou Yan   Email: yankz@sxu.edu.cn

Fangqin Cheng   Email: cfangqin@sxu.edu.cn

Figures

Fig. S-1 XRD patterns of the as-received kaolinite.

Fig. S-2 XRD patterns of Kln-Na2CO3 quasi-binary system (No. 1~9) and Kln-Qtz-Na2CO3 quasi-ternary system (No. 10~45) calcined at 850 °C

Table

Table S-1 PDF information referred to the defined phase

Fig.S-1 XRD patterns of the as-received kaolinite

Table S-1 PDF information referred to the defined phases

| Phase Name | Abbreviation | Chemical Formula | PDF Number |
| --- | --- | --- | --- |
| Kaolinite | Kln | Al2Si2O5(OH)4 | 02-189-6951 |
| Quartz | Qtz | SiO2 | 01-167-0146 |
| Sodium carbonate | Na | Na2CO3 | 01-164-1148 |
| Low-temperature carnegieite | L-phase | NaAlSiO4 | 96-101-0958 |
| Nepheline | Nep | NaAlSiO4 | 96-100-8762 |
| Zeolite | Zeo | NaAlSiO4 | 01-192-6489 |
| Sodium aluminum silicate-1 | SAS-1 | Na1.55Al1.55Si0.45O4 | 96-200-2895 |
| Sodium aluminum silicate-2 | SAS-2 | Na1.95Al1.95Si0.05O4 | 96-200-2892 |
| Sodium trisilicate | St | Na2Si3O7 | 01-164-1293 |
| Sodium metasilicate | Sm | Na2SiO3 | 00-016-0818 |
| Sodium pyrosilicate | Sp | Na6Si2O7 | 00-027-0784 |

Fig. S-2 XRD patterns of Kln-Na2CO3 quasi-binary system (No. 1~9) and Kln-Qtz-Na2CO3 quasi-ternary system (No. 10~45) calcined at 850 °C