Supplemental table 4: Dimensions of 33 gold and silver objects from Casa Parroquial. (1) Largest cluster of objects sharing the same manufacture techniques. (2) Thickness observed under the SEM microscope.

|  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **General category** | **N° Id Lab** | **Id museum** | **Burial** | **Height**  **(mm)** | | **Width**  **(mm)** | | **Thickness (max)** | | **Weight (g)** |
| **max** | **min** | **max** | **min** | **μm2** | **mm** |
| Port. vessel | popm141 | 18.087 | 1 | 109 | 104 | 65 | 56 | - | 2.8 | 206.0 |
| Ring | popm089 | 18.119 | 3 | 11 | 11 | 19 | 15 | - | 0.5 | 1.9 |
| Sheet | popm009 | 18.113 | 7 | 27 | 21 | 22 | 21 | 33 | 0.03 | 0.3 |
| Sheet | popm011 | 18.114 | 30 | 25 | 25 | 16 | 20 | 0.02 | 0.2 |
| Sheet | popm008 | 18.115 | 31 | 29 | 17 | 15 | 25 | 0.03 | 0.2 |
| Sheet frag | popm003 | 18.116 | 24 | 23 | 5 | 3 | 13 | 0.01 | 0.1 |
| Sheet | popm002 | 1086 | 32 | 20 | 28 | 20 | 54 | 0.1 | 0.2 |
| Band | popm001 | 18.109 | 8 | 77 | 67 | 29 | 26 | 113 | 0.1 | 2.4 |
| Pendant | popm010 | 18.110 | 26 | 19 | 19 | 11 | 87 | 0.1 | 0.6 |
| Headdress | popm085 | 18.107 | 11 | 73 | - | 30 | 3 | - | 0.2 | 3.6 |
| Headdress | popm087 | 18.108 | 13 | 154 | 131 | 37 | 115 | - | 0.2 | 32.4 |
| Band1 | popm079 | 18.094 | 16 | 144 | 141 | 28 | 27 | - | 0.2 | 5.5 |
| Band1 | popm080 | 18.095 | 144 | 140 | 29 | 29 | - | 0.1 | 6.9 |
| Headdress | popm083 | 18.102 | 102 | - | 18 | 1 | - | 0.3 | 4.0 |
| Headdress | popm082 | 18.096 | 102 | - | 17 | 1 | - | 0.2 | 4.5 |
| Pendant1 | popm077 | 18.097 | 48 | 45 | 28 | 24 | - | 0.1 | 1.8 |
| Pendant1 | popm078 | 18.103 | 48 | 45 | 27 | 24 | - | 0.3 | 1.8 |
| Pendant1 | popm074 | 18.098 | 14 | 13 | 12 | 12 | - | 0.1 | 0.2 |
| Pendant1 | popm076 | 18.099 | 18 | 18 | 12 | 12 | - | 0.1 | 0.3 |
| Pendant1 | popm075 | 18.100 | 18 | 16 | 13 | 13 | - | 0.2 | 0.3 |
| Pendant1 | popm073 | 18.101 | 18 | 17 | 12 | 12 | - | 0.1 | 0.3 |
| Pendant1 | popm051 | 18.104 | 17 | 16 | 13 | 13 | - | 0.1 | 0.3 |
| Pendant1 | popm047 | 18.105 | 18 | 17 | 12 | 11 | - | 0.1 | 0.4 |
| Pendant1 | popm050 | 18.106 | 16 | 16 | 13 | 13 | - | 0.1 | 0.3 |
| Sheet frag | popm007 | C.P.16 | 37 | 32 | 29 | 28 | 42 | 0.04 | 0.9 |
| Pendant1 | popm081 | 18.093 | 18 | 50 | 48 | 50 | 47 | - | 0.2 | 4.0 |
| *Kero* | popm140 | 18.088 | 168 | 167 | 163 | 88 | - | 1.2 | 274.0 |
| *Kero* | popm139 | 18.089 | 165 | - | 193 | 105 | - | 2.2 | 283.0 |
| Band | popm017 | 18.091 | 173 | 132 | 62 | 48 | 224 | 0.2 | 36.0 |
| Band | popm018 | 18.092 | 196 | 154 | 56 | 49 | 232 | 0.2 | 35.8 |
| Ring | popm088 | 18.090 | 21 | 18 | 16 | 21 | 20 | - | 0.4 | 4.8 |
| Headdress | popm084 | 18.111 | 22 | 120 | - | 50 | 19 | - | 0.3 | 14.4 |
| Headdress | popm086 | 18.112 | 110 | - | 46 | 1 | - | 0.2 | 7.6 |
| **Total** | | | | | | | | | | **935g** |