SUPPLEMENTARY MATERIAL

to the article

“Periodic cation segregation in Cs0.44[Nb2.54W2.46O14] quantified by high-resolution scanning transmission electron microscopy”

M. Heidelmann1,2,*, J. Barthel1,2, G. Cox3, T. E. Weirich1,4

1 Central Facility for Electron Microscopy, RWTH Aachen University, 52074 Aachen, Germany

2 Ernst Ruska-Centre for Microscopy and Spectroscopy with Electrons, Forschungszentrum Jülich GmbH, 52425 Jülich, Germany

3 BASF SE, Polymer Physics Department, 67065 Ludwigshafen, Germany

4 Institute of Crystallography, RWTH Aachen University, 52056 Aachen, Germany

* Corresponding author, E-mail:  m.heidelmann@fz-juelich.de

Supplementary Data

HAADF-STEM-SUM-CALIB.DM3: Calibrated HAADF STEM image provided in Gatan Digital Micrograph 3 image format. The data represents the average of 20 STEM images of CsNbWO in [001] projection. The average was calculated after positional alignment of the 20 original images based on a cross-correlations analysis.

CNWO.CIF: Crystal structure definition file containing an updated structure model with individual Nb/W occupation levels.

CNWOo8-1UC.CEL: Crystal structure definition file used for STEM image simulations with the Dr. Probe simulation software.

Supplementary Figures

Figure S1: Image shift measured over the series of 20 successively acquired STEM images. The maximum shift between two images is less than 0.15 nm.