Supplementary Material:

Understanding the Nature of Crystallographic Bonds by Establishing the Correlation between Ion Pair Chemistry and their Separation in Detector Space

Distributions were taken from 10 nm thick representative regions within the central region of interest. The layer (AlGaN or GaN) and growth method (MBE or MOCVD) are indicated above each set of figures.

Ga+-N+ evaporated from AlGaN

| MBE-1 | MOCVD-1 |
| --- | --- |
| FWHM = 2.2 mm Median = 1.5 mm | FWHM = 2.1 mm Median = 1.4 mm |
| MBE-2 | MOCVD-2 |
| FWHM = 2.2 mm Median = 1.5 mm | FWHM = 1.9 mm Median = 1.4 mm |

Ga+-N+ evaporated from GaN

| MBE-1 | MOCVD-1 |
| --- | --- |
| FWHM = 2.5 mm Median = 1.5 mm | FWHM = 1.9 mm Median = 1.4 mm |
| MBE-2 | MOCVD-2 |
| FWHM = 2.7 mm Median = 1.5 mm | FWHM = 1.8 mm Median = 1.3 mm |

Ga+-N2+ evaporated from AlGaN

| MBE-1 | MOCVD-1 |
| --- | --- |
| FWHM = 2.0 mm Median = 1.5 mm | FWHM = 2.2 mm Median = 1.7 mm |
| MBE-2 | MOCVD-2 |
| FWHM = 2.2 mm Median = 1.5 mm | FWHM = 2.3 mm Median = 1.6 mm |

Ga+-N2+ evaporated from GaN

| MBE-1 | MOCVD-1 |
| --- | --- |
| FWHM = 2.0 mm Median = 1.5 mm | FWHM = 2.2 mm Median = 1.7 mm |
| MBE-2 | MOCVD-2 |
| FWHM = 2.2 mm Median = 1.6 mm | FWHM = 2.2 mm Median = 1.6 mm |

Ga+-Ga+ evaporated from AlGaN

| MBE-1 | MOCVD-1 |
| --- | --- |
| FWHM = 1.6 mm Median = 1.3 mm | FWHM = 2.0 mm Median = 1.5 mm |
| MBE-2 | MOCVD-2 |
| FWHM = 2.0 mm Median = 1.3 mm | FWHM = 1.9 mm Median = 1.4 mm |

Ga+-Ga+ evaporated from GaN

| MBE-1 | MOCVD-1 |
| --- | --- |
| FWHM = 1.8 mm Median = 1.5 mm | FWHM = 1.7 mm Median = 1.5 mm |
| MBE-2 | MOCVD-2 |
| FWHM = 1.8 mm Median = 1.4 mm | FWHM = 1.9 mm Median = 1.5 mm |

Al+-N+

| MBE-1 | MOCVD-1 |
| --- | --- |
| FWHM = 3.3 mm Median = 2.1 mm | FWHM = 3.5 mm Median = 2.6 mm |
| MBE-2 | MOCVD-2 |
| FWHM = 3.5 mm Median = 2.2 mm | FWHM = 3.3 mm Median = 2.2 mm |

Al+-N2+

| MBE-1 | MOCVD-1 |
| --- | --- |
| FWHM = 2.8 mm Median = 2.8 mm | FWHM = 2.7 mm Median = 2.8 mm |
| MBE-2 | MOCVD-2 |
| FWHM = 2.7 mm Median = 2.5 mm | FWHM = 2.7 mm Median = 2.7 mm |

Al++-N+

| MBE-1 | MOCVD-1 |
| --- | --- |
| FWHM = 2.7 mm Median = 1.9 mm | FWHM = 2.8 mm Median = 1.9 mm |
| MBE-2 | MOCVD-2 |
| FWHM = 2.6 mm Median = 1.9 mm | FWHM = 2.9 mm Median = 1.9 mm |

Al++-N2+

| MBE-1 | MOCVD-1 |
| --- | --- |
| FWHM = 2.7 mm Median = 2.5 mm | FWHM = 2.8 mm Median = 2.4 mm |
| MBE-2 | MOCVD-2 |
| FWHM = 2.6 mm Median = 2.3 mm | FWHM = 2.9 mm Median = 2.3 mm |

Al+++-N+

| MBE-1 | MOCVD-1 |
| --- | --- |
| FWHM = 2.6 mm Median = 1.6 mm | FWHM = 2.3 mm Median = 1.5 mm |
| MBE-2 | MOCVD-2 |
| FWHM = 2.7 mm Median = 1.6 mm | FWHM = 2.5 mm Median = 1.6 mm |

Al+++-N2+

| MBE-1 | MOCVD-1 |
| --- | --- |
| FWHM = 2.0 mm Median = 1.6 mm | FWHM = 1.9 mm Median = 1.5 mm |
| MBE-2 | MOCVD-2 |
| FWHM = 2.2 mm Median = 1.6 mm | FWHM = 1.8 mm Median = 1.6 mm |