Supplementary Information for

Possible Role of Prussian Blue Nano Particles in Chemical Evolution: Interaction with Ribose Nucleotides

Rachana Sharma, Md. Asif Iqubal  and Kamaluddin*

Department of Chemistry, Indian Institute of Technology Roorkee,

Roorkee-247667 (U.K), India

Author for Correspondence

*Dr. Kamaluddin

Department of Chemistry

Indian Institute of Technology Roorkee

Roorkee-247667 (U.K), India

Tel.: +91-1332-285796

Fax: +91-1332-274473

Email: kamalfcy@iitr.ernet.in

Figure S1: A thermogravimetric and differential thermal analysis curve of Prussian blue

Figure S2: UV-visible spectrum of Prussian blue. Inset: Digital camera image of PB nanoparticles

Figure S3: The typical XRD pattern of Prussian blue. Inset: crystal structure sketch map of PB consisting of alternating iron(II) and iron(III) located on a face centered cubic lattice.

Figure S4: Effect of contact time on ribonucleotide adsorption

Figure S5:  Effect of amount of adsorbent of ribonucleotide on adsorption

Table S1: Characteristics of the Ribonucleotides

| Name | Abbreviations | Structure of Nucleotide | Solubility (g/L) | pKa |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | pKa1 (RMP ⇄ RMP- + H+) | pKa2 (RMP- ⇄ RMP2- +H+) |
| Adenosine 5΄-monophosphate | 5΄-AMP | R = Adenine (A) | 3.3 | 0.9 | 6.1 |
| Guanosine 5΄-monophosphate | 5΄-GMP | R = Guanine (G) | 3.6 | 0.7 | 6.1 |
| Cytidine 5΄-monophosphate | 5΄-CMP | R = Cytosine (C) | 16.3 | 0.8 | 6.3 |
| Uridine 5΄-monophosphate | 5΄-UMP | R = Uracil (U) | 12.0 | 1.0 | 6.4 |

Table S2: Elemental composition of Prussian blue

| Weight of the sample (mg) | % C | %N | % H | %Fe |
| --- | --- | --- | --- | --- |
| 1.6130 | 19.02 (19.43) | 22.25(22.67) | 2.527(2.51) | 33.47(35.27) |

(Bracket values representing theoretical values)

Table S3: Typical infrared spectral frequencies (cm-1) of ribonucleotides before and after absorption on Prussian blue

| Ribonucleotide | δNH2 | υC-4=O | υPO32-(symmetric) | υPO32-(antisymmetric) |
| --- | --- | --- | --- | --- |
| 5׳-AMP | 1636 (1645) | ---- | 985 (978) | 1114 (1103) |
| 5׳-GMP | 1646 (1642) | 1697(1685) | 973(978) | 1043(1080) |
| 5׳-UMP | ---- | 1675(1682) | 992(981) | 1109 (1083) |
| 5׳-CMP | 1675(1688) | ---- | 979 (985) | 1107(1088) |

(Bracket values representing infrared spectral frequencies (cm-1) of ribonucleotides before adsorption)