Supplementary Information

Carbon Nanomaterials for Applications on Supercapacitors

Youning Gong1, Qiang Fu1,2, Chunxu Pan 1,2, *

1 School of Physics and Technology, and MOE Key Laboratory of Artificial Micro- and Nano-structures, Wuhan University, Wuhan, 430072, China

2 Center for Electron Microscopy, Wuhan University, Wuhan, 430072, China

*Author to whom correspondence should be addressed.

E-mail: cxpan@whu.edu.cn; Tel: +86-27-68752481 ext. 8168

Table S1 Comparison of capacitive performance of different carbon-based electrodes

| Carbon material type | Electrolyte | Specific capacitance | Rate capability | Ref |
| --- | --- | --- | --- | --- |
| Hollow-cored CNSs | 2 M H2SO4 | 251 F/g at 50 mV/s | 76% (50 to 500 mV/s) | [9] |
| CNTs on Ni foams | 6 M KOH | 25 F/g at 200 mV/s | 72% (0.25 to 5 A/g) | [15] |
| N-doped CNTs | 6 M KOH | 48 F/g at 0.25 A/g |  | [19] |
| CNFs | 1 M H2SO4 | 73.20 F/g at 200 mV/s |  | [22] |
| N-doped coiled CNFs | 6 M KOH | 120 F/g at 0.25 A/g |  | [21] |
| Reduced graphene oxide | 6 M KOH | 67.9 F/g at 1 A/g |  | [28] |
| High-quality graphene paper | 6 M KOH | 129.0 F/g at 1 A/g | 49% (1 to 10 A/g) | [26] |
| N-doped graphene in ammonia flame | 6 M KOH | 246.4 F/g at 1 A/g | 53.8% (1 to 6 A/g) | [29] |
| CNS/NiCo2O4 core-shell sub-microspheres | 6 M KOH | 1420 F/g at 1 A/g | 72% (1 to 10 A/g) | [10] |