Spatial Control of the Threshold Voltage of Low-Voltage Organic Transistors by Microcontact-Printing of Alkyl- and Fluoroalkyl-phosphonic Acids

Ikue Hirata1, Ute Zschieschang2, Frederik Ante2, Tomoyuki Yokota1, Kazunori Kuribara1, Tatsuya Yamamoto3, Kazuo Takimiya3, Masaaki Ikeda4, Hirokazu Kuwabara4, Hagen Klauk2, Tsuyoshi Sekitani1, and Takao Someya1,5*

1 School of Engineering, The University of Tokyo, 7-3-1 Hongo, Bunkyo-ku, Tokyo 113-8656, Japan

2 Max Planck Institute for Solid State Research, Heisenbergstrasse 1, 70569 Stuttgart, Germany

3 Department of Applied Chemistry, Faculty of Engineering, Hiroshima University, Higashi-Hiroshima, Hiroshima 739-8527, Japan

4 Functional Chemicals RD Laboratories, Nippon Kayaku Co., Ltd., Kita, Tokyo 115-8588, Japan

5 Institute for Nano Quantum Information Electronics, The University of Tokyo, 4-6-1 Komaba, Meguro-ku, Tokyo 153-8505, Japan

Correspondence should be sent to someya@ee.t.u-tokyo.ac.jp.

Details of Figure 1(c)

Ideally, FC18-PA is expected to have smaller leak current density, however, actual devices were affected by many factors such as drift currents by small pinholes, sweep direction and the number of sweeps. The two minima observed in the dipped samples were shifted due to the independent sweep in the positive direction and in the negative direction.

Table SI. Summary of the threshold voltages and field-effect mobilities of DNTT transistors with SAMs of C41 or FC prepared by stamping or dipping, or without SAM.

Figure S1. AFM images of DNTT layers deposited on AlOx and on dipped or stamped SAM layers. The scan area is 2.5 × 2.5μm2. The grain sizes of each sample were (a) on AlOx 2.4 × 104 nm2, (b) on dipped HC14-PA 3.2 × 104 nm2, (c) on dipped FC18-PA 8.3 × 104 nm2, (d) on stamped HC14-PA 3.4 × 104 nm2, and (e) on stamped FC18-PA 3.1 × 104 nm2.

Figure S2. Optical image of a load inverter with stamped SAMs. The load transistor has channel width of 2 mm and channel length of 50 µm. The drive transistor has channel width of 35 mm and channel length of 50 µm.

Table SI

|  | VTH (V) | mobility (cm2/V·s) |
| --- | --- | --- |
|  | average | standard deviation | average | standard deviation |
| HC14-PA (dipping) | -1.34 | 0.068 | 1.90 | 0.122 |
| FC18-PA (dipping) | -0.27 | 0.052 | 0.81 | 0.026 |
| HC14-PA (stamping) | -1.19 | 0.071 | 1.05 | 0.314 |
| FC18-PA (stamping) | -0.36 | 0.048 | 0.79 | 0.373 |
| without SAM | -1.26 | 0.151 | 0.31 | 0.091 |