Plasticity-induced oxidation reactivity on Ni(100) studied by scanning tunneling spectroscopy

F. W. Herbert,1 K. J. Van Vliet1 and B. Yildiz2

1Department of Materials Science & Engineering, Massachusetts Institute of Technology, 77 Massachusetts Avenue, Cambridge, MA 02139 USA

2Department of Nuclear Science & Engineering, Massachusetts Institute of Technology, 77 Massachusetts Avenue, Cambridge, MA 02139 USA

Address all correspondence to byildiz@mit.edu and krystyn@mit.edu

Supplementary Material

Supplementary Material Fig. 1: I-V averaged from over >100 point spectra taken on flat terrace regions and at dislocation steps. This data was used to calculate the dI/dV curves in FIG. 1.

Supplementary Material Fig. 2: STM images of a different set of perpendicular dislocation steps formed by in situ indentation (a) in UHV prior to O2 exposure, and (b) after 100 L O2 exposure showing an increasing density of white dots from the formation of oxide nuclei and islands.  Imaging conditions: -0.15 V, 1 nA. Scale bar: 10 nm.