Supplemental Information

Control of Thermal and Optoelectronic Properties in 
Conjugated Poly(3-alkylthiophenes)

Victor Ho,†, ‡ Bryan S. Beckingham ‡ Hoi H. Ng, † Rachel A. Segalman†,‡,*

† Department of Chemical and Biomolecular Engineering, University of California, Berkeley, California 94720

‡ Materials Science Division, Lawrence Berkeley National Laboratory, Berkeley, California 94720

* To whom correspondence should be addressed: segalman@berkeley.edu

General Methods

The 1H NMR spectra were measured on a Bruker AV-500 spectrometer using ~1 wt% polymer solutions in deuterated chloroform (Cambridge). Molecular weights and polydispersities were determined by size exclusion chromatography (SEC) collected on a Viscotek TDA 302 SEC with four Viscotek T-columns (one T-6000, T-5000, T-4000, and T-3000 column) and calibrated with polystyrene standards. The response was measured using a refractive index (RI) detector. Tetrahydrofuran (THF) at 35 °C was used as the mobile phase at a flow rate of 1 mL min-1. Differential scanning calorimetry (DSC) measurements were acquired using a Thermal Advantage Q20 calorimeter at a scan rate of 10 °C min-1. An indium standard was used to calibrate the instrument and nitrogen was used as the purge gas. Melting transitions were taken as the peak temperature of the second heating scan.

Structural Characterization

Bulk wide angle X-ray scattering (WAXS) samples were prepared by melt pressing polymer into 1 mm thick aluminum washers and thermally annealed under argon at 20°C below the melting transition for 10 minutes. Room temperature WAXS experiments were conducted at beamline 1-4 of the Stanford Synchrotron Radiation Laboratory (SSRL) equipped with a Rayonix165 CCD detector. Two-dimensional diffraction images were radially averaged calibrated using a silver behenate (AgB) standard. Crystal-crystal transitions were not observed upon heating samples through the melting transition.

Detailed Synthetic Procedure

Materials. All reagents and solvents were used as received from Sigma-Aldrich unless otherwise noted. Degassed tetrahydrofuran (THF) was purified by passage through an activated alumina column (Advanced Specialty Gas Equipment, 7x12 mesh) and was collected in flame-dried, air-free flask. Poly(3-alkylthiophenes) (P3ATs) were synthesized according to the GRIM procedure established in the literature.

Representative Synthesis of Poly(3-(2’-ethyl)-hexylthiophene)-Poly(3-hexylthiophene) Random Copolymers. General procedure for synthesis of P3AT random copolymers follows GRIM method presented by McCullough and coworkers1 and adapted by others for random copolymerization. 2, 3 A 250 mL three neck flask was flame-dried and back-filled with nitrogen. 2,5-dibromo-3-(2’-ethyl)-hexylthiophene (7.0 g, 20. mmol) and 2,5-dibromo-3-hexylthiophene (3.0 g, 9.1 mmol) were added by syringe followed by addition of anhydrous THF. A solution of 2.0 M tert-butylmangesium chloride (14.6 mL, 29.2 mmol) in diethyl ether was added by syringe and the reaction solution was refluxed for 90 minutes. After cooling to room temperature, dry Ni(dppp)Cl2 (184 mg, 0.33 mmol) was added and the solution was allowed to react for 45 minutes. Solution turned red upon addition of nickel catalyst and retained color for the duration of the reaction. The polymer was then precipitated in methanol and collected by vacuum filtration. The powder was then extracted with methanol, acetone, and chloroform with a Soxhlet apparatus. Hexanes was used for washing of P3EHT:P3HT-65 and P3HT. The final product was collected as a colored powder from the chloroform phase by precipitation in methanol and was dried under vacuum overnight.

Scheme S1. Synthesis of P3EHT:P3HT-x random copolymers by GRIM polymerization

Figure S1: 1H NMR of spectra of (a) P3HT, (b) P3EHT, (c) P3EHT:P3HT-19, (d) P3EHT:P3HT-35, (e) P3EHT:P3HT-48, (f) P3EHT:P3HT-63, and (g) P3EHT:P3HT-70. Random copolymer composition was determined from the relative peak areas of resonances in the aromatic proton region.

Ultraviolet-Visible (UV-Vis) Spectroscopy Measurements

Sample Preparation. UV-Vis measurements were made with Varian Cary 50 instrument between 300 and 900 nm. Thin films were prepared by spin coating at 1500 rpm from 1 wt% polymer solutions in chlorobenzene on either glass or silicon substrates. Films were annealed at 20°C below the melting transition under argon for 1 minute.

Spano Model. The Spano model has been used to describe the aggregate absorption in thin films. The absorption data was fit with Equation 1, where S is the Huang-Rhys factor (which has been set to 1 for this study), m and n are vibrational states, W is the excitonic bandwidth, Ep is the energy of the C=C stretching mode, E0-0 is the energy of the 0-0 transition, and σ is the Gaussian line width which can be related to the electronic disorder. It should be noted that in this form, E0-0 combines both the energy of the 0-0 transition in the gas phase and the gas-crystal shift factor, D. The final term of the equation represents the vibronic progression by the summation of Gaussians with line widths, σ. The vibronic transitions are offset by integer multiples of Ep and a correction which addresses the fact that transitions in H-aggregates are only allowed to the top of the vibronic band. The oscillator strengths of individual transitions are modified by terms which account for Franck-Condon intensities of a single molecule (the first term) and mixing between excitons of different vibronic bands (the second term). 4-7 It should be noted that high energy deviations from the experimental data represent absorbance by unaggregated regions and higher energy electronic transitions while those at low energy may be due to aggregate absorption to lower energy vibronic transitions of the 0-0 band. The model was fit to the collected absorption data in the regime dominated by aggregate absorption (1.93 to 2.25 or 2.03 to 2.35 for P3HT- or P3EHT-like aggregates).

Table S1: Fitting parameters to UV-vis spectra of thin films

| Sample | W (meV) | E0-0 (eV) | Ep (meV) | σ (meV) |
| --- | --- | --- | --- | --- |
| P3HT | 55 | 2.03 | 176 | 73 |
| P3EHT:P3HT-19 | 57 | 2.03 | 169 | 73 |
| P3EHT:P3HT-35 | 90 | 2.02 | 185 | 80 |
| P3EHT:P3HT-48 | 102 | 2.03 | 179 | 79 |
| P3EHT:P3HT-63 | 118 | 2.12 | 178 | 80 |
| P3EHT:P3HT-70 | 129 | 2.12 | 190 | 87 |
| P3EHT | 157 | 2.13 | 205 | 94 |

Figure S2: Representative UV-vis absorption profiles for (a) P3HT, (b) P3EHT:P3HT-19, (c) P3EHT:P3HT-35, (d) P3EHT:P3HT-48, (e) P3EHT, (f) P3EHT:P3HT-70, and (g) P3EHT:P3HT-63 with fits to Equation S1. Individual vibronic transitions are presented as green, red, teal, purple, and yellow curves the summation of which shown as a gray curve. Parameters for fits are collected in Table S1 as average and standard deviation of three thin films.

Table S2: Monomer feed ratios and polymer compositions

| Sample | Feed P3EHT mol% | P3EHT mol%a |
| --- | --- | --- |
| P3EHT:P3HT-19 | 18.7 | 18.5 |
| P3EHT:P3HT-35 | 37.0 | 34.7 |
| P3EHT:P3HT-48 | 46.9 | 47.7 |
| P3EHT:P3HT-63 | 68.2 | 62.7 |
| P3EHT:P3HT-70 | 75.0 | 69.5 |

a As determined by 1H NMR spectroscopy

Table S3: Crystalline reflections

| Sample | 100 (nm-1) | 010 (nm-1)a | 020 (nm-1) a | 200 (nm-1) |
| --- | --- | --- | --- | --- |
| P3HT | 3.6 | - | 15.9 | 7.2 |
| P3EHT:P3HT-19 | 3.7 | - | 16.0 | 7.3 |
| P3EHT:P3HT-35 | 3.5 | - | 15.5 | 7.1 |
| P3EHT:P3HT-48 | 3.6 | - | 15.3 | 7.2 |
| P3EHT:P3HT-63 | 4.0 | 5.5 | - | 8.0 |
| P3EHT:P3HT-70 | 4.1 | 6.5 | - | 8.2 |
| P3EHT | 4.1 | 6.3 | - | 8.3 |

a Empty values are either disallowed by symmetry (orthorhombic unit cell) or difficult to assign due to large peak widths from disorder within polymer crystallites.

References

1.	R. S. Loewe, P. C. Ewbank, J. Liu, L. Zhai and R. D. McCullough: Regioregular, Head-to-Tail Coupled Poly(3-alkylthiophenes) Made Easy by the GRIM Method: Investigation of the Reaction and the Origin of Regioselectivity. Macromolecules. 34, 4324 (2001).

2.	P. T. Wu, G. Ren and S. A. Jenekhe: Crystalline Random Conjugated Copolymers with Multiple Side Chains: Tunable Intermolecular Interactions and Enhanced Charge Transport and Photovoltaic Properties. Macromolecules. 43, 3306 (2010).

3.	Y. Zhang, K. Tajima and K. Hashimoto: Nanostructure Formation in Poly(3-hexylthiophene-block-3-(2-ethylhexyl)thiophene)s. Macromolecules. 42, 7008 (2009).

4.	F. C. Spano: Modeling disorder in polymer aggregates: The optical spectroscopy of regioregular poly„3-hexylthiophene thin films. J. Chem. Phys. 122, 234701 (2005).

5.	F. C. Spano: Absorption in regio-regular poly(3-hexyl)thiophene thin films: Fermi resonances, interband coupling and disorder. Chem. Phys. 325, 22 (2006).

6.	S. T. Turner, P. Pingel, R. Steyrleuthner, E. J. W. Crossland, S. Ludwigs and D. Neher: Quantitative Analysis of Bulk Heterojunction Films Using Linear Absorption Spectroscopy and Solar Cell Performance. Adv. Funct. Mater. 21, 4640 (2011).

7.	D. T. Duong, M. F. Toney and A. Salleo: Role of confinement and aggregation in charge transport in semicrystalline polythiophene thin films. Phys. Rev. B: Condens. Matter. 86, 205205 (2012).