# Supplementary Information

# Guidelines in Predicting Phase Formation in High-Entropy Alloys

# Y. Zhanga)

# State Key Laboratory for Advanced Metals and Materials, University of Science and Technology Beijing, Beijing 100083, China

# S.G. Ma

# Insittute of Applied Mechanics and Biomedical Engineering, Taiyuan University of Technology, Taiyuan 030024, China

# P.K. Liaw

# Department of Materials Science and Engineering, The University of Tennessee, Knoxville, TN 37996, USA

# Z. Tang

# Department of Materials Science and Engineering, The University of Tennessee, Knoxville, TN 37996, USA

# Y.Q. Cheng

# Chemical and Engineering Materials Division, Oak Ridge National Laboratory, Oak Ridge, TN 37830, USA

# M.C. Gao

# National Energy Technology Laboratory, Albany, OR 97321, USA

# URS Corporation, P.O. Box 1959, Albany, OR 97321, USA

# Z.P. Lu

# State Key Laboratory for Advanced Metals and Materials, University of Science and Technology Beijing, Beijing 100083, China

a)To whom correspondence should be addressed.

E-mail: drzhangy@ustb.edu.cn.

- Supplementary Table S1

Table S1. Phases or critical casting thickness, Zc or critical cooling rate, Rc, valence electron concentration, VEC, enthalpy of mixing, ΔHmix, entropy of mixing, ΔSmix, critical solution temperature, Tc, average melting point, Tm, Ω (Ω = TmΔSmix/(ΔHmix(), and atomic-size difference, δ for some typical HEAs and BMGs.

| Alloys | Phases/Zc (mm) or Rc (K/s) | VEC | ΔHmix (kJ/mol) | ΔSmix (J/mol.K) | Tc (K) | Tm (K) | Ω | δ (%) | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Al0.25CrCuFeNi2 | FCC | 8.71 | 0.36 | 12.14 | 29.89 | 1,712.64 | 57.31 | 2.93 | This work |
| Al0.5CrCuFeNi2 | FCC | 8.45 | -2.51 | 12.60 | 199.37 | 1,677.23 | 8.41 | 3.82 | This work |
| Al1.0CrCuFeNi2 | FCC+BCC | 8.00 | -5.78 | 12.98 | 458.50 | 1,615.25 | 3.63 | 4.82 | This work |
| Al1.5CrCuFeNi2 | FCC+BCC | 7.62 | -8.05 | 13.01 | 618.50 | 1,562.81 | 2.53 | 5.38 | This work |
| Al2.0CrCuFeNi2 | BCC | 7.29 | -9.63 | 12.89 | 747.57 | 1,517.86 | 2.03 | 5.71 | This work |
| Al3.0CrCuFeNi2 | BCC+ordered BCC | 6.75 | -11.50 | 12.42 | 925.73 | 1,444.81 | 1.56 | 6.03 | This work |
| CoCrFeNiAl | BCC | 7.20 | -12.32 | 13.38 | 915.36 | 1,675.10 | 1.83 | 5.25 | [S1] |
| CoCrFeNiCu | FCC | 8.80 | 3.20 | 13.38 | 239.13 | 1,760.00 | 7.36 | 1.07 | [S1] |
| CoCrFeNiCuAl0.3 | FCC | 8.47 | 1.56 | 14.43 | 108.09 | 1,713.22 | 15.85 | 3.15 | [S1] |
| CoCrFeNiCuAl0.5 | FCC | 8.27 | -1.52 | 14.70 | 103.43 | 1,684.86 | 16.29 | 3.82 | [S1] |
| CoCrFeNiCuAl0.8 | BCC+FCC | 8.00 | -3.61 | 14.87 | 242.77 | 1,646.00 | 6.78 | 4.49 | [S1] |
| CoCrFeNiCuAl | BCC+FCC | 7.83 | -4.78 | 14.90 | 320.60 | 1,622.25 | 5.06 | 4.82 | [S1] |
| CoCrFeNiCuAl1.3 | BCC+FCC | 7.60 | -6.24 | 14.85 | 420.49 | 1,589.45 | 3.78 | 5.19 | [S1] |
| CoCrFeNiCuAl1.5 | BCC+FCC | 7.46 | -7.04 | 14.78 | 475.54 | 1,569.27 | 3.30 | 5.38 | [S1] |
| CoCrFeNiCuAl1.8 | BCC+FCC | 7.26 | -8.08 | 14.65 | 552.41 | 1,541.22 | 2.79 | 5.54 | [S1] |
| CoCrFeNiCuAl2 | BCC+FCC | 7.14 | -8.65 | 14.53 | 595.26 | 1,523.86 | 2.56 | 5.71 | [S1] |
| CoCrFeNiCuAl2.3 | BCC | 6.97 | -9.38 | 14.35 | 654.85 | 1,499.60 | 2.29 | 5.84 | [S1] |
| CoCrFeNiCuAl2.5 | BCC | 6.87 | -9.78 | 14.21 | 690.47 | 1,484.50 | 2.15 | 5.91 | [S1] |
| CoCrFeNiCuAl2.8 | BCC | 6.72 | -10.28 | 14.01 | 735.33 | 1,463.31 | 1.99 | 5.99 | [S1] |
| CoCrFeNiCuAl3 | BCC | 6.63 | -10.56 | 13.86 | 763.19 | 1,450.06 | 1.90 | 6.09 | [S1] |
| CoCrFeNiCuAlSi | BCC+FCC | 7.29 | -18.86 | 16.18 | 1,165.36 | 1,631.50 | 1.40 | 4.51 | [S1] |
| MnCrFeNiCuAl | BCC | 7.50 | -5.11 | 14.90 | 342.12 | 1,580.58 | 4.62 | 4.73 | [S1] |
| CoCrFeNiMnGe | BCC+FCC | 7.33 | -15.17 | 14.90 | 1,015.27 | 1,695.50 | 1.67 | 3.25 | [S1] |
| CoCrFeNiMn | FCC | 8.00 | -4.16 | 13.38 | 310.64 | 1,792.40 | 5.77 | 0.92 | [S1] |
| CoCrFeNiMnCu | FCC | 8.50 | 1.44 | 14.90 | 96.63 | 1,720.00 | 17.80 | 0.99 | [S1] |
| CoCrNiCu0.5Al | BCC | 7.44 | -10.17 | 13.15 | 773.88 | 1,609.67 | 2.08 | 5.74 | [S1] |
| TiCoCrFeNiCuAlV | BCC+FCC | 7.00 | -13.94 | 17.29 | 807.07 | 1,735.19 | 2.15 | 5.87 | [S1] |
| CoCrFeNiCu0.5 | FCC | 8.56 | 0.49 | 13.15 | 37.26 | 1,804.67 | 48.44 | 1.06 | [S1] |
| CoCrNiCuAl | BCC+FCC | 7.80 | -6.56 | 13.38 | 490.56 | 1,584.50 | 3.23 | 5.19 | [S1] |
| CoCuNiAl | BCC+FCC | 8.25 | -8.00 | 11.52 | 695.87 | 1,447.40 | 2.08 | 5.77 | [S1] |
| CuNiAl | BCC+FCC | 8.00 | -8.44 | 9.13 | 924.00 | 1,339.80 | 1.45 | 6.20 | [S1] |
| CuNi | FCC | 10.50 | 4.00 | 5.76 | 695.05 | 1,543.00 | 2.22 | 1.63 | [S1] |
| Co0.5CrFeNiCuAl | BCC+FCC | 7.73 | -4.50 | 14.70 | 305.86 | 1,608.82 | 5.26 | 4.91 | [S1] |
| CoCr0.5FeNiCuAl | BCC+FCC | 8.00 | -5.02 | 14.70 | 341.18 | 1,572.82 | 4.61 | 5.02 | [S1] |
| CoCrFe0.5NiCuAl | BCC+FCC | 7.82 | -5.55 | 14.70 | 377.67 | 1,605.09 | 4.25 | 5.00 | [S1] |
| CoCrFeNi0.5CuAl | BCC+FCC | 7.64 | -3.90 | 14.70 | 265.24 | 1,612.64 | 6.08 | 4.91 | [S1] |
| CoCrFeNiCu0.5Al | BCC | 7.55 | -7.93 | 14.70 | 539.76 | 1,646.27 | 3.05 | 5.02 | [S1] |
| Ti0.5CoCrFeNiCu | FCC | 8.36 | -3.70 | 14.70 | 252.04 | 1,776.91 | 7.05 | 4.46 | [S1] |
| Ti0.5CoCrFeNiAl | BCC1+BCC2 | 6.91 | -17.92 | 14.70 | 1,222.83 | 1,699.73 | 1.39 | 6.11 | [S1] |
| TiCoCrFeNiAl | BCC1+BCC2 | 6.67 | -21.56 | 14.90 | 1,445.59 | 1,720.25 | 1.19 | 6.58 | [S1] |
| Al11.1(TiCoCrFeNiCuVMn)88.9 | BCC+FCC | 7.43 | -12.74 | 18.27 | 698.48 | 1,711.28 | 2.45 | 5.75 | [S1] |
| Al20(TiCoCrFeNiCuVMn)80 | BCC | 7.36 | -15.44 | 17.99 | 855.24 | 1,633.50 | 1.91 | 6.01 | [S1] |
| TiCr0.5FeNiCuAl | BCC+FCC | 7.09 | -15.40 | 14.70 | 1,051.63 | 1,640.55 | 1.56 | 6.45 | [S1] |
| TiCrFeNiCuAl | BCC+FCC | 7.00 | -13.67 | 14.90 | 918.90 | 1,681.58 | 1.83 | 6.29 | [S1] |
| TiCr1.5FeNiCuAl | BCC+FCC | 6.92 | -12.26 | 14.78 | 825.15 | 1,716.31 | 2.08 | 6.14 | [S1] |
| TiCr2FeNiCuAl | BCC+FCC | 6.86 | -11.10 | 14.53 | 762.48 | 1,746.07 | 2.29 | 5.99 | [S1] |
| TiCr3FeNiCuAl | BCC+FCC | 6.75 | -9.31 | 13.86 | 672.07 | 1,794.44 | 2.67 | 5.72 | [S1] |
| TiCoCrFeNiCuAl | BCC1+BCC2+FCC | 7.29 | -13.80 | 16.18 | 855.64 | 1,668.50 | 1.95 | 6.23 | [S1] |
| CoCrFeNiCuAlV | BCC+FCC | 7.43 | -7.76 | 16.18 | 478.95 | 1,705.07 | 3.56 | 4.69 | [S1] |
| Ti0.5Co1.5CrFeNiAl | BCC+FCC | 7.08 | -17.17 | 14.54 | 1,176.26 | 1,705.58 | 1.45 | 6.02 | [S1] |
| Ti0.5Co2CrFeNiAl | BCC+FCC | 7.23 | -16.43 | 14.23 | 1,148.01 | 1,710.54 | 1.49 | 5.91 | [S1] |
| Ti0.5Co3CrFeNiAl | BCC+FCC | 7.47 | -14.93 | 13.49 | 1,108.69 | 1,718.47 | 1.55 | 5.69 | [S1] |
| Ti0.5CoCrFeNiCu0.75Al0.25 | FCC | 8.00 | -7.28 | 15.55 | 467.45 | 1,757.61 | 3.76 | 5.03 | [S1] |
| Ti0.5CoCeFeNiCu0.5Al0.5 | BCC+FCC | 7.09 | -10.84 | 15.75 | 689.81 | 1,738.32 | 2.52 | 5.25 | [S1] |
| Ti0.5CoCrFeNiCu0.25Al0.75 | BCC1+BCC2 | 7.00 | -15.26 | 15.55 | 982.30 | 1,719.02 | 1.75 | 5.83 | [S1] |
| CoCrFeNiCu0.25Al | BCC | 7.38 | -9.94 | 14.34 | 694.56 | 1,660.00 | 2.39 | 5.13 | [S1] |
| CoFeNiCuV | FCC | 8.60 | -1.78 | 14.90 | 119.46 | 1,833.67 | 15.35 | 2.63 | [S1] |
| CoCrFeNiCu0.75Al0.25 | FCC | 8.40 | -0.71 | 14.32 | 49.58 | 1,738.78 | 35.07 | 3.00 | [S1] |
| CoCrFeNiCu0.5Al0.5 | FCC | 8.00 | -4.60 | 14.54 | 316.31 | 1,717.55 | 5.43 | 4.00 | [S1] |
| CoCrFeNiCu0.25Al0.75 | BCC+FCC | 7.60 | -8.47 | 14.32 | 591.06 | 1,696.33 | 2.87 | 4.71 | [S1] |
| Ti0.5CoCrFeNiCu0.25Al | BCC1+BCC2 | 7.09 | -15.50 | 15.54 | 1,002.90 | 1,684.87 | 1.68 | 6.01 | [S1] |
| Ti0.5CoCrFeNiCu0.5Al | BCC1+BCC2 | 7.25 | -13.42 | 15.86 | 848.35 | 1,671.25 | 1.97 | 5.90 | [S1] |
| CoCrFeNi | FCC | 8.25 | -3.75 | 11.53 | 325.83 | 1,860.50 | 5.71 | 1.06 | [S1] |
| CoCrFeNiAl0.25 | FCC | 7.94 | -6.75 | 12.71 | 531.17 | 1,805.97 | 3.40 | 3.25 | [S1] |
| CoCrFeNiAl0.375 | FCC | 7.80 | -7.99 | 12.97 | 616.28 | 1,781.04 | 2.89 | 3.80 | [S1] |
| CoCrFeNiAl0.5 | BCC+FCC | 7.67 | -9.09 | 13.15 | 689.22 | 1,757.50 | 2.55 | 4.22 | [S1] |
| CoCrFeNiAl0.75 | BCC+FCC | 7.42 | -10.90 | 13.33 | 820.16 | 1,714.13 | 2.09 | 4.83 | [S1] |
| CoCrFeNiAl0.875 | BCC+FCC | 7.31 | -11.66 | 13.37 | 868.78 | 1,694.12 | 1.95 | 5.06 | [S1] |
| CoCrFeNiAl1.25 | BCC | 7.00 | -13.42 | 13.34 | 1,012.22 | 1,639.79 | 1.62 | 5.55 | [S1] |
| CoCrFeNiAl1.5 | BCC | 6.82 | -14.28 | 13.25 | 1,071.79 | 1,607.68 | 1.50 | 5.77 | [S1] |
| CoCrFeNiAl2 | BCC | 6.50 | -15.44 | 12.98 | 1,193.46 | 1,551.50 | 1.30 | 6.04 | [S1] |
| CoCrFeNiAl2.5 | BCC | 6.23 | -16.09 | 12.63 | 1,285.44 | 1,503.96 | 1.17 | 6.19 | [S1] |
| CoCrFeNiAl3 | BCC | 6.00 | -16.41 | 12.26 | 1,330.19 | 1,463.21 | 1.10 | 6.26 | [S1] |
| MnCrFe1.5Ni0.5Al0.3 | BCC | 7.19 | -5.51 | 12.31 | 448.04 | 1,747.34 | 3.90 | 3.32 | [S1] |
| MnCrFe1.5Ni0.5Al0.5 | BCC | 7.00 | -6.77 | 12.67 | 534.74 | 1,711.17 | 3.20 | 4.03 | [S1] |
| MoCrFeNiCu | FCC | 8.20 | 4.64 | 13.38 | 347.03 | 1,985.00 | 5.72 | 2.92 | [S1] |
| Ti0.5Co1.5CrFeNi1.5 | FCC | 8.09 | -10.74 | 12.86 | 832.43 | 1,848.00 | 2.22 | 4.60 | [S1] |
| Ti0.5Co1.5CrFeNi1.5Mo0.1 | FCC | 8.05 | -10.64 | 13.38 | 794.34 | 1,866.70 | 2.35 | 4.72 | [S1] |
| CoCrFeNiCuAl0.5V0.2 | FCC | 8.16 | -2.50 | 15.44 | 161.88 | 1,703.01 | 10.52 | 3.87 | [S1] |
| CoCrFeNiCuAl0.5V0.4 | BCC+FCC | 8.05 | -3.34 | 15.76 | 211.81 | 1,719.92 | 8.12 | 3.80 | [S1] |
| CoCrFeNiCuAl0.5V1.2 | BCC+FCC | 7.69 | -5.73 | 15.98 | 358.36 | 1,777.49 | 4.96 | 3.99 | [S1] |
| CoCrFeNiCuAl0.5V1.4 | BCC+FCC | 7.61 | -6.14 | 15.91 | 385.73 | 1,789.79 | 4.64 | 4.00 | [S1] |
| CoCrFeNiCuAl0.5V1.6 | BCC+FCC | 7.54 | -6.50 | 15.82 | 411.28 | 1,801.40 | 4.38 | 4.00 | [S1] |
| CoCrFeNiCuAl0.5V1.8 | BCC+FCC | 7.47 | -6.81 | 15.72 | 432.55 | 1,812.38 | 4.19 | 4.00 | [S1] |
| CoCrFeNiCuAl0.5V2 | BCC+FCC | 7.40 | -7.08 | 15.60 | 454.56 | 1,822.77 | 4.01 | 3.99 | [S1] |
| MnCrFeNiCu | BCC+FCC | 8.40 | 2.72 | 13.38 | 203.33 | 1,710.00 | 8.41 | 0.92 | [S1] |
| Mn2CrFeNi2Cu | FCC | 8.43 | 0.44 | 12.98 | 33.90 | 1,713.00 | 50.53 | 0.99 | [S1] |
| MnCr2Fe2NiCu | BCC+FCC | 8.00 | 2.61 | 12.89 | 202.37 | 1784.86 | 8.82 | 0.84 | [S1] |
| Mn2Cr2Fe2Ni2Cu | FCC | 8.11 | 0.10 | 13.14 | 7.61 | 1,749.11 | 229.83 | 0.91 | [S1] |
| Mn2CrFe2NiCu2 | BCC+FCC | 8.50 | 4.69 | 12.97 | 361.33 | 1,654.88 | 4.58 | 0.83 | [S1] |
| MnCrFe2Ni2Cu2 | FCC | 8.88 | 3.88 | 12.97 | 299.62 | 1,680.88 | 5.61 | 0.95 | [S1] |
| Mn2Cr2FeNi2Cu2 | BCC+FCC | 8.44 | 2.37 | 13.14 | 180.53 | 1,697.00 | 9.40 | 0.97 | [S1] |
| MnCr2Fe2Ni2Cu2 | BCC+FCC | 8.56 | 3.56 | 13.14 | 271.05 | 1,729.33 | 6.38 | 0.94 | [S1] |
| W27.3Nb22.7Mo25.6Ta24.4 | BCC | 5.53 | -6.49 | 11.50 | 565.41 | 3,177.60 | 5.62 | 2.27 | [S1] |
| W21.1Nb20.6Mo21.7Ta15.6V21 | BCC | 5.43 | -4.54 | 13.33 | 340.31 | 2,950.49 | 8.67 | 3.18 | [S1] |
| Ti0.3CoCrFeNi | FCC+HCP | 7.95 | -8.89 | 12.83 | 693.86 | 1,866.47 | 2.69 | 4.06 | [S1] |
| Ti0.1CoCrFeNiAl0.3 | FCC | 7.80 | -8.93 | 13.47 | 661.49 | 1,799.24 | 2.72 | 4.06 | [S1] |
| TiCoNiCuAlZn | BCC | 8.17 | -17.89 | 14.90 | 1,208.72 | 1,680.12 | 1.39 | 6.43 | [S1] |
| CoCrFeNiMo0.3 | FCC | 8.09 | -4.15 | 12.83 | 323.73 | 1,932.67 | 5.97 | 2.92 | [S1] |
| CoCrFeNiAl0.3Mo0.1 | FCC | 7.84 | -7.26 | 13.44 | 540.30 | 1,820.81 | 3.37 | 3.74 | [S1] |
| CoCrFeNiCuAlMo0.2 | BCC+FCC | 7.77 | -4.47 | 15.60 | 286.55 | 1,633.31 | 5.70 | 4.95 | [S1] |
| AlCoCrFeNiNb0.1 | BCC | 7.16 | -13.32 | 13.92 | 956.69 | 1,696.18 | 1.77 | 5.50 | [S2] |
| Al1.5CoCrFeNiTi | BCC | 6.38 | -20.73 | 14.78 | 1,402.42 | 1,659.73 | 1.18 | 6.64 | [S3] |
| Al2CoCrFeNiTi | BCC | 6.14 | -21.63 | 14.53 | 1,488.64 | 1,607.86 | 1.08 | 6.64 | [S3] |
| Al0.2Co1.5CrFeNi1.5Ti0.5 | FCC | 7.91 | -12.50 | 13.67 | 914.06 | 1,815.91 | 1.98 | 5.00 | [S4] |
| FeCoCrNiPd | FCC | 8.60 | -5.60 | 13.38 | 418.50 | 1,853.80 | 4.43 | 3.76 | [S5] |
| FeCoCrNiPd2 | FCC | 8.83 | -6.11 | 12.98 | 470.96 | 1,849.33 | 3.92 | 4.33 | [S5] |
| TaNbHfZrTi | BCC | 4.40 | 2.72 | 13.38 | 203.28 | 2,524.20 | 12.42 | 4.01 | [S6] |
| AlCoCrFeNiSi0.2 | BCC | 7.08 | -16.39 | 14.22 | 1,152.51 | 1,675.56 | 1.45 | 5.15 | [S7] |
| AlCoCrFeNiSi0.4 | BCC | 6.96 | -19.84 | 14.70 | 1,349.60 | 1,675.98 | 1.24 | 5.07 | [S7] |
| AlCoCrFeNiSi0.6 | BCC | 6.86 | -22.76 | 14.78 | 1,539.78 | 1,676.38 | 1.09 | 4.98 | [S7] |
| AlCoCrFeNiMo0.1 | BCC | 7.18 | -12.13 | 13.92 | 871.63 | 1,699.02 | 1.95 | 5.30 | [S8] |
| Ti0.8CoCrFeNiCu | FCC+Laves phase | 8.14 | -6.75 | 14.89 | 452.07 | 1,785.66 | 3.95 | 5.26 | [S1] |
| TiCoCrFeNiCu | FCC+Laves phase | 8.00 | -8.44 | 14.90 | 564.98 | 1,791.00 | 3.17 | 5.65 | [S1] |
| Ti1.5CoCrFeNiAl | BCC1+BCC2+Laves phase | 6.46 | -23.91 | 14.78 | 1,608.91 | 1,737.62 | 1.08 | 6.93 | [S1] |
| CoCrFeNiCuAlMn | BCC+FCC+unknown phase | 7.71 | -5.63 | 16.18 | 348.73 | 1,607.64 | 4.61 | 4.57 | [S1] |
| CrFeNiCuZr | BCC+compounds | 7.80 | -14.40 | 13.38 | 1,077.41 | 1,831.60 | 1.70 | 9.91 | [S1] |
| Ti0.5Co1.5CrFeNi1.5Mo0.5 | FCC+σ phase | 7.92 | -10.25 | 14.17 | 724.81 | 1,935.25 | 2.67 | 5.09 | [S1] |
| Ti0.5Co1.5CrFeNi1.5Mo0.8 | FCC+σ phase | 7.83 | -9.96 | 14.21 | 699.98 | 1,980.95 | 2.83 | 5.28 | [S1] |
| TiCoCrNiCuAl | BCC+Cu+Cr | 7.17 | -16.67 | 14.58 | 1,150.17 | 1,644.75 | 1.43 | 6.50 | [S1] |
| CoCrFeNiCuAl0.5V0.6 | BCC+FCC+σ phase | 7.95 | -4.07 | 15.92 | 255.63 | 1,735.73 | 6.79 | 3.94 | [S1] |
| CoCrFeNiCuAl0.5V0.8 | BCC+FCC+σ phase | 7.86 | -4.71 | 16.00 | 294.21 | 1,750.53 | 5.95 | 3.97 | [S1] |
| CoCrFeNiCuAl0.5V | BCC+FCC+σ phase | 7.77 | -5.25 | 16.01 | 327.96 | 1,764.42 | 5.38 | 3.98 | [S1] |
| CoCrFeNiCuAl0.5B0.2 | FCC+boride | 8.09 | -4.00 | 15.44 | 258.90 | 1,708.73 | 6.60 | 5.77 | [S1] |
| CoCrFeNiCuAl0.5B0.6 | FCC+boride | 7.75 | -8.01 | 15.92 | 503.38 | 1,751.76 | 3.48 | 8.07 | [S1] |
| CoCrFeNiCuAl0.5B | FCC+ordered FCC+boride | 7.46 | -11.03 | 16.01 | 688.27 | 1,789.50 | 2.60 | 9.52 | [S1] |
| TiCoCrFeNiCuVMn | FCC+BCC+σ phase +unknown phase | 7.50 | -8.13 | 17.29 | 469.74 | 1,808.50 | 3.85 | 5.19 | [S1] |
| Al40(TiCoCrFeNiCuVMn)60 | BCC+Al3Ti+unknown phase | 5.70 | -18.29 | 15.97 | 1,148.43 | 1,458.50 | 1.27 | 6.09 | [S1] |
| CoCrFeNiCuAlMn | BCC+FCC+unknown phase | 7.71 | -5.63 | 16.18 | 348.73 | 1,607.64 | 4.61 | 4.57 | [S1] |
| CoCrFe0.6NiAlMo0.5 | BCC+σ phase | 7.02 | -12.32 | 14.61 | 841.53 | 1,784.04 | 2.12 | 5.61 | [S1] |
| CoCrFeNiAlMo0.5 | BCC+σ phase | 7.09 | -11.44 | 14.70 | 779.91 | 1,786.00 | 2.29 | 5.47 | [S1] |
| CoCrFe1.5NiAlMo0.5 | BCC+σ phase | 7.17 | -10.50 | 14.53 | 723.92 | 1,788.08 | 2.47 | 5.30 | [S1] |
| CoCrFe2NiAlMo0.5 | BCC+σ phase | 7.23 | -9.70 | 14.23 | 680.55 | 1,789.85 | 2.63 | 5.15 | [S1] |
| Co0.5CrFeNiAlMo0.5 | BCC+σ phase | 6.90 | -11.72 | 14.53 | 805.23 | 1,787.60 | 2.22 | 5.54 | [S1] |
| Co1.5CrFeNiAlMo0.5 | BCC+σ phase | 7.25 | -11.08 | 14.53 | 762.68 | 1,784.67 | 2.34 | 5.39 | [S1] |
| Co2CrFeNiAlMo0.5 | BCC+FCC+σphase | 7.38 | -10.70 | 14.23 | 752.55 | 1,783.54 | 2.37 | 5.29 | [S1] |
| TiCoCrNiCuAl | BCC+Cu+Cr | 7.17 | -16.67 | 14.90 | 1,125.19 | 1,946.58 | 1.73 | 6.50 | [S1] |
| CoCrNiCuAlAu | FCC+AuCu | 8.33 | -6.45 | 14.90 | 432.33 | 1,543.42 | 3.57 | 6.14 | [S1] |
| CoCrFeNiCuAlMo0.4 | BCC+α phase | 7.72 | -4.20 | 15.91 | 263.84 | 1,701.80 | 6.45 | 5.05 | [S1] |
| CoCrFeNiCuAlMo0.6 | BCC+α phase | 7.67 | -3.95 | 16.08 | 245.82 | 1,737.95 | 7.07 | 5.13 | [S1] |
| CoCrFeNiCuAlMo0.8 | BCC+α phase | 7.62 | -3.72 | 16.16 | 230.43 | 1,771.99 | 7.69 | 5.20 | [S1] |
| CoCrFeNiCuAlMo | BCC+α phase | 7.57 | -3.51 | 16.18 | 216.84 | 1,804.07 | 8.32 | 5.25 | [S1] |
| AlCoCrFeNiNb0.25 | BCC+Laves | 7.10 | -14.66 | 14.34 | 1,022.48 | 1,726.29 | 1.69 | 5.83 | [S2] |
| AlCoCrFeNiNb0.5 | BCC+Laves | 7.00 | -16.53 | 14.70 | 1,127.12 | 1,772.82 | 1.58 | 6.24 | [S2] |
| AlCoCrFeNiNb0.75 | BCC+Laves | 6.91 | -18.03 | 14.85 | 1,213.51 | 1,815.30 | 1.50 | 6.55 | [S2] |
| CoCrFeNiTi | FCC+BCC+CoTi2 | 7.40 | -16.32 | 13.38 | 1,219.65 | 1,877.60 | 1.54 | 6.13 | [S3] |
| Al0.5CoCrFeNiTi | FCC+BCC+CoTi2+FeTi | 7.00 | -16.79 | 14.70 | 1,142.63 | 1,791.77 | 1.57 | 6.44 | [S3] |
| AlCoCrFeNiTi | FCC+BCC+CoTi2+FeTi | 6.67 | -19.22 | 14.90 | 1,290.37 | 1,720.25 | 1.33 | 6.58 | [S3] |
| AlCoFeMo0.5Ni | BCC+σ | 7.33 | -12.74 | 13.15 | 969.23 | 1,708.89 | 1.76 | 5.93 | [S9] |
| AlCoCr0.5FeMo0.5Ni | BCC+σ | 7.20 | -12.08 | 14.53 | 831.19 | 1,750.06 | 2.11 | 5.69 | [S9] |
| AlCoCrFeMo0.5Ni | BCC+σ | 7.09 | -11.44 | 14.70 | 778.25 | 1,786.00 | 2.29 | 5.47 | [S9] |
| AlCoCr1.5FeMo0.5Ni | BCC+σ | 7.00 | -10.83 | 14.53 | 745.37 | 1,814.92 | 2.43 | 5.27 | [S9] |
| AlCoCr2FeMo0.5Ni | BCC+σ | 6.92 | -10.27 | 14.23 | 721.75 | 1,839.38 | 2.55 | 5.10 | [S9] |
| Co1.5CrFeNi1.5Ti | FCC+η | 7.75 | -15.61 | 13.21 | 1,181.66 | 1,856.17 | 1.57 | 5.83 | [S4] |
| Al0.2Co1.5CrFeNi1.5Ti | FCC+η | 7.60 | -17.12 | 13.97 | 1,225.33 | 1,826.40 | 1.49 | 6.01 | [S4] |
| AlTiFeCrNiCu | BCC1+BCC2+Fe2Ti | 7.00 | -13.67 | 14.90 | 917.43 | 1,651.58 | 1.80 | 6.29 | [S10] |
| AlCoCrFeNiSi0.8 | BCC+δ phase | 6.76 | -25.23 | 14.87 | 1,696.75 | 1,676.74 | 0.99 | 4.90 | [S7] |
| AlCoCrFeNiSi | BCC+δ phase | 6.67 | -27.33 | 14.90 | 1,834.86 | 1,677.08 | 0.91 | 4.82 | [S7] |
| AlCoCrFeNiMo0.2 | BCC+α phase | 7.15 | -11.95 | 14.22 | 840.46 | 1,722.02 | 2.05 | 5.35 | [S8] |
| AlCoCrFeNiMo0.3 | BCC+α phase | 7.13 | -11.78 | 14.43 | 816.00 | 1,744.15 | 2.14 | 5.40 | [S8] |
| AlCoCrFeNiMo0.4 | BCC+α phase | 7.11 | -11.60 | 14.59 | 795.68 | 1,765.46 | 2.22 | 5.44 | [S8] |
| AlCoCrFeNiMo0.5 | BCC+α phase | 7.09 | -11.44 | 14.70 | 778.25 | 1,786.00 | 2.29 | 5.47 | [S8] |
| Ti2CoCrFeNiCu | compounds | 7.43 | -14.04 | 14.53 | 969.59 | 1,813.14 | 1.87 | 6.69 | [S1] |
| AlCrMoSiTi | ordered BCC+Mo5Si3 | 4.60 | -34.08 | 13.38 | 2,558.53 | 1,918.90 | 0.75 | 4.91 | [S1] |
| AlTiVYZr | conpounds | 3.80 | -14.88 | 13.38 | 1,112.41 | 1,802.10 | 1.62 | 10.35 | [S1] |
| ZrTiVCuNiBe | compounds | 6.00 | -24.89 | 14.90 | 1,670.34 | 1,820.67 | 1.09 | 11.09 | [S1] |
| ZrHfTiCuFe | compounds | 6.20 | -15.84 | 13.38 | 1,188.66 | 1,949.40 | 1.64 | 9.84 | [S1] |
| ZrHfTiCuCo | compounds | 6.40 | -23.52 | 13.38 | 1,748.83 | 1,941.20 | 1.11 | 10.21 | [S1] |
| TiCoCrNiCuAlY0.5 | Cu2Y+AlNi2Ti+Cu+Cr | 6.85 | -18.32 | 16.00 | 1,152.01 | 1,935.38 | 1.68 | 7.53 | [S1] |
| TiCoCrNiCuAlY0.8 | Cu2Y+AlNi2Ti+Cu+Cr | 6.68 | -19.00 | 16.16 | 1,176.49 | 1,929.45 | 1.64 | 12.73 | [S1] |
| TiCoCrNiCuAlY | Cu2Y+AlNi2Ti+Cu +Cr+unknown phase | 6.57 | -19.37 | 16.18 | 1,188.76 | 1,925.79 | 1.62 | 13.45 | [S1] |
| Zr57Ti5Al10Cu20Ni8 | 20 (Zc) | 5.78 | -31.50 | 10.18 | 3,073.64 | 1,813.45 | 0.59 | 9.69 | [S1] |
| Zr38.5Ti16.5Cu15.25Ni9.75Be20 | 1.4 (Rc) | 5.25 | -33.20 | 12.47 | 2,649.78 | 1,828.35 | 0.69 | 13.36 | [S1] |
| Zr39.88Ti15.12Cu13.77Ni9.98Be21.25 | 1.4 (Rc) | 5.14 | -34.27 | 12.34 | 2,779.18 | 1,834.26 | 0.66 | 13.59 | [S1] |
| Zr42.63Ti12.37Cu11.25Ni10Be23.75 | 5 (Rc) | 4.91 | -36.90 | 11.97 | 3,074.07 | 1,844.44 | 0.60 | 14.05 | [S1] |
| Zr41.2Ti13.8Cu12.5Ni10Be22.5 | 50 (Zc) | 5.03 | -36.72 | 12.18 | 3,015.21 | 1,839.28 | 0.61 | 13.82 | [S1] |
| Zr44Ti11Cu10Ni10Be25 | 12.5 (Rc) | 4.80 | -37.07 | 11.73 | 3,134.71 | 1,849.48 | 0.59 | 14.27 | [S1] |
| Zr45.38Ti9.62Cu8.75Ni10Be26.25 | 17.5 (Rc) | 4.69 | -37.23 | 11.46 | 3,237.00 | 1,845.09 | 0.57 | 14.49 | [S1] |
| Zr46.75Ti8.25Cu7.5Ni10Be27.5 | 28 (Rc) | 4.58 | -37.03 | 11.16 | 3,301.70 | 1,848.95 | 0.56 | 14.70 | [S1] |
| La55Al25Ni5Cu10Co5 | >9 (Zc) | 4.45 | -32.31 | 10.02 | 3,245.35 | 1,200.78 | 0.37 | 16.19 | [S1] |
| Nd60Al15Ni10Cu10Fe5 | 4~6 (Zc) | 5.95 | -27.37 | 9.99 | 2,735.79 | 1,313.18 | 0.48 | 17.11 | [S1] |
| Nd61Al11Ni8Co5Cu15 | 6 (Zc) | 6.28 | -27.43 | 9.82 | 2,781.13 | 1,307.13 | 0.47 | 17.46 | [S1] |
| Cu47Ti33Zr11Si1Ni8 | 4 (Zc) | 7.77 | -17.56 | 10.07 | 1,739.20 | 1,669.63 | 0.96 | 8.46 | [S1] |
| Cu47Ti33Zr11Si1Ni6Sn2 | 6 (Zc) | 7.65 | -17.02 | 10.45 | 1,628.88 | 1,645.17 | 1.01 | 8.36 | [S1] |
| Fe61B15Mo7Zr8Co7Y2 | >5 (Zc) | 6.76 | -30.13 | 10.30 | 2,929.81 | 1,992.27 | 0.68 | 13.20 | [S1] |
| Fe61B15Mo7Zr8Co6Y2Al1 | >5 (Zc) | 6.70 | -30.30 | 10.54 | 2,875.23 | 1,983.91 | 0.69 | 13.24 | [S1] |
| Fe61B15Mo7Zr8Co5Y2Cr2 | >5 (Zc) | 6.70 | -29.97 | 10.65 | 2,816.24 | 1,999.53 | 0.71 | 13.20 | [S1] |
| Au49Ag5.5Pd2.3Cu26.9Si16.3 | >5 (Zc) | 9.84 | -29.39 | 10.35 | 2,811.51 | 1,377.64 | 0.49 | 5.30 | [S1] |
| Dy46Al24Co18Fe2Y10 | 5 (Zc) | 4.18 | -33.26 | 10.95 | 3,067.20 | 1,533.60 | 0.50 | 13.71 | [S1] |
| Ti40Zr25Ni3Cu12Be20 | 3.2 (Rc) | 4.62 | -25.88 | 11.60 | 2,233.78 | 2,010.40 | 0.90 | 12.03 | [S1] |
| Ti40Zr25Cu9Ni8Be18 | 8 (Zc) | 4.75 | -28.26 | 11.98 | 2,344.33 | 1,852.02 | 0.79 | 12.31 | [S1] |
| Ti45Cu25Ni15Sn3Be7Zr5 | 5 (Zc) | 6.51 | -21.22 | 11.90 | 1,776.34 | 1,705.29 | 0.96 | 9.08 | [S1] |
| Ti50Ni24Cu20B1Si2Sn3 | 1 (Zc) | 6.83 | -27.87 | 10.31 | 2,706.03 | 1,731.86 | 0.64 | 7.89 | [S1] |
| Ti50Zr15Cu9Ni8Be18 | 6 (Zc) | 4.75 | -26.37 | 11.30 | 2,321.29 | 1,833.82 | 0.79 | 11.64 | [S1] |
| Ti55Zr10Cu9Ni8Be18 | 6 (Zc) | 4.75 | -25.43 | 10.70 | 2,369.77 | 1,824.72 | 0.77 | 11.18 | [S1] |
| Ti53Cu15Ni18.5Al7Hf3Si3B0.5 | 2 (Zc) | 6.09 | -32.23 | 11.28 | 2,834.94 | 1,757.66 | 0.62 | 7.28 | [S1] |
| Ti53Cu15Ni18.5Al7Sc3Si3B0.5 | 2 (Zc) | 6.06 | -31.75 | 11.28 | 2,828.93 | 1,697.36 | 0.60 | 7.54 | [S1] |
| Ti53Cu15Ni18.5Al7Ta3Si3B0.5 | <1.5 (Zc) | 6.12 | -31.28 | 11.28 | 2,783.33 | 1,781.33 | 0.64 | 6.96 | [S1] |
| Ti53Cu15Ni18.5Al7Nb3Si3B0.5 | <1.5 (Zc) | 6.12 | -31.22 | 11.28 | 2,757.88 | 1,765.04 | 0.64 | 6.96 | [S1] |
| ZrHfTiCuNi | 1.5 (Zc) | 6.60 | -27.36 | 13.38 | 2,034.53 | 1,932.80 | 0.95 | 10.21 | [S1] |
| Mg65Cu20Zn5Y10 | 6 (Zc) | 4.40 | -5.98 | 8.16 | 733.54 | 1,085.64 | 1.48 | 12.70 | [S1] |
| Mg65Cu15Ag5Pd5Y10 | 7 (Zc) | 4.30 | -13.24 | 9.10 | 1,452.51 | 1,074.86 | 0.74 | 9.27 | [S1] |
| Mg65Cu15Ag5Pd5Gd10 | 10 (Zc) | 4.30 | -13.24 | 9.10 | 1,463.18 | 1,053.49 | 0.72 | 9.27 | [S1] |
| Mg65Cu7.5Ni7.5Zn5Ag5Y10 | >4 (Zc) | 4.33 | -7.35 | 9.96 | 738.16 | 1,107.24 | 1.50 | 9.53 | [S1] |
| Sr20Ca20Yb20(Li0.55Mg0.45)20Zn20 | ≥3 (Zc) | 4.09 | -12.15 | 14.53 | 836.62 | 922.03 | 1.10 | 15.49 | [S11] |
| Sr20Ca20Yb20Mg20Zn10Cu10 | ﹤5 (Zc) | 3.70 | -10.60 | 14.53 | 729.35 | 1,040.07 | 1.43 | 16.35 | [S11] |
| Sr20Ca20Yb20Mg20Zn20 | 2 (Zc) | 4.20 | -13.12 | 13.38 | 980.50 | 973.54 | 0.99 | 15.25 | [S11] |
| Er20Tb20Dy20Ni20Al20 | 2 (Zc) | 4.40 | -37.60 | 13.38 | 2,809.98 | 1,554.90 | 0.55 | 13.66 | [S11] |
| Ce60Al15Ni15Cu10 | 3 (Zc) | 4.85 | -30.60 | 9.19 | 3,328.12 | 1,178.23 | 0.35 | 15.29 | [S12] |
| Ce65Al10Ni10Cu10Nb5 | 5 (Zc) | 4.60 | -19.86 | 9.32 | 2,131.72 | 1,236.25 | 0.58 | 14.18 | [S12] |
| Ce57Al10Ni12.5Cu15.5Nb5 | 2 (Zc) | 5.22 | -22.06 | 10.39 | 2,123.63 | 1,268.38 | 0.60 | 15.53 | [S12] |
| Ni45Ti20Zr25Al10 | 2 (Zc) | 6.60 | -45.41 | 10.46 | 4,341.54 | 1,792.15 | 0.41 | 10.35 | [S13] |
| Ni40Cu6Ti16Zr28Al10 | 3 (Zc) | 6.72 | -42.79 | 11.77 | 3,636.80 | 1,773.23 | 0.49 | 10.52 | [S13] |
| Ni40Cu5Ti17Zr28Al10 | 4 (Zc) | 6.65 | -43.25 | 11.67 | 3,704.93 | 1,779.11 | 0.48 | 10.48 | [S13] |
| Ni40Cu5Ti16.5Zr28.5Al10 | 5 (Zc) | 6.65 | -43.41 | 11.65 | 3,725.05 | 1,780.02 | 0.48 | 12.07 | [S13] |
| Ni39.8Cu5.97Ti15.92Zr27.86Al9.95Si0.5 | 5 (Zc) | 6.71 | -43.58 | 11.97 | 3,640.71 | 1,772.80 | 0.49 | 10.50 | [S13] |
| La62Al14Cu20Ag4 | 8 (Zc) | 4.92 | -26.72 | 8.50 | 3,144.19 | 1,191.97 | 0.38 | 15.49 | [S14] |
| La62Al14(Cu5/6Ag1/6)20Ni2Co2 | 16-20 (Zc) | 4.86 | -26.89 | 9.48 | 2,837.31 | 1,208.43 | 0.43 | 15.70 | [S14] |
| La62Al14(Cu5/6Ag1/6)14Ni5Co5 | >20 (Zc) | 4.77 | -27.31 | 10.06 | 2,716.09 | 1,233.12 | 0.45 | 16.02 | [S14] |
| La64Al14(Cu5/6Ag1/6)12Ni5Co5 | 26 (Zc) | 4.61 | -27.06 | 9.72 | 2,784.33 | 1,230.25 | 0.44 | 15.68 | [S15] |
| La65Al14(Cu5/6Ag1/6)11Ni5Co5 | 30 (Zc) | 4.53 | -26.86 | 9.54 | 2,816.67 | 1,228.82 | 0.44 | 15.51 | [S15] |
| La66Al14(Cu5/6Ag1/6)10Ni5Co5 | 26 (Zc) | 4.45 | -26.73 | 9.35 | 2,859.79 | 1,227.38 | 0.43 | 15.32 | [S15] |
| La68Al14(Cu5/6Ag1/6)8Ni5Co5 | <16 (Zc) | 4.29 | -26.33 | 8.94 | 2,946.00 | 1,224.51 | 0.42 | 14.93 | [S15] |
| Co64.8Fe7.2B19.2Si4.8Nb4 | 2 (Zc) | 7.38 | -24.16 | 8.83 | 2,736.59 | 1,922.41 | 0.70 | 10.02 | [S16] |
| Co57.6Fe14.4B19.2Si4.8Nb4 | 2.5 (Zc) | 7.30 | -24.27 | 9.88 | 2,457.05 | 1,925.36 | 0.78 | 10.05 | [S16] |
| Co50.4Fe21.6B19.2Si4.8Nb4 | 3.5 (Zc) | 7.23 | -24.34 | 10.54 | 2,309.46 | 1,928.31 | 0.83 | 10.08 | [S16] |
| Co43.2Fe28.8B19.2Si4.8Nb4 | 4 (Zc) | 7.16 | -24.37 | 10.91 | 2,233.40 | 1,931.26 | 0.86 | 10.12 | [S16] |
| Co45.5Fe2.5Cr15Mo14C15B6Er2 | 12 (Zc) | 6.88 | -33.41 | 12.82 | 2,606.38 | 2,327.43 | 0.89 | 13.79 | [S17] |
| Co43Fe5Cr15Mo14C15B6Er2 | 15 (Zc) | 6.85 | -33.46 | 13.34 | 2,508.89 | 2,369.44 | 0.94 | 13.80 | [S17] |
| Pr60Al10Ni10Cu20 | 5 (Zc) | 5.30 | -27.52 | 9.05 | 3,039.84 | 1,260.75 | 0.41 | 15.94 | [S18] |
| Nd60Al10Ni10Cu20 | 5 (Zc) | 5.30 | -27.48 | 9.05 | 3,035.42 | 1,311.75 | 0.43 | 15.70 | [S18] |
| Gd36Y20Al24Co20 | 3 (Zc) | 4.20 | -34.26 | 11.26 | 3,043.58 | 1,509.56 | 0.50 | 14.49 | [S18] |
| La32Ce32Al16Ni5Cu15 | 10 (Zc) | 4.55 | -23.80 | 12.11 | 1,964.75 | 1,209.06 | 0.62 | 15.72 | [S19] |
| La32Ce32Al16Ni5Cu12Co3 | 10 (Zc) | 4.49 | -27.96 | 12.74 | 2,195.61 | 1,221.42 | 0.56 | 15.05 | [S19] |
| La32Ce32Al16Ni5Cu10Co5 | 12 (Zc) | 4.45 | -25.71 | 12.11 | 2,122.94 | 1,229.66 | 0.62 | 15.11 | [S19] |
| La32Ce32Al16Ni5Cu3Co12 | <10 (Zc) | 4.31 | -27.92 | 12.74 | 2,191.94 | 1,258.50 | 0.57 | 15.33 | [S19] |
| (CeLaPrPd)65Co25Al10 | 15 (Zc) | 5.64 | -47.60 | 14.62 | 3,256.49 | 1,396.78 | 0.43 | 16.78 | [S20] |

# II．Supplementary References

- X. Yang and Y. Zhang: Prediction of high-entropy stabilized solid-solution in multi-component alloys. Mater. Chem. Phys. 132, 233 (2012).

- S.G. Ma and Y. Zhang: Effect of Nb addition on the microstructure and properties of AlCoCrFeNi high-entropy alloy. Mater. Sci. Eng. A 532, 480 (2012).

- K.B. Zhang and Z.Y. Fu: Effects of annealing treatment on phase composition and microstructure of CoCrFeNiTiAlx high-entropy alloys. Intermetallics 22, 24 (2012).

- M-H. Chuang, M-H. Tsai, W-R. Wang, S-J. Lin, and J-W. Yeh: Microstructure and wear behavior of AlxCo1.5CrFeNi1.5Tiy high-entropy alloys. Acta Mater. 59, 6308 (2011).

- M.S. Lucas, L. Mauger, J.A. Muñoz, Y.M. Xiao, A.O. Sheets, S.L. Semiatin, J. Horwath, and Z. Turgut: Magnetic and vibrational properties of high-entropy alloys. J. Appl. Phys. 109, 07E307 (2011).

- O.N. Senkov, J.M. Scott, S.V. Senkova, D.B. Miracle, and C.F. Woodward: Microstructure and room temperature properties of a high-entropy TaNbHfZrTi alloy. J. Alloys Compd. 509, 6043 (2011).

- J.M. Zhu, H.M. Fu, H.F. Zhang, A.M. Wang, H. Li, and Z.Q. Hu: Synthesis and properties of multiprincipal component AlCoCrFeNiSix alloys. Mater. Sci. Eng. A 527, 7210 (2010).

- J.M. Zhu, H.M. Fu, H.F. Zhang, A.M. Wang, H. Li, and Z.Q. Hu: Microstructures and compressive properties of multicomponent AlCoCrFeNiMox alloys. Mater. Sci. Eng. A 527, 6975 (2010).

- C-Y. Hsu, C-C. Juan, W-R. Wang, T-S. Sheu, J-W. Yeh, and S-K. Chen: On the superior hot hardness and softening resistance of AlCoCrxFeMo0.5Ni high-entropy alloys. Mater. Sci. Eng. A 528, 3581 (2011).

- J.H. Pi, Y. Pan, L. Zhang, and H. Zhang: Microstructure and property of AlTiCrFeNiCu high-entropy alloy. J. Alloys Compd. 509, 5641 (2011).

- X.Q. Gao, K. Zhao, H.B. Ke, D.W. Ding, W.H. Wang, and H.Y. Bai: High mixing entropy bulk metallic glasses. J. Non-Cryst. Solids 357, 3557 (2011).

- B. Zhang, R.J. Wang, D.Q. Zhao, M.X. Pan, and W.H. Wang: Properties of Ce-based bulk metallic glass-forming alloys. Phys. Rev. B 70, 224208 (2004).

- D.H. Xu, G. Duan, W.L. Johnson, and C. Garland: Formation and properties of new Ni-based amorphous alloys with critical casting thickness up to 5 mm. Acta Mater. 52, 3493 (2004).

- Q.K. Jiang, G.Q. Zhang, L.Y. Chen, Q.S. Zeng, and J.Z. Jiang: Glass formability, thermal stability and mechanical properties of La-based bulk metallic glasses. J. Alloys. Compd. 424, 183 (2006).

- Q.K. Jiang, G.Q. Zhang, L. Yang, X.D. Wang, K. Saksl, H. Franz, R. Wunderlich, H. Fecht, and J.Z. Jiang: La-based bulk metallic glasses with critical diameter up to 30 mm. Acta Mater. 55, 4409 (2007).

- C.T. Chang, B.L. Shen, and A. Inoue: Co-Fe-B-Si-Nb bulk glassy alloys with superhigh strength and extremely low magnetostriction. Appl. Phys. Lett. 88, 011901 (2006).

- T. Zhang, Q. Yang, Y.F. Ji, R. Li, S.J. Pan, J.F. Wang, and T. Xu: Centimeter-scale-diameter Co-based bulk metallic glasses with fracture strength exceeding 5000 MPa. Chinese Sci. Bull. 56, 3972 (2011).

- S. Li, X.K. Xi, Y.X. Wei, Q. Luo, Y.T. Wang, M.B. Tang, B. Zhang, Z.F. Zhao, R.J. Wang, M.X. Pan, D.Q. Zhao, and W.H. Wang: Formation and properties of new heavy rare-earth-based bulk metallic glasses. Sci. Technol. Adv. Mater. 6, 823 (2005).

- Q.K. Jiang, G.Q. Zhang, L.Y. Chen, Q.S. Zeng, and J.Z. Jiang: Centimeter-sized (La0.5Ce0.5)-based bulk metallic glasses. J. Alloys. Compd. 424, 179 (2006).

- R. Li, S.J. Pang, H. Men, C.L. Ma, and T. Zhang: Formation and mechanical properties of (Ce-La-Pr-Nd)-Co-Al bulk glassy alloys with superior glass-forming ability. Scripta Mater. 54, 1123 (2006).

- A.L. Greer: Metallic glasses. Science 267, 1947 (1995).

- G. Kumar, H.X. Tang, and J. Schroers: Nanomoulding with amorphous metals. Nature 457, 868 (2009).