Supplementary Material

TABLE SI: List of experimental parameters during tension-tension fatigue testing of three Cu-Si nanowires. The "in situ" cycles were performed slowly with strain-data recording by DIC, while the other cycles were performed fast without direct recording of strain data.

| Specimen | Diameter (nm) | Minimum stress (GPa) | Maximum stress (GPa) | Number of cycles (-) | Frequency (Hz) | Failure after cycle (-) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 130 ± 10 | 0.7 ± 0.1 | 1.4 ± 0.2 | 1 | 0.01 (in situ) |  |
|  |  |  |  | 2 - 2718 | ~ 0.08 | 2718 |
| 2 | 170 ± 10 | 0.2 ± 0.0 | 0.7 ± 0.1 | 1 | 0.002 (in situ) |  |
|  |  |  |  | 2 - 2499 | ~ 0.24 |  |
|  |  |  |  | 2500 | 0.003 (in situ) |  |
|  |  |  |  | 2501 - 4999 | ~ 0.23 |  |
|  |  |  |  | 5000 | 0.002 (in situ) |  |
|  |  |  |  | 5001 - 17493 | ~ 0.22 | 17493 |
| 3 | 140 ± 10 | 0.3 ± 0.0 | 1.0 ± 0.1 | 1 | 0.002 (in situ) |  |
|  |  |  |  | 2 - 500 | ~ 0.14 |  |
|  |  |  |  | 501 | 0.001 (in situ) |  |
|  |  |  |  | 502 - 8149 | ~ 0.14 |  |
|  |  |  |  | 8150 | 0.001 (in situ) |  |
|  |  |  |  | 8151 - 9999 | ~ 0.12 |  |
|  |  |  |  | 10000 | 0.002 (in situ) |  |
|  |  |  |  | 10001 - 10854 | ~ 0.11 |  |
|  |  |  |  | 10855 - 18301 | ~ 0.25 |  |
|  |  |  |  | 18302 | tensile test (in situ) | Intentionally fractured after cycle 18302 |