Supplementary Information

FIG. S3. SEM images of NiO.

FIG. S4.  External surfaces of NiO TEM images (a), (b) and (c) shows that of hollow cylinder; (d), (e) and (f) shows that of helices

# Text boxes

| Spectrum processing Peaks possibly omitted : 1.742, 2.045 keV |
| --- |
| Element | Weight% | Atomic% |
| C K | 16.23 | 29.97 |
| O K | 38.07 | 52.77 |
| Ni K | 45.70 | 17.26 |

FIG. S1. EDAX of Nickel precipitate.

FIG. S2. EDAX of NiO.

| Element | Weight% | Atomic% |
| --- | --- | --- |
| C K | 1.66 | 5.30 |
| O K | 17.52 | 42.07 |
| P K | 1.37 | 1.70 |
| S K | 0.50 | 0.60 |
| Ni K | 76.09 | 49.78 |
| Pt M | 2.86 | 0.56 |