Supporting Information for

Preparation of Mn-doped ZrO2/TiO2 photocatalysts for efficient degradation of Rhodamine B

Hua Chen,a Guohua Jiang, a,b,c,* Tengteng Jiang,a Lei Li, a Yongkun Liu, a Qin Huang, a Wenxing Chen a,b,c

a Department of Materials Engineering, Zhejiang Sci-Tech University, Hangzhou 310018, P. R. China.

b National Engineering Laboratory for Textile Fiber Materials and Processing Technology (Zhejiang), Hangzhou 310018, P. R. China.

c Key Laboratory of Advanced Textile Materials and Manufacturing Technology (ATMT), Ministry of Education, Hangzhou 310018, P. R. China.

Fig. S1 TEM image (A), SAED pattern (B), HR-TEM images (C-E) of ZrO2-TiO2.

Fig. S2 Nitrogen desorption isotherm, corresponding pore-size distribution, and UV/Vis diffuse reflectance spectra of the (0%, 0.5%, 1%,1.5%) Mn-doped ZrO2–TiO2 samples.

Table S1. speciﬁc surface area,	Mean pore diameter,	total pore volume of the (0%, 0.5%, 1%,1.5%) Mn-doped ZrO2–TiO2 samples

| sample | speciﬁc surface area (m2/g) | Mean pore diameter (nm) | total pore volume (ml/g) |
| --- | --- | --- | --- |
| 0 | 141.717 | 7.310 | 0.259 |
| 0.5 | 160.509 | 6.601 | 0.265 |
| 1 | 157.495 | 6.893 | 0.263 |
| 1.5 | 150.001 | 7.001 | 0.262 |

Table S2. the composition of the 0.5% Mn-doped ZrO2/TiO2 nanocomposite from XPS analysis.

| Name | Atomic % |
| --- | --- |
| Mn2p | 0.41 |
| O1s | 41.84 |
| Zr3d | 10.72 |
| Ti2p | 6.72 |
| C1s | 40.31 |

Table S3. the composition of the nondoped ZrO2/TiO2 nanocomposite from XPS analysis

| Name | Atomic % |
| --- | --- |
| O1s | 43.41 |
| Zr3d | 9.96 |
| Ti2p | 7.63 |
| C1s | 39.01 |

Fig. S3 STEM mode image (A), EDS (B) and Elemental mapping (C−E) ZrO2-TiO2 nanocomposite

# Footnotes

* Corresponding author. Tel: +86 571 86843527; E-mail address: ghjiang_cn@zstu.edu.cn (G. Jiang)