Supplementary Information

Mechanical Properties of APbX3 (A=Cs or CH3NH3; X=I or Br) Perovskite Single Crystals

Yevgeny Rakita, Sidney R. Cohen* †, Nir Klein Kedem, Gary Hodes, David Cahen*

Materials and Interfaces Department and †Surface Science Laboratory (Chemical Research Support),

Weizmann Institute of Science, Rehovot. 76100, Israel

* corresponding authors:  sidney.cohen@weizmann.ac.il ;  david.cahen@weizmann.ac.il

Figure S1: Characteristic Load vs. Displacement curves of APbX3 crystals. The number in the round parenthesis indicates the crystallographic plane facing the indenter.

Lead alloys

Figure S2: Ashby 2D map: density vs. Young’s modulus. Experimentally derived values (from this work or other cited works – see Table 1) are added in the area, designated “ABX3” to which the arrow points: Red - CH3NH3PbBr; Black - CH3NH3PbI3; Yellow - CH3NH3SnI3; Orange - CsPbBr3; Green - CsPbI3; Magenta – PbI2 ; Blue – PbBr2. Reprinted with permission from Ashby, M. F. Materials Selection in Mechanical Design, Fourth Edition. (Elsevier/ Butterworth-Heinemann, Amsterdam, 2011).

Figure S3: Ashby 2D map: linear thermal expansion coefficient vs. Young’s modulus. Experimentally derived values (from this work or other cited works – see Table 1) are added in the area, designated “ABX3” to which the arrow points: Red - CH3NH3PbBr; Black - CH3NH3PbI3; Orange - CsPbBr3; Magenta – PbI2; Blue – PbBr2. Reprinted with permission from Ashby, M. F. Materials Selection in Mechanical Design, Fourth Edition. (Elsevier/ Butterworth-Heinemann, Amsterdam, 2011).

Weak I-I VdW

strong I-Pb
(mostly) ionic bond

00

c axis

c(0001) plane

PbI2

CH3NH3PbI3

c

a

b

c

a

I

Pb

C

b

N

Figure S4: Ball-and-stick crystal structure representation of (top) PbI2 and (bottom) CH3NH3PbI3, illustrating the close relation between the Pb-I in the c(0001) plane and in CH3NH3PbI3.

Table S1: Values for Figure 3.

|  | B-X bond distance (@ RT) [Å] | K [GPa] |
| --- | --- | --- |
| CH3NH3PbI3 | 3.16 | 12.2 |
| CH3NH3PbBr3 | 2.97 | 15.6 |
| CH3NH3PbCl3 CH3NH3SnI3 | 2.86 3.13 | 16.5 * 12.6 |
| CsPbI3 | 3.23 | 19.8 |
| CsPbBr3 | 2.96 | 15.5 |
| MgSiO3 | 1.64 | 264 |
| SrTiO3 | 1.95 | 183 |
| GdMnO3 | 2.03 | 190 |
| PbBr2 | 3.14 | 23.5 |
| c-plane PbI2 | 3.23 | 16.7 |

* the bulk modulus of CH3NH3PbCl3 was estimated using the measured Young’s modulus of the (100) plane from Ref. 19 (see below), 19.8 GPa, and assuming a Poisson ratio of 0.3.

_______________

Ref.19: Sun, S., Fang, Y., Kieslich, G., White, T. J. & Cheetham, A. K. Mechanical properties of organic–inorganic halide perovskites, CH3NH3PbX3 (X = I, Br and Cl), by nanoindentation. J. Mater. Chem. A, .  6, 2622–2628  (2015). doi:10.1039/C5TA03331D