Supporting Information

NaphthaleneDiimide-Based Polymeric Semiconductors. Effect of Chlorine Incorporation and n-Channel Transistors Operating in Water

Gi-Seong Ryu1, Zhihua Chen,2 Hakan Usta,3* Yong-Young Noh1,4*and Antonio Facchetti2,5*

1 Advanced Energy and Electronic Materials Research Center, Dongguk University, 30, Pil-dong-ro, 1-gil, Jung-gu, Seoul 100-715, Republic of Korea

2 Polyera Corporation, 8045 Lamon Avenue, Skokie, Illinios 60077, United States

3 Department of Materials Science and Nanotechnology Engineering, Abdullah Gül University, Kayseri, Turkey

4 Department of Energy and Materials Engineering, Dongguk University, 30, Pil-dong-ro, 1-gil, Jung-gu, Seoul 100-715, Republic of Korea

5 Center of Excellence for Advanced Materials Research (CEAMR), King Abdulaziz University, Jeddah, Saudi Arabia

*Correspondence to: Prof. Antonio Facchetti (E-mail:afacchetti@polyera.com), Prof. Yong-Young Noh (E-mail:yynoh@dongguk.edu),Prof. Hakan Usta (E-mail:hakan.usta@agu.edu.tr)

Table S1. Electrical parameters of top-gate/bottom-contact OTFTs based on P(NDI2HD-T2Cl2), P(NDI2HD-T2Cl2) (High Mw), and P(NDI2OD-T2Cl2) as a function of semiconductor solution concentration and annealing temperature.

|  | Conc. | Annealing Temp. | Mobility | VTh | SS | Ion/Ioff | Ioff |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | (mg/ml) | (℃) | (cm2/V·sec) | (V) | (V/ dec) | - | (A) |
| NDI2HD -T2Cl2 | 1 | 100 | 0.008 ± 0.002 | 15.60 ± 1.59 | 22.22 ± 0.53 | ~ 104 | ~ 10-9 |
|  | 1 | 150 | 0.009 ± 0.003 | 16.26 ± 1.41 | 22.84 ± 1.18 | ~ 105 | ~ 10-10 |
|  | 1 | 200 | 0.011 ± 0.003 | 20.32 ± 1.76 | 15.75 ± 1.60 | ~ 105 | ~ 10-11 |
|  | 1 | 300 | 0.003 ± 0.002 | 31.92 ± 2.04 | 13.01 ± 0.91 | ~ 105 | ~ 10-11 |
|  | 5 | 100 | 0.016 ± 0.004 | 12.74 ± 2.09 | 20.76 ± 0.54 | ~ 103 | ~ 10-8 |
|  | 5 | 150 | 0.025 ± 0.004 | 16.78 ± 1.22 | 20.20 ± 0.84 | ~ 103 | ~ 10-9 |
|  | 5 | 200 | 0.029 ± 0.003 | 18.76 ± 1.33 | 18.56 ± 1.10 | ~ 104 | ~ 10-9 |
|  | 5 | 300 | 0.033 ± 0.006 | 23.81 ± 0.57 | 14.83 ± 0.51 | ~ 104 | ~ 10-9 |
| NDI2OD -T2Cl2 | 1 | 100 | 0.019 ± 0.007 | 21.49 ± 3.50 | 18.66 ± 0.72 | ~ 103 | ~ 10-9 |
|  | 1 | 150 | 0.025 ± 0.008 | 22.66 ± 1.50 | 17.80 ± 0.84 | ~ 104 | ~ 10-9 |
|  | 1 | 200 | 0.037 ± 0.013 | 20.93 ± 1.87 | 17.48 ± 1.24 | ~ 105 | ~ 10-8 |
|  | 1 | 300 | 0.020 ± 0.013 | 30.17 ± 0.92 | 11.32 ± 0.54 | ~ 106 | ~ 10-12 |
|  | 5 | 100 | 0.022 ± 0.005 | 18.56 ± 2.42 | 16.86 ± 0.86 | ~ 103 | ~ 10-8 |
|  | 5 | 150 | 0.044 ± 0.015 | 15.81 ± 2.66 | 20.41 ± 0.88 | ~ 103 | ~ 10-8 |
|  | 5 | 200 | 0.039 ± 0.013 | 18.44 ± 5.43 | 20.22 ± 1.10 | ~ 103 | ~ 10-8 |
|  | 5 | 300 | 0.057 ± 0.010 | 23.29 ± 1.02 | 13.37 ± 0.65 | ~ 105 | ~ 10-10 |
|  | 10 | 100 | 0.024 ± 0.006 | 11.23 ± 2.53 | 21.67 ± 0.90 | ~ 103 | ~ 10-8 |
|  | 10 | 150 | 0.040 ± 0.007 | 13.78 ± 2.66 | 23.17 ± 0.62 | ~ 103 | ~ 10-8 |
|  | 10 | 200 | 0.034 ± 0.009 | 20.69 ± 3.04 | 18.85 ± 1.15 | ~ 103 | ~ 10-8 |
|  | 10 | 300 | 0.053 ± 0.013 | 24.70 ± 3.51 | 11.29 ± 0.48 | ~ 105 | ~ 10-10 |

Figure S1. HOMO and LUMO pictorial representations for the polymer model structures I-V.

Figure S2. Evolution of OTFT charge carrier mobilities (a) and the corresponding X-ray diffraction (XRD) scans (b) of P(NDI2HD-T2Cl2)-based thin-films with annealing temperature.

Figure S3. Contact resistance of P(NDI2HD-T2Cl2)-based OTFTs with various concentration of P(NDI2HD-T2Cl2) solution.

Figure S4. Representative n-channel output curves (Vg = 80V) for top-gate/bottom-contact OTFT devices of the indicated semiconductors.

Figure S5. Representative p-channel transfer curves for top-gate/bottom-contact OTFT devices of the indicated semiconductors.

Figure S6. Representative transfer curves for P(NDI2HD-T2Cl2) and P(NDI2OD-T2) OTFT devices with PMMA and CYTOP gate dielectrics upon aging in air at ~ 60% RH.

Figure S7. Representative transfer curves for P(NDI2HD-T2Cl2) and P(NDI2OD-T2) OTFT devices with PMMA upon immersion in water for the indicated time.

Figure S8. Optical image of a OTFT array with CYTOP as gate dielectric after immersion in water for one week and drying using a flow of nitrogen. Dielectric film delamination is clearly visible.

Figure S9. Bias stress stability for the indicated devices after 35 min.