Supplementary Information

Tellurium doped Lanthanum Manganite as Catalysts for the Oxygen Reduction Reaction

V. Celorrio,1 L. J. Morris,1, 2 M. Cattelan,1 N.A. Fox,1 D. J. Fermin1

1School of Chemistry, University of Bristol, Cantocks Close, Bristol, BS8 1TS

2EPSRC Centre for Doctoral Training in Catalysis, School of Chemistry, Cardiff University, Main Building, Park Place, Cardiff, CF10 3AT, UK.

FIG. S1 SEM images of a) La0.77Te0.23MnO3 and b) La0.90Te0.10MnO3.

FIG. S2 Representative TEM images of a) La0.77Te0.23MnO3 and b) La0.90Te0.10MnO3.

FIG. S3 Histogram showing the particle size distribution for LaMnO3, La0.90Te0.10MnO3, and La0.77Te0.23MnO3 as determined from TEM micrographs.

FIG. S4 Mn 2p3/2 photoemission peak for the various La1-xTexMnO3
samples. A shift towards lower binding energies is observed as x increases,
suggesting an increase in Mn2+/Mn3+ ratio.

FIG. S5 Rotating ring-disc curves for oxygen reduction on a Vulcan modified glassy carbon electrode in O2-saturated 0.1 M KOH solution at different rotation speeds. The Pt ring was held at a constant potential of 1.10 V.

FIG. S6 Rotating ring-disc curves for oxygen reduction on La0.77Te0.23MnO3 particles supported on Vulcan modified glassy carbon electrode in O2-saturated 0.1 M KOH solution at different rotation speeds. The Pt ring was held at a constant potential of 1.10 V.

FIG. S7 HO2- yield (a) and number of electrons transferred (b) calculated from measurements of iDISK and iRING of the different composite electrodes in O2-saturated 0.1 M KOH at 1600 rpm. The HO2- yield can be calculated using equation S1:

Equation S1

where iR is the ring current and N is the collection coefficient (N = 0.42).  The effective number of electrons involved in the ORR (n) is estimated from equation S2:

Equation S2

Table S1. Unit-cell parameters and statistics obtained from Rietveld refinement of the XRD patterns.

|  | LaMnO3 | La0.90Te0.10MnO3 | La0.77Te0.23MnO3 |
| --- | --- | --- | --- |
| Space Group | R3c | R3c | R3c |
| a [Å] | 5.4936(2) | 5.496(2) | 5.5006(5) |
| b [Å] | 5.4936(2) | 5.496(2) | 5.5006(5) |
| c [Å] | 13.3713(6) | 13.337(7) | 13.344(1) |
| Laocc | 1.00 | 0.90(1) | 0.77(8) |
| Teocc | --- | 0.10(9) | 0.23(8) |
| Unit Cell Volume [Å3] | 349.47(2) | 348.9(3) | 349.64(6) |
| dMn-O [Å] | 1.943(3) | 1.943(6) | 1.9451(3) |
| χ2 | 3.68 | 3.02 | 2.03 |
| Rp [%] | 2.68 | 2.53 | 3.43 |
| Rwp [%] | 3.48 | 3.38 | 4.36 |
| Rexp [%] | 1.85 | 1.94 | 3.06 |
| RBragg [%] | 1.31 | 3.60 | 6.02 |

Table S2. Mean particle diameters measured from TEM images

|  | d / nm |
| --- | --- |
| LaMnO3 | 39.9 ± 11.3 |
| La0.90Te0.10MnO3 | 48.4 ± 18.4 |
| La0.77Te0.23MnO3 | 67.9 ± 38.3 |

Table S3. Number density of electroactive Mn sites (Mn) calculated from integration of the cathodic current in the range of 0.2 to 1.2 V. The final oxidation state is +2, while two limiting cases are considered for the the initial Mn oxidation state: from the mean oxidation state of the A-site with La3+ and Te4+ (Case 1), or Mn3+ state independently of the A-site composition (Case 2).

| Sample | Charge / C | Initial Mn oxidation state Case1 | Mn / cm-2 (Case 1) | Mn / cm-2 (Case 2) |
| --- | --- | --- | --- | --- |
| LaMnO3 | (2.6 ± 0.1)×10-4 | 3.00 | (1.3 ± 0.8)×1016 | (1.3 ± 0.8)×1016 |
| La0.90Te0.10MnO3 | (1.0 ± 0.5)×10-4 | 2.90 | (7.1 ± 0.4)×1015 | (4.9 ± 0.4)×1015 |
| La0.77Te0.23MnO3 | (1.2 ± 0.3)×10-4 | 2.77 | (5.2 ± 0.2)×1015 | (6.2 ± 0.2)×1015 |