Supporting Information

Electrical and Optical Characteristics of Solution processed MoOx and ZnO QDs Heterojunction

Hemant Kumar *, ϯ, Yogesh Kumar ϯ, Gopal Rawat ϯ, Chandan Kumar ϯ, Bratindranath Mukherjee ¥, Bhola N. Palі and Satyabrata Jit*, ϯ

ϯDepartment of Electronics Engineering,  ¥Department of Metallurgy,  іSchool of Material Science and Technology,  Indian Institute of Technology (Banaras Hindu University), Varanasi-221005, India

Index

Figure S1: TEM image of as-grown ZnO QDs and histogram of particle size.…………............................	(1)

Figure S2: Selected Area Electron Diffraction (SAED) pattern of as-grown ZnO QDs.…………..............	(2)

Figure S3: Ag contact on solution processed MoOx before heat treatment……………………...................	(2)

Figure S4: Ag contact on solution processed MoOx after heat treatment……………………......................	(2)

Figure S5: Ag contact on thermally deposited MoOx before heat treatment ……………………................	(3)

Figure S6: Ag contact on thermally deposited MoOx after heat treatment ……………………...................	(3)

Figure S1: TEM image of as-grown ZnO QDs and histogram of particle size

Figure S2: Selected Area Electron Diffraction (SAED) pattern of as-grown ZnO QDs

Figure S3: Ag contact on solution processed MoOx before heat treatment

Figure S4: Ag contact on solution processed MoOx after heat treatment

Figure S5: Ag contact on thermally deposited MoOx before heat treatment

Figure S6: Ag contact on thermally deposited MoOx after heat treatment