Supplementary material

Eco-friendly synthesis of egg-white capped silver nanoparticles for rapid, selective and sensitive detection of Hg(II)

Antonio Tirado-Guizar1*, Geonel Rodriguez-Gattorno1, Francisco Paraguay-Delgado2, Gerko Oskam1, Georgina E. Pina-Luis3

1Departamento de Física Aplicada, Centro de Investigación y de Estudios Avanzados del Instituto Politécnico Nacional (CINVESTAV-IPN), Mérida, Yucatán 97310, México

2Centro de Investigación en Materiales Avanzados S.C. Departamento de Física de Materiales, Av. Miguel de Cervantes 120, Complejo Industrial Chihuahua, CP 31109 Chihuahua, Chih., México.

3Centro de Graduados e Investigación en Química, Instituto Tecnológico de Tijuana, A.P. 1166, Tijuana 22500, BC, México

Table S1. Reaction conditions for the synthesis of EWAg Nps

| Sample | AgNO3 (mL) | Water (mL) | Egg white ((L) | NaBH4 ((L) |
| --- | --- | --- | --- | --- |
| Ag1 | 1 | 24 | 0 | 400 |
| Ag2 | 1 | 24 | 50 | 400 |
| Ag3 | 1 | 24 | 100 | 400 |
| Ag4 | 1 | 24 | 150 | 400 |
| Ag5 | 1 | 24 | 250 | 400 |
| Ag6 | 1 | 24 | 250 | 10 |
| Ag7 | 1 | 24 | 250 | 100 |
| Ag8 | 1 | 24 | 250 | 200 |

Figure S1. UV-Visible absorbance spectra of the as-prepared EWAg NPs at different egg-white concentrations.

Figure S2. XPS spectrum (Hg 4f-region) of the material formed by reaction of EWAg NPs in a 100 μM Hg2+ solution.

TABLE S2. Comparison of the analytical performance of the EWAg NPs sensor with similar methods for the detection of Hg2+.

| Nanosensor | Dynamic range (nM) | Detection limit (nM) |
| --- | --- | --- |
| Au/Mercaptopropionic acid[1] | 250-500 | 100 |
| Ag/Gum kondagogu[2] | 50-500 | 50 |
| Ag/Cysteine[3] | 0-30000 | 250 |
| Ag/Egg-white (This work) | 0-50000 | 510 |

References

- C.-C. Huang and H.-T. Chang: Parameters for selective colorimetric sensing of mercury(II) in aqueous solutions using mercaptopropionic acid-modified gold nanoparticles. Chem. Commun. 12, 1215 (2007).

- L. Rastogi, R. B. Sashidhar, D. Karunasagar, and J. Arunachalam: Gum kondagogu reduced/stabilized silver nanoparticles as direct colorimetric sensor for the sensitive detection of Hg2+ in aqueous system. Talanta 118, 111 (2014).

- C. Jiang, Z. Guan, S. Y. Rachel Lim, L. Polavarapu, and Q.-H. Xu: Two-photon ratiometric sensing of Hg2+ by using cysteine functionalized Ag nanoparticles. Nanoscale 3, 3316 (2011).